## Slide 1: Point defects in semiconductors as quantum platform Ongoing research at the Semiconductor Physics Section
Lasse Vines
University of Oslo
lassevi@fys.uio.no

## Slide 2: Semiconductor Physics Section LENS – Light and Electricity from Novel Semiconductors
Office: Kristen Nygårds hus (3.etg.)
Lab: MiNa-Lab
Clean room(440 m2) and 9 Characterization labs
~45 people:
MiNa-Lab
Norwegian Micro- and Nanofabrication Facility
- 5 Profs.
- 4 admin/engineers
- 10 postdocs/researchers
- 12 PhD students.
- 15 Master students
Application-motivated basic research...
focus on defects, doping and diffusion, synthesis of novel semiconductors and ion beam physics, towards applications within solar cells, QT, power electronics and sensors

## Slide 3: Choice of material platform for physical realizations of QT
Superconductors
Trapped ion
Atomic vapor
Optical gratings
Quantum dots
Defects in semiconductors
…
Superconductors
Optical gratings
Quantum dots
Point defects
www2.physics.ox.ac.uk
Trapped ions

## Slide 4: Point defects in semiconductors for QT
Certain point defects can act as isolated two level systems with possibility for spin manipulation and single photon emission properties satisfying the qubit requirements

## Slide 5: Point defects in semiconductors for QT
Certain point defects can act as isolated two level systems with possibility for spin manipulation and single photon emission properties satisfying the qubit requirements
Example: The NV- center in diamond
N atom next to C vacancy
Spin state with S = 1
Spin state is stable for milliseconds even at RT  what you need for QC
Spin state can be optically initialized, entangled and read out
Excite with laser  single-photon emission

## Slide 6: Point defects in semiconductors for QT
Sensing applications

## Slide 7: Point defects in semiconductors for QT

## Slide 8: Single photon emission from point defects
Ec
Ev
Ideal single-photon source:
Triggered (on-demand)
g(2)(0) = 0
Indistinguishable photons
High repetition rate
Room temperature
Chip integration

## Slide 9
Identification and single photon emission (SPE) from point defects in Silicon
Si reveal several other SPEs, e.g. W, T and C-center, but also several unknown defects suitable for telecom wavelengths
Point defects suitable as solid state qubits and single photon emitters (SPE)
- First identification of SPE in Si, the G-center
W. Redjem, ..., A. Y. Kuznetsov, ... G. Cassabois, Nature Electronics, 3, 738, (2020)
A. Durand, ... , A. Y. Kuznetsov, ... A. Dreau, Phys. Rev. Lett., 126, 083602 (2021)

## Slide 10: Formation of qubit candidates through ion implantation

## Slide 11: Charge state identification and control of quantum defects in Silicon Carbide
SiC hosts several well-known “quantum defects”
Only one charge state is bright
The charge state can be controlled by and electric field
VSi, exhibit a quadratic Stark shift
M. Bathen, ..., L. Vines, npj Quantum Information, vol. 5, 111 (2019)
M. Bathen and L. Vines, Advanced Quantum Technologies, 4, 2100003 (2021)
M. Bathen,... L. Vines and U. Grossner, Defect and Diffusion Forum, 425, 35 (2023)
Emission control
Stark effect (for tuning and sensing)

## Slide 12: Ongoing projects
Strain effect on emission lineshape
G. C. Vasquez, M. Bathen ..., L. Vines, Nano Lett., vol. 20, p. 8689 (2020)
SPE's in SiC polymorphs and other materials
E. Ousdal, M. Bathen, A. Galeckas, A. Kuznetsov, L. Vines, submitted to J. Appl. Phys (2024)

## Slide 13: Predicting solid state material platforms for quantum technologies
Crystal structure from large datasets were used as a starting point to predict suitable material hosts for quantum emitters.
Unconventional parameters was found to be important for the material selection
Resulted in a list of potential material candidates for experimental investigation
O. Hebnes, M.Bathen, Ø. Schøyen, S. Winther-Larsen, L. Vines and M. Hjorth-Jensen, npj Computational Materials (2022) 8:207

## Slide 14
Thank Th
lassevi@fys.uio.no
Thank you for the attention!
Andrej
Lasse
Augustinas
Vegard
Marianne
David
Erlend
Alireza
Mariann
Luis Roberto Jimenez Arteta
Joseph Panana Vera
Christopher

## Slide 15: What is quantum sensing ?
Definitions:
Use of quantum system with quantized energy levels to measure a physical quantity
Use of quantum coherence (i.e., wavelike spatial or temporal superposition states) to measure a physical quantity.
Use of quantum entanglement to improve the sensitivity or precision of a measurement, beyond what is possible classically
Degen et al., Rev. Mod. Phys., Vol. 89, No. 3, (2017)

## Slide 16: Ongoing QT research at the University of Oslo
Nanoparticle and epitaxial quantum dots
Point defects
Liquid He quantum dots
Properties of quantum materials
Machine learning for new quantum materials

## Slide 17: Semiconductor materials for QT
Silicon carbide
Point defects
Silicon
Point defects
Spin qubit CMOS devices
Diamond
Point defects
Gallium arsenide
Quantum dots
Hexagonal boron nitride
Point defects
2D-TMDCs
Bound excitons
Notes: Although platforms exist, still scarce
Also, dont understand why in some materials, and not in others

## Slide 18: Quantum technologies promise new capabilities
Communi-cation
Computing
Sensors
Extreme conditions
Signals in cells
Nanoscale
Predict the weather
Better logistics and optimization
Finance
Predict new medicines and materials for e.g. solar cells and batteries
Quantum internet
Quantum cryptography
Secure communication
Notes: Gorpu into three categories.

## Slide 19
Questions?