## Slide 1: TU Wien Contribution during FCC Study (2016-2021)
Low Temperature Physics and Superconductivity

## Slide 2: Research Projects
Nb3Sn Conductor R&D
Beam Screen Development (HTS)
Marie Skodowska-Curie ITN EASITrain

## Slide 3
16 T dipole magnets
1500 A/mm2
4.2 K
Nb3Sn Conductor R&D
Low impedance coating for reduction of beam-induced RF image currents
Operation at 50 K for reduced cryogenic power consumption
Beam Screen Development (HTS)

## Slide 4: Goal of the investigation
Microstructure
Local super-conducting properties
Macroscopic performance of super-conductors
SEM, TEM
EDX
SHPM, SQUID- magnetometry
Irradiation

## Slide 5: Investigations at ATI
Measurements of the critical currents
Irradiation experiments of superconducting materials
Magnetic field mapping
Search for material inhomogeneities
Finding the relationship between microstructure and superconducting properties
Low Temperature Physics and Superconductivity

## Slide 6: How to achieve Jc=1500 A/mm2?
16 T dipole magnets
1500 A/mm2
4.2 K
Nb3Sn Conductor R&D
Two main concepts:
Artificial pinning
Reduction of inhomogeneities

## Slide 7: Introduction
Superconducting properties (e.g. TC, BC2, JC) in Nb3Sn wires are influenced by:
Composition
Morphology
Composition gradients
Sn: Nb1−β Snβ
Additives: Ti, Ta
grain size (grain boundaries)
 JC
 TC, BC2
 spatial TC distribution
Defects (APC)

## Slide 8: Irradiation experiments
Irradiation of short wire samples in the TRIGA Mark-II reactor at Atominstitut
Sequential irradiation in relatively small steps in order to assess fluence dependence of superconducting properties
Very important also for nuclear fusion

## Slide 9: Irradiation experiments
Critical current density increases significantly in irradiated wires because of nano-sized defects.
FCC target was obtained in industrial Nb3Sn wire!
Only model system. Later realized by oxide nano-particles in prototype wires.
Baumgartner, T. et al., Sci. Rep. 5, 10236; doi: 10.1038/srep10236 (2015).

## Slide 10: Artificial pinning centers
Ortino, M. et al., Supercond. Sci. Technol. 34, 035028; doi: 10.1088/1361-6668/abd5f4 (2015).
“Addition” of Zr-O nanoparticles
Collaboration with USA: Ohio State University, Hypertech, Fermilab

## Slide 11: Magnetometry - SHPM
Micro Hall Scanner
Principle:
  Measurement of local magnetic field, either in applied magnetic field or with remnant magnetization
Experiment
  Field up to 8 T, range: 3 x 3 mm2 @ 1 µm
Goal
  Evaluating TC gradients by scanning in the Meißner state at different temperatures
  Assessing inhomogeneities in Jc by inversion of the Biot-Savart law
Scanner head with mounted sample

## Slide 12: Sample preparation for Micro Hall Scanner
Thin slice of less than 10 µm prepared by mechanical polishing with diamond disks
Parallel and even surfaces essential
Polishing induces damage on the sample
4 K @ 1 T

## Slide 13: Magnetic Inhomogeneities
RRP-Ti wire, scanned in the Meißner state at different temperatures
Change in screened area reveals TC gradient in the sub-elements
For finding inhomogeneities in JC, scans at fields of several Tesla will be performed
RRP-Ti wire @ 10 K / 100 mT
RRP-Ti wire

## Slide 14: Meißner scans of RRP-Ti wire
Meißner Scans on 10 µm thin slice of RRP-Ti wire
Screening radius depends on temperature due to gradient in Sn content
Dependency of TC from the Sn content
Small change in Sn content heavily impacts TC

## Slide 15: Sample Preparation of subelement
Preparing thin slices of etched subelements using FIB for SHPM measurements

## Slide 16: Magnetic Inhomogeneities
Hall scans of subelement at 5 K
FIB preparation of individual single subelements is feasible
For detection of inhomogeneities of JC Hall scans at higher applied fields will be performed
50 mT
500 mT

## Slide 17: Investigations at USTEM
FEGTEM
TEM
FEGSEM
DBFIB
DBFIB
Composition gradients in Nb3Sn wires
Irradiation Effects
Tl1223 for beam screens
Artificial pinning centers (APC)
Carbon-Cluster in MgB2
Coated conductors YBCO

## Slide 18: Composition Gradients
Magnetometry and calorimetry lead to different distribution functions
Caused by Sn distribution within individual grains
Thomas Baumgartner et al, SUST 30, (2017)

## Slide 19: Nb3Sn Conductor R&D
Fermilab
Rutherford cable
Subelements
(Filaments)
Strands

## Slide 20: Investigated Nb3Sn wires
PIT-Ta
Internal Sn–Ti RRP
FEGSEM
EDX map
Subelement
Diagrams redrawn from: M.Jewell, Thesis, (2008), UW-Madison
Nb3Sn
Nb
Ti
Cu
500 µm
1
2
3
Clustered layout
Distributed Nb + Ta

## Slide 21: Sn distribution within PIT-Ta
Center
Barrier
DSn: 0.08 %/µm
Center
GB

## Slide 22: Irradiated RRP-Ti wire

## Slide 23: Irradiation experiments
BF
DF
Formation of nanosized defects

## Slide 24: Tl1223 for Beam Screens
Synchrotron radiation must be absorbed at 50 K
Vacuum requirements
Cryogenic efficiency
Power consumption
Cu is not sufficient
YBCo or Tl based HTS are an option
Tl-HTS produced at CNR Spin / Genova

## Slide 25: What influences sc properties
Misagligned 1223 grains
Impurities

## Slide 26: Beam Screen Development (HTS)
O, Ca rich
Tl-1212
O, Ca, Sr rich
Tl-1223
Ag
Tl-1212
Ag
Tl-1223
O, Ca, Pb rich
Notes: The first samples produced typically show plate-like big grains (approx. 200 µm) spread out all over the Ag substrate. In particular, it was observed that the surface is mostly characterized by Tl-1212 grains (whose formation is energetically more favourable) covering the Tl-1223 ones and by O, Ca and Sr rich areas.

## Slide 27: Beam Screen Development (HTS)
1223
1223
1223
1223
1234?
1234?
1223
Cu
Correlation of sc properties with microstructural features
Notes: The first samples produced typically show plate-like big grains (approx. 200 µm) spread out all over the Ag substrate. In particular, it was observed that the surface is mostly characterized by Tl-1212 grains (whose formation is energetically more favourable) covering the Tl-1223 ones and by O, Ca and Sr rich areas.

## Slide 28: µHall: Magnetic field mapping
Comparison between remnant magnetic field and local composition of the superconductor
Notes: The first samples produced typically show plate-like big grains (approx. 200 µm) spread out all over the Ag substrate. In particular, it was observed that the surface is mostly characterized by Tl-1212 grains (whose formation is energetically more favourable) covering the Tl-1223 ones and by O, Ca and Sr rich areas.

## Slide 29: Nb3Sn with artificial pinning
Formation of ZrO2 or HfO2 precipitates
Grain size refinement (more grain boundaries)
Additional pinning centers

## Slide 30: Nb3Sn with APC
TEM
TKD
Grain refinement determined by TKD

## Slide 31: Nb3Sn with APC
Sample thickness determined by EELS
Estimation of APC density
5900–6400 precipitates/µm3

## Slide 32: Scientific Output FCC related
2016 – 2021
14 Publications in Journals
11 Poster Presentations
20 Talks
3 PhD and 2 PhD