## Slide 1
Progress of the High Field Magnet R&D at IHEP
Qingjin Xu
Jan 14 2022
中国科学院高能物理研究所
Institute of High Energy Physics, CAS
Colleagues & Collaborators
IHEP-CAS: Chengtao Wang, Yingzhe Wang, Juan Wang, Chunyan Li, Rui Kang, Huanli Yao, Zhen Zhang, Jinrui Shi, Ze Feng, Wei Li, Ao Feng, Menglin Wang, Huan Yang, Ling Zhao, Zhilong Hou, Zhongxiu Liu,,… HIPS-CAS: Huajun Liu, Tao Zhao, Yanlan Hu,…
IEE-CAS: Dongliang Wang, Xianping Zhang, Yanwei Ma,… Toly Electric: Yu Zhao, Hean Liao, Bingxing Lu,…
IMP-CAS: Wei Wu, Xianjin Ou, Dongsheng Ni, Wenjie Liang,… Baoding Tianwei Electric: Tao Xing, Xiongzhuang Li, Jun Jiao,…
THU: Timing Qu, Yufan Yan,……

## Slide 2
Magnet Design Scope for SPPC
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2013
Site of the project | China | Europe
Baseline technology | IBS 12~24 T to reach 75-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **

## Slide 3
Chart: Applied Magnetic Field (T)
| 5 | 10 | 15 | 20
REBCO: B ∥ Tape plane | 4599.7996 | 4264.0246 | 3416.6751 | 3085.9004
REBCO: B ⊥ Tape Plane | 3664.9998 | 2919.9995 | 2379.9996 | 1796.1537 | 1447.6924 | 1188.462 | 1034.3652 | 956.923 | 851.8301 | 780.8449 | 719.9995 | 679.4359 | 626.087 | 593.2388 | 563.4783 | 535.3843 | 516.5215 | 469.5647 | 433.0766 | 406.956 | 391.3041 | 367.6926 | 360.0003 | 344.3473 | 328.6954 | 322.3077
Bi-2212: 50 bar OP | 2187.8458 | 2018.5437 | 1897.0961 | 1799.3564 | 1729.1673 | 1666.7736 | 1608.1837 | 1558.7923 | 1516.4066 | 1473.2906 | 1436.5687 | 1398.9095 | 1365.3787
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: High Field MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar | 1379.4097 | 1269.0093 | 1128.2455 | 1107.3276
YBCO B perp ln extrap | 322.2305 | 315.4585 | 296.3443 | 267.862 | 242.7389
YBCO par ln extrap | 3024.7539 | 2573.1471 | 2188.967 | 2051.8662
IBS 2016
(short sample)
500A/mm2
IBS 2018 100-m tape
IBS 2021 100-m tape
IBS Technology: Status and Outlook

## Slide 4
100-m Long Ba122 Tapes by Rolling Process
In 2020, Jc of a 100-m 7-core tape using the new fabrication technique reached 500 A/mm2 @ 4.2 K, 10 T.
Tape width 4.8 mm, tape thickness 0.3 mm. Ic > 260 A, Je>180 A/mm2.
In 2018, Jc of such tape is 300 A/mm2 @ 4.2 K, 10 T.
IBS Technology: Status and Outlook
Prof. Y. Ma’s
Group, IEE-CAS

## Slide 5
4.2 K, 10 T (short sample): Jc=1100 A/mm2
Performance of HIP Ba122 Tapes with Cu/Ag Stabilizer
Size of the grains was around 0.5 um, smaller than that in the Hot-pressed samples.
The Jc may be improved with the increase the grain size.
Liu 2021 Sci. China Mater.
Doi:10.1007/s40843-020-1643-1
IBS Technology: Status and Outlook
Prof. Y. Ma’s
Group, IEE-CAS

## Slide 6
Preparition of bent IBS tape
Cracks appear regularly in part of the superconducting cores under tensile stress !
Minimum bending diameter measurement of the IBS tapes
OMI of D10 bent tape
Sample results by ASIPP in 2018
Sample results by IHEP in 2021
IBS Technology: Status and Outlook

## Slide 7
Fabrication of D20-17 turn-double pancake coils with IBS tapes
Series IBS double pancake solenoids
Coil winding of the IBS double pancake solenoids with 20-mm inner diameter
IBS double pancake solenoids after heat reaction
Impregnated Series IBS solenoids
IBS Technology: Status and Outlook
Fabrication of High Field IBS solenoids

## Slide 8
Performance test of the series IBS solenoids at 20 T background field
Ic of the series IBS solenoids reached 75 A at 20 T, and stable operation with 100 A
80A hold 100s
100A hold 80s
Quench Criteria
0.5A/s ramp rate
34mm inner diameter 17turn double pancake 6 coils in series.
IBS Technology: Status and Outlook
34mm inner diameter 17turn double pancake 6 coils in series.

## Slide 9
Performance test of the double pancake IBS solenoid at 30 T background field
Ic of the IBS double pancake solenoid reached 67 A at 30 T. New record!
D20-17turn-IBS double pancake coil
30T background magnet @ Hefei
34mm inner diameter, 17turn double pancake coil
IBS Technology: Status and Outlook

## Slide 10
Parameter | Value
Background field | 0-10 T
Rate | 1 A/s
Maximum pressure on IBS | 120 MPa
Racetrack Coils with 100-m Long IBS Tapes
IBS Technology: Status and Outlook

## Slide 11
Zhang, et al., SuST,. 34 (2021) 035021
Two racetrack coils have been made using the 100 m length IBS tapes.
The coils reached 86.7% of critical current of the short sample at 4.2 K and 10 T.
with highest compressive stress of 120 MPa.
Comments from SUST reviewers：
…the new results that can have a strong impact on the conductor and magnet community.
…demonstrated the great potential of Iron-Based Superconductor in the development of next-generation accelerators.
IBS Technology: Status and Outlook
Racetrack Coils with 100-m Long IBS Tapes

## Slide 12
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Tc reached 55K
IBS solenoid at 24 T
Racetrack at 8 T
The engineering current density of the long-length IBS still needs a significant improvement, to reach the similar level as ReBCO or Bi-2212 conductors.
The materials of stabilizer should be shifted to copper or any other low-cost metals to realize the low cost of IBS.
Structure and fabrication methods of IBS and corresponding coils should be further optimized to minimize the Jc degradation at high field and high stress.
And many other issues like detailed magnetic and mechanical properties study of IBS, quench detection and protection of the IBS coils / magnets and etc.
IBS solenoid at 30 T
Racetrack at 10 T
2022

## Slide 13
Magnet Design
Superconductor
Impregnation quality control
Thermal stress control
Mechanical strength and stability
Quench protection
Hot spot, voltage,…
Material,
Cross section, Processing,…
Jc, RRR, Cu ratio,
Filament size,
Jc and RRR degradation
Stress and dimension control
Coil Fabrication
Magnet
Assembly
Performance
Qualification
Magnetic field strength,
EM force, quench protection,…
Magnetic field quality,
Persistent current effect,
Coil stress,…
Jc & strain curve of the superconductor
Pre-stress control
Dimension control,
Mechanical Stability
Training, Thermal-magnetic instability,
Thermal cycle,…
R&D Route for LTS High-field Accelerator Magnets

## Slide 14
Development of a NbTi+Nb3Sn twin-aperture model dipole magnet from 2017.
Dipole field reached 12 T @ 4.2 K in May 2021 and 12.47 T after a thermal cycle.
R&D of the 1st NbTi+Nb3Sn Model Dipole Magnet

## Slide 15
2018
2019
2021
R&D of the 1st NbTi+Nb3Sn Model Dipole Magnet
~90% SSL

## Slide 16
16 T Dipole: Nb3Sn 12~13 T + HTS 3~4 T
Development of the 16-T Hybrid Dipole Magnet

## Slide 17
Development of a Roebel-like HTS Transposed Cable
Development of the 16-T Hybrid Dipole Magnet
The 1st prototype cable
The 2nd prototype cable
In-plane
bending

## Slide 18
IBS prototype cable
Cable length: 5 m
Pitch length: 200 mm
Cable thickness: 10.5 mm
Reaction temp.: 860C
Test radius: 200 mm
Current：>1300 A
Iron Based Superconductor
Hastelloy
Cross section of the cable
Development of the 16-T Hybrid Dipole Magnet
Development of a Roebel-like HTS Transposed Cable

## Slide 19
R&D Roadmap for Next Years

## Slide 20
Status of the HL-LHC MCBRD CCT Magnets
Layout of the HL-LHC Magnets and Contributors
The 1st prototype magnet passed performance test at 4.2K in China, delivered to CERN in Aug 2020, and passed performance test at CERN in Dec 2020.

## Slide 21
The 1st series magnet passed performance test at 4.2K in China and delivered to Europe in Oct 2021.
The remaining 11 sets of magnets will be delivered to Europe at a rate of 2~3 months per magnet
1-Aperture-02
1-Aperture-01
Status of the HL-LHC MCBRD CCT Magnets

## Slide 22
Strong domestic collaboration in China for the advanced superconductor R&D (HTS & Nb3Sn): to significantly raise their performance and lower their cost.
Jc of 100-m long 7-core Iron-Based Superconducting tape has reached 500 A/mm2 @ 4.2 K, 10 T, corresponding to Ic >200 A, Je>140 A/mm2.
Quench current of the Iron-Based Superconducting double pancake solenoid coil reached 67 A at 30 T, new world record!
10+ T twin-aperture model dipoles being developed at IHEP, reached 12.47 T at 4.2 K in July 2021, aiming to reach 16 T (Nb3Sn+HTS) in 3 years, and 20 T in 10 years.
International collaboration on high field magnet technology for next-generation particle accelerators are highly welcome!
Summary

## Slide 23
Thanks for your attention
Yuyuantan Park, Beijing, 2022.1