## Slide 1
High Field Magnet R&D
for the Next-generation Accelerators
Qingjin XU
for the Superconducting Magnet Group
Accelerator Division, IHEP-CAS
Jan 24 2024

## Slide 2
2
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2013
Site of the project | China | Europe
Baseline technology | IBS 20~24 T to reach 125-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **
Design Scope for the Next-generation Accelerators

## Slide 3
Roadmap of the High Field Magnet R&D at IHEP
3
Challenges: Stress control, quench protection, field quality control,……
2018-2021, 12.47T @4.2K
NbTi + Nb3Sn
2021-2023 16T @ 4.2K
Nb3Sn + HTS

## Slide 4
16 T Model Dipole LPF3: Nb3Sn 13 T (Common Coil with 55 mm gap) + HTS 3 T inserts (Block & CCT with 20 mm)
Development of the 16-T Model Dipole LPF3
4

## Slide 5
5
The Nb3Sn coils for LPF3
Chengtao Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 6
6
The ReBCO block insert coils for LPF3
Parameters | Values
L0 | 409.6 mm
L1 | 540.2 mm
Rhard | 800 mm
Aend | 6 °
R1 | 9.5 mm
Z1 | 120 mm
Ze Feng et al
Development of the 16-T Model Dipole LPF3

## Slide 7
7
The ReBCO CCT instert coils for LPF3
典型CCT线圈结构示意
“斜螺线管”型CCT线圈结构示意
Rui Kang et al
Development of the 16-T Model Dipole LPF3

## Slide 8
8
2023.8.29 Assembly completed
8
Stress monitoring during
assembly with FBG
Pre-stress applied with commercial hydraulic jack
Pre-stress and assembly of LPF3
Yingzhe Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 9
9
Current decay curve at the operating current
Varistor plus CLIQ to protect the Nb3Sn coils. The maximum hot spot is ~ 230 K
NI configuration plus dump resistor to protect the 2 HTS insert coils
Quench protection of LPF3
Rui Kang, Hongjun Zhang et al
Feasibility study of applying the no-insulation coil on accelerator magnets
Development of the 16-T Model Dipole LPF3
Jinrui Shi et al

## Slide 10
Performance test ongoing from Sep 2023
The Nb3Sn coils were trained firstly, maximum current reached ~85% of Iop in Dec 2023.
HTS block coil was ramped independently to 100% of Iop with negligible terminal voltage
Present test results indicate the promising performance of the LTS and HTS coils. Test to be continued in Feb 2024
10
Wei Li et al
Development of the 16-T Model Dipole LPF3

## Slide 11
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2016
IBS 2019
IBS 2022
IBS 2025
IBS Technology: Status and Outlook
11
90% Stainless-steel & 10% Sliver stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.

## Slide 12
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 60 A at 4.2 K and 32 T, world’s highest record up to now.
The First IBS Solenoid Coil at 32 T background field
12
Chunyan Li et al
2024 Supercond. Sci. Technol. 37 015001
Successfully fabricated a double pancake coil and
a series-connected coil consisting of six DP coils

## Slide 13
IBS Technology: Status and Outlook
13
Quench propagation study of the IBS tapes and coils
Experimental data shows significant quench propagation in the IBS tape! More testing will be carried out.
Poster: WP-P-12
Chunyan Li et al

## Slide 14
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Je= 100 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 24 T
Racetrack at 8 T
Je= 300 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA transposed cable
Je > 450 A/mm2
@ 10 T, 4.2 K
2022
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Je of IBS expected to be similar as ReBCO in 5 years with better mechanical properties and lower cost
14

## Slide 15
Milestone of the HL-LHC CCT Magnet Project
Development of CCT Magnets for HL-LHC
15
Agreement signed
btw IHEP and CERN
The qualified prototype delivered to CERN
The CCT magnet from China under test at CERN
All the 12 series CCT magnets delivered to CERN
Installation to tunnel
HL-LHC commissioning

## Slide 16
Development of CCT Magnets for HL-LHC
16
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.

## Slide 17: Training of MCBRD02 & MCBRD03
Development of CCT Magnets for HL-LHC
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.
17

## Slide 18: Training of MCBRD04
Development of CCT Magnets for HL-LHC
18
Satisfying performance at 4 K for both apertures, tested at IMP-CAS

## Slide 19
4 series CCT magnets have been fabricated, successfully reached the design target and delivered to CERN
Components for 2 series magnets being shipped to CERN
Production rate for the rest of series magnets: every 3 month per magnet; to be completed by mid 2025
Development of CCT Magnets for HL-LHC
 | Coil name | Winding method | Location | Coil stand-alone performance (4.2 K) | Magnet performance at 4.2 K
MCBRD01 | MCBRD_CB01 | Wet wind | CERN | 530 A | Both apertures reached ultimate current 422 A, and passed 4-hour stability test at 4.2 K
 | MCBRD_CB03 | Direct wind |  | 410 A (training stopped due to the availability of the test station) | 
 | MCBRD_CB02 | Direct wind | CERN | Failed to reach the design current | 
MCBRD02 | MCBRD_CB04 | Wet wind | CERN | 422 A (training stopped due to the availability of the test station) | Both apertures reached ultimate current 422 A, and passed 4*1 hour stability test at 4.2 K
 | MCBRD_CB06 | Wet wind |  | 530 A | 
MCBRD03 | MCBRD_CB09 | Direct wind with new channel size | CERN | 530 A | Both apertures reached ultimate current 422 A, and passed stability test at 4.2 K
 | MCBRD_CB12 | Direct wind with new channel size |  | 526 A (25 quenches) | 
 | MCBRD_CB14 | Direct wind with new channel size | BAMA | 530 A (30+34 quenches), put in quarantine | 
MCBRD04 | MCBRD_CB13 | Direct wind with new channel size | IMP | 530 A (20+33 quenches) | Both apertures reached ultimate current 422 A, and passed stability test at 4.2 K
 | MCBRD_CB17 | Direct wind with new channel size | IHEP | 524 A (47 quenches) | -
MCBRD05 | MCBRD_CB18 | Direct wind with new channel size | IHEP | 530 A (43 quenches) | To be assembled
 | MCBRD_CB19 | Direct wind with new channel size | IHEP | 530 A (63 quenches) | -
 | MCBRD_CB20 | Direct wind with new channel size | IHEP | To be stand-alone tested | 
MCBRD_CB10, 11, 15, 16 |  | Shipped to CERN for fabrication |  |  | 

## Slide 20
Summary
Long-term advanced superconducting magnet R&D for future high-energy accelerators is ongoing at IHEP-CAS
16 T (Nb3Sn+HTS) model dipole has been fabricated at IHEP-CAS and under performance test at 4.2 K. Present results show very promising and encouraging performance
Strong domestic collaboration for the advanced superconductor R&D (HTS & Nb3Sn): Stainless-steel-Silver stabilized IBS tape achieved the highest Je in 2022! Significantly reduced the cost and raised the mechanical properties
HL-LHC CCT magnets going well, to be installed in the tunnel in 2026
20
Thanks for your attention!