## Slide 1
CEPC Vacuum chamber NEG coating & heating spraying production line
Yongsheng Ma
Vacuum group, IHEP,CAS
Jan 15th 2025

## Slide 2: Outline
- Preview of CEPC vacuum system
-Production line of vacuum chambers
-Prototype of cathode for NEG coating
-Spraying for heating film R&D
-Conclusion
-Acknowledgement

## Slide 3: Preview of CEPC vacuum system
Accelerator | length/m
LINAC | 1,601+335
Damping ring | 147
Booster | 100,000
Collider | 200,000
Transport line | 4,680
Total length/m | 306,763
 | E | I | ρ
 | Gev | A | m
Higgs | 120 | 0.0167 | 10700
W | 80 | 0.084 | 10700
Z | 45.5 | 0.803 | 10700
tt | 180 | 0.0033 | 10700
Machine and Vacuum Parameters
Technical developments in TDR

## Slide 4: Vacuum requirements and configuration
 | Energy | Material | Cross Section/mm | Length/m | Dynamic pressure /Torr
LINAC | 30 GeV | Stainless steel, copper | Φ20~30 | 1,601+ 335 (BTL) | Acc <2×10-7 E-gun<2×10-8
Damping ring | 1.1 GeV | Extruded aluminum 6061 | Φ30/Al 6061 | 147 | <2×10-8
Booster | 30 to 180 GeV | Extruded aluminum 6061 | Φ56/thickness of 2mm | 100,000 | <3×10-8 tt<4×10-8
Collider | 45.5~180 GeV | Extruded copper, NEG film SEY<1.2 | Φ56/thickness of 2mm | 100,000×2 | Z<8×10-10 tt<1×10-8
MDI | 45.5~180 GeV | Copper/tungsten alloy, NEG film | Φ20 | 12 | <3×10-9
LTB | 30 GeV | Stainless steel | Φ56 | 3,000 | <1×10-7
BTC(CTB) | 6 GeV | Stainless steel | Φ56 | 240×6 | <1×10-7
DL | 1.1 GeV | Stainless steel | Φ30 | 240 | <1×10-7

## Slide 5: EDR goal, scope and plan
1. Vacuum chambers massive NEG coating and heating spraying production line development
The conventional NEG coating method is not suitable for the CEPC project, as there is a need to coat a total length of 190km of vacuum chambers within a 5-year timeframe. Implementing a production line can enhance stability, ensure timely production, and reduce labor costs. Therefore, a production line incorporating NEG coating and heating spraying will be developed to explore a new method for constructing vacuum chambers for the CEPC.
The construction of the vacuum chambers for the collider rings will be completed in 5 years with the use of 2 production lines, each equipped with 1 welding oven, 7 and 2 NEG coating and spraying setups.
2024: The whole production line design and biding. key components and processing like flanges sealing automatically, heating spraying will be developed.
2025: the production line construction and debugging.
2. Optimization of NEG coating:
NEG coating is used to sustain the vacuum of beam pipe and suppress the e-clouds of positron ring. Because the resistance of NEG coating increases with the thickness increases, but the life of the NEG coating decreases significantly when the thickness is less than 200nm, it is necessary to optimize the thickness and impedance of NEG coating.
2024: Optimization the thickness of NEG coating distribution along the vacuum chamber.
2024~2025: The new composition and construction development to increase the pumping properties of NEG coating, especially increase its reactivation times (life-times).
2026~2027: Optimization the resistance of NEG coating.
Composition of 2025 CEPC proposal.

## Slide 6: CEPC vacuum chamber production line
Items | Specifications
Dimension | L 11400-d56-D62
Weight | 50~100kg
NEG coating | Thickness：200nm±30% SEY<1.1 S、Q、life-times
Spraying heating | Thickness<0.5mm Heating temperature <300℃
Important nodes and progress
Technical scheme review
Procurement bidding
2024.10
2024.12
Requirement
Due to the difference in length, two production lines will be used to complete the production of vacuum chambers for the CEPC collider. The quantity of NEG coating and spraying facilities for the two lines varies to match the production speed.
With two production lines, the all vacuum chambers of collider will be finished in 5 years.
Advantages
More stable process, less manpower, less NEG coating facility, more adaptive capacity in production, etc.

## Slide 7: Production line composition
Classification | Sub-devices | Parameters | Note
Electron-beam welder | Electron-beam gun Power supply Vacuum chamber | Meets the Length of 11.4m vacuum chamber 6 working position | Design and manufacturing
Brazing | Mechanical holder Power supply | 350℃ 11.4m long | Low temperature brazing in air by conductivity heating, expecting stead by double hole copper tube
Heating film spraying facility | Electron-beam gun Power supply Controller Mechanical Structure | Meets the Length of 11.4m vacuum chamber Multilayer Spray Ceramic and conductivity layer | R&D
NEG coating tower | Pumping system Vacuum measurement Power supply Vacuum chambers Discharge Gas Cathode、controller | Meets the Length of 11.4m vacuum chamber 6 working position Background vacuum <5e-7Pa Baking temperature 200℃ | Developing to be more fitted the production line
Measurement and testing | Dimension measurement Leakage testing | Dimension measurement 11.5m/0.1mm Leakage testing 1e-10 mbar·L/s | Design and manufacturing
Cleaning | rinsing | deionized water rinsing | Design and manufacturing
Production line auxiliary equipment | Moving band robot arm system controller | Meets the Length of 11.4m vacuum chamber | Design and manufacturing

## Slide 8: Procedure of NEG coating, spraying
Spraying
Sandblasting
Spraying_Isolation_layer
Spraying_Conductivity-layer
Spraying_Isolation-layer
Spraying_Contactor-layer
Cleaning
Outside
Inside
NEG coating
vacuum chambers, cathodes assembling by mechanical arms (flanges sealing).
Leakage testing.
Deliver the assembles to vacuum oven/ baking/ NEG coating;
Disassembly the vacuum chambers
Function | Materials | Thichness/um
Transition-layer | MCrAlY alloy | 50~100
Isolation-layer | Al2O3 cermic | ~150
Conductivity-layer | NiCr alloy | ~100~200
Isolation-layer | Al2O3 cermic | ~150
Contactor-layer | Copper | ~50

## Slide 9
NEG coating mechanism & method
Outside magnet （solenoid）
Kr+
磁环
Inside magnet
CSNS, BEPCII vacuum chambers;
Nb coating;
HEPS, LHC, MAX IV, SIRIUS, APS_U etc.
Cathode wire
Magnetron sputtering cathode
Notes: 在磁场的约束下，形成等离子体。Kr原子被等离子体电离形成Kr+，在电场加速作用下打向阴极靶，从而形成溅射作用。TiZrV原子沉积到铜基底表面形成NEG薄膜

## Slide 10: Massive production of NEG coating for CEPC——Upgrade plan
Due to the diameter of CEPC is D56, we plan to replace the cathode wire with a magnetron sputtering cathode
Permanent magnet instead of the solenoid which supplies magnetic field for DCMS;
By combining the low vacuum chamber outside of the vacuum chambers to be coated with NEG, the high vacuum process is simplified;

## Slide 11
NEG coating, VC assembly and disassembly with automatic robot arms.
Cathodes driven
Cathodes
VC assembly
Vacuum oven
layout & composition of NEG coating facility

## Slide 12: Prototype of vacuum chambers assembly

## Slide 13: Prototype of cathode for NEG coating
23000mm(23 meters)
Magnets
Isolating and supporting ring
Magnetron Cathode
~12000mm(12 meters)
Water cooling pipe
dynamic sealing for water pipe
The magnets will be driven by motor when NEG coating
Motor for magnets driven

## Slide 14: VC baking & Why spray heating film
Necessity:
In order to meet the ultra-high vacuum requirement of achieving a dynamic vacuum level of 3.0E-10 mbar.
NEG coating reactivation
The baking is the most crucial procedure in achieving ultra-high vacuum
N2
O2
H2
H2O
CO2
N2
H2
H2O
CO2
CO
O2
Heat
High
vacuum
or
inert gas
MO
MC
O
C
Too thick
Lifetime is very short under SR of CEPC

## Slide 15: Spray for heating film
Conductivity layer
Ceramic layer
Ceramic layer
Cu/ceramic transition layer
Vacuum chamber
I
Conduction
Convection
Radiation
Multilayer heating film will be coated outside of the vacuum chamber which composited by ceramic and conductivity layer
The heating temperature could reach 250℃
Heating layer
Thickness： 0.5mm
solution
Plasma spraying
Processing of spray
Cu/Ag NW
Electric heating circuit
De-icing for airplane
Related commercial products

## Slide 16: Multiple-layers spraying
Plasma spraying
Gun power：≤55KW
Process gases：Ar/N2、Ar/H2、N2/H2、Ar/He
Current：200A-800A
Electric arc spraying
Gun power： 22 KW
Efficiency：0.98
Current：max. 400 A
Voltage：max. 10 - 70 V

## Slide 17: Prototype of Spraying heating film and tests
Chart: Temperature vs Heating Power
| 0.10608465608465609 | 0.10661375661375663 | 0.16633597883597886 | 0.16865079365079366 | 0.24285714285714285 | 0.24523809523809523 | 0.28759920634920633 | 0.28888888888888892 | 0.3351851851851852 | 0.33703703703703708 | 0.38690476190476192 | 0.38740079365079372 | 0.44232804232804235 | 0.44550264550264551 | 0.50370370370370388 | 0.50595238095238104 | 0.56726190476190474 | 0.57023809523809532 | 0.63584656084656088 | 0.63961640211640214 | 0.70899470899470907 | 0.71230158730158732 | 0.75000000000000011 | 0.78958333333333341
管外温度 | 37.3 | 53.9 | 62.2 | 90 | 91 | 122.4 | 122.7 | 138.2 | 138.9 | 158 | 158.4 | 175.8 | 176.2 | 196.7 | 197 | 215.7 | 217 | 237 | 237.5 | 260 | 260.3 | 279.2 | 279.1 | 299.4
功率面密度W/cm2
管外温度/℃
Dimension: L400*D24 Substrate: copper
Function | Materials | Thichness/um
Transition-layer | MCrAlY alloy | 50~100
Isolation-layer | Al2O3 cermic | ~150
Conductivity-layer | NiCr alloy | ~100~200
Isolation-layer | Al2O3 cermic | ~150
Contactor-layer | Copper | ~50
Reheating test more than 12 times
Adhesion test in ultrasonic resining

## Slide 18: Conclusion
Production line of vacuum chambers NEG coating and spraying heating will be R&D in 2 years;
NEG coating by magnetron sputtering cathode method R&D will be carried out to adapt the production line;
Prototype of Spraying heating film and tests have been carried out, which shows a good results;
NEG coating optimization for low impedance film, Spraying for heating film plan to be carried out ;

## Slide 19
A significant amount of work has been completed in the CDR and TDR, and I would like to thank all those who have contributed to these efforts.
Thanks for the HEPS, FCC-ee project;
Acknowledgement
Thanks for your attention