## Slide 1
High Field Magnet R&D
for the Next-generation High Energy Particle Accelerators
Qingjin XU
for the Superconducting Magnet Group
Accelerator Division, IHEP-CAS
Jan 2025, HKUST

## Slide 2
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2013
Site of the project | China | Europe
Baseline technology | IBS 20~24 T to reach 125-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **
Design Scope for Next-generation Accelerators

## Slide 3
Roadmap of the High Field Magnet R&D at IHEP
Challenges: Stress control, quench protection, field quality control,……
2018-2021, 12.47T @4.2K
NbTi + Nb3Sn
2021-2025 16T @ 4.2K
Nb3Sn + HTS

## Slide 4
The ReBCO block insert coils for LPF3
Parameters | Values
L0 | 409.6 mm
L1 | 540.2 mm
Rhard | 800 mm
Aend | 6 °
R1 | 9.5 mm
Z1 | 120 mm
Ze Feng et al
Development of the 16-T Model Dipole LPF3

## Slide 5
16 T Model Dipole LPF3: Nb3Sn 13 T (Common Coil with 55 mm gap) + HTS 3 T inserts (Block & CCT)
Development of the 16-T Model Dipole LPF3

## Slide 6
The Nb3Sn coils for LPF3
Chengtao Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 7
The ReBCO CCT instert coils for LPF3
典型CCT线圈结构示意
“斜螺线管”型CCT线圈结构示意
Rui Kang et al
Development of the 16-T Model Dipole LPF3

## Slide 8
2023.8.29 Assembly completed
Stress monitoring during
assembly with FBG
Pre-stress applied with commercial hydraulic jack
Pre-stress and assembly of LPF3
Yingzhe Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 9
Current decay curve at the operating current
Varistor plus CLIQ to protect the Nb3Sn coils. The maximum hot spot is ~ 230 K
NI configuration plus dump resistor to protect the 2 HTS insert coils
Quench protection of LPF3
Development of the 16-T Model Dipole LPF3
Jinrui Shi et al

## Slide 10
Performance test ongoing from Sep 2023
The Nb3Sn coils were trained firstly, maximum current reached ~85% of Iop in Dec 2023, but showed an unstable plateau at 11 T due to one of the outmost Nb3Sn coil, probably due to insufficient pre-stress during assembly
HTS block coil was ramped independently to 100% of Iop with negligible terminal voltage
Wei Li et al
Development of the 16-T Model Dipole LPF3
55 mm 双孔径

## Slide 11
The 2nd Performance test in Feb 2024
Development of the 16-T Model Dipole LPF3
The Nb3Sn coils showed very unstable performance in the 6300-7000 A region due to one of the inner most coils, but finally passed this region and reached ~87% of Iop in the beginning of March 2024
HTS block coil was ramped independently to 120% of Iop to test its ultimate performance, but one of the lead was damaged due to the quench.

## Slide 12
Reassembly of the magnet with enhanced pre-stress
Xin Chen et al
Development of the 16-T Model Dipole LPF3
应变片监测磁体组装、降温、励磁过程
光栅光纤监测磁体组装及测试过程
2024 年 1 月

## Slide 13
Development of the 16-T Model Dipole LPF3
已完成新的铌三锡线圈所需的20芯、24芯、26芯及42芯卢瑟福缆的制作，线圈的绕制、热处理及固化
AP: 20 mm
75 mm
Wound in parallel in seven layers
2180 A
HTS Coil 9+7 T design
已完成新HTS 线圈的制作，液氮测试结果达到设计值
Fabrication of the new Nb3Sn & HTS Coils Jun. to Oct. 2024
目标磁场：10 T (LTS) + 6 T (HTS)
加速器领域国内外尚无HTS高场(>10T)下成功应用先例：快速励磁、高能量密度、场质量…

## Slide 14
Accident in Mar 14 2024
Development of the 16-T Model Dipole LPF3
The operator forgot to follow the most important step of the test manual: turn on the quench detection system, and powered the Nb3Sn coils to high current directly. 2 of 6 Nb3Sn coils were serious damaged during a quench
Plan for next months: establish a hardware interlock protection system, and re-fabricate 2 new Nb3Sn coils and 2 HTS coils, to reach 16 T by the end of 2024

## Slide 15
Development of the 16-T Model Dipole LPF3
LTS 线圈 + HTS 线圈桶外组装
线圈组件竖直吊装
线圈轴向找齐
LPF3-U 磁体组装
预紧力施加步骤及key片厚度 | 竖直方向 |  | 水平方向 |  | 轴向 |  |  |  | 
 | 西 | 东 | 北 | 南 | 西北 | 东南 | 东北 | 西南 | 中
1.西打压，无示数：（7.6+2）+0.5 | 36 | 8 | -29 | -37 |  |  |  |  | 
2.东打压，14Mpa：（4.6+2）+1+0.2 | 205 | 201 | -134 | -142 |  |  |  |  | 
3.南打压，＜5MPa：4+2（中间3*2） | 155 | 168 | 8 | 114 |  |  |  |  | 
4.北打压，＜50MPa：4+2（中间2*2+1+0.5） | 37 | 1 | 184 | 398 |  |  |  |  | 
5.西打压，＜50MPa：7.6+2+1 | 105 | 353 | 241 | 457 |  |  |  |  | 
6.西塞不锈钢块+2+1+0.5 |  |  |  |  |  |  |  |  | 
7.东打压，60MPa：4.6+2+1+0.5 | 606 | 171 | 281 | 512 |  |  |  |  | 
11.15 9：42 | 607 | 164 | 277 | 504 |  |  |  |  | 
8.轴向打压： | 603 | 164 | 279 | 512 | 1288 | 1718 | 1584 | 1401 | 
9.旋转90°（东朝上→南朝上） | 606 | 174 | 308 | 514 | 1281 | 1709 | 1541 | 1380 | 
10.南打压：80MPa/66MPa 4+2+0.5-3*2-4+2+0.2*2 | 473 | 253 | 373 | 584 | 1281 | 1679 | 1609 | 1337 | 
11.北打压:120MPa 4+2+0.5-3*2-4+2+0.5 | 511 | 432 | 576 | 773 | 1257 | 1712 | 1517 | 1372 | 
12.轴向打压： | 515 | 430 | 580 | 776 | 3228 | 3353 | 3409 | 3210 | 
13.南塞不锈钢片（yoke与pad间隙太小，塞不进不锈钢块） |  |  |  |  |  |  |  |  | 
14.东打压：100MPa：4.6+2+2 | 1229 | 597 | 672 | 863 | 3238 | 3277 | 3302 | 3276 | 
15.东塞不锈钢片 |  |  |  |  |  |  |  |  | 
16.北打压：150MPa 4+2+0.5+0.2-3*2-4+2+0.5 | 1061 | 789 | 705 | 886 | 3166 | 3287 | 3234 | 3243 | 
17.西北单侧打压：150MPa 4+2+0.5+0.2-3*2-4+2+0.5+0.2 | 935 | 913 | 707 | 829 | 3166 | 3287 | 3234 | 3243 | 
18.东北单侧打压：160MPa 4+2+0.5+0.2+0.2-3*2-4+2+0.5+0.2 | 1122 | 794 | 722 | 928 | 3163 | 3275 | 3284 | 3252 | 
11.18 15：34 | 1079 | 762 | 681 | 901 | 3114 | 3234 | 3199 | 3216 | 
19.西北单侧打压：170MPa 4+2+0.5+0.2+0.2-3*2-4+2+0.5+0.2+0.2 | 906 | 939 | 719 | 938 | 3113 | 3258 | 3162 | 3209 | 
北塞不锈钢片 |  |  |  |  |  |  |  |  | 
11.19 14:40 | 891 | 924 | 727 | 927 | 3090 | 3238 | 3166 | 3193 | 
20.加轴向中间杆 |  |  |  |  | 3061 | 3214 | 3138 | 3163 | 3388
铝筒和轴向拉杆上的应变水平均略高于0.7 mm 模拟结果，本次预紧力施加足够
Reassembly of the LPF3-U magnet Oct. to Nov. 2024

## Slide 16
Development of the 16-T Model Dipole LPF3
LPF3-U 磁体组装完成
2024.11.22
LPF3-U 磁体 Nb3Sn 线圈 training test
铌三锡线圈起始经历三次锻炼即励磁至 6905 A （~9.6 T）；最高电流达到 7080 A （设计电流的 97 %）
铌三锡线圈与 HTS 线圈磁耦合较大，导致背场励磁时中心孔径内磁场延迟较大（~0.5h），同时 HTS 感生电流导致临近铌三锡（3#，4#）线圈场强增大；大部分失超发生在3# 线圈（失超典型电压曲线如下图所示）
受限于氦循环系统的产液速率，每轮测试最多进行 3 次 training tests，随后间隔 1-2 天等待产液；因此磁体总体测试时间较长，且由于磁体在产液等待期间存在温升，再次降温后励磁多数存在一定 detraining
Magnets still have great potential for performance improvement. More R&D needed on training tests……
Main challenges: The LTS coils are strongly coupled with the HTS coils in magnetic field and stress during LTS training. the HTS induced current enhance the field strength and stress of the adjacent LTS coil, and the frequent training quench of LTS can easily cause irreversible degradation of the HTS coil.
Test of the LPF3-U magnet Nov. 2024 to Jan. 2025

## Slide 17
Development of the 16-T Model Dipole LPF3
LTS：9 T
内插 HTS 无绝缘线圈在 77 K 下独立测试时磁场近无延迟，与背场磁体联合测试存在较大磁场响应时间；
9 T 背场下 HTS 首次励磁至 900 A， 实时场强1.8 T （随后电源误动作切断电源）；再次联合测试 HTS 励磁至 1700 A，实时场强2.6 T （LTS 失超致无稳定后磁场测试值）; 最后一次联合测试HTS 励磁至 2500 A，实时场强2.72 T，维持时LTS再次失超；其中HTS 1号线圈电压明显高于其他线圈；
The HTS coils subjected to several excitation tests in both self-field and 9 T background field, with a maximum excitation current of 2.5 kA (115 % of the design current) in 9 T background field. HTS coils provide a magnetic field significantly below the design value: long delay time? current short circuit inside the coil? irreversible degradation?
计划磁体复温后进行 HTS 线圈检查及维修，同时研制一套新的 HTS 线圈，降低延迟时间，避免层间及骨架可能的分流。
Fabrication of the new HTS coil to be completed in mid-February, and a new round of test to be done in late February 2025
Test of the LPF3-U magnet Nov. 2024 to Jan. 2025

## Slide 18
Development of the 16-T Model Dipole LPF3
切片-组装的设计，避免了复杂结构的连续加工，将骨架加工的成本降低至原来的1/10；
超导带带材全程在线槽中无侧弯绕制，并拟最终使用焊锡固化，极大提升机械性能；
利用加工好的骨架顺利试绕，马上开展测试，基于结果继续优化线圈结构；
不锈钢带试绕
线圈完成绕线
R&D of the New CCT coil for LPF3-U magnet

## Slide 19
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2016
IBS 2019
IBS 2022
IBS 2025
IBS Technology: Status and Outlook
90% Stainless-steel & 10% Sliver stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.

## Slide 20
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 49 A at 4.2 K and 35 T, world’s highest record up to now
The First IBS Solenoid Coil at 35 T background field
Chunyan Li et al
2024 Supercond. Sci. Technol. 37 015001
Fabricated double pancake coils and a series-connected coil consisting of six DP coils and test at 35T

## Slide 21
IBS Technology: Status and Outlook
Quench propagation study of the IBS tapes and coils
Chunyan Li et al

## Slide 22
IBS Technology: Status and Outlook
Quench propagation study of the IBS tapes and coils
Chunyan Li et al
In 15~17K, when the transmission current of iron-based superconductor is 14-179A, the corresponding NZPV value is 0.4– 7cm/s

## Slide 23
J. Wang et al, Superconductivity 3 (2022) 100019
IBS Technology: Status and Outlook
Development of the kA class IBS transposed cable
Juan Wang et al

## Slide 24
IBS Technology: Status and Outlook
Development of the world’s first 5kA class IBS transposed cable
Juan Wang et al
World’s first IBS transposed cable reached 4660A at 4.2K、0.5T

## Slide 25
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Je= 100 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 24 T
Racetrack at 8 T
Je= 300 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA transposed cable
Je > 450 A/mm2
@ 10 T, 4.2 K
2022
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Je of IBS expected to be similar as ReBCO in 5 years with better mechanical properties and lower cost

## Slide 26
Milestone of the HL-LHC CCT Magnet Project
Development of CCT Magnets for HL-LHC
Agreement signed
btw IHEP and CERN
The qualified prototype delivered to CERN
The CCT magnet from China under test at CERN
All the 12 series CCT magnets delivered to CERN
Installation to tunnel
HL-LHC commissioning

## Slide 27
Development of CCT Magnets for HL-LHC
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.

## Slide 28: Training of MCBRD02 & MCBRD03
Development of CCT Magnets for HL-LHC
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.

## Slide 29: Training of MCBRD04
Development of CCT Magnets for HL-LHC
Satisfying performance at 4 K for both apertures, tested at IMP-CAS

## Slide 30
7 series CCT magnets have been fabricated, successfully reached the design target and delivered to CERN
Production rate for the rest of series magnets: every 3 month per magnet; to be completed by Oct 2025
Development of CCT Magnets for HL-LHC
 | Nickname CERN | Manufacturer | Remarks | Status | Location
MCBRD05 |  |  |  |  | IMP
AP1 | MCBRD_CB18 | BAMA | 532A, 42 quenches | 394A (3 quenches); 422A (+6 quenches) | 
AP2 | MCBRD_CB19 | BAMA | 530A, 68 quenches | 394A (7 quenches); 422A (+10 quenches) | 
MCBRD06 |  |  |  | On the way to CERN | 
AP1 | MCBRD_CB14 | BAMA | 530 A (30+34 quenches) |  | 
AP2 | MCBRD_CB21 | BAMA | 530 A (119quenches) |  | 
MCBRD07 |  |  |  |  | 
 | MCBRD_CB20 | BAMA | 530A (68 quenches) |  | BAMA
 | MCBRD_CB23 | BAMA | 530A (76 quenches) | 3.2KV-20.4GΩ | IHEP
 | MCBRD_CB22 | BAMA | 489A (124 quenches), put in quarantine | 3.2kV-71GΩ | IHEP
MCBRD08 |  |  |  |  | 
 | MCBRD_CB24 | BAMA | VPIing |  | BAMA
 | MCBRD_CB25 | BAMA | Waiting for VPI |  | BAMA
MCBRD09 |  |  |  |  | 
 | MCBRD_CB26 | BAMA | Outer former winding |  | BAMA
 | MCBRD_CB27 |  |  |  | 
MCBRD10 |  |  |  |  | 
 | MCBRD_CB28 |  |  |  | 
 | MCBRD_CB29 |  |  |  | 

## Slide 31
Summary
Long-term advanced superconducting magnet R&D for future high-energy accelerators is ongoing at IHEP-CAS
16 T (Nb3Sn+HTS) model dipole has been fabricated at IHEP-CAS and under performance test at 4.2 K. Re-fabrication of damaged coils completed in October 2024, reassembly and test from November 2024
Strong domestic collaboration for the advanced superconductor R&D (HTS & Nb3Sn): Stainless-steel-Silver stabilized IBS tape achieved the highest Je in 2022! IBS coil Ic reached 49A at 35 T. 5kA class transposed cable developed.
HL-LHC CCT magnets going well, to be installed in the tunnel from 2026
Thanks for your attention!