## Slide 1: Magneto-Thermoelectrics in Cryogenic, Room, and High-Temperature Regimes
Darja Gačnik, Katja Klinar, Radel Gimaev, Oumayma Chdil, Andrej Kitanovski
MATERIAL AND DEVICE INNOVATIONS

## Slide 2
1 Why thermoelectrics?
2
thermoelectric effect (TE):
PELTIER EFFECT
SEEBECK EFFECT
[Huo B. and Guo C. Y., Molecules 2022]

## Slide 3
1 Why thermoelectrics?
3
thermoelectric effect (TE):
potential applications - environmentally-friendly, no mechanically moving parts, no emissions
  waste heat recovery by energy harvesting
    HIGH – ROOM TEMP.: automobile exhaust, industrial waste excess heating power
    CRYO. – ROOM TEMP.: cryo-medium (LN2, LNG) excess cooling power
PELTIER EFFECT
SEEBECK EFFECT
[Sun et al., Energy Conversion and Management 2005]
[Ge et al., Energy 2021]

## Slide 4
1 Why thermoelectrics?
4
thermoelectric effect (TE):
potential applications - environmentally-friendly, no mechanically moving parts, no emissions
  waste heat recovery by energy harvesting
    HIGH – ROOM TEMP.: automobile exhaust, industrial waste excess heating power
    CRYO. – ROOM TEMP.: cryo-medium (LN2, LNG) excess cooling power
  solid-state cooling – electrical (adaptive) control
    electronic systems, laser diodes, infrared detectors, superconducting systems and quantum qubits
  solid-state thermal management
  TE thermal switches: adaptive thermal control
  TE thermal diodes: enhanced heat flow in one direction by using TE materials with different s
PELTIER EFFECT
SEEBECK EFFECT

## Slide 5
1 Why thermoelectrics?
5
benefits: lightweight, small, inexpensive
challenges: TE material selection, optimal device performance
difficult to obtain high !
Minimize by enhancing phonon scattering?
(point defects, dislocations, nanostructures, multiscale defect structures)
DOESN’T WORK FOR CRYOGENICS!
MAGNETIC-FIELD ENHANCEMENT!
[Mao et al., Nature materials 2021]

## Slide 6
1 Why magneto-thermoelectrics?
6
enhancing thermoelectric effect by applying external magnetic fields
potential applications:
  (adaptive) cryogenic cooling
  magnetic field sensing
challenges:
  TE material selection
  magnetic field generation
  optimal device performance
DEVICE-LEVEL OPTIMIZATION APPROACH
[Our progress toward quantum error correction]
H2FLY - Realizes hydrogen-powered zero-emission aviation.
[D. Gačnik, personal archive, Airbus UpNext’s ASCEND – Advanced Superconducting and Cryogenic Experimental powertraiN Demonstrator]
MTE

## Slide 7
7
DEVICE-LEVEL OPTIMIZATION:
  operational temperature: cryogenic, room-, and high-temperature regimes
  MAGNET type:
    low-T & high-T superconductors
    permanent ferromagnets
    (electromagnets)
  MTE material:
  optimized Seeback coefficient – max. voltage output
  optimized – max. efficiency
  optimized and – best MTE performance!
  thermal management: magnet-induced, resistive (Joule), and parasitic heat losses
  manufacturability: balancing rare earth material costs
2 Magneto-thermoelectrics device
TEMPERATURE-DEPENDENT!
TEMPERATURE-DEPENDENT!
TEMPERATURE-DEPENDENT!

## Slide 8
8
MAGNET type:
  ~ 2 T up to 25 K: low-T superconducting magnets – 4 K: up to 25 T, 20 K: up to 6 T
  ~ 2 T up to 90 K: high-T superconducting magnets – 4 K: up to 100 T, 20 K: up to 50 T
  ~1.4 - 2 T in all cryogenic regime: permanent magnets (Nd₂Fe₁₄B, SmCo)
MTE material:
  10 – 100 K: Bi & Bi-Sb Alloys
  → under 5-9 T (anisotropic Fermi surface)
  90 – 110 K: high-Tc superconductors (YBa₂Cu₃O₇, Bi-2223)
  → under 3-8 T (vortex movement in the vortex-liquid phase)
  150 – 300 K: topological insulators (Bi₂Te₃, Sb₂Te₃)
  → under 1-3 T (spin-momentum-locked surface-state disruption)
3 Cryogenic magneto-thermoelectrics

## Slide 9
9
MTE material – tailored to temperature range, and optimization, and applied magnetic field
3 Cryogenic magneto-thermoelectrics

## Slide 10
10
MTE material – novel processing techniques new (M)TE candidates?
3 Cryogenic magneto-thermoelectrics
conducting polymer polyaniline (Pani) doped with camphor sulfonic acid synthesized in semi-crystalline nanostructures
[Nath et al., Applied Physics Lectures 2014]

## Slide 11
11
passive legs based on HTSC (YBa2Cu3O7) films
n-legs from Bi0.91Sb0.09
CRYOGENIC MAGNETO-THERMOELECTRIC COOLER
[Sidorenko et al., Cryogenics 2020]
3 Cryogenic magneto-thermoelectrics

## Slide 12
12
MAGNET type:
  0.3 - 2 T: permanent magnets (Nd₂Fe₁₄B, SmCo)
  0.5 - 5 T: electromagnets – water/air cooling, tunable field strength
  5 - 7 T: PM+ EM hybrid magnets – water/air cooling, tunable field strength
  3 - 5 T (at 77 K): SC magnets – (local) LN2 cooling, tunable field strength
4 Near-room-temperature magneto-thermoelectrics
Material Class | Example Materials | T Range (K) | S (0T) [µV/K] | S (2T) [µV/K] | ZT (0T) | ZT (2T)
Heusler Alloys | Co₂MnSi, Co₂FeAl, Co₂TiSn | 200 – 400 K | 150 – 250 | 180 – 300 | 0.05 – 0.3 | 0.15 – 0.4
Half-Heusler Alloys | CoTiSb, FeNbSb, NiMnSb | 250 – 400 K | 100 – 200 | 130 – 250 | 0.1 – 0.4 | 0.25 – 0.5
Manganites | La₁₋ₓCaₓMnO₃, LaSrMnO₃ | 200 – 350 K | 150 – 250 | 180 – 280 | 0.08 – 0.3 | 0.2 – 0.45
Topological Materials | Mn₃Sn, Fe₃Sn₂, MnBi₂Te₄ | 200 – 350 K | 200 – 300 | 250 – 350 | 0.15 – 0.5 | 0.35 – 0.75

## Slide 13
13
MTE material:
  120 – 350 K: Topological Materials
4 Near-room-temperature magneto-thermoelectrics
Bi88Sb12
[Pan et al., Nature Materials 2025]
Potential application:
LOW-TEMPERATURE THERMOELECTRIC COOLER

## Slide 14
14
MAGNET type:
  0.3 - 2 T: permanent magnets (Nd₂Fe₁₄B, SmCo)
  0.5 - 5 T: electromagnets – water/air cooling, tunable field strength
  5 - 7 T: PM+ EM hybrid magnets – water/air cooling, tunable field strength
5 High-temperature magneto-thermoelectrics
Material Class | Example Materials | T Range (K) | S (0T) [µV/K] | S (2T) [µV/K] | ZT (0T) | ZT (2T)
Skutterudites | CoSb₃, FeSb₃ | 500 – 800 K | 100 – 150 | 120 – 180 | 0.2 – 0.7 | 0.4 – 1.0
Si-Ge Alloys | Si-Ge (p-type, n-type) | 700 – 1000 K | 80 – 120 | 100 – 150 | 0.5 – 1.0 | 0.8 – 1.5
Antiferromagnetic Compounds | Mn₁₋ₓCrₓSb, MnTe | 600 – 900 K | 150 – 250 | 180 – 300 | 0.3 – 0.9 | 0.6 – 1.3
Ferromagnetic Oxides | La₁₋ₓSrₓMnO₃, SrRuO₃, Fe₂O₃ | 600 – 1000 K | 100 – 200 | 130 – 250 | 0.2 – 0.8 | 0.5 – 1.1

## Slide 15
15
5 High-temperature magneto-thermoelectrics
Potential application:
HIGH-TEMPERATURE MULTIFUNCTIONAL COMPOSITE MAGNET ENABLING GIANT TRANSVERSE THERMOELECTRIC CONVERSION
[Ando et al., preprint 2024]

## Slide 16
6 Conclusions
16
magnetic field application enhances thermoelectric performance
  enables tunable Seebeck coefficient () and efficiency ()
  expands TE applications beyond conventional materials
MTE materials – optimized for different temperature regimes and corresponding applications
  Cryogenic: Bi-Sb, YBa₂Cu₃O₇ (HTSC) quantum & space cooling
  Room-T: Mn₃Sn, Fe₃Sn₂ → magnetic field sensors, cooling
  High-T: Skutterudites, Si-Ge → waste heat recovery
MTE applications: magnetic field sensors, energy harvesting, MTE solid-state cooling
challenges & future directions thermal management: control of magnetically induced heating, Joule losses device optimization: hybrid magnets and optimal operational temperature ranges, new MTE materials scalability: overcoming rare-earth dependency for real-world applications

## Slide 17: Thank you.
The authors acknowledge the financial support of the Slovenian Research Agency for the research core funding No. P2-0223 and Magccine project, which has received funding from the EU’s Horizon Europe research and innovation programme through the EIC under the grant agreement No. 101161135.

## Slide 18
18
thermal management:
  magnet-induced heating
    eddy currents: induced in conductive TE materials when exposed to AC or varying magnetic fields
    magnetoresistance: field-dependent resistance in some TE leads to additional Joule heating
    vortex dynamics: in type-II SC magnets vortex movement leads to dissipative losses in the vortex-liquid phase
  resistive (Joule) heating
    MCE material and el. contacts
    at metal-TE interfaces electrical contact resistance causes localized heating
    resistive stabilizer in SC magnets (and electromagnets)
  parasitic heat losses
    radiative heat transfer
    thermal link to the ambient
2 Magneto-thermoelectric device
TEMPERATURE-DEPENDENT!

## Slide 19
19
MTE material:
  optimized Seeback coefficient S – max. voltage output
    magnetic field sensors: high S ensures a strong voltage response to small B-field variations
    TE devices: even small ΔT can generate large voltage
    TE cooling systems: high S enables a stronger Peltier effect
  optimized ZT – max. efficiency
    power generation: waste heat recovery, energy harvesting, space applications
    thermal-to-electrical conversion for sustainable energy systems
    MTE devices where efficiency is the primary goal
  optimized S and ZT – best MTE performance!
    thermoelectric-magnetic hybrid systems (high efficiency + strong mag. field tunability)
    transverse thermoelectric devices (ANE, Nernst, spin Seebeck effects in MTE devices)
2 Magneto-thermoelectric device