## Slide 1
Ultrastable Lasers
New Developments and Challenges
Uwe Sterr, Jialiang Yu, Thomas Legero, Sofia Herbers,
Daniele Nicolodi, Mona Kempkes, Chun Yu Ma, Fritz Riehle
Physikalisch-Technische Bundesanstalt, Braunschweig Germany
Dhruv Kedar, John M. Robinson, Jun Ye
JILA, NIST and University of Colorado, Boulder, CO, USA
The 9th Symposium on Frequency Standards and Metrology
Kingscliff, Australia , 16-20 October 2023

## Slide 2: Progress of cavity-stabilized lasers
S. Häfner,
PhD thesis (2015)
40 cm ULE
21 cm silicon
@ 124 K
21 cm
silicon
@ 124 K
6 cm
silicon
@ 4 K
48 cm
ULE
JILA/
PTB
PTB/
JILA
PTB
PTB/
JILA
JILA/
NIST
10-16
1 × 10-17 ?
Notes: Long history both room temperature and cryogenic cavities. Now with silicon 4 times 10-17. I want to show the next step towards the 1 times 10-17 range.

## Slide 3: Transportable 1400 nm Sr clock laser
fused-silica mirror substrates
crystalline AlGaAs/GaAs
mirror coatings
20 cm ULE glass spacer
S. Herbers, S. Häfner, S. Dörscher, T. Lücke, U. Sterr and C. Lisdat Opt. Lett. 47, 5441-5444 (2022)
acceleration sensitivity: 3(3)×10-11/g

## Slide 4: Cryogenic silicon optical resonator
Silicon spacer
dielectric mirror coatings
L = 212 mm
T = 124 K zero thermal expansion
Si2
Si3

## Slide 5: Cryogenic silicon optical resonator
Two systems with dielectric coatings
L = 212 mm
T = 124 K
Stability limited by thermal noise to 4×10-17
Si3 moved to JILA in 2017
next steps - reduce thermal noise
D. Matei et al., Phys. Rev. Lett. 118, 263202 (2017)

## Slide 6: Flywheel for an optical timescale
daily measurements to Sr-lattice clock with 25 % uptime
estimated error < 150 ps over one month
cavity drift in June 2023:
-48 µHz/s
-4.1 Hz/day
at 1542 nm
(about 1000 times less than ULE)

## Slide 7: Brownian Noise in Fabry-Perot Cavities
High-finesse optical cavity
L
thermal noise for a 20 cm long cavity:
K. Numata, A. Kemery, J. Camp, Phys. Rev. Lett. 93, 250602 (2004)
thermal noise reduction:
go to low temperatures T
enlarge cavity length L
choose low loss material
enlarge mode diameter
Fluctuation-dissipation theorem relates length fluctuations to mechanical loss jx
T =124 K

## Slide 8: AlGaAs crystalline mirror coatings
GaAs/
AIGaAs
DBR disc
silicon
substrate
Cole et al., Nat. Phot. 7 (2013) 644
Cavity length | L = 212 mm
Mirrors | 2x plano-concave (2 m ROC)
Finesse | 380 000 at 124 K
Free Spectral Range | 707 MHz
Birefringent mode splitting | 200 kHz
Thermal noise | mod sy(t) = 1×10-17
 = 2.5×10-5
 = 5×10-4
sy(t) = 1×10-17
sy(t) = 4×10-17
coating: nslow > nfast
Slow Axis
Fast Axis
GaAs

## Slide 9: Novel noise contributions at low temperatures
birefringent noise
even with stabilized laser power
anticorrelated in fast and slow axis
correlation length < mode diameter
so far only observed at 4K, 16K, 124K
global excess noise
remaining noise when averaging birefringent noise
exceeds Brownian thermal noise
correlation length > mode diameter
light-modified birefringence
non-thermal, light-induced change of cavity resonance
different sign for fast and slow axis
time constant of many hours !
Dnstat ≈ 10-4
Dnphoto ≈ 10-8
Dnnoise ≈ 10-10

## Slide 10: Novel noise contributions at low temperatures
light-modified birefringence
non-thermal, light-induced change of cavity resonance
different sign for fast and slow axis
time constant of many hours !
Dnstat ≈ 10-4
Dnphoto ≈ 10-8
linear electro-optic effect ?
Dn ≈ r41 n03 E
electro-optic tensor component r41 = 1.5 pm/V
refractive index GaAs n0 ≈ 3.48
E ≈ 3 kV/m
small compared to electric field strengths in heterojunctions
Possible explanation:
Light is exciting carriers in the AlGaAs / GaAs
semiconductor building up electric field along
the coating ?
S. Namba, J. Opt. Soc. Am. 51, (1961) 76 L. Ho, C. Buhrer, Appl. Opt. 2, 647 (1963)

## Slide 11: Measurements at 124 K and 4 K
PTB 21 cm Si cavity at 124 K
JILA 6 cm Si cavity at 4 K
Birefringent noise
1/f excess noise
Non-thermal

## Slide 12: Stability at 124 K
Origin of remaining noise:
Brownian thermal noise?
j(124 K) ≫ j(300 K) ?
Other unidentified noise?
Birefringent noise can be removed with polarization averaging
The remaining frequency stability sy ≈ 4×10-17 is still higher than predicted thermal noise
AlGaAs single polarization
AlGaAs polarization averaged
dielectric coating
expected Brownian noise
technical noise

## Slide 13: Spatial noise correlation on mirror
Local noise
Global noise
Coating Brownian thermal noise
Birefringent noise
Cavity temperature fluctuation
Vibrations
Thermo-optic noise (т > 1 s)
etc.
Notes: For local noise, the freq. fluc. Of the two HG modes are partially uncorrelated.
We used the method described in the following slides to determine the spatial correlation of birefringent noise, it turned out that birefringent noise is also a local noise

## Slide 14: Measurement of Brownian thermal noise

## Slide 15: Brownian thermal noise
Mode | HG00 | HG01 | HG00-HG01
Integration profile |  |  | 
Scaling of mod |  |  | 
Predicted noise level | mod | mod | mod
Measured/calculated |  |  | 
Mode | HG00 | HG01 | HG00-HG01
Integration profile |  |  | 
Predicted noise level |  |  | 
Measured/calculated |  |  | 
Determine upper limit of coating Brownian thermal noise
φ(124 K) ≈ φ(300 K)
mod
mod

## Slide 16: Further investigations at room temperature

## Slide 17: Sensitivity to external light
GaAs (115.6 nm)
Al0.92Ga0.08As (133.2 nm)
Fused Silica
Δn (Iext)
38.5 layer pairs
LED

## Slide 18: Wavelength-dependent sensitivity
GaAs (115.6 nm)
Al0.92Ga0.08As (133.2 nm)
Fused Silica
Δn (Iexr)
38.5 layer pairs
LED
fractional sensitivity (arb. u.)

## Slide 19: Outlook
EMPIR – European Metrology Programme
cryogenic cavities,
e.g.
10 mK closed-cycle dilution cryostat
12 kg silicon spacer
@ FEMTO-ST
spectral holes
nanostructured mirrors
large modes
vibration isolation

## Slide 20: Nanostructured mirrors
R ≈100%
reflectance (%)
wavelength (µm)
Stefanie Kroker’s group at TU Braunschweig:
silicon nano-grating on low index fused silica substrate
- low thermal noise
fused silica
silicon
J. Dickmann and S. Kroker, Phys. Rev. D 98, 082003 (2018)
Meta-Etalon mirror
combine grating R1 ≈ 99.9 % with rear dielectric mirror R2 ≈ 99.9 %
thermal noise is mostly determined by silicon grating
sy = 4×10-18 @ 124 K possible
First results of cavity with one meta-etalon:
Finesse 12 000
R ≈ 99.95%
S. Dickmann et al.
Commun. Phys. 6, 16 (2023)
dielectric coating

## Slide 21: Large mode area cavities
Larger mode size:
smaller averaged thermal coating noise
21
1
-1
1
1
-1
concentric
plane parallel
Large modes
at the edge of stability
Problems:
mirror manufacturing
cavity assembly, tolerances: mode shifts 1 mm for 10 arcsec deviation
R1 | R2 | rel. sy
1 m | plane | 1.00
2 m | plane | 0.84
5 m | plane | 0.67
10 m | plane | 0.56
20 m | plane | 0.47
50 m | plane | 0.37

## Slide 22: Transportable 124 K Si system
compressor
CryoFan
pulse tube cold head + heat exchanger
heat
exchanger
resonator
with locking mechanism
Cool cavity to 124 K by circulating cold gas between pulse tube cooler and cavity environment
Lock cavity during transport

## Slide 23: Summary
  Summary
  silicon cavities at 124 K with dielectric coating reach thermal noise limit instability of 4×10-17
  crystalline coatings so far do not provide lower instability
  Outlook
  low-noise nanostructured meta-etalons F ≈ 12 000
  operation at 4 K
  transportable systems
  Funding
SFB 1227
EXC2123 QuantumFrontier
Max Planck-RIKEN-PTB Center for
Time, Constants and Fundamental Symmetries

## Slide 25: LN2-based 124K cooling system
Replace the open loop LN2 system by a He-gas cooled, closed-cycle cooling to get a stand-alone and low-maintenance system.
drawbacks:
LN2 infrastructure needed
about 400 liters LN2/ week needed
two refills per week (holidays, X-mas …)
about 10 W cooling power needed

## Slide 26: 124 K Cryostat
temperature fluctuations
vertical vibration noise
T. Kessler et al., Nature Phot. 6, 687-692 (2012)
required vibration sensitivity
∆L/L < 10-10 / ms-2
~ 5 · 10-6 ms-2/Hz1/2
4 · 10-8 K
αSi (T0 - 50 mK) < 1·10-9 K-1

## Slide 27: Long-term drift
Long-term frequency drift
~ 4 Hz/day - 2.4×10-19/s
about 103 times smaller than ultralow expansion materials at room temperature
less than Hubble constant
H0 = 2.27×10-18/s
Cavity frequencies vs. H-Maser
June 2023:
-48 µHz/s
-4.1 Hz/day

## Slide 28: Parasitic Etalons
MJD
Periodic frequency fluctuation
related to air pressure
Cavity rear
Optics
Cavity front
R
L
Parastic etalons
Model: ∆p → ∆n → ∆φ → δν
Rp = 1.2 × 10-6, L = 0.41 m
optimized: Rp < 5 × 10-8
light is fed back to cavity mode
with parasitic reflectivity
to
field changes mirror reflectivity (as seen from inside the cavity):

## Slide 29: Thermal-noise Zoo
Brownian (thermal) noise: internal friction in coating, mirror, spacer
Thermo-elastic: thermal expansion from temperature fluctuations
Thermo-refractive: refractive index change from temperature fluctuations
many more ...
M. L. Gorodetsky Thermal noises and noise compensation in high-reflection multilayer coating, Phys. Lett. A 372, 6813-6822 (2008)
Thermal noise Sx(f) for fused silica mirror with SiO2 / Ta2O5 coating at 300 K l = 1542 nm, w = 400 µm
kBT

## Slide 30: Evaluation of technical noise
All technical noise sources are suppressed to below 10-17
residual amplitude modulation (RAM)
vibrations with additional low frequency servo loop
….

## Slide 31: AlGaAs coating - transient response
All thermal noise contributions are proportional to mechanical loss factor f:

## Slide 32: Transient response – power dependence
298 K
124 K
So far no simple explanation
semiconductor properties?
electric fields from internal photoeffect?
electrooptic/photorefractive effect?
Further investigations necessary:
temperature
spatial correlations
relation to noise

## Slide 33: Compound Mirror Performance
J. Dickmann and S. Kroker, Phys. Rev. D 98, 082003 (2018)
R1 = 0.999
R1 = 0.993
R1 = 0.9999
dielectric coatings
Ultrahigh reflectivity: combine grating R1≈ 99.9 % + rear dielectric mirror R2 ≈ 99.9 %
Thermal noise mostly determined by silicon grating - sy = 4×10-18 @ 124 K possible

## Slide 34: Improvements on Silicon Systems
Goals:
Stand-alone system
(towards field use)
Reduce impact of by vibrations by
additional feedback on AVI and feedforward technique (WP2)

## Slide 35: He-based closed cycle cryostat
Cryo system from TransMIT arrived at PTB
Check cooling performance and vibration level on test system.
Replace LN2-based cooling system of Si5 (124 K, 21 cm silicon, AlGaAs coatings)

## Slide 36: Crystaline AlGaAs / GaAs multilayer
G. Cole et al., Nat. Phot. 7 (2013) 644, Winkler et al., Optica, 8 (2021) 686, G. Cole, Proc. SPIE, (2012) 8458, 845807
epitaxially grown crystaline multilayer (1064 nm, 1156 nm, 1397 nm, 1550 nm)
typ. Silicon or
Fused Silica
GaAs/
AIGaAs
DBR disc
transferred to arbitrary optical substrates
high refractive index GaAS
low refractive index AlxGa1-xAs
Low optical absorption and scatter (A+S < 16 ppm)
lower mechanical loss than dielectric coatings
F = 400 000
dn = 1.8 kHz
JILA (6 cm)
4 K
PTB (21 cm)
124 K
F = 290 000
dn = 8.6 kHz
SiO2 /Ta2O5
reduced Brownian Thermal Noise

## Slide 37: Birefringent noise – power dependence
D. Kedar et al. Optica 10, 464 (2023) https://doi.org/10.1364/OPTICA.479462
J. Yu, et. al,, arXiv:2210.15671 [physics.optics] https://doi.org/10.48550/ARXIV.2210.15671
Notes: We see power dependence, but don’t understand the effect

## Slide 38: Excess noise
Global noise
The excess noise:
Long correlation length
1/f slope in PSD
Independent of optical power
Notes: we observed an excess noise which is possibly related to the semiconductor property of the coatings.
On a level comparable to the thermal noise level of dielectric coatings.

## Slide 39: Change of splitting by intracavity power
w0 = 0.5 mm
GaAs (115.6 nm)
Al0.92Ga0.08As (133.2 nm)
Fused Silica
Δn (Icavity)
38.5 layer pairs