## Slide 1: Compact and Manufacturable Ultrastable Optical Reference Cavities: 10-14 Stability in Less Than 10 mL Volume
Franklyn Quinlan
NIST Time and Frequency Division
fquinlan@nist.gov
9th Symposium on Frequency Standards and Metrology
October 2023

## Slide 2: Preview
Microwave signals with optical clock stability
Compact optical reference cavities
2.54 cm

## Slide 3: Optical clock frequency down conversion
Goal: establish that an optical frequency comb and high-speed photodetector can support optical clock stability (10-18) stability on a 10 GHz carrier
Leopardi et al, Optica 4 p. 879 (2017)

## Slide 4: Optical clock frequency down conversion
Goal: establish that an optical frequency comb and high-speed photodetector can support optical clock stability (10-18) stability on a 10 GHz carrier
Baynes et al, Optica 2 p. 141 (2015)
10 GHz carrier

## Slide 5: Phase coherent down-conversion
Highly correlated phase records
Scaling should be given by (259 THz/10 GHz)
T. Nakamura et al, Science 368, p. 889 (2020)
Optical clock signals provided by A. Ludlow & team

## Slide 6: Phase coherent down-conversion
Highly correlated phase records
Scaling should be given by (259 THz/10 GHz)
Correlation coefficient= 0.998
rms timing error: 900 attoseconds
T. Nakamura et al, Science 368, p. 889 (2020)

## Slide 7: Frequency down-conversion
State-of-the-art optical clocks
Optical-to-microwave frequency ratio:
OFD1: 25912.2626487667098(25)
OFD2: 25915.8720255287493985(25)
T. Nakamura et al, Science 368, p. 889 (2020)

## Slide 8: Accuracy of optical-to-microwave conversion
 | Optical Frequency (Yb1-Yb2) | fractional
Optical beat note | -0.0152862 Hz | (-5.8986±0.095)×10-17
Microwave + calculation | -0.0152926 Hz | (-5.9011±0.096)×10-17
Parameters | Values
Absolute frequency of Yb1 (including all AOM shifts) | 259147886795431.25 Hz (±2.1×10-16)
 | 126.5 MHz
Hydrogen maser shift | 1 – 6.46×10-13 (fractional)
Mode number of comb1 () | 1243788
Mode number of comb2 ( | 1658615
Frequency tuning word of DDS () | 103069168
Frequency tuning word of SDR () | 59821114
difference frequency () | -12.694921924988 Hz
(from Eq. 20) | -0.0152926 Hz
Parameters | Values
 | 259147886795431.25 Hz (±2.1×10-16)
 | 126.5 MHz
Hydrogen maser shift | 1 – 6.46×10-13 (fractional)
 | 1243788
 | 1658615
 | 103069168
 | 59821114
 | -12.694921924988 Hz
 | -0.0152926 Hz

## Slide 9: Preview
Microwave signals with optical clock stability
Compact optical reference cavities
2.54 cm

## Slide 10: Compact optical reference cavities
(to scale)
30 cm
NIST Yb clock laser cavity
Stability ~1-2x10-16 at 1 second

## Slide 11: Compact optical reference cavities
High finesse
Mirrors with large radius of curvature
Manufacturable – no more individual hand assembly
Passive vacuum pumping – no more ion pumps
Fractional frequency stability at 10-14 or better
30 cm
NIST Yb clock laser cavity
Charles McLemore performing an optical contact bond
16 mm
Wish list

## Slide 12: Applications of compact ultrastable cavities
Mobile optical clocks
Low noise microwave generation
Environmental sensing
Marra, et al. Science 361, 6401 (2018)
Marra, et al. Science 376, 6595 (2022)
Mazur, et al. arXiv:2303.06528 (2023)
Frequency (Hz)
Frequency PSD (dBHz2/Hz)
Fortier et al, Nat. Photon. 5 (2011)
Xie et al, Nat. Photon. 11 (2017)
Jammi et al, CLEO 2022

## Slide 13: Applications of compact ultrastable cavities
Mobile optical clocks
Low noise microwave generation
Environmental sensing
Marra, et al. Science 361, 6401 (2018)
Marra, et al. Science 376, 6595 (2022)
Mazur, et al. arXiv:2303.06528 (2023)
Fortier et al, Nat. Photon. 5 (2011)
Xie et al, Nat. Photon. 11 (2017)
Jammi et al, CLEO 2022
400 km span

## Slide 14: Survey of the state-of-the-art in FP stabilized lasers
G.D. Cole, et al., Nat. Photon. 7, 644 (2013)
D. Leibrandt, et al., Opt. Exp. 19, 3471 (2011)
D. Leibrandt, et al., Phys. Rev. A 87, 023829 (2013)
A. D. Ludlow, et al. Opt. Lett. 32, 641 (2007)
B. Argence, et al., Opt. Exp. 20, 25409 (2012)
D. Świerad, et al. Sci. Reports 6 33973 (2016)
cryogenic cavity
T. Kessler, et al. Nat. Photon. 6, 687 (2012)
D. G. Matei, et al., arxiv: 1702.04669 (2017)
B. C. Young, et al. Phys. Rev. Lett. 82, 3799 (1999)
Y. Yiang, et al. Nat. Photon. 5, 158 (2011)
M. Schioppo, et al., Nat. Photon. 11, 48 (2017)
Jun Ye’s group at JILA
S. Häfner, et al. Opt. Lett. 9, 2112 (2015)
J. Davila-Rodriguez, et al., Opt. Lett. 42, 1277 (2017)
S. Webster & P. Gill, Opt. Lett. 36, 3572 (2011)
C. McLemore, et al. PRA 18 054054 (2022)
M. Kelleher et al, arXiv:2301.08822 (2023)
Original plot credit: J. Davila-Rodriguez

## Slide 15: A glass menagerie
In-vacuum bonded cavities
Microfabricated mirror-based cavities

## Slide 16: Microfabricating high finesse mirrors
N. Jin, et al., Optica 9, 965-970 (2022)
Kharel, et al., APL Photonics, 3, 066101 (2018).
FS or ULE
Increasing Reflow
Reactive Ion Etch
Mirror Fabrication
Stop reflow
Tailorable mirror ROC and size
Photoresist pattern is transferred to substrate via RIE
Photoresist disk
Mirror reflectivity > 99.9996%
ROC
ROC
Cavity ringdown & finesse
Mirror profiles
Large ROC
Small ROC
Mirror layout

## Slide 17: Million finesse micromirrors
Demonstrated ROC covers ~4 orders of magnitude
Applications range from cavity QED (small ROC) to optical clocks (large ROC)
1 million-level finesse produced with high yield
Naijun Jin, et al., Optica 9, 965-970 (2022)
Survey of state-of-the-art mirror finesse
Finesse compendium

## Slide 18: Micromirror cavities
C. A. McLemore, et al., Phys. Rev. Appl. 18, 1 (2022)
Micromirrors are paired with a single flat mirror
Three independent cavities in a single 8 mL volume structure
Each cavity has a finesse ≥ 0.9 million

## Slide 19: Micromirror cavity phase noise and stability
Thermal noise limited performance
measurement setup

## Slide 20: Micromirror cavity + chip-scale laser
SOA
EOM
PDH Servo
To AOM frequency
Stabilized laser output
Diode laser injection-locked to SiN ring
1 Hz integrated linewidth laser
Cavity thermal noise limited to ~4 kHz
10-14 fractional frequency stability at 1 s
J. Guo et al, Sci. Adv. 8 (2022)
μFP cavity
RBW = 10 Hz
Phase noise
AOM
SIL Laser
Linewidth
Q > 12 billion

## Slide 21: Micromirror cavities – reduction in size
Cavity ringdown statistics
Mirror profile
Example cavity ringdown
Finesse = 462,000
½”
1”
3 μ-mirrors
1550 nm
1 μ-mirror
1396 nm
Half-inch diameter decreases volume from 8 mL to 2 mL
Protected annulus on micromirror substrate guarantees reliable bond
Finesse is sufficient to reach thermal noise limit
ROC: 0.8 m
Sim. scattering loss: 0.6 ppm
Mirror fab steps
contact annulus
μ-mirror

## Slide 22: Cavity in a custom can
Heat shield/rigid holder
½” diameter cavity
Macor base
Custom vacuum can
Fixed pigtailed collimator
External Alignment Jig
Assembled Vacuum System
fiber input
epoxy
Performance currently under evaluation

## Slide 23: A glass menagerie
In-vacuum bonded cavities

## Slide 24: Phase noise vs. air pressure
Meas. limit
Test cavity
Spacer length: 6.3 mm
Spacer diameter: 27 mm
Mirror thickness: 6.35 mm
Cavity is placed within a vacuum chamber with pressure monitoring
Optical phase noise is measured at different pressure settings
Tests indicate only modest vacuum ~1 torr is required to reach thermal noise limit
0.23
Optical Phase Noise

## Slide 25: In-vacuum cavity bonding
19.05 mm
25.4 mm
Residual gas noise
Gas molecules perturb the optical phase as they transit the beam
Noise model*:
*Zucker & Whitcomb, LIGO (1994)
Thermal noise limited phase noise
Still holding vacuum and going strong!
Excess noise
500 Pa (3.75 torr)

## Slide 26: “Bake n’ bond” cavity
Thermal noise limited phase noise out to 10 kHz offset without a vacuum enclosure!

## Slide 27: “Bake n’ bond” cavity
Thermal noise limited phase noise out to 10 kHz offset without a vacuum enclosure!

## Slide 28: What’s next?
Vacuum bonding
+
micromirrors
Dice into individual cavities
In-vacuum bond cavity arrays

## Slide 29: “minicube” cavity – preliminary results
10 mm
7 mm
7 mm
In-vacuum micro-FP: bonded and diced at Yale
Cavity with micro-fabricated mirror
Cavity in NIST-made holder
Preliminary phase noise
Noise matches thermal noise limit from ~10 Hz to ~200 Hz
Bake n’ bond could improve noise from 200 Hz to 10 kHz

## Slide 30: Summary
Microwave signals with optical clock stability
High finesse micro-mirror cavities
Low phase noise with in-vacuum bonding
“minicube” cavities

## Slide 31: Lots of contributors!
Funding
Peter Rakich
Naijun Jin
John Bowers
Joel Guo
Joe Campbell
Steven Bowers
Kerry Vahala
Andrew Ludlow
Scott Papp
Tara Fortier
Scott Diddams
Andrey Matsko
Vladimir Iltchenko
Wei Zhang

## Slide 33: Optical clock diagram

## Slide 34: OFD frequency

## Slide 35: OFD noise
Optical cavity @1070 nm
Er:Comb 208MHz
Er:Comb 156MHz
10 GHz
10 GHz +1.5MHz
Common
optical reference
SDR
PC
(ADC)
Phase deviation
Phase noise
Allan deviation, etc..
MHz
Two independent OFD systems
Digital sampling
Noise of reference was cancelled out
Estimate OFD system noise
48th harmonic
64th harmonic
Sampling rate: 100 Hz
No cycle slip for 12 hours
1.5 mrad
Phase fluctuation

## Slide 36: Linewidth
Optical Clock
Microwave

## Slide 37: Linewidth
Optical Clock
Microwave

## Slide 38: Linewidth
Optical Clock
Microwave

## Slide 39: Linewidth
Microwave is still transform-limited after 44000 seconds
Difference between measured sinewave and “perfect” sinewave not visible on a linear scale