## Slide 1: Low Noise Sapphire Resonators and Oscillators
1 Michael Tobar
1 Eugene Ivanov
WSG: Synthesizer Design and Frequency Generation/Synchronization Schemes for High-Performance Wireless Systems
1Quantum Technologies and Dark Mater Research Laboratories, Department of Physics, University of Western Australia, 6009, WA Australia

## Slide 2: Summary
QDM Lab at UWA an Introduction
High-Q Sapphire Resonators
  Basic Properties
  Whispering Gallery (WG) Modes
  Material Properties with WG Modes
    Dielectric and Magnetic (ESR)
  Sapphire Loaded Cavity (SLC) Resonator
    No Self Noise
Resonator-Oscillators
  Description of Noise
    Time Domain and Frequency Domain
    Types of Noise
    Phase Noise and Leeson’s Model
  How to Reduce Phase Noise
    Detect Phase Noise and feedback Cancellation (PLL)
1

## Slide 3: QDM Lab

## Slide 4: QDM Lab

## Slide 5
Computer Scientist
Invented COBOL

## Slide 6
Precision Measurements @ QDM Lab Uni of Western Australia
13 Patents: Radar, Gradiometer, Sensing, Oscillators, Resonators
QDM has realized many best tests on Dark Matter, Quantum Gravity and Relativity

## Slide 7: QDM Lab Precision Metrology
Metrological Systems:
Photonic
WGM Resonators
Specially Designed Microwave Cavities
Atomic/Spins
H - Maser
Atomic Clocks
Spin Waves
Spin Ensembles in Solids
Acoustic
Superfluid
BAW Resonator
Science of precise measurement
Physics at low energies

## Slide 8
J. Phys. D: App. Phys, 26, 2276-2291, 1993
J.Phys D: App. Phys, 28, 1729-1736, 1995
Phys. Rev. Lett, 74, 1908, 1995
Rev. of Sci. Instrum., 67(7), 2435-2442, 1996
My PhD project 1989 ->1993 UWA PhD Searching GW Signal Burst at 720 Hz
CSO
Photons
Ponons
Spins
Cryogenic Resonant Bar Gravity Wave Detectors
-> Ultra precise optomechanical position measurement
-> Low phase noise read-out and pump oscillator

## Slide 9
Tunable Dielectric Cavity

## Slide 10: High-Q Sapphire Resonators
Crystal Dielectric Resonators
  -> Low loss tangent and anisotropic -> High-Q (>105@RT >105@4K)
  -> Permittivity ~ 10 -> Whispering Gallery Mode (WGM)
WGHm,1,1 (quasi-TM)– transverse magnetic, Ez and Hr
WGEm,1,1 (quasi-TE) – transverse electric, Hz and Er
-> High-Q and low temperature sensitivity resonators
-> High stability oscillators
-> Low phase noise oscillators
-> Test fundamental physics
-> Engineered Quantum Systems: spins, phonons and photons
IEEE Trans. on MTT, 9(12) 2077-2083, 1991.
IEEE Trans. on MTT, 47,6) 752-759, 1999.
Meas. Sci. Technol., 10(4) 387-392, 1999
Phys. Rev. Lett., 90, 060402, 2003.
Phys. Rev. Lett., 95, 040404, 2005.
Nature Comm., 6, 8174, 2015.

## Slide 11: Resonator basic properties
Frequency (Hz)
Amplitude
f0
fbw
QL = f0 / fbw
QL = 109 f0 = 10 GHz fbw = 10 Hz
S21: Transmission Spectrum
Loaded Q-factor
1
2
S21

## Slide 12: Sapphire Whispering Gallery
WSC-1
Temperature Q-factor (10 GHz)
300 K 2 10 5
77 K 3 10 7
4. 2 K 4 10 9
Permittivity Tensor Anisotropic
Uniaxial: ex = ey
Isotropic: ex = ey= ez

## Slide 13: WG Modes and Material Properties
Use a numerical technique to calculate the parallel, e//, and perpendicular, e, permittivities from the measured frequencies of a nearby Ez (quasi TM or WGH) and Hz (quasi TE or WGE) mode;
F1(f(H), e, e//)=0 ; F2(f(E), e, e//)=0
2) Calculate numerically the Electrical Energy Filling factors;
3) Calculate the loss-tangents parallel and perpendicular to the c-axis from the measured unloaded Q-factors. For WG modes ignore the surface resistance of the cavity since G is large.

## Slide 14
IEEE TRANSACTIONS ON MICROWAVE THEORY AND TECHNIQUES, VOL. 47, NO. 6, JUNE 1999, pp. 752-759

## Slide 15: Temperature Coefficients
4) From the Temperature Coefficients of Frequency (TCF) calculate Temperature Coefficients of Permittivity (TCP,ae)
D is the diameter of the cylinder : L is the length.
Must know Temp Coefficient of Expansion: parallel aL; perpendicular, aD.
D
L
Whispering Gallery Mode

## Slide 16: Sapphire Loaded Cavity (SLC)
WGHx,1,1 – quasi-transverse magnetic, Ez and Hr
WGEx,1,1 – quasi-transverse electric, Hz and Er
High-Q low temperature sensitivity -> High stability oscillators -> Low phase noise oscillators -> Test fundamental physics
ME Tobar and AG Mann, "Resonant frequencies of higher order modes in cylindrical anisotropic dielectric resonators" IEEE Trans. on MTT, vol 39, no. 12, 2077-83, 1991.

## Slide 17
Cryogenic Sapphire Oscillators (CSO) 1989-Now
Precision Frequency Measurement
Averaging time

## Slide 19: Whispering Gallery Modes: m>0 Degenerate mode pair Spins can break time reversal symmetry

## Slide 20: Some of Our Resonators
WG Modes
Reentrant Lattice
Reentrant: 3D LC
TE + TM Cylindrical modes
The Anyon Cavity Resonator

## Slide 21: CSO Operates Atomic Clock @ the Projection Noise Limit: Paris Observatory SYRTE since 1999
Now: Atomic or Spin Qubits at the Quantum Limit
Yb ion qubits.
Also, other systems will need low phase noise pump oscillators

## Slide 22: Sapphire Resonators add no (little) Noise

## Slide 23: Resonator Oscillators
Simplified Diagram of a Resonator-Oscillator
Noise Characterization
Two-sample deviation, also called “Allan deviation”
Spectral density of phase deviations
Spectral density of fractional frequency deviations
Single Sideband Phase noise
y()
S(f)
Sy(f)
L(f)
S(f) = (f0/f)2Sy(f); L(f)  ½ [S(f)]
 = averaging time, f0 = carrier frequency, and f = Fourier frequency.

## Slide 24: Description of Noise in Oscillators
A precision oscillator attempts to generate a pure sine wave
Amplitude and frequency instabilities exist
Oscillator voltage output may be represented in the time domain as:
Represented in the frequency domain as:
Amplitude instability with time
Apply
Wiener-Kintchine
Theorem
Carrier (Sin wave)
Spectral Density of Phase Deviations
Amplitude Noise
Phase/frequency instability with time

## Slide 25: Description of Noise in Oscillators
Two ways to express the imperfections in a sinusoidal wave (time and frequency domains)
Best description depends on the time scale: Short time scales (< 1 s) FFT of the signal => spectrum: Medium to long time scales (>1s) => frequency counter, f(t)

## Slide 26: Time Domain Representation of Frequency (Phase) Instabilities
Frequency counter counts zero crossings over a time interval, t, a time series of frequencies fk, averaged over tk is created.
Experimentally, the fractional frequency instability is characterized by the Allan Variance over M samples;
The Square Root Allan Variance (Allan Deviation) is regarded as the rms frequency fluctuation over the time interval t.

## Slide 27: Frequency Domain Representation of Frequency/Phase Instabilities
S(f)

## Slide 28: Types of Noise (Log-Log Plots)
y()
-1
-1
0
White
phase
Flicker
phase
White
freq.
Flicker
freq.
Random
walk freq.
-1/2
1/2
White phase
White frequency
Flicker Frequency
Random Walk
Flicker phase
Fourier Frequency, f
S(f)


## Slide 29: Lesson’s Model
Noise in free running oscillator depends on the amplifier phase noise and Cavity Q-factor = f0/Df (f is Fourier frequency)

## Slide 30: Phase Noise in Microwave Oscillators
Signal out
j
Resonator
Amplifier
Df
fres
~ Df
F
Oscillator phase noise spectrum
How to reduce this noise?
-> Detect noise then cancel
-> Sensitivity of phase detection new limit
-> Ultimate sensitivity?

## Slide 31: How to Reduce Phase Noise in a Resonator-Oscillator
Use a phase detector in the loop to detect the noise feed-back and cancel -> Phase Locked Loop (PLL)
Ultimate limit is the noise in the detector, which in principle can be thermal due to a Carrier Suppression Interferometer.
Practical limitations exist like the gain required to feed back and cancel the amplifier noise
IEEE MGW LETTERS. P-108, VOL. 5. NO. 4, APRIL 1995
Mixer phase detector
IEEE MGW LETTERS. P-312, VOL. 6. NO. 9, APRIL 1995
General phase detector
PLL
PLL

## Slide 32
1993 Developed the Carrier Suppression Interferometer as a phase detector
Only limited by fundamental thermal noise! Instantly improved phase noise ~ 1000
Several International Patents
UWA Licensed the technology to PSI Pty Ltd, delayed publication
IEEE TRANSACTIONS ON MTT, VOL. 54, NO. 8, P 3284, AUGUST 2006
IEEE Trans. on UFFC, vol.45, no. 6, pp. 1526-1536, 1998
A MAJOR BREAK THROUGH IN MICROWAVE SENSING AND LOW-NOISE OSCILLATORS

## Slide 33
ROOM TEMPERATURE LOW NOISE SAPPHIRE OSCILLATORS: MADE COMPACT OR RACK MOUNT
Microwave Stripline Components: Compact Design

## Slide 34: History of Commercialization
10 UWA Patents to do with low noise oscillators
Resurgence ->Now low noise oscillators necessary to drive some quantum qubits to work at with high fidelity

## Slide 35: References
[1] EN Ivanov, ME Tobar, RA Woode, “Applications of Interferometric Signal Processing to Phase Noise Reduction in Microwave Oscillators.” IEEE Trans. on MTT, vol. 46, no. 10, pp. 1537-1545, Oct. 1998.
[2] EN Ivanov and ME Tobar, “Low phase noise microwave oscillators with interferometic signal processing”, IEEE Trans. MTT, vol. 54, no. 8, pp. 3284-3294, 2006.
[3] EN Ivanov, ME Tobar, “Low Phase Noise Sapphire Crystal Microwave Oscillators: Current Status,” IEEE Trans. Ultrason. Ferroelectr. Freq. Control, vol. 56, no. 2, pp. 263-269, 2009.
[4] R Bara-Maillet, SR Parker, N Nand, Nitin, J-M le Floch, ME Tobar, “Microwave to Millimetre Wave Synthesis Chain Phase Noise Performance,” IEEE Trans. UFFC, vol. 62, no. 10, pp. 1895-1900, 2015.
[5] R Bara, J-M Le Floch, ME Tobar, PL Stanwix, S Parker, JG Hartnett, EN Ivanov, "Generation of 103.75 GHz CW Source with 5.10-16 Frequency Instability Using Cryogenic Sapphire Oscillators" IEEE Microw. Wireless Comp. Lett., vol. 22, no 2, pp. 85-87, 2012.

## Slide 36
WML-6
Microwave Sapphire Oscillators
E. N. Ivanov and M. E. Tobar
School of Physics, The University of Western Australia
Talk Outline
Introduction: Microwave loop oscillator
Low-phase noise microwave oscillators
Measurements of Phase Fluctuations
Frequency-stable microwave oscillators
Outlook: Cryogenic sapphire oscillators

## Slide 37
Microwave Loop Oscillator
Phase noise of transmitted signal (Out 1)
Resonator-induced phase noise
Phase noise of incident signal on resonator (Out 2)
Amplifier phase noise
Computed phase noise spectrum of a loop oscillator (green trace)
Loop oscillator is assumed to be based on the 10 GHz sapphire resonator with the loaded Q-factor of 100 000
Noise in oscillator depends on the amplifier phase noise and Cavity Q-factor = 2*f0.5/Df

## Slide 38: Low Phase Noise Oscillators @ UWA
~ Df
F
Oscillator phase noise spectrum
Signal out
Resonator (SLC)
Amplifier
Df
fres
j
Lesson’s Model
IEEE MGW LETTERS. P-108, VOL. 5. NO. 4, APRIL 1995
Mixer phase detector
Cancel Noise with Phase Detector (Room Temp)

## Slide 39: CARRIER SUPPRESSION INTERFEROMETER PHASE DETECTOR
In 1993 we developed the interferometer as a phase detector, only limited by basic fundamental thermal noise if designed properly
The novel technique is covered by several international patent
applications and granted patents -> results published 1995 -> delayed publication of how to1998.

## Slide 40
1993 Developed the Carrier Suppression Interferometer as a phase detector
Only limited by fundamental thermal noise! Instantly improved phase noise ~ 1000
Several International Patents
UWA Licensed the technology to PSI Pty Ltd, delayed publication
IEEE TRANSACTIONS ON MTT, VOL. 54, NO. 8, P 3284, AUGUST 2006
IEEE Trans. on UFFC, vol.45, no. 6, pp. 1526-1536, 1998
A MAJOR BREAK THROUGH IN MICROWAVE SENSING AND LOW-NOISE OSCILLATORS

## Slide 41
IEEE Trans. UFFC, vol. 45, no. 6, 1526, 1998
Microwave Interferometry: Application to Precision Measurements and Noise Reduction Techniques
Phase
Noise floor
Phase Noise Measurement
of Device Under Test DUT
fc = Flicker of corner of amplifier
Pinp = incident power on DUT
LDUT = Loss in DUT
T0 = ambient temperature
Tamp = Amplifier Noise temperature

## Slide 42: Recycled Carrier Suppression Interferometer
Noise floors of different 9 GHz interferometric measurement systems:
(1) Conventional coaxial interferometer;
(2) coaxial interferometer with power recycling;
(3) waveguide interferometer with signal recycling

## Slide 43: Low-Phase Noise Oscillators with Interferometric Signal Processing
Bias
Amplifier
Output
BPF
VCP
Resonator
Circulator
Mixer
LNA
umix
fosc - fres
Oscillator phase noise due to intrinsic fluctuations in the electronics of the frequency discriminator
To = 300 K
Df ~ 50 kHz & Pdiss ~ 300 mW & To + Tamp~ 400 K
Expected phase noise 0.5 Sj (1 kHz) ~ -163 dBc/Hz
Achieved performance 0.5 Sj (1 kHz) ~ -157 dBc/Hz
IEEE Trans. on MTT, vol. 46, N10, P 1537 1998
High-Q resonator becomes DUT:
Becomes low noise frequency discriminator

## Slide 44: Phase Noise Performance
Phase-noise performance of a 9-GHz oscillator.
Curve 1: measured phase noise of the free-running oscillator.
Curve 2: measured phase noise of frequency-stabilized oscillator.
Curve 3: phase noise due to the frequency-servo finite-loop gain.
Curve 4: phase noise due to readout-system effective noise temperature.
Curve 5: phase noise due to intrinsic phase fluctuations of microwave circulator.
Curve 6: phase noise due to oscillator amplitude fluctuations.
IEEE Trans. on MTT, vol. 46, N10, P 1537 1998

## Slide 45: Low Phase-Noise Microwave Oscillators With Interferometric Signal Processing
IEEE TRANSACTIONS ON MTT, VOL. 54, NO. 8, P 3284, AUGUST 2006
Two-Oscillator Measurement System

## Slide 46: Results
Phase-noise spectra of a 9-GHz high-power oscillator with interferometric
signal processing.
Phase and amplitude noise spectra of a 9-GHz high-power frequency stabilized
oscillator.

## Slide 47
Phase Noise Spectrum of a 9 GHz Frequency Stabilized Oscillator
Q ~ 200 000
IEEE Trans. on UFFC, vol. 56, no. 2, p 263 2009
Low Phase-Noise Sapphire Crystal Microwave Oscillators: Current Status
SSB phase-noise spectra of a high-power microwave oscillator in different modes of operation:
free-running oscillator,
free-running oscillator with an additional phase control system, and
frequency-stabilized oscillator.

## Slide 48
Oscillator Phase Noise Reduction: Reduced Noise Amplifier
Based on Mixer Phase Detector
Fits to SSB phase noise spectra of the 10 GHz loop oscillators
( resonator Q-factor 100 000)
Loop oscillators featuring reduced phase noise amplifiers
Error signal generated from the phase comparison of incident and transmitted through the resonator
Error signal generated from the phase comparison of incident and reflected through the resonator

## Slide 49
Microwave Oscillators with Interferometric Signal Processing
Microwave interferometry: application to precision measurements and noise reduction techniques, IEEE Trans. on UFFC, vol. 45, no. 6, Nov. 1998, pp. 1526-1537.
Microwave oscillators with interferometric signal processing
Error signal generated from the phase comparison of incident and transmitted through the resonator
Error signal generated from the phase comparison of incident and reflected through the resonator

## Slide 50
Interferometric Frequency Discriminator
(IFD)
Frequency Discriminator phase noise floor
Microwave interferometry: application to precision measurements and noise reduction techniques, IEEE Trans. on UFFC, vol. 45, no. 6, Nov. 1998, pp. 1526-1537.
Microwave Oscillators with Interferometric Signal Processing: 2
Oscillator noise PSD @ high loop gain
The IPD ->
Construct oscillator with phase noise approaching the limit set by fluctuations of the resonator resonant frequency.

## Slide 51
Measurements of Frequency Discriminator Phase Noise Floor
Frequency-to-Voltage conversion measurements
Frequency Discriminator phase noise floor
Frequency discriminator voltage noise floor measurements
Frequency ~ 9 GHz
QL ~ 100 000
Pinc ~ 50 mW
Step 1
Step 2
Step 3

## Slide 52
SSB phase noise spectra of a 9 GHz sapphire crystal oscillator:
Resonator loaded Q-factor ~ 10 5
Free-running oscillator
Phase Noise an Oscillator with Interferometric Signal Processing
“Low Phase Noise Sapphire Crystal Microwave Oscillators: Current Status”, IEEE Trans. on UFFC, v. 56, no.2 , pp.263-269 , 2009.

## Slide 53
Microwave Oscillator with Automatic Carrier Suppression
Frequency-stabilized microwave oscillator with a feedback loop controlling interferometer amplitude mismatch
Applications outside the lab environment:
Phase and amplitude balance of the Interferometric Phase Detector (IPD) must be maintained.
Phase balance of IPD controlled with Frequency Control Loop, locking oscillator frequency to the resonator.
Amplitude balance of IPD is kept with an additional control system whose sensor is sensitive to interferometer amplitude mismatch.

## Slide 54
Measurements of the Noise Suppression Factor (NSF) of the AM-mismatch Control System
Oscillator Tuning: AM-mismatch Control System Noise Suppression Factor
Amplitude control system does not have to be broadband,
Compensate for the slow changes AM-mismatch caused by variations in the ambient temperature.
In-situ measurements of the noise suppression factor of the AM-mismatch control system, shown.

## Slide 55
SSB phase noise of an individual 9 GHz oscillator
Results of Phase Noise Measurements
Two almost identical sapphire oscillators operating near 9 GHz with IFDs and automatic carrier suppression.
Two complementary noise measurement techniques used.
One oscillator was phase-locked to another by varying microwave power dissipated in the sapphire crystal.
Secondly, the oscillators were detuned by approximately 2 MHz, combined phase noise measured with Symmetricom 5125A digital phase noise test set

## Slide 56
Low Phase Noise Sapphire Oscillator with Improved Frequency Stability
Power-to-frequency conversion of the 10 GHz sapphire resonator ~ 2…4 kHz / mW
Phase-referenced sapphire oscillator: Concept (left) and Implementation (right)
Sapphire oscillators, considered so far, suffer from a serious drawback – poor frequency stability caused by the strong dependence of sapphire dielectric permittivity on temperature.
Phase-locking the sapphire oscillator to the 5 MHz Oven Controlled Crystal Oscillator (OCXO) phase referencing of the sapphire oscillator to the OCXO is achieved with the PLL altering microwave power dissipated in the sapphire resonator

## Slide 57
Measurements of Power-to-Frequency Conversion
Transfer function measured by VNA:
Magnitude (top) and Phase (bottom) of the voltage-to-frequency conversion ratio (dfosc/duVCA) inferred from the VNA data
Measurements of the sapphire oscillator frequency tuning coefficient dfosc/du.
Tuning coefficient of the frequency synthesizer
Pedestal due to the residual voltage-to-phase conversion of the Voltage Controlled Attenuator (VCA)

## Slide 58
Phase-locked Sapphire Oscillator: Phase Noise
SSB phase noise of various 9 GHz signal sources
PLL bandwidth ~0.4 Hz
Well designed PLL should also be efficient in suppressing its phase fluctuations outside the loop bandwidth.
At 20 to 100 kHz, oscillator phase noise is comparable with the best noise levels reported.
At F < 3 kHz, the phase noise of the SLC oscillator is relatively high due to the residual phase noise of the VCA inside the interferometer.

## Slide 59
Phase-locked Sapphire Oscillator: Frequency Stability
Fractional frequency stability of the phase-referenced sapphire oscillator
Measurements time 4 hours
Beat note vs time
Sapphire oscillator phase-referenced to the 5 MHz OCXO (8607 module from Oscilloquartz)
Beat note ~300 kHz to avoid frequency counter triggering error, gate time 1 sec

## Slide 60
Outlook: Noise Filtering by Cryogenic Resonator
Phase noise spectra of the free-running cryogenic sapphire oscillator
Resonant frequency ~ 11.2 GHz
Temperature ~ 6 K & Peak contrast ~ 60 dB
Oscillator frequency ~ 11. 2 GHz
Sapphire resonator transmission coefficient
4K, Sapphire Q-factors >few billion.
Design with contrast of the transmission peaks > 60 dB
Transmission through such a resonator -> fast phase and amplitude fluctuations become greatly suppressed

## Slide 61
Outlook: Cryogenic Microwave Oscillators
Experimental setup and phase noise spectra of the 11.2 GHz frequency-stabilized cryogenic sapphire oscillator
Excess phase noise above 10 Hz -> vibration sensitivity of the cryogenic sapphire resonator.
Vibration isolation must be significantly improved to approach the predicted phase noise performance of the cryogenic oscillator.
To be the focus of our future research.
4-channel readout permits more accurate noise measurements relative to the two-channel setup due to the reduced noise contributions associated with the reference oscillators and the mixers

## Slide 62
E. N. Ivanov and M. E. Tobar, "Noise Suppression with Cryogenic Resonators," in IEEE Microwave and Wireless Components Letters, doi: 10.1109/LMWC.2021.3059291 , 2021.
Combining high stability and Low Phase Noise in one 4K System
EN Ivanov, ME Tobar, “Power-to-Frequency Conversion in Cryogenic Sapphire Resonators”, IEEE Microwave and Wireless Technology Letters, 2023 DOI: 10.1109/LMWT.2023.3264975