## Slide 1: Design & production of silicon sensors for phenix mpc-ex
Jiman Ha
(Yonsei Univ.)
For PHENIX MPC-EX collaboration

## Slide 2: MPC-EX
참여그룹
  국외 : Brookhaven Nation Laboratory, Iowa State University, University of California-Riverside, Los Alamos National Laboratory
  국내 : Yonsei University, ETRI, Ewha Womens University, Hanyang University, Chonbuk National University
발표관련 기여
  Sensor design : BNL, Yonsei & ETRI
  Sensor production : Yonsei & ETRI
  Sensor test : Yonsei, Ewha Womens University

## Slide 3: MPC-EX for PHENIX
Application as a pre-shower for EMCal (Electromagnetic calorimeter)

## Slide 4
SEG0
SEG1
SEG2
y
z
PAD
STRIP
W
-RM<y<RM
Electromagnetic Shower
(A schematic view)
(EM Shower by single e)
~1X0 x 20

## Slide 5
Sensor Design

## Slide 6: Sensor Geometry
# of PAD column =32
# of PAD row =4
Total # of PADs = 128
6.2 cm
6.2 cm
0.18cm
1.5cm

## Slide 7: SOME DESIGN DETAILS
PADs of Sensor
Bonding PADs
Biased/Floating Guardring
Floating Guardring
(3 layer structure)
Edge Rounding

## Slide 8: Mask design of silicon sensor

## Slide 9
Production Mask

## Slide 10: How do we make it? (CMOS process)
High purity Si wafer
Oxidation
Ion implant
Oxide layer deposition
Etch for contact
Metal layer deposition
Passivation

## Slide 12
Simulations

## Slide 13: Capacitance–voltage Relation
Wafer – Resistivity = 6, 9, 12, 18kΩ∙cm / Thickness = 405μm, Orientation = <100>
Full Depletion Voltage = 90V(6kΩ∙cm),60V(9kΩ∙cm),45V(12kΩ∙cm),30V(18kΩ∙cm )
Full Depletion
Bias Voltage (V)

## Slide 14: Current-Voltage relation (ongoing work)
Leakage current abruptly rise!
No Breakdown !
Leakage current flows from no bias guardring
Full Depletion
No breakdown upto 200V but somewhat large leakage current
Notes: large because carriers in no bias guardring doping region drift to Active region through depletion region by potential difference.

## Slide 15: Current-Voltage relation (ongoing work)
Full Depletion
No Breakdown !
.
No breakdown upto 200V and reduced leakage current

## Slide 16
Fabrication Monitoring

## Slide 17: AlignMENT

## Slide 18: AlignMENT

## Slide 19: 완성된 Wafer 사진

## Slide 20: Summary
MPC-EX is a pre-shower detector in Si/W sandwich structure.
We designed and fabricated a prototype of the relevant Si sensor.