## Slide 1: Nuclear criticality safety relevant data with the DICER instrument at LANSCE *
7th International Workshop On Nuclear Data Evaluation for Reactor Applications (WONDER-2026)
June 29th - July 3rd 2026
LA-UR-26-25300
Experiendo cognoscitur
Th. Stamatopoulos1, P. Koehler1, E. Bond2, S. Chasapoglou1, A. Couture1, B. DiGiovine3,
S. Essenmacher1, A. Marenco4, G. Rusev2, J. Svoboda1
Physics Division
Chemistry Division
Weapons Engineering Verification & Validation Division
Plutonium Supply & Disposition Division
*Funded by DOE-NNSA-NCSP

## Slide 2: Table of Contents
Non-traditional neutron transmission measurements
Neutron transmission at LANL and DICER
A few highlights
  133Cs
  239Pu
  149Sm
  63Cu
Criticality program at LANSCE

## Slide 3
Non-traditional Neutron transmission measurements

## Slide 4
DICER (Device for Indirect Capture Experiments for Radionuclides) was developed in 2022 to provide neutron capture rates for radionuclides where minuscule amounts of materials are available.
As a spin off, it provides data for criticality safety in cases where the availability of material is limited (purity, hazards, cost reduction etc)
Instead of the typical sample-in/sample-out measurements, DICER utilizes a binocular approach where both measurements, take place simultaneously.
Neutron
detectors
Neutron
beam
Collimator
Non-traditional measurements transmission: Binocular approach
Target/moderator
~15m
~15m
Not to scale

## Slide 5
First ever binocular collimation system (1 mm)
  A. Stamatopoulos et al., IEEE Trans. Nucl. Science 70, (2023)
  A. Stamatopoulos et al., Nucl. Intrum. Meth. A (1025) 166166, (2022)
  A. Stamatopoulos et al., Neutron News 33, 12 – 14 (2022)
First ever tof measurement on 88Zr
  A. Stamatopoulos et al., Phys. Rev. Lett. 134, 112702 (2025)
  A. Stamatopoulos et al. Phys. Rev. C 111, 034613 (2025)
  A. Matyskin et al, Scientific Reports 13, 1736 (2023)
  A. Stamatopoulos et al., EPJ., Conf. 260, 03006 (2022)
  A. Stamatopoulos et al., J. Rad. Nucl. Chem. 331, (2022)
Development of microjet printing for sample fabrication
Development of 0.1 mm binocular collimator
Preparing for first ever measurement on 88Y (new chemical compound, production through (p,x) on Sr etc)
A few highlights

## Slide 6
Neutron transmission at LANL

## Slide 7
1 km long LINAC
Up to 800 MeV protons
Multi-user proton (p) and neutron (n) facility
  Isotope Production Facility (IPF) (100 MeV p)
  Proton irradiation (pRad) (800 MeV p)
  Ultra Cold Neutrons (UCN) (<300 neV n)
  Lujan Center (meV – keV n)
  WNR (keV – MeV n)
  Target 4 (500 - 800 MeV p)
LANSCE: The Los Alamos Neutron Science Center

## Slide 8
800MeV protons impinge on a W target.
Up to 20 Hz duty cycle
Proton pulse of 145 ns FWHM, tunable down to 7 ns
Old target (Mark-III) in back-scattering geometry
New target (Mark-IV) since 2022 provides more flux and better resolution
Neutron targets at Lujan
Old Mark-III
New Mark-IV

## Slide 9
Mark-IV enhances the >keV neutron spectrum: Field-of-view on the target
Better resolution: Under-moderated target
Mark-IV (M4) : New neutron target at Lujan, est. 2022
DICER 32 m
DICER 64 m
(development)
Simulation
Ratio

## Slide 10
Description of the apparatus:
Device for Indirect Capture Experiments on Radionuclides (est 2022)
A. Stamatopoulos et al., NIMA (1025) 166166, 2022
A. Stamatopoulos et al., IEEE Trans. Nucl. Science 70, (2023)
A. Stamatopoulos et al., Neutron News 33, 12 – 14 (2022)

## Slide 11
Sophisticated collimation system
Rotating beam blocker
Binocular collimator
Aperture stop
Rotating inner cylinder with 3 holes
30 cm in length
Provides 0 - 2 beams
Stepped design to avoid neutron stream paths
Remotely controlled
Divided in a top and bottom part
Sample is installed in the collimator in the Maxwell kinematic stops
1.5 cm length, 1 cm diameter sample envelope
1 mm collimation
Kinematic stops ensure repeatability when installing the top part.
Cuts off the beam penumbra
Ensures two sharp beam spots at a 31 m, 9.5 cm in diameter

## Slide 12
Sophisticated collimation system
Rotating beam blocker
Binocular collimator
Aperture stop

## Slide 13
Single and multi pixel detectors
A commercial 235U loaded fission chamber is installed at ~7.8 m from the neutron source, to monitor the flux.
Two types of single pixel 6Li-glass neutron detectors are available
  ORELA type: Dual PMT detector. - Chi-nu type : Single PMT detector. Less material in beam PMT in contact with glass Poorer light collection More material in beam
The Large Area Picosecond Photo-detector (LAPPD) is a multi-channel plate (MCP) based detector, able to provide spatial information (nominally ~mm)
Currently exploring CLYC detectors and trying to develop new scintillators will good efficiency from meV - MeV

## Slide 14
DICER64
Through an LDRD-ECR award a feasibility study of a 64 m station was carried out
Signal/Background is better at 64m
Effort to combine transmission with Prompt Gamma Activation Analysis (PGAA)

## Slide 15
0.1 mm collimator @ DICER
Experiments on even more rare and/or radioactive nuclei: 0.1 mm collimator is driven by an upcoming measurement on 88Y (150 μg, 2 Ci/74 Gb)
Gold collimator with 500 lbs of tungsten for shielding
Robotic material handling

## Slide 16
A few highlights

## Slide 17
Laundry list
191Ir
193Ir
natCl
natCd
natGd
natBi
197Au
239Pu
95Mo
natCu
147Sm
149Sm
88Zr
133Cs
63Cu
103Rh
151Sm
88Y
natY
40Ar
239Pu (keV–MeV)
35Cl
143Nd
240Pu
167-171Tm
73,74,75As
56,57,58Co
85Kr
36Ar
40K
70Zn
72,73Ge
77,82Se
98,99Ru
107Pd
145-156Eu
153,157Gd
160,161Tb
163,166Ho
169Er
175Yb
179,180mTa
173,174Lu
185W
186Ru
191Os
110mAg
Measured
Will be measured in the near future
134Cs
147Nd
147Pm
135Xe
Could be measured
Criticality safety interest
Criticality safety interest-will be discussed

## Slide 18
133Cs

## Slide 19
Discrepancy between recent data (2011 Yoon, 2019 Block) and benchmarks ( CEA Cadarache, Leal ORNL/TM-2005/65 )
JEFF3 (same as JEFF4, ENDF80, ENDF81) needs to decrease
Most recent data are 3σ higher than JEFF, but agree within 1σ with each other
Most recent capture data agree within 1σ with the (n,tot) evaluations
Motivation

## Slide 20
Experiments in literature used caesium compounds
Metallic caesium is pyrophoric
Small amount is crucial to operational risk mitigation
We worked with NIDC and ORNL
Huge shoutout to Jenny Conner from the Stable Isotopes group
3 samples with 3 blanks: 1.1 mg, 14.4 mg, 26.8 mg
Cs in flame sealed ampules
The samples

## Slide 21
Sample handling
Despite the small amount, there is still a concern, and we have to execute the experiment within the safety basis
Sample unboxing in a resurrected glovebox
Argon atmosphere to avoid ignition in case the ampules were compromised

## Slide 22
Experimental campaign and preliminary results
Data were taken with:
  2 samples : 1.1 mg (1.1 mm thick) and 14.4 mg ( 8 mm thick)
  Empty ampules
  No samples
  With and without Cd filter
Data span from 2 meV up to ~20 keV
1% difference with evaluations (within uncertainties) at thermal
Preliminary
ENDF-81
thin
Thick

## Slide 23
239Pu
239Pu
W canister
Pb spherical plug

## Slide 24
239Pu(n,tot): Why?
Data are need up to 20 eV
Usual issue is the purity of the sample:
  239Pu comes with 240Pu, which has a big resonance at ~1.05 eV
  Hard to accurately characterize that resonance: a 240Pu experiment will utilize a sample that has some 239Pu (fissile)
Correlations in the analysis
Even small % of 240Pu have an effect

## Slide 25
The pure sample
99.96% 239Pu, 0.04% 240Pu from Chemistry Division at LANL
Only ~100 mg available.
DICER only needs 1 mg
Liquid sample, enclosed in a W canister and sealed with hand-pressed Pb plugs
Liquid sample ensures uniformity: 239PuCl4 in 6M D2O●DCl solution

## Slide 26
Preliminary results
Sample was free of measurable 240Pu
Preliminary results favor the ENDF/B-VIII.0 evaluation
Analysis is almost complete and a manuscript will be submitted for publication to Phys. Rev. C.
Preliminary
Preliminary
239Pu
240Pu
239Pu

## Slide 27
149Sm

## Slide 28
n+149Sm: Capture and transmission
149Sm: fission product + neutron poison
Accumulates in a reactor, like 135Xe but it doesn’t decay away
Detector for Advanced Neutron Capture Experiments (DANCE) (See E. Leal-Cidoncha’s talk for DANCE details)
~4π calorimeter
DANCE to get the capture yields
DANCE also provides multiplicities
Different multiplicity distributions for different spins
DANCE is used as a spinometer

## Slide 29
n+149Sm: R-Matrix analysis & Resonance parameters
Fits in capture and transmission data using SAMMY
About 40 spins were incorrectly assigned
Resolved 58 new resonances (215 vs 157 in evaluations)
More info on LA-UR-23-32571
Resolved doublet @ 15 eV
Evaluated Γn is too large

## Slide 30
The transmission sample
Sm2O3 powder in capillary tubes sealed with Al plugs
Sm2O3 is hygroscopic
Samples were “baked” at 200 oC under vacuum for ~3 days
Previous Sm studies: samples baked at 1000 0C in atmospheric pressure for a few minutes.
There is concern if our method truly results in dry samples
We used Thermogalvanic Analysis (TGA) and studied the mass change at different temperatures
Highest mass change: 700 0C (~8%)
Consistent with the mass change we observed in the transmission before and after baking the sample
ND2025 proceedings describe the study.
7.5(13)%

## Slide 31
n+149Sm: Non-Statistical behavior
Statistically significant change in the Γγ distributions around 200 eV was observed.
Findings will be submitted for publication to Phys. Rev. Lett. (similar findings in 147Sm)
Phys. Rev. Lett.
Phys. Rev. C

## Slide 32
Oscillations in cross sections
Sm work gave rise to an interesting observation
Neutron-capture cross sections are exhibiting a statistically significant oscillating behavior
Oscillations are an autocovariance. Is this autocovariance information preserved in cross-section processing for criticality applications?

## Slide 33
63Cu

## Slide 34
63Cu, funded by LANL-LDRD
Through the PARADIGM project, we’re employing ML to identify differential and integral experiments and reduce time in nuclear data evaluations: 3 vs 25 years! (see N. Walton’s talk)
63Cu(n,tot) was identified as an important experiment to showcase the new nuclear data pipeline.
Thin and thick samples were cast at ORNL
Efforts are expected to finish by the end of September
First time DICER measured above 100 keV
Preliminary
Phys. Rev. X 15, 021086

## Slide 35
Criticality program at LANSCE

## Slide 36
LANSCE NCSP 5-year outlook
US DOE NCSP 5-year execution plan https://ncsp.llnl.gov/program-management/ncsp-five-year-execution-plan
LANSCE provides differential nuclear data for (n,x) reactions from meV-MeV
The following table shows NCSP funded experiments (will be) conducted at LANSCE apart from 63Cu
Reaction | Executed |  |  |  |  |  |  |  | To be executed |  |  |  |  |  |  |  | 
PFNS @ Chi-Nu (WNR) | 240Pu |  |  |  |  |  |  |  | 233U |  |  |  |  |  |  |  | 
(n,γ) @ DANCE (Lujan) | 233U | 143Nd |  | 133Cs |  | 63Cu |  | 151Sm | 151Sm |  |  | 240Pu |  |  |  | 242Pu | 
(n,p) @LENZ (Lujan and WNR) | 35Cl |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
(n,f)* @ SREFT (WNR) |  |  |  |  |  |  |  |  | 237Np |  |  |  | 240Pu |  |  |  | 
(n,n’γ)** @ CoGNAC (WNR) |  |  |  |  |  |  |  |  | 50, 52, 53Cr |  | 58,60Ni |  |  |  | 90,91,92,94,96Zr |  | 
(n,tot)** @ DICER (Lujan) | 149Sm |  | 239Pu |  | 133Cs |  | 63Cu |  | 35Cl | 143Nd |  | 151Sm |  | 236U (ORNL) |  |  | 240,242Pu
* Under development
**New capabilities at LANSCE

## Slide 37
Thank you for your attention!

## Slide 38
9Back-up slides

## Slide 39
The technique in a nutshell
Resonances can be used across an energy region ΔΕ to calculate the 3 ingredients needed to extract or constrain the average capture cross section
Average level spacing (N: number of resonances in the ΔΕ interval).
Neutron strength function for s-waves , where
  g is the spin factor for a resonance with spin J
  Γ0n is the reduced neutron width
Average radiation width <Γγ>
The capture cross section is related to these quantities
k : Wave number
W : Width fluctuation factor

## Slide 40
Proof of principle: in brief
Data on 151Sm(n,tot) from Kirouac and Einland (10.1103/PhysRevC.11.895)
Resonance data up to 300 eV (120 resonances)
Resonances were fitted with SAMMY
13 Γγ values were obtained
<Γγ> = 96.5(14) meV
Level spacing D0 = 1.10(7) eV
Strength function 104xS0 = 3.58(59)
TALYS was adjusted to these values and compared with recent (n,γ) data
  Level density parameter α(Sn)
  Optical model potential depth
  Optical model potential diffuseness
  Photon strength function was normalized to give the <Γγ> value https://nds.iaea.org/talys/tutorials/talys.pdf
Good agreement with the data in EXFOR