## Slide 1: Towards Low-MTE Photocathodes in Accelerators
Oksana Chubenko
Department of Physics, Northern Illinois University

## Slide 2
Introduction
High-quality electron beams =
bright beams
High-quality photocathodes =
low mean transverse energy,
robustness + long operational lifetime under realistic photoinjector conditions (5-100 MV/m to extract ~ 50-1000 pC/mm2 of charge densities/bunch)
high quantum efficiency,
High charge density regime:
,
MTE ~ kBT ~ 25 meV at room temperature
Factors, limiting MTE:
requirements of the high charge density
disordered nature of photocathode materials
surface roughness and work function variations
prompt response time
Frame, Marzouk, Chubenko et al, Instruments 7, 48 (2023).
→ MTE ~ few 100s meV
Bazarov et al., Phys. Rev. Lett. 102, 104801 (2009).

## Slide 3
Low-electron-affinity semiconductor photocathodes
Low-electron-affinity semiconducting photocathodes are better candidates to operate under high laser fluences.
Multi-photon absorption limits MTE!
Bae et al. J. App. Phys. 124, 244903 (2018)
Knill et al., Phys. Rev. Accel. Beams 26, 093401 (2023)

## Slide 4
Cesium-antimonide photocathodes
Cesium-antimonide photocathodes (Cs-Sb):
promising candidates for generating extremely bright electron beams for XFELs, UED, and UEM.
can be easily deposited through thermal evaporation at moderate temperatures.
thin films (several 10s of nm).
Substrate

## Slide 5
A. Kachwala, P. Saha, P. Bhattacharyya, E. Montgomery, O. Chubenko, and S, Karkare, Appl. Phys. Lett. 123, 044106 (2023)
Cesium-antimonide photocathodes demonstrate thermal-limit MTE and relatively high QE at photoemission threshold.
Photon Energy, eV
Cesium-antimonide photocathodes
Operational photon energy affects MTE!

## Slide 6
Cesium-antimonide photocathodes
Saha, Chubenko et al, Appl. Phys. Lett. 120, 194102 (2022).
Cesium-antimonide films grown on lattice-matched single crystal strontium titanate (STO) substrates demonstrate roughness-induced MTE < 10 meV even at large applied fields.
Surface roughness and work function variation limit MTE!

## Slide 7
Cesium-antimonide photocathodes
Disordered crystal structure limits MTE!
Parzyck et al, Phys. Rev. Lett. 128, 114801 (2022).
Epitaxial growth of cesium-antimonide films on lattice-matched single crystal SiC substrates.
RHEED images of an annealed SiC substrate and a 10 u.c. Cs3Sb film.
High red QE from single crystal Cs3Sb

## Slide 8
Cesium-antimonide photocathodes
Detailed modeling and advanced growth and characterization are required to achieve desired stoichiometry.
Daniel Franklin,
T21 (Tuesday)
Hagino et al, Phys. Stat. Sol. 17, 609 (1966).
Near Cs3Sb
Cs-rich
High yield
Stoichiometric variation
Parzyck et al., APL Mater. 11, 101125 (2023)
robustness against oxidation is up to 15 times greater
Cs3Sb vs CsSb
Stoichiometry influences photoemission!
DFT + Monte Carlo investigation of stoichiometry influence on photoemission

## Slide 9
Alkali-antimonide photocathodes (Cs-Sb, Na-K-Sb):
Low MTE
High QE
Thin films → prompt response time
Robustness + long operational lifetime under realistic photoinjector conditions ?
✅
✅
✅
Testing alkali-antimonide photocathodes in accelerators

## Slide 10
Previous experience:
many tests in DC guns
very few tests of bialkali-antimonides in high field RF/SRF guns
no RF tests of Cs-Sb films grown on SC substrates.
Complications:
photocathode sensitivity to vacuum conditions
incompatibility between photocathode growth systems and photoinjectors
Oxidation of Cs-Sb films after ~ 5 min in air
New INFN-style
Old INFN-style
University labs
FermiLab, SLAC, UCLA, Cornell
Argonne
Witness gun
ACT gun
AWA drive gun
Testing alkali-antimonide photocathodes in accelerators
Flag-style sample holder

## Slide 11
Testing alkali antimonide photocathodes at AWA Facility
Argonne Cathode Teststand (ACT):
L-band 1.3 GHz single-cell photocathode RF gun.
Emittance measurement capability.
Close proximity to NIU.
Currently suitable for testing air-stable materials only.
Unique plug design.
Planned ACT updates:
Update the pump system to achieve ~10-10 Torr.
Integrate NIU-compatible photocathode plug suitable for testing different photocathode substrates.
Possibility of adding the deflecting cavity for photocathode response time measurements.
Shao et al, IPAC 2018

## Slide 12
NIU Photoemission Research Lab
Pulsed Laser Deposition system
Thermal Evaporation system
Oksana Chubenko,
T35 (Tuesday)
This Talk

## Slide 13
Growth of alkali-antimonide films at NIU
Thermal evaporation system previously used to grow Cs-Te films on old INFN-type photocathode plug at Fermilab.
Pincer with
built-in heater
Carriage for 5 INFN-style plugs
Vacuum Suitcase
SAES dispensers

## Slide 14
Growth of alkali-antimonide films at NIU
New plug enables growth of low-MTE Cs3Sb films on semiconductor substrates.
Compatible with ACT
New NIU plug
ACT plug
NIU plug in ACT
Old INFN-style plug

## Slide 15
Growth of alkali-antimonide films at NIU
Developed vacuum suitcase compatible with ACT.
K. J. Lesker sample transfer device with rolling metal & ceramic bearings for smooth, low friction actuation, with minimal outgassing.
NEXTorr® UHV pump.
Two VAT GVs.

## Slide 16
Growth of alkali-antimonide films at NIU
Further system upgrades:
More efficient particle sources
SAES dispensers
Effusion cell
Implement RHEED system or other mechanism for controlled epitaxial growth of alkali antimonide photocathodes with desired stoichiometry.

## Slide 17
Summary
High-quality photocathode development through epitaxial growth of atomically smooth crystalline materials.
Developed experimental setup for the epitaxial growth of alkali antimonide photocathodes on lattice-matched substrates.
Extensive testing and characterization of photocathodes will be carried out in the L-band RF gun of ACT.
This project aims to bridge the gap between university-based photocathode R&D and the reliable deployment of high-quality photocathodes in accelerator facilities.

## Slide 18
Acknowledgements
Thank you!
Tariqul Hasan (NIU)
Grad students:
John Power (ANL)
Scott Doran (ANL)
Eric Wisniewski (ANL)
Gongxiaohui Chen (ANL)
Philippe Piot (ANL)
Collaborators:
Grace Straub (NIU)
Undergrad students:
The Center for Bright Beams (CBB), NSF award PHY-1549132.
Launching of Early-Career Academic Pathways in the Mathematical and Physical Sciences (LEAPS-MPS), NSF Award Number 2532996.
Funding agencies: