## Slide 1: Indirect Characterization of Photoinjector Parameters & their Correlations
David Garcia
Advanced Accelerator Concepts 2026
2026/07/28

## Slide 2: Outline
Motivation
Measurement of the cathode re-entrance and intrinsic emittance
  Degeneracies
Surrogate model + MCMC technique
Extracting the photocathode intrinsic emittance from a beam with:
  Projected emittance growth
  Space charge emittance growth
Towards a measurement of the cathode time response
Conclusion & Outlook

## Slide 3: Motivation
Electron sources for next generation FELs & UED machines must be well tuned in order to provide high brightness beams
Characterization of hard to measure parameters often requires additional diagnostics
  Intrinsic emittance: apertures/slits
  Pulse length: transverse deflecting cavity

## Slide 4: Pegasus S-band Gun
OPA produces a short pulse tunable through the visible and UV spectrum
Photoelectrons accelerated to 3MeV & focused using solenoid
Charge, laser energy & transverse distribution at both the cathode & YAG screen are recorded

## Slide 5: Semiconductor Photocathodes
UC03: Cs3Sb
Load-lock chamber behind RF permits exchange of air sensitive cathode under UHV conditions (<1e-9 Torr)
  1 Cs-Te & 2 Cs3Sb cathodes grown at SLAC & transported to UCLA
UC04: Cs3Sb
UC01: Cs-Te

## Slide 6: Analytic Analysis of Solenoid Scan
95% emittance extracted from solenoid scan using linear transport formalism
  Low charge (<100fC) and short pulse (<1ps) minimize emittance growth from Coulomb force and RF field

## Slide 7: Surrogate Model & Degeneracies
RF focusing from the re-entrance of the cathode plug is degenerate with the MTE
Neural Net trained on a library of General Particle Tracer simulations that span the input space of the RF gun gives a fast surrogate model of the RF gun
  Laser shape & duration (FWHM)
  MTE & charge
  Gun phase & power
  Cathode plug position

## Slide 8: MCMC Methods
Markov Chain Monte Carlo (MCMC) methods use Bayesian inference to retrieve posterior probability distributions of the model parameters given the data set D
  Information on measured parameters (charge, gun phase, …) enter through prior probabilities
GW-MCMC algorithm uses an ensemble of simultaneous walkers
  Walkers talk to each other & give collective effects
  Affine invariance means the algorithm works well on oddly shaped spaces
Posterior probability
Likelihood
Prior probability

## Slide 9: MCMC results
Fit measured data from Cs-Te with a 2 stage MCMC routine:
  1st stage is run with a uniform distribution of walkers in the input space
  2nd stage used regions of high likelihood from the 1st stage to seed ½ of the walkers

## Slide 10: MCMC results
Fit measured data from Cs-Te with a 2 stage MCMC routine:
  1st stage is run with a uniform distribution of walkers in the input space
  2nd stage used regions of high likelihood from the 1st stage to seed ½ of the walkers

## Slide 11: Space Charge Emittance Growth
Space charge emittance growth is only negligible for a small set of circumstances
  Our far YAG screen cannot reconstruct the MTE because the beam is too dense for too long
  Beam out of VHF guns is too soft (<1MeV)
Rho parameter quantifies when a beam is emittance dominated () or space charge dominated ()
Screen | Position (m) | at waist | Regime
YAG 2 |  |  | Emittance
YAG 3 |  |  | Space charge
Screen | Position (m) |  | Regime
YAG 2 |  |  | Emittance
YAG 3 |  |  | Space charge

## Slide 12: Intrinsic Emittance with Space Charge
Analytic reconstruction of the MTE fails for YAG3, but the MCMC routine can retrieve the MTE for scans taken on YAG3

## Slide 13: Intrinsic Emittance with a Long Pulse
Simulate stretching the laser from 100 fs to 4.5 ps
  Suppress nonlinear photoemission near threshold
  The RF gun will give a time varying transverse kick, resulting in a projected emittance growth for long beams

## Slide 14: Indirect Measure of Pulse Length
The energy of the electron beam leaving the RF gun is correlated with the launch phase
  A longer pulse will sample many different energies, especially at high phase, resulting in a larger energy spread

## Slide 15: Time Response vs. Wavelength
The FWHM () of the electron beam emitted at each wavelength is fit using GPT simulations to calculate the time response ( )
Temporal broadening near threshold transitions to prompt emission when nonlinear
Wavelength (nm) | Laser Pulse Length (fs) | Electron Pulse Length (fs) | Time Response (fs)
260 |  |  | 
300 |  |  | 
350 |  |  | 
Wavelength (nm) | Laser Pulse Length (fs) | Electron Pulse Length (fs) | Time Response (fs)
260 |  |  | 
300 |  |  | 
350 |  |  | 

## Slide 16: Conclusion & Outlook
We plan to use these techniques to characterize advanced semiconductor cathodes in the Pegasus RF gun to push towards a 6D characterization of photocathode performance in an RF gun
  Most useful for long pulse analysis close to threshold
  Next batch of cathodes coming to UCLA early fall from both SLAC & ASU
Future expansions
  More accurate treatment of the initial charge distribution
  Train NN that spans a larger input space

## Slide 17: Acknowledgments
PBPL
  Advisor: Pietro Musumeci
  Support from post docs & students
  Past PBPL students who have worked on this project: Eric Cropp, Gilles Silvi
Collaborators who have or will grow cathodes for testing at UCLA
  SLAC: T. Vecchione & G. Adhikari
  Cornell: Maxson Lab
  ASU: Karkare Lab
Funding
  CBB/NSF
  DOE

## Slide 18: Boersch Effect
Coulomb repulsion of the electron beam will increase the energy spread if too dense
  Correlation plots show this effect becomes negligible as the beam is stretched