## Slide 1: Copper Coated PEEK Based RF Cavity Power and Q Factor Testing
Benjamin Sims (AOT-AE)
John W. Lewellen (LAMP)
WG4 4:00pm 7-27-2026
LA-UR-26-26233

## Slide 2
Polyether Ether Ketone (PEEK) Based Cavities
Simple PEEK Cavity Diagram
Copper coated polymer structures have been implemented in many radiofrequency applications
Examples include
  Lightweight and unique antennas
  Waveguides
  Prototype and Cold test RF structures
PEEK
Copper Layer
E Field
B Field

## Slide 3
Designing and Building Cavities
Cavity Simulation to Characterization
Simulation
Fabrication
Plating
Characterization
Fabrication designs
10 micron
thickness

## Slide 4
Simulation and Fabrication designs
Designed in CST
Cavity Cuts
  Equatorial Cut
    Typical design approach
    RF currents cross cavity cut
  Longitudinal Cut
    Emerging approach for high-gradient cavities
    RF currents do not cross the cavity cut
      Currents move parallel to cut line

## Slide 5
Testing a verity of materials
COTS PEEK
Commercial off the Shelf (COTS) materials
3 Different Types of PEEK were tested
  Basic PEEK plastic
  30% glass-filled PEEK
  30% carbon fiber-filled PEEK
PEEK
30% Carbon Filled PEEK
30% Glass Filled PEEK

## Slide 6
Cavity Characterization
Quality Factor and Resonant Frequency Data Tables
Measurements Approach:
  Port 1 critical coupled
  Port 2 strongly under coupled
  Est. accuracy ± 10%
CST Cavity RF design
  Design Resonant frequency - 5.33 GHz
  Design Q0 ~10,800
  assumption can lead to over estimation of Q0
 | PEEK | 30% GF PEEK | 30% CF PEEK
Equatorial | 9,400 | 9,840 | 13,500
Longitudinal | 11,200 | 9,440 | 10,070
 | PEEK [GHz] | 30% GF PEEK [GHz] | 30% CF PEEK [GHz]
Equatorial | 5.29 | 5.29 | 5.29
Longitudinal | 5.27 | 5.29 | 5.28
Measured Q0
Measured Frequency

## Slide 7
RF Power Testing
RF Power diagram
From Polymer Accelerator Structures, J. Lewellen
Signal generator
Gated to provide pulsed power to cavity
Adjusted to match cavity frequency as the cavity expanded under RF heating
Power Amplifier
Provides high average power to cavity
Circulator
Directs reflected power from cavity into a load
Protects amplifier from sudden cavity failure
Envelope Detector Diodes
Measures RF power sent to, and reflected from, cavity.
Directional Coupler
Diverts a small fraction of forward and reflected power

## Slide 8
Power Testing Levels
Power Delivered to Cavities
1 W Average, 5 W Peak, 20% Duty Factor, 10-minute duration
10 W average power, 20 W peak, 50% Duty Factor, 10-minute duration
20 W Average Power, 40 W Peak, 50% Duty Factor, 30-minute duration
2 μs
5 μs
5 μs
8 μs
5 μs
5 μs
5 W
40 W
20 W

## Slide 9
Cavity temperature rise
20 W Average Power Testing Data
Biggest Temperature change of ~70°F
20W Avg, 40W Peak
RF Power turned off at 30 min
Cooled down for 5 min
Input frequency was monitored and modified to deliver critical coupling while cavity was in use
Chart: Temperature change over time Latitudinal Cut
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39
PEEK | 0 | 0.4 | 2.8 | 6 | 9.4 | 13 | 15.9 | 19 | 22.4 | 24.9 | 27.4 | 30.2 | 32.6 | 35.2 | 38.8 | 39.8 | 41.8 | 43.9 | 46 | 47.7 | 49.7 | 51.2 | 52.4 | 53.8 | 55.3 | 57 | 58.3 | 59.4 | 60.8 | 62 | 63.6 | 64.5 | 68.4 | 67.3 | 65.3 | 63.5 | 60.8
GF | 0 | 0.5 | 5.1 | 8.4 | 12.1 | 15.3 | 18.6 | 21.8 | 24.9 | 27.9 | 30.7 | 33.6 | 36.1 | 38.7 | 40.9 | 42.9 | 45.1 | 47.1 | 49 | 51.1 | 52.9 | 54.6 | 56.3 | 58.1 | 59.5 | 61.3 | 63.1 | 64.6 | 66.3 | 67.9 | 69.5 | 70.2 | 70.9 | 69.3 | 67.2 | 64.9
CF | 0 | 2.4 | 6.4 | 10.1 | 13.9 | 17.3 | 20.8 | 23.6 | 26.5 | 29.4 | 32.3 | 34.5 | 37 | 39.4 | 41.5 | 43.7 | 45.7 | 47.5 | 49.5 | 51.2 | 52.7 | 54.4 | 56.2 | 58 | 59.8 | 61.2 | 62.7 | 64.3 | 65.7 | 67 | 68.1 | 66.5 | 63.8 | 61 | 57.9 | 55.7
Chart: Temperature change over time Equatorial Cut
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37
PEEK | 0 | 0.9 | 3.3 | 6.1 | 9 | 11.9 | 14.6 | 17 | 19.9 | 22.7 | 25.3 | 28 | 30.8 | 33.6 | 36.3 | 39 | 41.6 | 44.2 | 47 | 49.5 | 51.4 | 53.7 | 55.6 | 57.8 | 59.8 | 61.7 | 63.3 | 65.1 | 66.6 | 67.7 | 69.4 | 70.3 | 69.7 | 68.7 | 67.4 | 65.8 | 64.5
GF | 0 | 3 | 5.3 | 8.2 | 11.2 | 13.8 | 16.2 | 19 | 22 | 24 | 26.5 | 28.8 | 31.3 | 33.9 | 36 | 38.7 | 40.8 | 43 | 45.1 | 47.2 | 48.8 | 50.5 | 52.5 | 53.8 | 55.3 | 56.9 | 58.2 | 59.7 | 61 | 61.9 | 63.1 | 62.8 | 60.7 | 58.6 | 56.5 | 54.7 | 53.2
CF | 0 | 3.6 | 7.6 | 11.6 | 14.8 | 17.9 | 20.6 | 23.8 | 26.7 | 29.7 | 32.4 | 35.2 | 37.4 | 40 | 42.2 | 44.6 | 46.8 | 48.9 | 51 | 53.2 | 55 | 56.6 | 58.6 | 60.4 | 62 | 63.6 | 65.4 | 66.7 | 68.3 | 69.8 | 71.2 | 69.2 | 65.9 | 63.2 | 60.8 | 58.7

## Slide 10
Material Comparison
Post Testing Cavity
No large discernable changes between materials
CF cavities cooled slightly faster
PEEK Cavities cooled the slowest
CF Cavities had the least resonant frequency change while heating
PEEK Cavities had the largest resonant frequency change while heating
Inner coating unblemished on all cavities
No, we did not use gloves

## Slide 11
Undamaged inner surface
PEEK Cavities Internal Post Testing
PEEK Cavities after all testing
Repeated use led to coating removal from some threads

## Slide 12
Cavity compression
Assembled PEEK Cavity
Repeated heating and cooling caused bolts to loosen
Resulted in a Q Factor drop following tests only for elliptical cut cavities
Tightening bolts restored Q factor to pre-power delivery levels

## Slide 13
Conclusion
No permanent deterioration in performance in any cavity following power testing
  Equatorial cut showed the largest degradation in performance due to expansion at the joint causing loosening over time
  Longitudinal cut performed better overall
Parameter | PEEK CAVITY / COPPER CAVITY
Fabrication Time | 1/4
Cost | 1/10
Weight | 1/10
Yield Strength | 2.5
Q Factor | Equal

## Slide 14: Questions?
Thank you for your time.