## Slide 1: ASTERIX: Development of TIG-Welded Four-Quadrant X-Band RF Accelerating Structures at INFN.
Luigi Faillace
INFN – LNF, Frascati (Rome), Italy

## Slide 2: Project Overview
The main goal of ASTERIX is the design, fabrication and high-power RF testing of a practical meter-long, four-quadrant, “open-type” X-band accelerating structure made of hard copper, joined and vacuum-sealed by TIG welding — a braze-free technique — targeting gradients above 100 MV/m.
Funded by Scientific Committee 5 of INFN
Collaboration
LNF coordination · mechanical & RF design
LNS RF couplers · multiphysics simulation
Roma1 wakefield & HOM characterisation
90 cm, four-quadrant, TIG-welded “open-type” structure with integrated mode-launcher, cooling channels and tuners.
ASTERIX (Accelerating STructures made of multiplE sectoRs In X-Band)
PI: Luigi Faillace INFN-LNF 3 years (2025-2027) Total budget = 400 kEuros
high accelerating gradients (>100 MV/m)
composed of four-quadrants (“open-type”)
made out hard copper
joined and vacuum sealed by using TIG welding (“braze-free” technique)

## Slide 3: ASTERIX INFN- team
LNF
Roma1
LNS
LNF | FTE | LNS | FTE | Roma1 | FTE
L. Faillace (Resp. Naz.) | 0.3 | G. Torrisi (RL) | 0.1 | L. Ficcadenti (RL) | 0.3
D. Alesini | 0.2 | D. Mascali | 0.05 | M. Petrarca | 0.2
M. Bellaveglia | 0.05 | G. Mauro | 0.1 | M. Migliorati | 0.2
S. Bini | 0.2 | G. Sorbello | 0.2 | G. Silvi | 0.2
F. Cardelli | 0.3 | T. Isernia | 0.3 | L. Palumbo | 0.4
M. Carillo | 0.2 | R. Palmeri | 0.3 |  | 
E. Chiadroni | 0.2 | A. Locatelli | 0.1 |  | 
A. Falone | 0.2 | C. De Angelis | 0.1 |  | 
A. Gallo | 0.15 | L. Vincetti | 0.1 |  | 
A. Giribono | 0.2 |  |  |  | 
A. Liedl | 0.1 |  |  |  | 
L. Piersanti | 0.1 |  |  |  | 
S. Pioli | 0.2 |  |  |  | 
B. Spataro | 0 |  |  |  | 
C. Vaccarezza | 0.2 |  |  |  | 
Tot./Unit | 2.6 |  | 1.35 |  | 1.3
L. Faillace
Advanced Accelerator Concepts 2026, Jul 26 – 31 Luskin Conference Center, UCLA

## Slide 4: Contributors
This work is made possible by the efforts :
INFN
SLAC(USA)
KEK (JAPAN)
External Collaborators: V. Dolgashev (SLAC), Tetsuo Abe (KEK)
University of Science and Technology of China: Yelong Wei, PhD student Zhicheng Huang in Frascati.
USTC (CHINA)
Laboratori di Frascati, Roma1 (Sapienza University) and Laboratori del Sud (Catania)

## Slide 5: History
MOU between SLAC and INFN-LNF within the world-wide collaboration on studies of RF breakdown physics in RF accelerating structures:
    from X-band (11-12 GHz) to other
    frequencies (S, C, Ka, W) .
DEMETRA (2016-18)
ARYA (2020-23)
MICRON (2022-24)
    Ka-band structures
    made of four quadrants
Resp. Loc. L. Faillace - LNF
Funded by CSN5 (A. Quaranta)
Funded by
CSN5 (V. Bonvicini)
ASTERIX
Accelerating Structures
made of multiplE sectoRs
In X-Band
62,52 mm
Single quadrant
RF power
Coupler:
4-port Mode Launcher
Courtesy of B. Spataro

## Slide 6: State-of-the-art
“Single-cell” cavities (open and closed; disk-type and multi-sector)
TW multi-cell structures (open and closed; disk-type and multi-sector)
Open-type multi-sector cavities, typically of small lengths (20-30 cm).
Dolgashev VA, Faillace L, Spataro B, Tantawi S, Bonifazi R. High-gradient rf tests of welded X-band accelerating cavities. Physical Review Accelerators and Beams. 2021 Aug 10;24(8):081002.
CLIC-G-OPEN
30 cm
KEK (Tetsuo Abe) 2023
X-band
4 quadrants
EBW welding
To be High-power tested.
(T. Abe)
TIG
EBW
open
T. Abe, et al., High-gradient test results on a quadrant-type X-Band single-cell structure.
30 cm
22 cm
CERN 2007 (Dobert, Grudiev, Wuensch et al)
X-band
4 quadrants
Clamped, high T-treated
High-power Tested:
 Gradient: 80 MV/m with 40 ns pulse length.
SLAC/CERN 2018 (Grudiev, Wuensch et al)
X-band
2 halves, open structure
Brazed
High-power tested:
 Gradient: 100 MV/m with 200 ns pulse length.
One quadrant
62.448 mm
26 cm

## Slide 7: Full TW multi-cell X-band structure
90 cm
Fabrication out of hard copper
Increase in vacuum pumping speed
Overall reduction of the fabrication costs
Easy insertion of HOM absorbing materials
TIG-welded
4-quadrants
«open-type»
27 cm
TIG welding joints
Integrated
mode-launcher
Cooling channels
tuners

## Slide 8: Full TW multi-cell X-band structure
Single quadrant
Alignment pins
TIG welding joints
Secondary vacuum chamber (extra pumping, easy insertion of HOMs absorbers in multi-bunch operation,…)
Engineering in collaboration with the manufacturing company Comeb srl, Rome.

## Slide 9
RF and Wakefields/HOMs Optimization
Low-precision Full-scale fabrication/mechanical characterization
Report 1
Report 2
Fabrication of small-scale
prototypes/mechanical Validation
Low and High RF power testing of small-scale protoypes
Fabrication of final
Full-scale structure and Mechanical Validation
Low and High-power Testing of Final full-scale structure
Report 6
Report 3
Report 4
Report 5
7 Milestones
6 Deliverables
End
2025
End
2026
Start
2025
End
2027
Report of the Feasibility Study (RF and Wakefields/HOMs);
Report of the Mechanical Engineering of the low-precision prototype with standard RF couplers for Mechanical, TIG welding and vacuum testing;
Report of the Mechanical Engineering of the small-scale structures with ad-hoc integrated RF Mode Launcher couplers;
Report of the low/high RF power testing of the small-scale structures;
Report of the Mechanical Engineering of the Full Structure with with ad-hoc integrated RF Mode Launcher couplers;
Final Report of low and High RF power testing of final full-scale structure.
Prototyping Activity
Final full-structure Tests
Feasibility Study
30 cm
4-port Mode-launchers (already INFN –
CSN5)
30 cm
Standard couplers
90 cm
4-port Mode-launchers (already INFN – CSN5)
90 cm
quadrant straightness and alignment
TIG welding process
vacuum tightness

## Slide 10: ASTERIX cell geometry for single-bunch mode
Gap/2
a
b
Arc center
be
ae
R
d
Rounding: 0.5mm

## Slide 11: Cell Optimization
Optimization Target:
Low peak electric field Ep, magnetic field Hp, modified Poynting vector Sc
High shunt impedance Rsh and Q
Elliptical ratio → Ep, Sc
Rounding top → Hp
Conventional disk-loaded structure:
Ep/Eacc ≈ 2.1
Hp/Eacc ≈ 2.6 mA/V
Sc/Eacc^2 ≈ 0.6 mA/V
Q = 6800-7500 (different rounding)
Rsh = 105MΩ/m
Iris radius fixed at a = 3.5mm
Ep/Eacc
Hp/Eacc
Sc/Eacc^2
The value will be shown later
3.8mA/V

## Slide 12: Modified Poynting Vector and Peak E field
t=2ae=2mm, gap = 1mm
t=2ae=2mm, gap = 0.5mm
t=2ae=2mm, gap = 1.5mm
Optimal value: Sc/Eacc^2 = 0.694 Ep = 2.26
Desired point: be = 1.7mm
Optimal value: Sc/Eacc^2 = 0.827 Ep = 2.44
Desired point: be = 1.5-1.6mm
Optimal value: Sc/Eacc^2 = 0.963 Ep = 2.60
Desired point: be = 1.6mm
Sc/Eacc^2 (mA/V)
Ep/Eacc
Sc/Eacc^2 (mA/V)
Ep/Eacc
Sc/Eacc^2 (mA/V)
Ep/Eacc
be (mm)
be (mm)
be (mm)

## Slide 13: Hp, Rsh and Q for gap=1mm
t=2mm, gap = 1mm
t=2mm, gap = 1mm
t=2mm, gap = 1mm
No significant influence
Optimal Q :7000
Optimal impedance: 98.21MΩ/m
Hp is hard to be reduced !!
Hp/Eacc (mA/V)
Quality factor Q
Eff. Shunt imp. Rsh (MΩ/m)
R (mm)
R (mm)
R (mm)

## Slide 14: RF design of the full-scale structure
Top: full 1-metre-long, four-quadrant structure model. Bottom: on-axis electric-field profile.
Parameter | Value
Frequency | 11.994 GHz
Accelerating gradient | 100 MV/m
Input power | 77 MW
Operating mode | 2π/3
Number of cells | 120
Full structure length | 1 m
Quality factor | 6931
Shunt impedance | 97.3 MΩ/m
Peak surface field, Ep | 245 MV/m

## Slide 15: RF–thermal–mechanical multiphysics
Closing the loop between RF losses, cooling, deformation and RF detuning
1 RF baseline
field profile
phase advance
2 Thermal
wall losses
temperature map
3 Mechanical
thermal expansion
deformation
4 RF feedback
S-parameters
field profile
CST/COMSOL cross-check: temperature distributions agree within about 1 °C.
Frequency and field profile/Phase show negligible variation due to temperature gradient distribution along structure

## Slide 16: Multipacting, wakefields and HOM studies
Risk reduction before high-power operation
Multipacting analysis
gradient scan on full quarter-cell model
gap-size study in internal technical report
electron population decays in simulations (no MP)
no critical multipactor observed in investigated range 0.1 mm – 1mm gap (the average SEY remains below unity across the explored gradient range, and the mean collision energy stays below the SEY-unity threshold)
Wakefields / HOM optimization
single- and multi-bunch operation considered
HOM mitigation compatible with open-sector concept
single-bunch case, a Gaussian beam with 1 mm rms bunch length and 200 pC of charge  1keV energy spread

## Slide 17: Mechanical design & prototype fabrication
During the first project year, LNF completed the mechanical drawings and engineering of the full-scale structure (without RF couplers), fabricated to validate:
TIG-welding process
Structure straightness & quadrant alignment
Vacuum performance
Machining — complete
Machine: Doosan DNM 750L CNC
Roughness: Ra < 1 um
All four quadrants machined on a single CNC capable of hosting the full-length parts.
Final CAD model — tuning pins, alignment pins, welding teeth, central pumping port and secondary vacuum chambers.
One quadrant on the inspection table (left); close-up showing individual machined cells (right).

## Slide 18: Joining and welding
The quadrants were joined by TIG welding, with inert gas flushed during the process to protect the weld and preserve the internal vacuum surfaces — the “braze-free” approach central to ASTERIX.
Left: ASTERIX prototype being TIG welded. Right: TIG-welded prototype on the CMM table for mechanical characterization.

## Slide 19: Qualification status
Vacuum Leak Check
A comparison of the dimensional measurements acquired before and after the welding process indicates only minor deviations at the inspected locations:
 straightness max error 20 um, over 1 m.
The observed dimensional variations are minimal and within the expected process capability
 the welding operation preserved the dimensional integrity of the component and was successfully completed without introducing significant deformation.
Result: Positive
Mechanical and vacuum tests on the welded prototype were performed and produced a positive outcome.

## Slide 20: Conclusions and Future Work
Two small-scale prototypes, in single-bunch geometry, to be LOW and HIGH power tested in 2026.
Low RF power measurements are performed at the INFN LATINO Lab.
Full length structure (single-bunch mode) to be machined and high RF powered tested at TEX Facility in Frascati by the end of 2027.
Thanks for your attention!
90 cm