## Slide 1: Update on the Long-Wave-Infrared Laser Capability at ATF
AAC 2026-07-27
Mikhail Polyanskiy, Marcus Babzien, Igor Pogorelsky, William Li, Dismas Choge

## Slide 2: A Different Laser Regime: 9 µm
Facility | Final amplifier technology | λ (µm) | Energy (J) | Pulse (fs) | Peak Power (TW) | Note
ELI-NP HPLS ELI-NP, Romania | Ti:Sapphire | 0.8 | 230 | 23 | 10,000 | 
ZEUS U Michigan | Ti:Sapphire | 0.8 | 50 | 25 | 2,000 | Design goal: 3 PW NSF user facility
NSF OPAL LLE, NY | OPCPA | 0.92 | 500 x 2 | 20 | 25,000 x 2 | Under design
BELLA Petawatt LBNL, CA | Ti:Sapphire | 0.8 | 40 | 40 | 1,000 | 
Texas Petawatt UT Austin | Nd:glass | 1.057 | 150 | 150 | 1,000 | 
ALEPH Colorado State | Ti:Sapphire | 0.8 | 26 | 30 | 850 | 
OMEGA EP LLE, NY | Nd:glass | 1.053 | 500 | 700 | 700 | 
Scarlet Ohio State | Ti:Sapphire | 0.8 | 15 | 40 | 400 | 
ATF 9-micron BNL, NY | CO2 | 9.2 μm | 10 J | 2,000 fs | 5 TW | 2–3 TW typical 25 TW in design Part of DOE user facility
~ 0.9 µm
~ 9 µm

## Slide 3: Electron in Laser Field
λ = 9 µm
λ = 0.9 µm
ncrit ~ 1021 cm-3
ncrit ~ 1019 cm-3
Plasma frequency
Critical plasma density ()
Quiver amplitude
Ponderomotive potential
Plasma in Laser Field
p+
e-

## Slide 4: Science with ATF 9-micron laser

## Slide 5: Science with ATF 9-micron laser
Tuesday 17:20 WG-1 Navid Vafaei-Najafabadi Optimizing laser parameters for blowout regime: from petawatt NIR to LWIR wakefield drivers
Thursday 13:30 WG-6 Yusuke Sakai Nonlinear Inverse Compton Scattering experiments enabled by Long-Wave Infrared Laser in BNL ATF
Thursday 14:10 WG-5 Apurva Gaikwad 1-D plasma lens by laser-driven elongated wakefield
Thursday 17:20 WG-2 Nicholas Dover Diagnosing near-critical-density laser plasma interaction and ion acceleration using dynamic optical probing
Monday poster session WG2 Anusorn Lueangaramwong Study of laser-driven ion accelerators via ultra-fast optical and electron radiography of high-density plasmas at ATF
Monday poster session WG1 Dismas Choge Laser-induced damage in optical components for high-power infrared laser systems
LWFA
LWFA
Compton
Ion Acceleration
Plasma dynamics
Laser technology

## Slide 6: Laser Status and FY27 User Parameters
Commissioning status
Laser operation was authorized earlier in 2026 following the extended ATF shutdown for the Accelerator Readiness Review (ARR).
Commissioning was subsequently interrupted by a component failure and limited personnel availability during ARR preparation.
Near-term milestone: CO2 preamplifier commissioning targeted for next week.
Full-power operation: targeted for August 2026.
FY27 user capability
    Central wavelength 9.24 µm
    FWHM bandwidth 0.10 µm
    FWHM pulse duration 2.0 ps 70 ps with compressor bypassed
    Pulse energy ≤7 J ≤10 J with compressor bypassed
    Peak power ≤3 TW
    Pulse repetition interval ≥90 s
    Additional operating modes
      Linearly polarized output with continuously rotatable polarization angle.
      Circular polarization available at reduced pulse energy, typically <0.5 J.
      mJ-level pulses at 1.5 Hz for experimental setup and alignment.

## Slide 7: Operational priorities and enabling R&D
Operation improvement priorities:
Improve beam quality and focusing, deliver 5 TW to users
Minimize downtime (e.g., alignment-related interruptions)
Improve in-line diagnostics, monitoring, and data logging
R&D priorities toward 25 TW
Develop and qualify critical optical components
Improve numerical modeling of laser components and system performance
Opt. Mater. Express 14, 696 (2024)
Dismas Choge – poster session tonight
Nonlinear refraction and absorption in LWIR optical materials
Ultrafast laser damage at 9.2 µm
DOE Accelerator Stewardship-supported materials R&D helps advance these priorities

## Slide 8: Example of incremental performance upgrade
NaCl / BaF2
Beam profiler
Parameter (@ 9.2 μm) | Unit | NaCl | BaF2
Solubility in water | g/L | 360 | 1.61
Modulus of rupture | MPa | 2.4 | 26.9
Refractive index | - | 1.500 | 1.412
Fresnel reflection | % | 4.0 | 2.9
Volume absorption | % / cm | 0.0 | 2.8
Nonlinear index | 10-20 m2/W | 3.5 | 1.7
Group-velocity dispersion | fs2/mm | -1010 | -2340
BaF2 window housing for high-pressure CO2 amplifier
Improved beam quality
3x thinner than NaCl

## Slide 9: ATF 9-micron laser & recent changes
NaCl→BaF2
NaCl→BaF2
Stretcher
15 μJ 350 fs
10 mJ 70 ps
20 J 70 ps
≤14 J, 2 ps
“5 TW”
@ 9.2 µm
Ge
100 mJ, 6 ns @ 1.064 µm
Coupler
[2 μJ] [140 ps]
Ti:S
OPA
Regenerative CO2 pre-amplifier
osc
Final CO2 amplifier
Compressor
P(CO2+N2+He) = 10 atm
16O : 18O = 50 : 50
C16O2 : C16O18O : C18O2 = 25 : 50 : 25
Seed laser
vacuum
air

## Slide 10: Next-generation concept
25 TW, 100 fs
Post-Compressor
Present system upgrade path
2 ps
5 TW
500 fs
15 TW
100 fs
25 TW
500 fs
3 TW
10 mJ seed
Post-compressor
Post-compressor
demonstrator
[ Report of the Basic Research Needs Workshop on Laser Technology. DOE & NSF, 2024]

## Slide 11: Summary
The ATF 9-micron laser is a unique instrument for advanced accelerator research and related applications.
The laser is being recommissioned following the extended ATF shutdown, with user operation planned for FY27.
Near-term upgrades will improve the present multi-TW system while establishing a path toward a few-cycle, 25-TW capability.
Future LWIR systems are expected to rely largely on solid-state technology, retaining a compact CO₂ amplifier as the high-energy core.
CO2
Solid state
CO2
S.S.
past
present
Solid state
CO2
goal