## Slide 1: Contrast enhancement results of a novel spatially-combined, pulse-stacked ultrafast fiber laser system
July 30th, 2026
David Feng1, Christopher Pasquale2, Yanwen Jing2, Michael Garner2, Almantas Galvanauskas2
A2-Working Group # 2. AAC 2026, UCLA.
1Lawrence Livermore National Laboratory, Livermore, CA 94550
2University of Michigan, Ann Arbor, MI 48109

## Slide 2
Presentation outline
Introduction & motivation (3 slides)
Experiment & setup (4 slides)
Results (5 slides)
Challenges (2 slides)
Conclusion (1 slide)

## Slide 3
Lasers for wakefield particle acceleration
Accelerating electrons to relativistic energies is expensive – km in length & can cost billions of dollars.
Lasers can reduce size & cost by driving strong electric fields in laser-based plasmas to accelerate particles.
Principle of laser wakefield electron acceleration.
Notes: -Intense laser pulse comes into gas jet
-Gas is ionized at the rising edge of pulse → plasma is formed
-Main pulse peak interacts with said plasma
-Electrons in plasma undergo periodic modulations of electron density (Langmuir wave)
-Ponderomotive force drives electrons away from propagation axis, charge separation brings them back
-”Plasma bubble” forms, electron bunches appears, get rapidly accelerated into laser propagation direction by its E-field
-Laser field can be stronger than conventional RF linear accelerators (~GeV/m), e-densities of 10^18 cm-3

## Slide 4
Challenges to deployment of such laser systems
A viable laser for MeV-GeV-class acceleration would require the following specifications:
  High peak power (>100 GW)
  High average power (>1 kW)
  Ultrafast (≤50 fs)
  High repetition rate (>1 kHz)
  High contrast (<10-6)
Pre-pulse contrast simulation.
Notes: All these parameters are typical of a laser capable of outputting electrons accelerated to MeV-GeV.
For sub-10 fs, ~800 nm laser intended to demonstrate LWFA:
Pulse energy: 3–10 mJ
Pulse duration: 5–8 fs
Peak power: approximately 0.4–2 TW
Average power: determined by repetition rate, but 1-2 kHz good enough for MeV scale electrons
Focused intensity: approximately to
Focal spot: 4–8 µm FWHM
Plasma density: several , can be ionization injection assisted
All these parameters are typical of a laser capable of outputting electrons accelerated to MeV-GeV.
For sub-10 fs, ~800 nm laser intended to demonstrate LWFA:
Pulse energy: 3–10 mJ
Pulse duration: 5–8 fs
Peak power: approximately 0.4–2 TW
Average power: determined by repetition rate, but 1-2 kHz good enough for MeV scale electrons
Focused intensity: approximately 1×10^18 to 1×10^19 " " W/cm^2
Focal spot: 4–8 µm FWHM
Plasma density: several 10^19 " " cm^(−3), can be ionization injection assisted

## Slide 5
Second harmonic generation as contrast enhancement
Second harmonic generation (SHG) as a contrast enhancement technique:
  Quadratic contrast enhancement of C2 from
  Achievable high conversion efficiency
  Simple setup
Cons:
  Does not remove relatively intense pre/post-pulses
  Parametric fluorescence at high enough intensities (loss to pulse wavelength packet)
  Temporal distortion from passing through a nonlinear crystal
Nonlinear crystal
Representation of SHG.
Notes: Add in the equation for SHG equation
-Can compensate for wavelength with geometry of the beam focus

## Slide 6: 12-Channel Spatially and Temporally Combined (CBC-CPSA) Fiber Laser System

## Slide 7: 12-Channel Spatially and Temporally Combined (CBC-CPSA) Fiber Laser System
12-channel CBC+CPSA Results:
  1mJ/fiber @ 2 kHz
  CBC efficiency: 90%
    ~20W for temporal combining
  Stacking efficiency: 80.2%
1mJx12 Channel Stacking
Energy per fiber (12 total) | 1 mJ
Repetition rate | 2 kHz
Pulse duration | 300 fs (transform limited)
Avg power/pulse energy into experiment | 6 W max, 3 mJ max
Beam size (elliptical major axis) | 10 mm
Notes: For 1mJx12ch combining, the stacking efficiency now is related to how much power in the stacker:
P=3W stacking efficiency: 80.2%
P=20W stacking efficiency: 60.8%
Rms stability:
1mJ (0428wfm3): 0.961%
3mJ (0604wfm5): 3.572% (another 3mJ shot on the same day has 1.648%)
6mJ (0714wfm3): 4.402%
No data for 1x12
2.105% for 1mJx12 when 60mW into stacker
3 mJ, unfocused beam → 25GW/cm^2

## Slide 8
Experimental setup
AOM (532nm)
PBS
Dump
Telescope
x0.75, 0.5, 0.25
NL crystal
Attenuator
DM
HWP
Beam entrance
HWP
DM
Residual fundamental
HWP
Focus
lens
TFP
PD
tp = 300 fs
d = 10 mm
1st order beam
0th order beam
Notes: We keep the 1st order beam because it can be time-gated on the detector/scope
Even though in this experiment, the pre-pulse & the main pulse were not separated by such a large time interval so the 1st order beam was not necessary
However we kept it just in case for future experiments

## Slide 9
Nonlinear Crystals Used
Equipment:
2mm-L, 50mm-D Type I LBO @ 1035 nm, (90,13.2)∘
10mm-L, 25.4mm-D LBO Type I LBO @ 1053 nm (90,12)∘
5mm-L, 50mm-D YCOB @ 1047nm (150, 0)∘
10mm-L, 50mm-D YCOB @ 1047nm (150, 0)∘
LBO crystal (Cristal Lasers).
YCOB boule (LLNL).
Notes: Angles are (theta, phi) at each respective wavelength. Our wavelength is at 1035nm, so we would need about at least 1 deg of tuning to get proper phase matching for LBO
For YCOB, it is assumed that the cut was phase-matched at 1047nm. This corresponds to about 0.5 deg of tuning to get to 1035nm phase matching.

## Slide 10
YCOB results
Experimental results for YCOB.
Original crystal contained several inner crystal defects; scratch-dig was worse than 20/10.
Better phase matching requires tilting about polarization axis, which was not attempted.
There was also absorption loss in the dichroic mirrors for both IR & visible.
Modeling by SNLO (2D) and comparison with experiment (dots).
Notes: Measurements collected with two separate power meters, one for IR, one for green
Average power was measured, beam profile measured beforehand
-YCOB crystal was cut by LLNL optic shop, so crystal axis was largely guessed in an educated manner (through deduction from the original labeling).

## Slide 11
LBO results
Crystal length of 10 mm.
Crystal length of 2 mm.
Notes: We could not get any higher than 36% overall.

## Slide 12
LBO results
Modeling by SNLO (2D) and comparison with experiment (dots).
Huge discrepancy in SNLO!
Notes: We could not get any higher than 36% overall.
2TW/cm^2 curves aren’t shown due to model not being able to accommodate such high peak intensities.

## Slide 13
Discussion of results
Why are we getting lower conversion efficiency than expected?
  Pulse of 300 fs, 2 mm, 280 uJ → ~33% efficiency
For 1035 nm, 300 fs in LBO: GVM = 51 fs/mm
  L = 2 mm →
  L = 5 mm →
  L = 10 mm →
  10 mm is much longer than interaction length!
Spectral acceptance bandwidth for 1035nm in LBO: 1nm-cm
  L = 1 mm →
  L = 2 mm →
  L = 5 mm →
  L = 10 mm →
  Other wavelengths are not optimally phase-matched!

## Slide 14
Discrepancies
Taking this into account in the modeling (phase mismatch, spectral acceptance bandwidth):
LBO crystal modeling results for different peak intensities.
Notes: And the efficiency at 2 mm is actually not much greater!
Phase mismatch is a huge key. 1-2 deg off could throw it off by a lot.
Used Gaussian as the main temporal pulse shape, did not take into account real pulse shape in lab

## Slide 15
Discrepancies
Additional nonlinear wavelength generation observed in the lab:
Some energy lost into generating other different colors.
Possible culprits:
Parametric fluorescence
fs filamentation optical emission from crystal
From damage to coating or defect
Live experiment in the lab showing a red ring around the power meter head.
Notes: If the audience knows what it is, they are free to comment
We started seeing this at around 100 GW/cm^2

## Slide 16
Contrast enhancement
Prepulse contrast:
Fundamental: 4.65 dB
SHG: 8.88 dB
Prepulse contrast enhancement:
8.88dB / 4.65dB = 1.91
Confirmed that the prepulse contrast enhancement is ~I2
Notes: >> 10*log10(0.3427)
ans =
-4.6509
>> 10*log10(0.1294)
ans =
-8.8807
>> 10*log10(0.1294) / (10*log10(0.3427))
ans =
1.9095
Prepulse contrast enhancement:
Fundamental: 34.27%
SHG: 12.94%

## Slide 17
Summary & future work
Two types of nonlinear crystals were used for contrast enhancement.
Efficiency was much lower than expected.
Should be mainly due to imperfect phase-matching of the crystal.
Observed some kind of optical emission after the crystal.
Return to Michigan, re-do experiments with crystal lengths between 2-10 mm (specifically 4, 5, 6 mm).
Completely characterize pulse before & after crystal – set up autocorrelator after SHG for fundamental pulse.
Better prepared, know how to improve diagnostics & what laser intensity range to run.