## Slide 1
22nd January 2026
Superconducting nanowire detectors towards astronomy applications
Boris Korzh
Quantum Technologies Group
Department of Applied Physics
University of Geneva, Switzerland
boris.korzh@unige.ch

## Slide 2: Superconducting nanowire single-photon detector (SNSPD)
Nanofabrication
Goltsman, et al, APL 79, 705 (2001)
Single-pixel detector
No need for full ‘Foundry’ process like SPADs
 Easier to tailor the devices for astronomy community
Some select fabrication facilities (Academic and National Lab):
Jet propulsion Lab, CA, USA
NIST, Boulder, CO, USA
MIT Nano, MA, USA
NICT, Japan
EPFL, CMi, Switzerland
TU Delft, Netherlands
Münster, Germany
KTH, Sweden
SIMIT, China
Nanjing, China
…..
Notes: Really visualize the SNSPD and this forms the story

## Slide 3: Different formats
Single-pixel
Interleaved pixel
Pixel array
Linear arrays
Quantum science
Fast count rates
Large collection area / spectroscopy
Imaging
Waveguide
Notes: Really visualize the SNSPD and this forms the story

## Slide 4: Superconducting nanowire detector mechanism
Allmaras, Modeling and Development of Superconducting Nanowire Single-Photon Detectors, Ph.D. Dissertation, Caltech (2020)
1. Current-biased superconducting nanowire
1
2
3
4
5
Typically operating at 0.3-5 kelvin
2. Photon absorption & Hotspot formation
3. Suppression of superconductivity
4. Normal domain growth – Fully digital
5. Recovery
Notes: Let me show you how it works Add general pictures of nanowires
- For reference

## Slide 5
Timing jitter | Intrinsic photon number resolution | Efficiency | Array size | Maximum count rate | Dark count rate | Active area | Cut-off wavelength
18 ps | None | 93% | 64 | 1 Gcps | 4 /s/mm2 | 0.001 cm2 | 5 μm
1 ps | 10 | 99 % | 107 | 10 Gcps | 1x10-6 /s/mm2 | 1 cm2 | 100 μm
4x10-5 /s/mm2
Records in 2016
Expected performance by 2030
2.6 ps
98%
29 μm
1.5 Gcps
3-5 photons
Current records for isolated devices
0.1 cm2
4x105
Advances in superconducting nanowire detectors
[1] Korzh et al, Nature Photonics 14, 250 (2020)
[2] Reddy et al, Optica 7, 1649 (2020)
[3] Oripov et al, Nature 622, 730 (2023)
[1]
[3]
[4] Craiciu et al, Optica 10, 183 (2023)
[5] Resta et al, Nano Letters (2023)
[6] Chiles et al, PRL 128, 231802 (2022)
[7] Taylor et al, Optica, (2023)
[7]
[4,5]
[3]
[2]
[6]
Quantum science
Remote sensing
Astronomy
Biomedical imaging
High energy physics
Notes: Let’s take a look at advanced since the 2015 Bell test
In fact, I contributed to 6/8 current records for SNSPDs
Including the factor of >5 factor improvement in timing resolution
As well as other important metrics for Quantum Science
 including intrinsic photon number resolution, array size and maximum count rate
We are on verge of the next revolutionary breakthrough in quantum optics by  access to multiple metric simultaneously
 This is the main main of this Starting grant - to group these metrics into a single device for the first time
+ impact QC and QI
Understanding of all of these metric individually is important for bringing them together
 I am well positioned to do this, given my contributions in the field so far

## Slide 6: Established and potential SNSPD Applications
Quantum computing
Deep space optical comm,
Quantum comm
Physical chemistry
315 nm
280 nm
200 nm
10 100
2013
2020
2023
2017
2017
Now
Exoplanet spectroscopy
Exoplanet imaging,
Stelar intensity interferometry
Far-UV astrophysics
Notes: Highlight the focus At the end I’ll come back to talk about this etc, how we are seeing ourselves in that domain Highlight what lead to a publication

## Slide 7: NASA Deep Space Optical Communication
7
~10 exa-photons / sec (1019)
~1 mega-photons / sec (106)
Wollman, Allmaras, Beyer, Korzh, Runyan, Narváez, Farr, et al. 2024. “An SNSPD-Based Detector System for NASA’s Deep Space Optical Communications Project.”
Received from 30 Million kilometers!
Notes: State how many photons we start with and at the end
4W and then ~10 photons?

## Slide 8: Engineering challenges solved
Wollman, Allmaras, Beyer, Korzh, Runyan, Narváez, Farr, et al. 2024. “SNSPD-Based Detector System for NASA’s Deep Space Optical Communications Project.” Optics Express 32 (27): 48185.
High-density cryogenic RF cabling
Scalable cryogenic readout electronics
High yield of large area detectors

## Slide 9: In first receiver in Europe
Link closed from 300 Million kilometers!
https://www.esa.int/Enabling_Support/Operations/ESA_wraps_up_300-million-kilometre_optical_communication_campaign
Swiss industry involvement:
Notes: - Example to illustrate how detectors can impact quantum communication
- QKD --> Alice sends ...
- key secured by laws of physics
- These states are encoded in timing of photons
- dark counts and timing --> errors
- Developed a record low dark count rate
- Build a specific system to leverage this  to this day it is the record for semiconductor device In future, for secure communication  need to increase distances
 Need to increase beyond single –inks  quantum repeaters

## Slide 10: Thermal coupling between layers
  Layer 1: SNSPDs = columns
  Layer 2: SNSPDs = rows
Allmaras, Wollman et al, Nano Letters 20, 2163–2168 (2020)
McCaughan, Zhai, Korzh, Allmaras et al, APL 121, 102602 (2022)
On-demand read out
1 photon  4 clicks
 Zero read noise!

## Slide 11: 400,000 pixel camera
Oripov, Rampini, Allmaras, Shaw, Nam, Korzh, and McCaughan, Nature 622, 730 (2023)
Gen 1. (proof-of-concept) performance:
Designed for UV-Vis
  4-10% efficiency
  Only due to prototype design decisions
Maximum count rates: 100 kcps
0.13 counts/sec background rate
Fabricated at
Initially developed for photon starved applications:
Far/deep-UV Astrophysics, Earth-like exo-planet imaging

## Slide 12: 400,000 pixel camera
Oripov, Rampini, Allmaras, Shaw, Nam, Korzh, and McCaughan, Nature 622, 730 (2023)
Future work
Boost efficiency
Increase count rates for practical applications
Largest superconducting camera by x20
Fabricated at
MKID camera

## Slide 13: Practical closed-cycle cryogenics
Mueller, Korzh, Runyan et al, Optica 8, 1586 (2021)
‘Bottom referenced’ cryostat with panels
Direct coupling to optical table
Vibration isolation included
Designed & Fabricated at UNIGE
23 cm
Compact version for 1 kelvin operation (>1 micron wavelengths)
2 kelvin version is sufficient for <1 micron wavelengths

## Slide 14: Summary
SNSPDs are fully digital and easy to customize
Single pixel devices:
  Timing jitter <5 ps RMS
  High efficiency for 375-1550 nm demonstrated
  Up to 29 um sensitivity demonstrated
Fast count rate arrays have been instrumented on telescopes for deep-space optical communication
  Being deployed at ground stations in Switzerland and internationally for space-to-ground quantum communication
2D arrays
  Proof-of-principle (Gen. 1) 400,000 pixels have been demonstrated
  Gen. 2 arrays will boost efficiency and count rates
1D arrays – in development
  Will combine good timing resolution and high count rates
1 mm
Notes: Condense this

## Slide 16: Second: Efficient multiplexing in time-domain
vph ≈ 0.01c (3 μm/ps) velocity helps us out this time!
 10 ps timing resolution enables 15 μm pixels to be resolved
Time-of-flight difference in a superconducting bus
McCaughan, Zhai, Korzh, Allmaras et al, APL 121, 102602 (2022)

## Slide 17: Far-IR – 43 meV (29 μm)
Taylor et al. 2023. “Low-Noise Single-Photon Counting Superconducting Nanowire Detectors at Infrared Wavelengths up to 29 Μm.” Optica 10: 1672.
Notes: Really visualize the SNSPD and this forms the story

## Slide 18
2nd Ground receiver in California - Goldstone
Allmaras, J., Korzh, B., Beyer, A., & Wollman, E. (2023). Large-area SNSPD array for RF/optical hybrid 7-segment pathfinder receiver. https://www.spiedigitallibrary.org/proceedings/Download?urlId=10.1117%2F12.2655467