## Slide 1: InP/InGaAs for Integrated Astrophotonics between 4 and 18 μm
Exoplanets and Habitability Group
SIAPS 2026
David Eglin – PhD Student
daeglin@ethz.ch
22.01.2026, Bern
Quantum Optoelectronics Group

## Slide 2: The Large Interferometer for Exoplanets (LIFE)
Bracewell nulling interferometer
A proposed space mission
Characterisation of Earth-like exoplanets
Thermal emission 4-18 μm
Nulling interferometry
Notes: ~3 m apertures
10-600 m baseline
Targets < 30 pc (100 lyrs)

## Slide 3: The Large Interferometer for Exoplanets (LIFE)
A proposed space mission
Characterisation of Earth-like exoplanets
Thermal emission 4-18 μm
Nulling interferometry
~3 m apertures
10-600 m baseline
targets < 30 pc (100 lyrs) away
beam combiner
Bracewell nulling interferometer
► Phase reversal ► Beam combination
Glauser et al., SPIE (2024)
Bracewell, Nature (1978)

## Slide 4: The Nulling Interferometer Cryogenic Experiment (NICE) – on chip
Bulk-optics demonstration of the LIFE requirements
Photonic implementation:
10-5 null depth ✓ | 20% photon conversion ✓
15 K ✗ | 1 nm RMS OPD drift ✓
4-18 μm ✗ | 
Ranganathan et al., SPIE (2024)
10-5 null depth | 40% throughput
15 K | 1.4 mrad phase mismatch
4-18 μm | 0.3% intensity mismatch

## Slide 5: Existing on-chip nullers
10-4 null | ~37% | 3.5-4 μm
ASGARD/NOTT (VLTI)
Sanny et al., A&A (2026)
Klinner-Teo et al., SPIE (2022), Spalding et al., SPIE (2024)
10-3 null | <87% (sim.) | 1.45-1.7 μm
GLINT (Subaru telescope)
Our requirements
10-5 null | 40% | 4-18 μm
LIFE
→ Different material:
InP/InGaAs
Notes: GLS glass (chalcogenide glass, gallium lanthanum sulphide), ULI (ultrafast laser inscription)
Borosilicate glass

## Slide 6: InP/InGaAs waveguides: Fabrication and characterisation
10 μm
Notes: Lens/WG NA mismatch (~0.33/1.4) Spot size ~50 μm
Coupling efficiency
1 dB = 20%
Lens/WG NA mismatch (~0.33/1.4) Spot size ~50 μm
Coupling efficiency ≲3%
1 dB = 20%

## Slide 7: Outlook: Achromatic phase shift “Bulk-optics-approach”
phase difference
~50 nm bandwidth
Photonic beam splitter
Possible nulling scheme
InP
InGaAs
Notes: Beam splitter equivalent to directional coupler

## Slide 8: Outlook: Dry-etch process
Pattern control
Exposed surface: degradation & impurities
Dry-etch
Wet-etch
0.5 dB/cm <5 μm
Zhang et al., Appl. Phys. Lett. (2022)
InP
InGaAs
InP

## Slide 9: Summary
Developments in astrophotonics allow on-chip nulling today
InP/InGaAs: promising for photonics-based LIFE mission
Wavelengths >11 μm and cryo have not yet been explored
We report waveguide losses and develop achromatic nulling schemes compatible with LIFE
Many thanks to…
…and the Exoplanets & Habitability and Quantum Optoelectronic groups at ETH Zurich!
Cvetojevic et al., A&A (2022)
Sascha Quanz
Jérôme Faist
Adrian Glauser
Contact:
David Eglin
daeglin@ethz.ch
PhD Student