## Slide 1: Laser ablation models and experimental activities in support of a LIBS diagnostics for the BiGyM linear plasma device for fusion-relevant applications S. Cipelli1,2
Final workshop of the NEFERTARI project (New Equipment for Fusion Experimental Research & Technological Advancements with Rfx Infrastructure)
Padova
March 24 – 27, 2026
1Istituto per la Scienza e Tecnologia dei Plasmi, CNR, 20125 Milano, Italy 2Centro Ricerche Fusione (CRF) – Università degli Studi di Padova, 35122 Padova, Italy

## Slide 2: Outline
LIBS: Laser Induced Breakdown Spectroscopy
Design of an in-situ LIBS on the BiGyM linear plasma device
Laser ablation modeling
  Nanosecond laser ablation
  Picosecond laser ablation
Experimental in-situ LIBS retention measurements on the PSI-2 linear device
Conclusions and future developments
Collaboration with WP9 CNR-ISTP Bari
1

## Slide 3: LIBS: Laser Induced Breakdown Spectroscopy
Information about chemical and isotopic composition
Main advantages:
Possibility of in-situ measurements
Remote detection
No sample preparation
Minimal damages to the target
Possible combination with laser-based cleaning techniques
Can operate in harsh environments (vacuum, presence of magnetic field and background plasma)
Promising diagnostics for PFCs monitoring in tokamaks and LPDs
2

## Slide 4: Design of an in-situ LIBS on the BiGyM linear plasma device
Nominal λ [nm] | 1064
Pulse duration [ps] | 29 ± 5
Max pulse energy [mJ] | 70
Repetition rate [Hz] | 10
Picosecond laser pulse
→ reduced Heat-Affected Zone (HAZ), improved depth resolution
High max pulse energy
→ high SNR, broad fluence range available
Focal lenght [mm] | 320
Min slit width [μm] | 10
Compact design
Correction of optical aberrations
Set of 3 interchangeable gratings
PMAX Intensified CCD camera (Gen II SR intensifier)
3

## Slide 5: Design of an in-situ LIBS on the BiGyM linear plasma device
BiGyM linear device laboratory
Diagnostics laboratory
Hole for the optical path
Hole for the optical path
EKSPLA laser
BiGyM pre-chamber
4

## Slide 6: Design of an in-situ LIBS on the BiGyM linear plasma device
Optical fiber
Laser beam guide
Technical drawing of an optical path connecting the laser system to the BiGyM pre-chamber
Top view
Side view
~8 m optical path length
Beam enclosed by safety tubes
Use of 3 fixed mirrors + 1 motorized steering mirror (for control of focusing position)
Focusing lens
Lens + optical fiber for collection of plasma light
5

## Slide 7: Laser ablation modeling
A schematic view of the LIBS process
Example of LIBS ablation craters on tungsten
3D reconstruction of ablation crater
Single pulse signal is influenced by:
Ablation crater dimensions (spatial resolution)
Thermal penetration depth (thermal-induced phenomena)
LASER ABLATION MODELING
As a support tool for the LIBS measurements interpretation
Prediction ablation crater characteristics
Simulation of the temporal evolution of temperature field
Important for nuclear fusion applications (retention)
Spatial information on retained H isotopes
Supports correct interpretation of LIBS signal (thermal-induced effects on particles)
6

## Slide 8: Nanosecond laser ablation modeling
Finite Element (FE) model developed using COMSOL Multiphysics®
Starting point: ns laser ablation (reference choice for most of the existing setups)
2D axisymmetric
Simulation of laser-target interaction
Vacuum conditions
ns pulse duration
Single pulse incidence
Equations & hypotheses
Heat transport equation →
Laser heat source →
Neglects air convection and thermal radiation
Includes temperature-dependent thermophysical properties and phase transitions
Neglects dynamics of vaporized material and plasma generation neglected
Mass density
Thermal conductivity
Isobaric heat capacity
Material reflectivity
Gaussian temporal profile and spatial distribution
Depends on the observed ablation regime
Normal evaporation
Phase explosion
Plasma shielding introduced with a semi-empirical approach
7

## Slide 9: Nanosecond laser ablation modeling
Experimental validation: laser irradiation of samples at CNR-ISTP Bari
50 μm
CNR-ICMATE
SEM
E = 1.8 mJ 10 pulses
Mechanical profilometer
Nd:YAG laser
τL = 10 ns
λ = 1064 nm
RR = 10 Hz
Crater surface analysis - W
2 materials
Tungsten
Silicon
Results for tungsten
No signs of violently expelled material (gentle ablation, normal evaporation)
Modeling hypothesis: consider only the central axisymmetric part of the pulse
8

## Slide 10: Nanosecond laser ablation modeling
Experimental validation: laser irradiation of samples at CNR-ISTP Bari
CNR-ICMATE
SEM
E = 1.8 mJ 10 pulses
Mechanical profilometer
Nd:YAG laser
τL = 10 ns
λ = 1064 nm
RR = 10 Hz
Crater surface analysis - W
2 materials
Tungsten
Silicon
COMSOL® T field
E = 1.8 mJ
Results for tungsten
50 μm
Molten region extending 700 nm below crater bottom
9

## Slide 11: Picosecond laser ablation modeling
Use of picosecond pulses:
→ Energy initially absorbed by electrons (1) and successively transmitted to lattice (2-3)
Plasma plume generated after ~100 ps (4) → virtually no laser-plasma interaction
Two Temperature model (TTM)
Equations & hypotheses
2D axisymmetry
2 heat transport equations
Gaussian laser heat source absorbed by el subsystem
BCs similar to those of ns ablation model
Neglects plasma shielding
electrons-phonons coupling constant
10

## Slide 12: Picosecond laser ablation modeling
Experimental validation: laser irradiation of samples at CNR-ISTP Bari (only tungsten)
Yb laser
τL = 10 ps
λ = 1030 nm
RR = 10 Hz
Measurement chamber
Low p environment (≈ 1 mbar)
Ar atmosphere
1.35 mJ
64 pulses
100 μm
CNR-ISTP Bari
Optical profilometer
Optical microscope
Results: model validation and max T evolution
11

## Slide 13: In-situ LIBS retention measurements on the PSI-2 linear device
PSI-2 LPD
6 m long machine
High-current arc-discharge source
~6 cm plasma column
Controlled sample exposure (bias voltage, sample temperature)
In-situ measurements of short-term D retention using LIBS
W (reference PFC material)
Ta (superior resistance to He-induced damages, higher retention expected)
Experimental goals:
Reconstruct D outgassing curves
Compare results for W with Ta, for which worse retention properties are expected
Objective of the activity: gain practical experience with in-situ LIBS on linear plasma devices
12
Exp time [min] | 190
Ion fluence [m-2] | 3.3∙1025
Eions [eV] | 80
Tsamples [°C] | 250
Exposure parameters
Measurements for successive times
Fitting and integration of Dα peak

## Slide 14: Conclusions
Individuation of suitable components for an in-situ LIBS on BiGyM (ps EKSPLA laser, Isoplane 320 spectrometer)
Preliminar design of LIBS optical path (8 m, 3 fixed mirrors, 1 steering mirror, focusing lens)
Development of a numerical model for ns laser ablation and successful validation for W and Si
Development of a numerical model for ps laser ablation and successful validation for W
In-situ LIBS measurements for short-term D retention assessment, highlighting differences between W and Ta
This work is based on a combined approach (preliminary design, modeling as support activity, experiments)
Future developments
Modeling activity: introduction of gas dynamics and ionization equations → prediction of plasma plume characteristics
Diagnostics development:
Optical path construction
Diagnostics commissioning
First measurements
Late summer 2026
Oct-Nov 2026
End of 2026
13

## Slide 15: Acknowledgments
CNR-ISTP Milano
  A. Cremona, A. Uccello, J. Scionti, I. Casiraghi, and the GyM team
CNR-ISTP Bari
  G. Dilecce, A. Hussain, P. F. Ambrico, D. Aceto
Forschungszentrum Jülich (FZJ)
  S. Brezinsek, Y. Rongxing, G. Sergienko, D. Matveev, E. Wüst, C. Kawan, S. Möller, and the active/passive spectroscopy group
CNR-ICMATE Milano
  D. Ripamonti
ENEA Frascati
  M. Iafrati, M. Alonzo, S. Almaviva
14

## Slide 16: Backup slides

## Slide 17: Nanosecond laser ablation modeling
Experimental validation: laser irradiation of samples at CNR-ISTP Bari
50 μm
CNR-ICMATE
SEM
E = 3.6 mJ 1 pulse
Mechanical profilometer
Nd:YAG laser
τL = 10 ns
λ = 1064 nm
RR = 10 Hz
Crater surface analysis - Si
2 materials
Tungsten
Silicon
Results for silicon
Signs of violently expelled material (phase explosion)
2 sets of simulations to take into account an experimental spot size variation

## Slide 18: Nanosecond laser ablation modeling
Experimental validation: laser irradiation of samples at CNR-ISTP Bari
50 μm
CNR-ICMATE
SEM
E = 3.6 mJ 1 pulse
Mechanical profilometer
Nd:YAG laser
τL = 10 ns
λ = 1064 nm
RR = 10 Hz
Crater surface analysis - Si
2 materials
Tungsten
Silicon
Results for silicon
Molten region extending 500 nm below crater bottom
COMSOL® T field
E = 3.6 mJ

## Slide 19: Picosecond laser ablation modeling
Experimental validation: laser irradiation of samples at CNR-ISTP Bari (only tungsten)
Yb laser
τL = 10 ps
λ = 1030 nm
RR = 10 Hz
Measurement chamber
Low p environment (≈ 1 mbar)
Ar atmosphere
1.35 mJ
64 pulses
100 μm
CNR-ISTP Bari
Optical profilometer
Optical microscope
Results: lattice T evolution
E = 3.4 mJ
ns laser ablation, F=20 J/cm2
Molten region extended 700 nm below crater bottom
ps laser ablation, F=12 J/cm2
Molten region extended 100 nm below crater bottom

## Slide 20: In-situ LIBS retention measurements on the PSI-2 linear device
PSI-2 LPD
In-situ LIBS diagnostics
6 m long machine
High-current arc-discharge source
~6 cm plasma column
Controlled sample exposure (bias voltage, sample temperature)
In-situ measurements of short-term D retention using LIBS
W (reference PFC material)
Ta (superior resistance to He-induced damages, worse retention properties expected)
Experimental goals:
Reconstruct D outgassing curves
Compare W with Ta, for which worse retention properties are expected
Exp time [min] | 190
Ion fluence [m-2] | 3.3∙1025
Eions [eV] | 80
Tsamples [°C] | 250
PSI-2 sample holder
Objective of the activity: gain practical experience with in-situ LIBS on linear plasma devices

## Slide 21: In-situ LIBS retention measurements on the PSI-2 linear device
LIBS measurements for successive times
Radial dependence of ion flux → measurements at different radial positions
Identification of the Dα peak for each spectrum
Peak fitting, numerical integration, and reconstruction of the outgassing curves
Normalized comparison W-Ta
Each point is a radial average
W: faster decrease for long times
Ta: higher outgassing for short times
No quantitative information about D concentration
D concentration derived from an ion beam technique (NRA)

## Slide 22: In-situ LIBS retention measurements on the PSI-2 linear device
LIBS measurements for successive times
Different radial positions because of radial radial flux variations
Peak fitting: pseudo-Voigt function
weight parameter
width
Center of distribution
W: direct D peak individuation
Ta: subtraction procedure
Dα: 656.1 nm
Dα: 656.1 nm
Each point is a radial average
W: faster decrease for long times
Ta: higher outgassing for short times
No quantitative information about D concentration
Probable presence of D into the bulk

## Slide 23: In-situ LIBS retention measurements on the PSI-2 linear device
Nuclear Reaction Analysis (NRA) measurements: absolute quantification of long-term D retention
Ta
W
Average concentration for a region of area 150×150 μm
Decreasing concentration from 0.15% to 0.05% going into the bulk
Higher average relative concentration than W
Increasing concentration from 2.5% to 4.5% going into the bulk
→ Strong contribution of bulk retention mechanisms