## Slide 1
Perspective of Superconducting RF cavities on high-Q and high-G
CNRS/IN2P3/IJCLab
Akira Miyazaki

## Slide 2
Perspective of Superconducting RF cavities on high-Q and high-G
CNRS/IN2P3/IJCLab
Akira Miyazaki
My personal bias
QED, axion,
Superconductivity,
Physics via RF

## Slide 3: Outline
Introduction
  Why do we need high-Q / high-G cavities?
State-of-the-art bulk niobium cavities
  How to understand & optimize high-Q / high-G cavities?
  Theory & engineering
Alternative materials
  Nb3Sn/Nb
  MgB2 & HTS
Practicalities
Conclusion

## Slide 4: Outline
Introduction
  Why do we need high-Q / high-G cavities?
State-of-the-art bulk niobium cavities
  How to understand & optimize high-Q / high-G cavities?
  Theory & engineering
Alternative materials
  Nb3Sn/Nb
  MgB2 & HTS
Practicalities
Conclusion

## Slide 5: Superconducting RF (SRF) cavities for particle accelerators
Resonant acceleration of particles synchronized with RF
Power dissipation with gradient
Challenge: minimize with high  higher
High-Q = lower surface resistance
An excellent solution: superconducting resonator
with superconducting gap
Electric fields: along the beam axis
Courtesy: F. Bouly

## Slide 6: SRF is useful and interesting but NOT a magic wand…
Pros: versatile for various needs with basically the identical technology
Cons: somewhat limited in gradient, more crucially lacking sustainability (LHe, pure Nb)
But extremely interesting in fundamental science
Nonequilibrium superconductivity has not been fully understood!
A lot of applications in other fields: photon sensors, qubits, DM & GW searches
Courtesy of
S. Belomestnykh
Nitrogen doping
standard ILC treatment
1.3 GHz
1.3 GHz ILC
800 MHz FCCee
1.3 GHz EuXFEL
100 MHz HIE-ISOLDE
400 MHz HL-LHC
352 MHz
ESS
2 GHz
MAGO
8.8 GHz
RADES

## Slide 7: Where do we need high-Q/high-G SRF cavities?
- Energy frontier storage ring (CW, high current)
 SuperKEKB, LEP2, LHC, FCCee, CEPC, FCChh
- Proton linac (long pulse / CW, high current)
 ESS, MYRRHA, PIPII, MuCol injector
- Electron linac (long pulse / CW, high current)
 EuXFEL, LCLSII, SHINE, etc
- Energy frontier e+/e– linear collider (long pulse / short pulse)
- Heavy ion linac (CW, low-high current)
 Srial2, SRILAC, HIE-ISOLDE, RAON, FRIB, ANL-ATLAS, etc
 High-G is absolute must  CLIC/C3/plasma is better wrt gradient
High current machines
High-Q SRF cavities may be the only solution
High-G has reservation
 high-G x high current has limitations in power (coupler window, power supply, amplifier, etc)
Decision making depends on various things: aperture, cryogenic infrastructure, high-power RF, overall technical readiness, …

## Slide 8: R&D toward high-Q/high-G…in the modern context
Carnot’s theorem
Required power
Impact of power dissipation depends on the operation temperature
1 W evacuation: 1 kW from 2 K vs 200 W from 4 K (vs <10 W from 70 K)
Simpler cryogenic system (2K needs 30 mbar pumping) is an advantage
Reasonable-Q at higher T can be a competitive option  new SC materials!
M. Seidel iSAS workshop 2023
S.Claudet et al, CERN 2013
(Carnot cycle)

## Slide 9: Outline
Introduction
  Why do we need high-Q / high-G cavities?
State-of-the-art bulk niobium cavities
  How to understand & optimize high-Q / high-G cavities?
  Theory & engineering
Alternative materials
  Nb3Sn/Nb
  MgB2 & HTS
Practicalities
Conclusion

## Slide 10: Linear response of condensed matter against classical RF
If the RF field is “small”
=
+
+ …
First order perturbation
Higher order terms ignored
equilibrium
equilibrium
The responding current is given by the equilibrium state (fluctuation-dissipation theorem)
A. Shimizu, UTokyo
(Suspicious in our case…)
: Fermi Liquid  Ohm’s law : BCS  Mattis Bardeen
Mattis & Bardeen Phys Rev 111 412 (1958)
R. Kubo, J. Phys. Soc. Jpn. 12, pp. 570-586 (1957)

## Slide 11: Linear response theory can be approximated by Fermi’s Golden rule
(photon energy) x (net # of absorbed photons)
All quasiparticles
: density of states (how many quantum states at energy : a kind of degeneracy)
: distribution function (how many electrons are in one state at energy )
Fermi-Dirac function in equilibrium state
2
Gap
Z. Physik 266 p.209 (1974)

## Slide 12: Remark: SRF is semi-classical
The right picture is just schematic for simplicity
looks like a photon but it is classical microwaves
We treat quantized electrons interacting with classical microwave  semi-classical!
This approach is valid if the intensity of the microwave is high:
A true photon is described by quantum field operator
Only important if you study quantum sensing and qubits (eg. Vacuum Rabi oscillation, etc)
Maybe a misleading schematic 

## Slide 13: Prediction from the Mattis Bardeen theory (1958)
G. Ciovati PhD thesis
Bulk niobium
+ surface engineering
Optimal
BCS-MB for niobium
Halbritter, KFK-Ext.03/70-06 (1970), https://publikationen.bibliothek.kit.edu/270004230
Optimized impurity on the RF surface (100 nm) is the key to maximize
Optimization has been identified via try & error (or serendipity)

## Slide 14: Surface engineering in clean vacuum furnaces
KEK
FNAL
JLAB
IJCLab
ZANON
DESY
Furnace baking with cryogenic pumps
Oxygen doping, nitrogen doping, etc
Some minor differences among the labs
Systematic studies on different parameters over various laboratories are on-going

## Slide 15: Impurity distribution via Secondary-ion mass spectrometry (SIMS)
Courtesy of Hannah Hu, FNAL
Only 100 nm from the surface contributes to the RF performance (London penetration depth 40 nm)
Mid-T baking (FCC, CEPC, PIPII) / N-doping (LCLSII, PIPII)  homogeneous O- distribution / N- distribution
120C baking (ILC standard)  inhomogeneous O- distribution

## Slide 16: Homogeneous impurity distributions: higher-Q
Magnetic impurity (Dynes)
BCS density of state
Takayuki Kubo, Phys. Rev. Applied 17, 014018, 2022
Magnetic scattering
Non-magnetic scattering
The overlap between and causes loss
The pole at D cause ; the states below D causes
Smearing of decreases and increases
Combination of magnetic (O?) and nonmagnetic (N?) impurity scattering can control a minimum of
Less room for excitation!

## Slide 17: Inhomogeneous disorder: higher-G
London equation with spatial inhomogeneity
Oxygen diffusion model
Current distribution
Enhancement in Bean-Livingston barrier
for uniform case
Low-T bake diffuses O from surface oxide and generates gradient in the impurity distribution
Such a distribution leads to the enhancement of the quench field i.e. higher-G
Microscopic model [V. Ngampruetikorn and J. A. Sauls Phys. Rev. Research 1, 012015(R) 2019] also suggests the similar results under the inhomogeneous disorder
120C 48h
SIMS data
E. M. Lechner et al J. Appl. Phys. 135, 133902 (2024)
120C 48h
120C 48h

## Slide 18: New research trends from 2012: nonequilibrium dynamics
Antonio Bianchi, SRF2025
Publication in preparation
Non-equilibrium
Dynamic
A. Gurevich PRL 113 087001 (2014)
Field-dependent
Depending on the surface impurity and RF frequency, the surface resistance depends on fields
Beyond the simple linear response (1st order perturbation i.e. no field dependence)
Crucial for the understanding of hyper high-Q SRF cavities for high-current machines (FCC & CEPC)

## Slide 19: Outline
Introduction
  Why do we need high-Q / high-G cavities?
State-of-the-art bulk niobium cavities
  How to understand & optimize high-Q / high-G cavities?
  Theory & engineering
Alternative materials
  Nb3Sn/Nb
  MgB2 & HTS
Practicalities
Conclusion

## Slide 20: Non niobium superconductors
Nb has the largest gap out of the pure elements
Alloys have higher gap and higher critical temperature
Non BCS superconductors (?)
Courtesy S. Posen
The main cause of the surface resistance is the thermally excited quasi-particles (NC electrons)
It can be suppressed by the gap (s-wave for BCS)
Larger gap  lower loss and /or same loss at higher T

## Slide 21: Nb3Sn thin film: 4 K operation equivalent to 2K Nb
Nb3Sn/Nb: previous barrier at 16 MV/m was due to thermal instability
 Still limited < 25 MV/m, but 1st implication up to 100 MV/m [N. Verboncoeur SRF2025]
1100C required for the Nb3Sn formation (Nb gets soften…)
 4 K cryocooler with 10 MV/m is the recent trend (non-high-G applications)
Nb3Sn/Cu to save Nb material: initiative for FCC; still preliminary stage
Nb bulk 2 K
Nb3Sn 4.4 K
1.3 GHz
Nb3Sn 2 K
S Posen et al 2021 SUST 34 025007
Sn-vapor deposition

## Slide 22: Even more fancy materials?
YBCO
11 GHz
Short pulse & T >> 4 K?
REBCO tape available
Iron-based SC
DC measurement by Z. Lin et al SUST 24 015991 (2021)
calculation by AM, IEEE Trans Appl Super 10601306
As handling is tricky  FeSe to start with
22
MgB2
Two band s-wave
d-wavegapless
s+/s- wave (?) gap full
http://arxiv.org/abs/2509.13668
Ke Chen TFSRF2024

## Slide 23: Outline
Introduction
  Why do we need high-Q / high-G cavities?
State-of-the-art bulk niobium cavities
  How to understand & optimize high-Q / high-G cavities?
  Theory & engineering
Alternative materials
  Nb3Sn/Nb
  MgB2 & HTS
Practicalities
Conclusion

## Slide 24: Do not forget reality for the real large machines!
Ultimate RF performance cannot be achieved if FE occurs!
Quality control is crucial for production yield WITH the beam
Cost reduction & faster process & standardization (industrialization!)
Robotics
Surface etching
Fabrication
Assembly@CEA
HPR@IJCLab
VEP@CEA
cEP@FNAL
hydroforming@KEK+CERN
BM@CERN
Internal EBW
@CERN
EuXFEL
statistics

## Slide 25: Outline
Introduction
  Why do we need high-Q / high-G cavities?
State-of-the-art bulk niobium cavities
  How to understand & optimize high-Q / high-G cavities?
  Theory & engineering
Alternative materials
  Nb3Sn/Nb
  MgB2 & HTS
Practicalities
Conclusion

## Slide 26: Conclusion: my perspective in SRF cavities
SRF cavities are versatile for various particle accelerators while its ultimate gradient is not as high as normal conducting cavities and plasma accelerators
  Decision making is compromised of many aspects! (Higgsino-like LSP 500GeV  multi-TeV e+/e-)
  For high-current / high-energy (above cyclotrons), SRF is (probably) the only option (FCC / CEPC)
SRF have been mainly studied by RF engineers and particle physicists ( yes, it’s me!) but the truly important research may be in the condensed matter physics / material science
  Fundamental understandings of nonequilibrium superconductivity is an outstanding challenge
  Exploring alternative materials to niobium is crucial for the sustainability of SRF!
Fundamental research is fascinating, but a one-off ultra-cavity is useless for accelerators
  We should not forget that accelerators are tool for something important (science, industry, etc)
  Industrialization through quality control and cost reduction is essential for the real machine!
The scope of (S)RF technology is not limited to accelerator applications
  Light dark matter (axions, dark photons) and high-frequency GW is without our reach
  Emerging research field as qubit and photon sensor applications is our neighbor
Interdisciplinary logistics: why not expand our field to more global science community?

## Slide 27: backup

## Slide 28: Present & future market
P. Dhakal “Nitrogen doping and infusion in SRF cavities: A review” Phys Open 5 100034 2020
Future circular machines & high current linac
For circular & high current linac
Extremely high-Q at relatively high gradient in large cavities
Extremely high gradient with relatively high-Q in a large # of cavities
For linear collider
Duty cycle >> 1%
Duty cycle <1%

## Slide 29: Three different families of superconductors
Copper oxide cuprate d-wave
Iron Arsenide pnictide s±-wave
Conventional BCS s-wave