## Slide 1
CEPC vacuum chamber production line
Yongsheng Ma
Vacuum group, IHEP,CAS
Jan 13th 2026

## Slide 2: Content
Preview of CEPC vacuum system
Production line development of NEG coating/ Spray for heating film in EDR
Prototype of thermal-spray heating layer and testing
Summary

## Slide 3: Preview of CEPC vacuum system
Accelerator | length/m
LINAC | 1,601+335
Damping ring | 147
Booster | 100,000
Collider | 200,000
Transport line | 4,680
Total length/m | 306,763
 | E | I | ρ
 | Gev | A | m
Higgs | 120 | 0.0167 | 10700
W | 80 | 0.084 | 10700
Z | 45.5 | 0.803 | 10700
tt | 180 | 0.0033 | 10700
Machine and Vacuum Parameters
Technical developments in TDR
Those prototypes have a good application in HEPS.

## Slide 4: Structure of vacuum chamber for CEPC collider rings
Alloy copper
NEG coating
Heating layer
56
VC with photon absorber
Notes: A thorough comparison of the advantages and disadvantages of the proposed distributed approach versus the photon stopper approach is necessary for effective management of synchrotron radiation;

## Slide 5: Benefits from NEG coating
NEG coating of 200nm is employed to suppress e-cloud of positron ring and absorb residual gases simultaneously. SEY will blow 1.2 after 24h activation of 180℃ and could even lower under higher activation temperature.
Similar to positron ring, NEG coating is proposed to vacuum chamber of electron storage ring to absorb extra gas load.

## Slide 6: VC baking & Why spray heating film
Necessity:
In order to meet the ultra-high vacuum requirement of achieving a dynamic vacuum level of 3.0E-10 mbar.
NEG coating reactivation
The baking is the most crucial procedure in achieving ultra-high vacuum
N2
O2
H2
H2O
CO2
N2
H2
H2O
CO2
CO
O2
Heat
High
vacuum
or
inert gas
MO
MC
O
C
Too thick
Lifetime is very short under SR of CEPC

## Slide 7: Spraying for heating film
Conductivity layer
Ceramic layer
Ceramic layer
Cu/ceramic transition layer
Vacuum chamber
I
Conduction
Convection
Radiation
Multilayer heating film will be coated outside of the vacuum chamber which composited by ceramic and conductivity layer
The heating temperature could reach 250℃
Heating layer
Thickness： 0.5mm
solution
Plasma spraying
Processing of spray
Cu/Ag NW
Electric heating circuit
De-icing for airplane
Related commercial products

## Slide 8: Preview of NEG coating/ Spray for heating film production line
Items | Specifications
Dimension | L 11400-d56-D62
Weight | 50~100kg
NEG coating | Thickness：200nm±30% SEY<1.1 S、Q、life-times
Spraying heating | Thickness<0.5mm Heating temperature <300℃
Requirement
Due to the difference in length, two production lines will be used to complete the production of vacuum chambers for the CEPC collider. The quantity of NEG coating and spraying facilities for the two lines varies to match the production speed.
The full quantity of vacuum chambers for the collider will be manufactured within five years, utilizing two production lines operating at a combined capacity of 4,500 units per year.
Advantages
More stable process, less manpower, less NEG coating facility, more adaptive capacity in production, etc.
Heating layer spraying
NEG coating
Cleaning

## Slide 9: Critical Step in the Production Line
Important nodes and progresses
Technical scheme review
Procurement bidding
Process Review prior to Manufacturing
Most of components have been manufactured 2025.11
The production line will be conditioned 2026.3
2024.10
2024.12
2025.6
Process Review prior to Manufacturing
Project kicker off
Manufacturer visit

## Slide 10: Production line composition
Classification | Sub-devices | Parameters | Note
Electron-beam welder | Electron-beam gun Power supply Vacuum chamber | Meets the Length of 11.4m vacuum chamber 6 working position | Design and manufacturing
Brazing | Mechanical holder Power supply | 350℃ 11.4m long | Low temperature brazing in air by conductivity heating, expecting stead by double hole copper tube
Heating film spraying facility | Electron-beam gun Power supply Controller Mechanical Structure | Meets the Length of 11.4m vacuum chamber Multilayer Spray Ceramic and conductivity layer | R&D
NEG coating tower | Pumping system Vacuum measurement Power supply Vacuum chambers Discharge Gas Cathode、controller | Meets the Length of 11.4m vacuum chamber 6 working position Background vacuum <5e-7Pa Baking temperature 200℃ | Developing to be more fitted the production line
Measurement and testing | Dimension measurement Leakage testing | Dimension measurement 11.5m/0.1mm Leakage testing 1e-10 mbar·L/s | Design and manufacturing
Cleaning | rinsing | deionized water rinsing | Design and manufacturing
Production line auxiliary equipment | Moving band robot arm system controller | Meets the Length of 11.4m vacuum chamber | Design and manufacturing

## Slide 11: Procedure of NEG coating & spraying of production line
Spraying (Air plasma spraying)
Sandblasting
Spraying_Isolation_layer
Spraying_Conductivity-layer
Spraying_Isolation-layer
Spraying_Contactor-layer
Cleaning
Outside
Inside
NEG coating
vacuum chambers, cathodes assembling by mechanical arms (flanges sealing).
Leakage testing.
Deliver the assembles to vacuum oven/ baking/ NEG coating;
Disassembly the vacuum chambers
Function | Materials | Thichness/um
Transition-layer | MCrAlY alloy | 50~100
Isolation-layer | Al2O3 cermic | ~200
Conductivity-layer | NiCr alloy | 50~100
Isolation-layer | Al2O3 cermic | ~200
Contactor-layer | Copper | ~50
Notes: Atmosphere plasma spray

## Slide 12
NEG coating, VC assembly and disassembly with automatic robot arms.
Cathodes driven
Cathodes
VC assembly
Vacuum oven
Layout & composition of NEG coating facility
Kr+
磁环
Inside magnet
DCMS for NEG coating

## Slide 13
Vacuum chamber automatic assembly
X
z
Sealing gasket installation
Flanges fastening

## Slide 14
VC inserted into the oven
VC & cathode support
UHV system for NEG coating
Vacuum chamber automatic assembly
Safety insurence
Due to the diameter of CEPC is D56, we plan to replace the cathode wire with a magnetron sputtering cathode
Permanent magnet instead of the solenoid which supplies magnetic field for DCMS;
By combining the low vacuum chamber outside of the vacuum chambers to be coated with NEG, the high vacuum process is simplified;

## Slide 15: Prototype of cathode for NEG coating
23000mm(23 meters)
Magnetron Cathode
~12000mm(12 meters)
After testing and conditioning, the cathode achieves a stable DCMS plasma discharge under 367 V and 1.1 A.
Motor for magnets driven
15

## Slide 16: Manufacturing progress of production line
The 12-meter cathode prototype for NEG coating is under manufacturing.
The oven for NEG coating, which provides a low vacuum environment and baking capabilities, is under manufacturing.

## Slide 17: Manufacturing progress of production line
The main components of vacuum oven for NEG coating have been manufactured and under are now being assembled.

## Slide 18: Plasma Spraying system
Sandblasting room
Plasma Spraying
& Laser etching room
The vacuum chamber will be transferred by motorized conveyance to the coating station, where a robotic arm will execute multi-layer deposition using an automated spray gun.
Notes: Reciprocating motion

## Slide 19: Heating coating spraying
项目 | 参数
驱动方式 | 旋转气缸驱动
遮蔽材质 | 不锈钢
轴向可调节范围 | 100mm
Etching by laser
Sandblasting
Plasma Spraying
The processing step for the heating coating spraying

## Slide 20: Length of 1.5m prototype of Spraying
Sandblasting
Spraying_Isolation_layer
Spraying_Conductivity-layer
Spraying_Isolation-layer
Installation
Spraying
A 1.5-meter prototype has been developed to validate key process steps that will be implemented in the production line.

## Slide 21: Elements and thickness of thermal-spray heating layer
NiCr Transition-layer
NiCr Conductivity-layer
Al2O3 isolation layer
Al2O3 isolation layer
Ni
Cr
Al
O
Al2O3：174um
Al2O3：173um
Cu
NiCr：64.5um
NiCr：59.5um
=471um
Thickness
＜0.5mm

## Slide 22: Prototype of thermal-spray heating layer and testing
Constant V=110V
D60-1500 mm
Dimension: L1500*D60 Substrate: copper
Several ten times reheating tests which shows a good lifetimes and performance

## Slide 23: Plasma spraying devices
The spraying system is similar to the system detailed in the following pictures.

## Slide 24: Summary
The production line for vacuum chamber NEG coating and thermally sprayed heating layers is currently under installation and will be commissioned by March 2026.
It is capable of handling vacuum chambers with a minimum dimension of 56 mm and a maximum length of 11.5 meters for NEG coating applications. There are no dimensional restrictions for the thermal-sprayed heating layer process.
This production line will be up and running soon—we’re open for business and welcome collaboration on related manufacturing tasks.
Additionally, a 1.5-meter prototype of the thermally sprayed heating layer has been fabricated, with relevant performance tests successfully completed.

## Slide 25
Thanks for your attention!