## Slide 1: CEPC polarized electron source R&D
Xiaoping Li, Zhe Duan, Valery Tyukin, Cai Meng, Wei Liu, Zhongtian Liu
环形正负电子对撞机
Circular Electron Positron Collider

## Slide 2
CEPC Electron Source
Generation of polarized electron beams
Polarized electron source related R&D
  Polarized electron source R&D plan for CEPC at IHEP
  Domestic R&D on the superlattice GaAs photocathode
  Preliminary test on the superlattice GaAs photocathode
  A Polarized electron gun design for CEPC
Summary
Content

## Slide 3
CEPC Electron Source
Generation of polarized electron beams
Polarized electron source related R&D
  Polarized electron source R&D plan for CEPC at IHEP
  Domestic R&D on the superlattice GaAs photocathode
  Preliminary test on the superlattice GaAs photocathode
  A Polarized electron gun design for CEPC
Summary
Content

## Slide 4
Parameter | Symbol | Unit | Baseline
Energy | Ee-/Ee+ | GeV | 30
Repetition rate | frep | Hz | 100
Bunch number per pulse |  |  | 1 or 2
Bunch charge |  | nC | 1.5
Energy spread | σE |  | 1.5×10-3
Emittance | εr | nm | 6.5
Baseline design of the CEPC Linac
  A 30GeV room temperature Linac
  A combination of S-Band (2860MHz) and C-Band (5720MHz)
  The Linac tunnel length is 1.8km
CEPC Linac

## Slide 5
CEPC Electron Source
Introduction to CEPC Electron Source
CEPC electron source parameters and its design
Parameter | Unit | Value
Type | - | Thermionic Triode Gun
Cathode | - | Dispenser cathode
Beam current | A | > 10
High voltage of anode | kV | 150
Bunch charge 1 | nC | 1.5 (e– injection)
Bunch charge 2 | nC | 10 (e+ production)
Repetition | Hz | 100
  Electron Gun (Baseline design)
    A traditional thermionic triode gun with two operation modes
    1.5nC for electron injection
    10nC for positron generation
  Has been verified at BEPCII and HEPS Linac
The electron source is used for generating an electron beam with a specific longitudinal distribution that can be accelerated for injection and positron production.

## Slide 6
CEPC Electron Source
Generation of polarized electron beams
Polarized electron source related R&D
  Polarized electron source R&D plan for CEPC at IHEP
  Domestic R&D on the superlattice GaAs photocathode
  Preliminary test on the superlattice GaAs photocathode
  A Polarized electron gun design for CEPC
Summary
Content

## Slide 7
Generation of polarized electron beams
Polarized electron generation
  One effective method for generating polarized electrons is using GaAs photocathode in a photocathode HV electron gun (Extremely high vacuum)
  The unique band structure of GaAs determines that electron beams with a certain polarization can be generated under the driving of circularly polarized laser at a specific wavelength
  For a common bulk GaAs, a maximum polarization in theory is 50%, considering depolarization effect it usually is about 30-35% at 780nm laser wavelength
Polarized electron generation from a common bulk GaAs

## Slide 8
Polarized electron generation
  Strained GaAs and its energy band structure
  For a strained GaAs, a maximum polarization in theory is 100%, considering depolarization effect it usually is about 85% at 780nm
  Constructing superlattice structure is an effective way to obtain strained GaAs
  This type of photocathode is not easy to obtain and needs to be grown on a substrate using MBE equipment
Polarized electron generation from superlattice GaAs
Generation of polarized electron beams

## Slide 9
CEPC Electron Source
Generation of polarized electron beams
Polarized electron source related R&D
  Polarized electron source R&D plan for CEPC at IHEP
  Domestic R&D on the superlattice GaAs photocathode
  Preliminary test on the superlattice GaAs photocathode
  A Polarized electron gun design for CEPC
Summary
Content

## Slide 10
A photocathode DC gun @IHEP
Scheme of PES R&D based on DC gun
Wien filter
Mott polarimeter
Polarized electron source R&D plan for CEPC at IHEP
Goals: Generation of electron beams with a bunch charge (≥2nC) and high polarization (≥85%)
Based on a photocathode DC gun developed by IHEP with an extremely high vacuum (10-10Pa)
Beam line setup and beam dynamics study has been carried out
Key components such as Wien filter and Mott polarimeter has been designed
We expect a beam commissioning scheduled in 2027
Polarized electron source related R&D

## Slide 11
Domestic R&D on the Superlattice GaAs photocathode
One of the most important part for Polarized electron source is Superlattice GaAs Photocathode
Since the beginning of 2025, we have been starting the R&D of Superlattice GaAs
In collaboration with a domestic company Acken Optoelectronics Ltd. @ Suzhou
Superlattice GaAs photocathode produced by MBE system, main requirements are Polarization ≥85% and QE ≥0.5%
The first the batch of photocathodes have been produced
Polarized electron source related R&D
GaAs | 5 nm | p=5×1019 cm-3
GaAs/GaAsP SL | (4/3 nm) ×14 | p=5×1017 cm-3
GaAsP0.35 | 2750 nm | p=5×1018 cm-3
Graded GaAsPx (x = 0~0.35) | 5000 nm | p=5×1018 cm-3
GaAs buffer | 200 nm | p=2×1018 cm-3
p-GaAs substrate (p>1018 cm-3) |  | 
MBE system in Acken
Structure of Superlattice layers
Samples of superlattice GaAs/GaAsP

## Slide 12
Domestic R&D on the Superlattice GaAs photocathode
Build a platform for photocathode performance test (both pol & QE), this platform has been designed and is currently under development, expected to start experimental study on superlattice GaAs this year
Including a photocathode load-lock chamber, an activation chamber and a testing laser system
A Mini-Mott polarimeter for a low energy electron beam has been designed, we will start to develop it ASAP
Polarized electron source related R&D
Platform for photocathode performance test

## Slide 13
Preliminary test on the Superlattice GaAs photocathode
From 2024, Valery Tyukin from Inst. of Nuclear Physics, JGU Mainz participated in research on PES (PIFI 2024/2025)
A superlattice GaAs wafer has been cut, and a quarter had been delivered to the Inst. of Nuclear Physics, JGU Mainz
Activation experiment of the Superlattice GaAs has been carried out in JGU Mainz
To test the performance of Superlattice GaAs (both QE and polarization)
As a very important experimental data for our Mott polarimeter calibration in future
Polarized electron source related R&D
Superlattice GaAs wafer cut in Acken
Valery Tyukin

## Slide 14
The SL structure is cut along blue lines
Piece on the left bottom is tested
SL in loadlock chamber
Preheating in loadlock chamber
Yo-Yo method, Cs + NF3
Maximal QE=3.4% @650nm
Preliminary test on the Superlattice GaAs photocathode
The QE is two to three times lower than that of bulk GaAs (Need more activation experiment to increase QE)
The lifetime of the Superlattice GaAs in preparation chamber is a few hundred hours, which is a good indicator
The central part of Superlattice will be used for future beam experiments on the main accelerator at Mainz
Polarized electron source related R&D

## Slide 15
Preliminary test on the Superlattice GaAs photocathode
Polarization measurement at an electron beam energy of 100.0 keV with a laser λ ∼ 776nm has been carried out
The effective Sherman function Seff is directly affecting the results of polarization measurement, and in this time experiment polarization is estimated at 70% when using Seff=0.28 that was determined years ago
The preliminary polarization measurement results show that Superlattice structure is working, the next step is to further confirm the polarization with an energy of several MeV on the main accelerator at Mainz with a higher accuracy
Polarized electron source related R&D
Asymmetry measurements: left and right detectors
Left detector
Right detector
Ames
P

## Slide 16
Preliminary test on the Superlattice GaAs photocathode
Considering the low QE results of Superlattice at Mainz, cross check of activation experiment was carried out on the platform of Chongqing University in China (only activation experiment and QE measurement) based on another quarter.
Yo-Yo method by using Cs+O2 activation
QE is 0.7% @785nm and 8.27%@650nm, and QE of Superlattice decreasing with the increase of heat clean temperature
For CEPC polarized electron source, Superlattice with a QE≥0.5% will be enough to meet the requirements
Polarized electron source related R&D
Activation experiment study on Superlattice GaAs at Chongqing University

## Slide 17
Polarized electron source related R&D
A Polarized electron gun design for CEPC
A 150kV HV photocathode electron gun has been designed (Beam parameters are consistent with the thermionic gun)
We proposed a two electron guns scheme and do not change the layout of the injector, share the bunching system
As an alternative solution for CEPC electron source
It can also be adopted in BEPCII as a polarized electron source
A 150kV HV photocathode electron gun
Two electron guns scheme for CEPC

## Slide 18
CEPC Electron Source
Generation of polarized electron beams
Polarized electron source related R&D
  Polarized electron source R&D plan for CEPC at IHEP
  Domestic R&D on the superlattice GaAs photocathode
  Preliminary test on the superlattice GaAs photocathode
  A Polarized electron gun design for CEPC
Summary
Content

## Slide 19
Summary
Introduction of electron source for CEPC.
The method of generating polarized electrons.
Introduced progress of polarized electron source related R&D plan.
Domestic R&D on the superlattice GaAs photocathode and preliminary test results.
A polarized electron gun design for CEPC.

## Slide 20
Thank you for your attention!