## Slide 1
Radon-222 Removal and Screening Capability at SNOLAB
Dr Nasim Fatemighomi (she/her)
SNOLAB Research Scientist
Queen’s University Adjunct Professor
2026/06/23
CAP2026, Ottawa, June 23rd 2026

## Slide 2
Outline
Introduction to SNOLAB physics and background sources
Why controlling radon background is important
Techniques applied to measure radon at SNOLAB
Radon Removal Techniques
Techniques to create low radon environment
Summary
Notes: Put a Rn isotope, less white space. Use the white space

## Slide 3
Introduction

## Slide 4
Situated 2 km Underground at Creighton Mine, Lively, Ontario
SNOLAB Underground Facility
Most experiments are looking for extremely rare signal
Background sources to be controlled and mitigated
Notes: Merge slide 4 and 5

## Slide 5
Background sources
Gammas () and betas () from natural radioactivity
Alphas () from natural radioactivity
  : interaction of s with detector material
  Surface alphas s
Muons
    Muon-induced neutrons
    Cosmogenic activation
13C
16O
Detector Medium
Detector Wall
Notes: For these experiments to be successful, they need to control and mitigate background , these are gamma and betas from natural radioactivity, alphas from natural radioactivity which can create neutrions by interacting with detector material. Can create surface alpha background which can have similar recoil energy as a dark matter candidate. Or muons. The focus of my talk today is radon induced background which can create gamma and betas from natural radioactivity and alphas from natural radioactivity.

## Slide 6
Radon in 238U Chain
222Rn is a progeny of 238U
It is a noble gas, ie. can travel
Emanates from material surfaces
Present in SNOLAB air 120 Bq/m3
Background source:
  Short-lived and long-lived progeny (,
  Surface
From Wikipedia

## Slide 7
Mitigation and controlling strategy
Strict material selection by performing radon emanation measurements
Regular monitoring of Rn levels
Rn removal from liquid and gas
Controlling radon ingress in the detector
Preventing surface contamination
Cleaning and removal of surfaces to remove 210Pb

## Slide 8
Radon Emanation Systems at SNOLAB

## Slide 9
Radon Emanation System Technique
Based on a design developed by Queen’s (M. Liu, et al. NIM A, 517 (1993), pp. 291-293)
Radon atoms collected by cooling down radon traps using liquid nitrogen (LN)
Radon released by warming up the traps (100C)
Radon transferred to a Lucas cell (LC) through volume sharing
LC is detached and put on top of a PMT for counting
Emanation Chamber
(negative pressure)
Notes: Bigger figures, remove white space, make the text more readable

## Slide 10
Vacuum Pump
Emanation
Chamber
SNOLAB Radon Emanation System
Background:
4 2 Rn atoms/day
Plan to increase the emanation chambers
Notes: Make the picture bigger, cover the whole slide, and put the information in text boxes ,

## Slide 11
Portable Lucas cells (LCs) with ZnS(Ag) coating
ZnS(Ag) scintillates with α particles → ideal for radon detection
Sixteen LC channels available
Radon Counting
2” diameter PMTs and CAEN electronics
2” diameter
4 μs window
Notes: Justify why LC compare to other type of like electorstatic chamber, cheap to produce, if you want to count 16 assays at the time you need to make 16 electrostatic chamber.. Which makes it expensive. I think this type of detector is unique to SNOLAB and while we should investigate other type of technology, high efficiency compare with electrostic chambers… I think we should push impoving this as well… talk about justin , keegan etc work … less sensitive to moisture and other impurities compare to electrostic and proportional counters. Less affected by noise during radon correction.

## Slide 12
LC Efficiency
Plan to purchase a 30.0 1.5 Bq RNC pylon source to measure efficiency at SNOLAB
Courtesy of J. Suys
Justin Suys CAP 2025
  I. Blevis, et al. NIM A, 517
  M. Liu, et al. NIMA, 517
GEANT4 simulation
Notes: Put Justin’s plot here, how to make the error in data smaller.

## Slide 13
LC Background
Increasing age
New LCs have background of 3 to 5 alpha counts day
LC 210Po background increases with 210Pb build up
Notes: Background cells build over time
Reduce the background, think about conclusion, ages

## Slide 14
Reducing LC Background
New low background Lucas cells were fabricated: 3 to 5 /day
R&D toward lower background ZnS(Ag) using selective precipitation technique (See Peter Qin’s talk:DAPI T2-1)
New Lucas cell
(made with commercial ZnS(Ag))
In-house ZnS(Ag)
scintillation
in-house ZnS(Ag)
Notes: Here talk about both making new LC and to make ZnS

## Slide 15
Measurement of 222Rn concentration in N2

## Slide 16
The UG Radon Board
Designed for vacuum radon emanation measurement
Was adopted to perform N2 gas assays
Cover Gas system filled with N2
vapor trap
Notes: . The commercial trap contained a helically wound titanium coil filled with a coolant called R290/R1150 (a blend of propane and ethylene) a

## Slide 17
Primary Trap Limitation for Gas Assays
Radon traps use porous materials to enhance trapping
Bronze wool highly efficient under high vacuum
Gas assay efficiency decreases with longer duration or >1 SLPM flow
Limited extracted gas volume constrains sensitivity (> 3.3 mBq/m3)
Need for traps with more porous material
S.M.A. Hussain MSc thesis (2022)

## Slide 18
Activated Charcoal Trap
Activated charcoal traps used for gas purification
  G. Heusser, et al. Appl. Radiat. Isot., 52 (2000)
Gas assays require both trapping & efficient radon release
Developed a portable activated charcoal trap to enhance radon trapping
  Nasim Fatemighomi et al: Nucl.Instrum.Meth.A 1076 (2025)
Used low background Calgon OVC 4 × 8 (coconut-based)
In-house nitric acid etching to remove ²³⁸U background
Radon emanation: 183 mBq/kg at room temperature
100μm
22 g trap

## Slide 19
Trap Efficiency Test Set-up
N₂ flow through the source introduces radon atoms to trap
Charcoal cooled with LN₂–alcohol mix to trap radon
Radon released from charcoal trap by heating
Released radon were extracted using the radon board

## Slide 20
Unlike bronze wool trap, charcoal trap is 100% efficient after one hour of assay duration
The trap is also 100% efficient for flow rate of up to 5 SLPM
The method developed to test this charcoal trap can be used to test other radon traps
Charcoal versus Bronze Traps

## Slide 21
Charcoal Trap Sensitivity and Use
N2 assay sensitivity 90Bq/m3
  Bronze wool sensitivity: 3.3 mBq/m³
SNOLAB LN2 plant
Trap used to measure radon in N₂ systems, incl. SNOLAB LN₂ plant boil-off
SNOLAB International Dewar

## Slide 22
Application on Experiments
PICO-500 (see Hantz Nozard talk: DAPI T2-1)
SNO+: provided radon level in the cover gas system

## Slide 23
Radon Removal Techniques

## Slide 24
Removal of Rn from liquid/gas
Rn
Boiled-off liquid/gas
Heater
Condenser
Liquid/gas
Cryogenic Distillation
Using Raoult’s law: the concentration (Rn) in the gas equals the vapor pressure times its mole fraction
Application: Liquid Xenon
Physical Adsorption
Making a cryogenic trap from activated charcoal
Application: Liquid Argon, boil-off N2
Making a trap with silver exchanged zeolite
Room temperature
Application: Liquid Argon, boil-off N2

## Slide 25
Silver Exchanged Zeolite for Rn Removal
S. Heinitz, et al. Nature: Sci Rep 13, 6811 (2023)
17 g adsorbent at room temperature
Demonstrates 10–100 times higher adsorption efficiency than activated charcoal at room temperature
Planned usage at SNOLAB radon removal from N₂ cover gas systems
Currently testing Ag-13X at room temperature at SNOLAB
Efficiency measurements of a radon trap is ongoing using surface board setup
Collaboration with Queen’s argon and xenon astroparticle group to develop a radon trap for argon and xenon systems
Nitrogen
Notes: Time that radon breakthrough the trap, ideal trap is lets everything through but radon

## Slide 26
Controlling Radon Ingress in the Experiments

## Slide 27
Radon Reduced air
Can use columns of activated charcoal (or silver exchanged zeolite) to create a low radon concentration environment
SuperCDMS achieved <0.1 Bq/m3
Such systems will be needed for future large-scale projects
arXiv:1708.08535

## Slide 28
N2 Cover Gas Systems
SNOLAB provides boil-off N2 to experiments by surface LN Dewar's, UG LN plant and N2 bottles
SNOLAB UG LN plant Boil-off had radon level of mBq/m3
Can achieve lower concentration if we use a zeolite trap

## Slide 29
SNO+ unique N2 Cover Gas system
Designed and fabricated at Queen’s University
Sealed system which adjusts for pressure fluctuation (up to 9%) in the lab
Main components:
  Three flexible bags
  Failsafe (pressure relief system)
  Universal interface
Current activity 0.1 Bq/m3
Meets SNO+ physics requirement
Notes: Slide 20 to 22 put it later at the end

## Slide 30
Acknowledgement
Research Students (SNOLAB/SNO+): Yusuf Ahmed, Juliette Deloye, Peter Qin, Justin Suys, Keegan Paleshi, Adil Hussain, Jerry Lu, Ariana Pearson, Julia Azzi, Madeleine Berube and Gurpreet Kainth and Connor Stubbs
Scientific Support Team: Lina Anselmo, Steven Maguire, Sharayah Read, Deena Fabris and Dimpal Chauhan

## Slide 31
Summary
SNOLAB’s rare-event experiments probe fundamental questions in particle physics
Controlling ²²²Rn-induced backgrounds is critical to achieving physics goals
SNOLAB continues to strengthen its radon mitigation program by:
  Building and operating low-background radon assay systems
  R&D toward making low background radon counting systems
  Developing advanced radon removal techniques
  Creating radon reduced environments with boil-off N2
  Maintaining existing radon systems
Majority of the work presented today is done by SNOLAB undergraduate research students

## Slide 32
Back up

## Slide 33
Water Radon Assay System
Designed and built by the SNO collaboration (DOI: 10.1016/j.nima.2003.10.103)
Operated by SNOLAB and SNO+ to monitor 222Rn level of SNO+ cavity UPW and SNOLAB UPW plant
Water trap
Degassser
Trap A
Trap B
The SNO+ experiment
Water shielding (7000 tonnes UPW)

## Slide 34
Water Radon Assay System
Water trap (-60 C)
Degasser
Radon extraction board
H2O from SNO+ cavity/UPW plant (19 SLPM)
Water return to cavity

## Slide 35
V203: Between Acrylic Vessel and PMTs
Results are consistent with SNO times
SNOLAB UPW plant radon level is (2.40.7)g238U/gH2O equivalent
= (0.14 0.04) Rn atoms/L

## Slide 36
Radon Calibration Source for Trap testing
A calibrating source was made using Nora Xp 5319 rubber floor tile
10cm
14 x 10 cm2 floor tiles
Calibration Can
Fit is based on²²⁶Ra-supported emanation and ²²²Rn outgassing from porous rubber tiles

## Slide 37
Detector Medium
Detector Wall
13C
16O