Critical Mg Doping Threshold in Spray-Pyrolyzed SnO₂ Thin Films: Balancing p-Type Conduction and Visible Transparency for Transparent Conducting Oxide Applications.

1OGUNMOLA Enoch Debayo, *2ADEOYE Abiodun Eyitayo, 1AJAYI Ayodeji Akintunde, 1ADEWUMI Adeyanju Patrick, 2MUSILIYU  Kazeem Adeleke, , 1MOREBISE Ademola Thomas, 3OLUYEMI Folasade Oladunni

1. Dept. of Mathematical and Physical Sciences, Afe Babalola University, Ado-Ekiti, Ekiti State, Nigeria

2. Department of Physics & SLT, Abiola Ajumobi Technical University, Ibadan, Nigeria

3. Dept. of Science Technology, The Federal Polytechnic, Ado-Ekiti, Ekiti State, Nigeria

*adeoye.abiodun@tech-u.edu.ng

Abstract

Transparent conducting oxides require precise doping to balance transparency and conductivity for electronics, photovoltaics, and sensors. This study identifies a critical 4 at.% Mg doping threshold in spray pyrolyzed SnO₂ thin films. Films with 0–8 at.% Mg were deposited from 0.1 M SnCl₄•5H₂O + MgCl₂•6H₂O at 350 ± 5 °C and annealed at 450 °C. X-ray diffraction confirmed rutile phase stability up to 4 at % Mg, with crystallite refinement from about 35 to 22 nm and increased microstrain from Mg²⁺ substitution. SEM/EDS indicated a uniform nanostructure and successful Mg2+-incorporation. UV–Vis measurements showed over 75 % transmittance and bandgap tuning from 3.65 eV to 3.85 eV then to 3.55 eV, consistent with Burstein–Moss and disorder effects. Hall measurements revealed n type conductivity peaking at 4 at.% Mg, with optimal carrier concentration and mobility and sheet resistance around 450 Ω/sq, before defect scattering reduced performance at higher doping. These findings establish spray pyrolyzed 4 at.% Mg:SnO₂ as an ITO competitive transparent conducting oxide, with a figure of merit of 1.2 × 10⁻³ Ω⁻¹, suitable for scalable transparent conductive applications.

Keywords: spray pyrolysis, transparent conducting oxides, doping threshold, Rutile phase stability, Burstein-Moss effect, four-point probe