## Slide 1
Ottawa, 2026/6
Co-author
Hoan Tran-Van1
Study of Li-ion diffusion in Li-Mg, Li-Zn, and Li-Sn alloys using transition path sampling in MLACS
1Département de Chimie, Biochimie et Physique, Institut de Recherche sur l’Hydrogène, Université du Québec à Trois-Rivières, Trois-Rivières, Québec, Canada
2INRS-UQTR Joint Research Unit in Materials and Technologies for Energy Transition
Prof. Gabriel Antonius1
Prof. François Allard1,2
1

## Slide 2
Outline
Study of Li ion diffusion in Li-Mg, Li-Zn, and Li-Sn alloys using transition path sampling in MLACS
2
Hoan Tran-Van

## Slide 3
Study of Li ion diffusion in Li-Mg, Li-Zn, and Li-Sn alloys using transition path sampling in MLACS
3
Hoan Tran-Van
All-solid-state Li-ion batteries
  High energy density, safety, recyclability
  EV demand: > 300 km + fast charging [1]
Challenges of Li metal anode
  Dendrite growth → short circuit, safety risk
  Dead Li and void formation → capacity loss
  Unstable SEI → side reactions, low efficiency
  Volume change → interface degradation
EV - Electric Vehicles
SHE - Standard Hydrogen Electrode
SEI – Solid electrolyte interphase
[1] M.M. Islam et al., Phys. Chem. Chem. Phys., 17, 3383-3393 (2015)
[2] X.B. Cheng et al., Chem. Rev. 117 (2017) 10403–10473
Critical limitations of Li metal anodes [2]
Why Li metal anode?
  High theoretical capacity: 3860 mAh g-1
  Lowest electrochemical potential: −3.04 V vs SHE
  Lowest density: 0.534 g cm-3
Li diffusion is a critical factor influencing the stabilization
1. The problems of Li metal anode
Notes: + The development of high energy density batteries is becoming increasingly important, particularly for applications such as electric vehicles, where continuous power supply over long driving ranges is required. In this context, safety, energy storage capacity, and recyclability are key factors that must be improved.
+ All-solid-state lithium-ion batteries (ASSLBs) have emerged as a promising solution to meet these requirements. Among various anode candidates, lithium metal exhibits the highest theoretical capacity, which is approximately ten times greater than that of conventional graphite anodes. However, the practical application of lithium metal anodes remains challenging due to their poor stability. Issues such as dendrite growth, unstable solid electrolyte interphase (SEI), dead lithium formation, void generation, and significant volume changes severely limit their performance and safety
+ Therefore, stabilizing the anode is crucial for improving the performance of solid-state lithium batteries. In this regard, lithium diffusion plays a critical role, as it strongly influences the structural stability and electrochemical behavior of the anode.

## Slide 4
2. Alloying for Li-based anodes
(a) Li and (b) Li–Mg anode structures, bulk & surface, during stripping/plating [4]
[3] M. Yang et al., Nat. Commun., 14, 2986 (2023)
[4] L. L. Kong et al., Adv Funct Mater., 29(13), 1808756 (2019)
Atomistic Investigation of Li-Ion Diffusion in Lithium Alloy Anode Materials: Li-Mg alloys
4
Hoan Tran-Van
Predict how alloying effectively changes diffusion and stability?
A diagram illustrating the multi-stage process of Li crystallization [3]
Mg can form a conductive framework
Notes: Interface instability causes problems with lithium metal batteries such as dendrite, void, dead Li, etc.
Li alloying is a useful solution to increase interface stability.

## Slide 5
2. Alloying for Li-based anodes
Phase | Li Im-3m | Li-Mg (70-90 at%Li)
DLi (cm2 s-1) | 1.6×10-10 [7] | 1.4-2.6×10-10 [7]
Li diffusion coefficients DLi
Atomistic Investigation of Li-Ion Diffusion in Lithium Alloy Anode Materials: Li-Mg alloys
5
Hoan Tran-Van
Phase | LiZn Fd-3m | Li7Sn3 P21/m
DLi (cm2 s-1) | 8.8-37×10-10 [5] | 3-5×10-7 [5]
Li-Mg
Low Li diffusion
Structural integrity
→ uniform Li deposition [4]
Li-Zn
Faster Li diffusion than Li
Low capacity [6]
Buffer/protection layer for Li metal → uniform Li deposition [6, 8]
Li-Sn
Faster Li diffusion than Li
Volume change [9]
Uniform transportation of the Li ions [9]
[5] Y. Huang et al., J. Mater. Chem. A, 10, 12350 (2022)
[6] X. Gu et al., Engineering Reports, 2021;3:e12339.
[7] M. Siniscalchi et al., ACS Energy Lett., 7, 3593 (2022)
[8] Q. Chen et al., ACS Appl. Mater. Interfaces, 13, 9985−9993 (2021)
[9] A. Serikkazyyeva et al., J. Alloys Compd., 965, 171381 (2023)
Li-M alloy
SEI
Electrolyte
Li metal
SEI
Electrolyte
Li-M alloy
Alloy as a buffer layer
Alloy anode
Enhanced Li diffusion can contribute to suppressing void and dendrite formation.
Notes: Li-Al: excellent mechanical properties, Li–Al alloy shows the highest compressive strength among all
the alloys
Ex

## Slide 6
3. Diffusion coefficient & activation energy
[10] A. Van der Ven et al., Chem. Rev., 120, 14, 6977–7019 (2020)
The diffusion coefficient:
The Li ion diffusion in Li-M alloys for anode application
6
Hoan Tran-Van
D0: the pre-exponential factor
Em: the migration energy for hopping
Efvac : the Li vacancy formation energy
Ea: the effective activation energy for Li diffusion
The activation energy:
Forward hop
Reverse hop
ΔKRA = Em
can be obtained from DFT calculations
can be obtained from NEB method
DFT - Density Functional Theory
NEB – Nudged Elastic Band method
Focus on migration barrier Em
Kinetically resolved activation (KRA) barrier [10]

## Slide 7
DFT-NEB
Higher accuracy
Higher computational costs for large supercell
Accuracy limited by interatomic potential
Lower computational costs for large supercell
MD-NEB
The Li ion diffusion in Li-M alloys for anode application
7
Hoan Tran-Van
MD – Molecular Dynamics method
MLIPs - Machine-learning interatomic potentials
MLACS - Machine Learning Assisted Canonical Sampling
Remove in NEB
MLACS-NEB workflow [11]
MLIPs address the trade-off issue
4. MLACS-NEB approach for screening fast Li-ion diffusion alloys
[11] A. Castellano et al., Comput. Phys. Commun., 316,109730 (2025)

## Slide 8
4. MLACS-NEB approach for screening fast Li-ion diffusion alloys
The Li ion diffusion in Li-M alloys for anode application
8
Hoan Tran-Van
Sampling process and energy profile of training configurations for MLIP in the MLACS workflow.
10-30 training configurations
Linear SNAP
10–100× speed-up compared to DFT-NEB
Li3Mg, Fm-3m, |ΔEm|=1.29×10-3 eV
Li, Im-3m, |ΔEm|= 8.17×10-4 eV
LiZn, Fd-3m, |ΔEm|= 1.34×10-4 eV
Li3Sn, Fm-3m, |ΔEm|= 2.14×10-3 eV

## Slide 9
5. Comparative analysis of Li-ion migration barriers
Convex hull and calculated structures
The Li ion diffusion in Li-M alloys for anode application
9
Hoan Tran-Van
Convex hull of formation energies
LiZn (xLi = 0.5): 1 polymorphs
LiZn
LiZn3
LiMg (xLi = 0.5): 6 polymorphs
Li2Mg (xLi = 0.667): 5 polymorphs
Li3Mg (xLi = 075) .: 6 polymorphs
Li5Mg (xLi = 0.833): 5 polymorphs
Li7Sn2 (xLi = 0.778): 1 polymorphs
Li3Sn (xLi = 0.75): 1 polymorphs
Li5Sn2 (xLi = 0.714): 1 polymorphs
LiSn (xLi = 0.5): 2 polymorphs
Li
Zn
Li
Sn
LiSn3
LiSn
Li13Sn5
Li3Sn
Li7Sn2
Li17Sn4
Near-degenerate structures → Boltzmann-weighted average

## Slide 10
5. Comparative analysis of Li-ion migration barriers
The Li effective migration barrier
Conventional cell structure of Li3Mg (Imm2) with vacancy formation energies and MEP from MLACS-NEB.
The Li ion diffusion in Li-M alloys for anode application
10
Hoan Tran-Van
Li transport prefers lowest-energy migration path
Path (1)
Li3Mg Imm2
Path (2)
Li4
Li3
Li3
Li5
Li5
Li4
d1 = 2.910 Å
d2 = 2.988 Å
Diffusion pathway selection

## Slide 11
5. Comparative analysis of Li-ion migration barriers
The Li effective migration barrier
The Li ion diffusion in Li-M alloys for anode application
11
Hoan Tran-Van
Phase | xLi | Em (eV)
Li2Mg (mixed phase) | 0.667 | 0.099
Li7Sn2 (Cmmm) | 0.778 | 0.077
LiZn (Fd-3m) | 0.5 | 0.040
Minimum Eₘ in Li–Mg, Li–Sn, and Li–Zn systems
Very low Em (0.04–0.1 eV) are accessible in Li–Mg, Li–Sn, and Li–Zn phases
Em is strongly structure-dependent
No universal correlation between Em ​and xLi is observed.
LiMg
LiSn (P2/m)
LiSn (I41/amd)
LiZn
Li2Mg
Li5Sn2
Li3Sn
Li3Mg
Li7Sn2
Li5Mg
Li
Error bars indicate the Boltzmann-weighted standard deviation
Supercells contain 108–256 atoms, satisfying the shortest vac-vac distance > 10 Å.
Linear SNAP with 2Jmax = 8 and rcut = 5 Å.
Eₘ vs xLi

## Slide 12
5. Comparative analysis of Li-ion migration barriers
Factors governing migration barriers
Coordination-Controlled Migration Barriers
The Li ion diffusion in Li-M alloys for anode application
12
Hoan Tran-Van
Low d → low Em ​ (baseline regime)
Coordination overlap → barrier amplification
Radius cutoff = 3.1 Å to determine coordination

## Slide 13
5. Comparative analysis of Li-ion migration barriers
Factors governing migration barriers
Phase-dependent relationship between d and Em
The Li ion diffusion in Li-M alloys for anode application
13
Hoan Tran-Van
Orthorhombic/monoclinic cluster at low d and low Em.
Phase indirectly reflects diffusion topology.

## Slide 14
6. Conclusion
The Li ion diffusion in Li-M alloys for anode application
14
Hoan Tran-Van
The obtained results
1
2
3
MLACS-NEB efficiently screens Li-ion migration barriers
Future work
1
2
3
Complete NEB calculations with other crystal structures
Perform calculations with Li–Mg solid solution
Evaluate vacancy formation energy
Li2Mg, Li7Sn2 and LiZn exhibit low Li migration barriers (Em < 0.1 eV)
Low Em is favored by short migration distance and the absence of common neighboring atoms

## Slide 15
Thank you
The Li ion diffusion in Li-M alloys for anode application
15
Hoan Tran-Van