## Slide 1: Novel Magnetic and Topological Nickel Monosilicides
science.uOttawa.ca
creatematerials.org
Dinura Hettiarachchi
Supervisor : Hang Chi
Department of Physics, University of Ottawa
Tuesday, June 23, 2026

## Slide 2: Motivation
Contact material
Low temperature manufacturing, low silicon consumption, and low resistance.
Unusual thermal expansion
Enormously anisotropic thermal expansion.
Potential relevance to Earth’s interior
Earth’s core consists of an Fe-Ni alloy containing a fraction of light elements such as Si.
Topological properties
Cubic NiSi (P213) has interesting topological properties.
Magnetic properties
In 2023, antiferromagnetic order was reported.

## Slide 3: Possible Magnetism
Ghosh, P. et al., Adv. Mater. 35, 2302120 (2023).
Reports antiferromagnetic behavior with uncompensated ferromagnetic moment.
Indicates the presence of anomalous Hall effect (AHE)?
(a) Neutron Scattering
(c) Hall Resistance
(b) Bulk Magnetometry
(d) Longitudinal Resistance
Altermagnet?
Singh, D. K. et al., Adv. Phys. Res. 4, 2400170 (2025).
AHE breaks T symmetry. Octahedrons of different color are not related by the P symmetry.
Suggested as the first realistic type 1 Altermagnet with non-collinear spin structure.

## Slide 4: Polymorphism of NiSi
NiSi has been experimentally synthesized in five different polymorphs.
Three bulk NiSi polymorphs are stable and recoverable under ambient conditions.
Structure Type | Space Group | Z | E0 (kJ mol-1)
B31 (MnP) | Pnma (, No. 62) | 4 | -886.3
B20 (ε-FeSi) | P213 (, No. 198) | 4 | -868.2
distorted CuTi | Pmmn (, No. 59) | 2 | -877.4
Structure Type | Space Group | Z | E0 (kJ mol-1)
B31 (MnP) |  | 4 | -886.3
B20 (ε-FeSi) |  | 4 | -868.2
distorted CuTi |  | 2 | -877.4
Dobson, D. P. et al., Phys. Earth Planet. Inter. 261, 196 (2016).
High P-T Polymorphs of NiSi

## Slide 5: Bulk Crystal Growth
Mixed Ni and Si powders in a 1:1 stoichiometric ratio.
Transferred the powder into a quartz tube and vacuum-sealed.
Sintered and slowly cooled to obtain NiSi crystals.

## Slide 6: NiSi Characterization - XRD
Database : PDF 01-070-9169
Rabadanov M. Kh. et al., Crystallography Reports 47, 33 (2002).
XRD data confirms the orthorhombic (Pnma) structure of NiSi.
There exists some impurity peaks that’s needs to be investigated.
Most probably they are from elemental Si.
(101)
(011)
(002)
(200)
(111)
(102)
(201)
(210)
(112)
(211)
(202)
(103)
(301)
(031)
(020)

## Slide 7: Thin Film Deposition
NiSi thin films
Choose Si (1 0 0) substrate.
Remove the native SiO₂ layer on the substrate using a buffered HF solution.
Deposit a thin Ni (2-50 nm) layer on the substrate using evaporation.
Anneal the sample at ~500 °C for 24 hrs.
Remove unreacted Ni using NH₄OH:H₂O₂:H₂O (1:1:5).
Julies B.A. et al., Thin Solid Films 347, 201 (1999).
Sidorenko S. et al., Defect and Diffusion Forum 280, 9 (2008).
NiSi

## Slide 8: Theoretical Studies
Structure Type | Space Group | Structure | Z | a (Å) | b (Å) | c (Å)
B31 (MnP) | Pnma (, No. 62) | Orthorhombic | 4 | 3.358 | 5.180 | 5.623
B20 (ε-FeSi) | P213 (, No. 198) | Cubic | 4 | 4.519 | 4.519 | 4.519
distorted CuTi | Pmmn (, No. 59) | Orthorhombic | 2 | 3.008 | 3.299 | 4.717
Structure Type | Space Group | Structure | Z | a (Å) | b (Å) | c (Å)
B31 (MnP) |  | Orthorhombic | 4 | 3.358 | 5.180 | 5.623
B20 (ε-FeSi) |  | Cubic | 4 | 4.519 | 4.519 | 4.519
distorted CuTi |  | Orthorhombic | 2 | 3.008 | 3.299 | 4.717
Crystal structures of (a) Pnma, (b) P213 and (c) Pmmn NiSi.

## Slide 9: Band Structure - Pnma
Band structure reveals clear metallic behavior.
Only two bands cross the Fermi level along most symmetry directions, resulting in a low density of states at the Fermi level.
Around the Fermi level, the Ni-d states and Si-sp states are strongly hybridized.

## Slide 10: Phonon Dispersion - Pnma
Phonon dispersion doesn’t reveal any imaginary phonon frequencies.
Low frequency vibrations are associated with Ni atoms while high frequency modes are dominated by Si atoms.
At 300 K, = 175.13 J mol−1 K−1, = 188.20 J mol−1 K−1, = 11.28 kJ mol−1.

## Slide 11: Transport Properties - Pnma
increases approximately linearly with temperature.
At 300 K and μ-EF ≈ 0, .
Seebeck Coefficient
Electrical Conductivity
Thermal Conductivity
Heat Capacity
indicates a significant influence of carrier concentration.
CV,elec is negligible compared to the lattice contribution.

## Slide 12: Band Structure - P213
Type 1 Weyl node appear in the path R-Γ.
Type 2 Weyl node appear in the path Γ-X.
W2
W1

## Slide 13: Topological Properties – Berry Curvature
k path
k slice

## Slide 14: Topological Properties
Bulk Spectra
Top Surface Spectra
Bottom Surface Spectra
Fermi Arc (001)
Projected Spectrum on the (001) surface of cubic NiSi.
W1
W2
W1
W2
Fermi arcs from the Weyl nodes clearly appear in the surface spectra.
These Fermi arcs almost transverse the entire slice space at the Fermi level.

## Slide 15: Conclusions
Key Findings
Transport properties of orthorhombic Pnma NiSi were predicted.
Interesting topological properties were identified in the high P-T cubic P2₁3 NiSi phase.
A comprehensive theoretical study was conducted on the high P-T Pmmn NiSi phase.
Bulk crystals of orthorhombic Pnma NiSi were successfully synthesized.
Next Steps
Incorporate magnetism and spin orbit coupling (SOC) into the theoretical studies.
Experimentally investigate the topological and transport properties of NiSi.

## Slide 16: Thank you!

## Slide 17: Questionable Magnetism Data
Observation
curves are largely symmetric about .
closely resembles that of .
At 20 K, both channels exhibit nearly identical V-shaped curves.
Similar switching features are present in both and . .

## Slide 18: Questionable Magnetism Data
Expected Field Symmetry
Why This Is Concerning
A true Hall signal should change sign upon reversing the magnetic field.
The measured Hall channel appears to contain a large even component, suggesting contamination by longitudinal resistance.
Possible Causes
Hall-contact misalignment.
Mixing of longitudinal and transverse voltages.
Incorrect probe wiring.
Quantity | Expected Symmetry
Longitudinal resistance | Even:
Hall resistance | Odd:
Quantity | Expected Symmetry

## Slide 19: Theory
Slide 4 – NiSi Polymorphs
Five experimentally synthesized phases of NiSi.
Hexagonal phase of NiSi has been reported only during the growth of NiSi thin films.
CsCl type NiSi phase cannot be recovered at ambient conditions, and the reported structural parameters correspond to 62 GPa.
There are two additional tetragonal phases of NiSi (γ-CuTi3 and distorted CsCl types23) that have been predicted by ab initio simulations.
NiSi Structure | Structure Type | Space Group | a (Å) | b (Å) | c (Å) | P (GPa) | T (K)
Orthorhombic | B31 (MnP) | Pnma (, No. 62) | 3.331 | 5.178 | 5.162 |  | 
Hexagonal | B81 (NiAs) | P63/mmc (, No. 194) | 3.28 |  | 5.23 |  | 
Cubic | B20 (ε-FeSi) | P213 (, No. 198) | 4.497 |  |  | 17.5±1 | 1223±50
Orthorhombic | distorted CuTi | Pmmn (, No. 59) | 3.027 | 3.274 | 4.698 | 17.5±1 | 1223±50
Cubic | B2 (CsCl) | Pmm (, No. 221) | 2.636 | 2.636 | 2.615 | 62 | 2100±150
NiSi Structure | Structure Type | Space Group | a (Å) | b (Å) | c (Å) | P (GPa) | T (K)
Orthorhombic | B31 (MnP) |  | 3.331 | 5.178 | 5.162 |  | 
Hexagonal | B81 (NiAs) |  | 3.28 |  | 5.23 |  | 
Cubic | B20 (ε-FeSi) |  | 4.497 |  |  | 17.5±1 | 1223±50
Orthorhombic | distorted CuTi |  | 3.027 | 3.274 | 4.698 | 17.5±1 | 1223±50
Cubic | B2 (CsCl) |  | 2.636 | 2.636 | 2.615 | 62 | 2100±150

## Slide 20: Theory
Slide 11 – Antiferromagnetism
Neutron Scattering Data - exhibits temperature dependence, across (001) and (002) peaks. Experimental data are well-described by resolution limited Gaussian line-shape, suggesting long-range magnetic order in NiSi.
Bulk Magnetometry Data - demonstrates the presence of a small uncompensated ferromagnetic moment embedded in the magnetic state.
Hall Measurements - curves show hysteresis, meaning the resistance depends on the magnetic-field history. That usually means the electronic transport is coupled to magnetic order. NiSi has a small uncompensated magnetic moment that breaks time-reversal symmetry and produces an anomalous Hall response. Shifted loop is taken as evidence of antiferromagnetic spin correlations.

## Slide 21: Theory
Slide 12 – Altermagnetism
Satisfies criteria for Type 1 altermagnet.
Initial theory of altermagnetism was build on colinear spin structure, but recent theoretical work suggest that there could exists non collinear spin structure altermagnets as well.
Property | Ferromagnet (FM) | Antiferromagnet (AFM) | Altermagnet (AM)
Net magnetization | Nonzero | Zero | Zero
Spin-up/down bands | Split | Degenerate | Split
Spin arrangement | parallel | translation/inversion | rotation or other
Fermi surfaces | Different for ↑ and ↓ | Same | Different for ↑ and ↓

## Slide 22: Theory
Slide 4 – Formation Energy
  E​(NiSi) - total energy of the NiSi unit cell
  E(Ni) - total energy of the elemental Ni unit cell (FCC)
  E(Si) - total energy of the elemental Si unit cell (Diamond)
  ZNiSi - number of NiSi formula units in the NiSi cell
  ZNi - number of Ni atoms in the Ni cell
  ZSi - number of Si atoms in the Si cell
Slide 5 – Crystal Structure
  Ni - 1s2 2s2 2p6 3s2 3p6 3d8 4s2 - 10 valance electrons
  Si - 1s2 2s2 2p6 3s2 3p2 - 8 valance electrons

## Slide 23: Data
Slide 6 – Band Structure
Fermi Energy - 10.303 eV

## Slide 24: Transport Properties - Pnma
N changes sign near the Fermi level, marking the transition between electron to hole dominated transport.
Carrier Concentration
Hall Coefficient
Power Factor
Rxyz remains small over most chemical potentials, indicating a strong carrier compensation.
PFxx peaks suggests that enhanced thermoelectric performance requires doping.

## Slide 25: Theory
Slide 9 – BoltzTrap2
Seebeck Coefficient : Can tune the sign of S (n-type vs p-type) by shifting the Fermi level (doping). S is modest. The temperature dependence suggests the position of EF relative to band edges or flat bands is important.
Electrical Conductivity : Wiggly behavior indicates complex band structure, multiple bands crossing EF or pockets in the density of states (DOS). Conductivity is highly sensitive to doping. Optimal σ likely near certain μ where bands align favorably.
Thermal Conductivity : All curves increase with T, roughly linearly for most doping. Wiedemann-Franz law seems roughly followed - metallic behavior.
Specific Heat : Nearly linear increase with T for all doping. Classic metallic Fermi gas behavior (Cv ≈ γT). Confirms metallic character; the slope γ relates to the DOS at EF: higher DOS means higher Cv and often higher σ.

## Slide 26: Theory
Slide 13 – Band Structure
Fermi Energy - 11.709 eV

## Slide 27: Phonon Dispersion - P213
Imaginary phonon frequencies appear near the Γ points.
At 300 K, 𝐶v,lattice = 179.69 J mol−1 K−1, 𝑆lattice = 217.92 J mol−1 K−1, 𝐹lattice = 0.79 kJ mol−1.

## Slide 28: Theory
Slide 20 –
Multiplying eigen states by overall phase factor doesn’t affect physical measurement. When eigen state moves from k1 and k2 in space in adiabatic passion (slow), the wavefunction pick up an extra phase – Berry Phase. Keep arrow in same direction without twisting (parallel transport), this ties to berry connection. Berry phase is only gauge invariant over a closed loop. Berry connection is gauge dependent. Berry curvature is gauge invariant. Berry phase only depends only on the geometry not on time. Dynamical phase depends on time. Berry phase is purely real.
Berry connection describes geometry connection to the quantum states
Berry Curvature – Magnetic potential(A) gauge dependent. But if we get curl of A, which is the magnetic field it is gauge invariant. Following this get the curl of Berry connection, which is the berry curvature.

## Slide 29: Theory
Slide 20 –
Hall effects, anomalous hall effects – Berry curvature acts as a effective magnetic field in momentum space. But entirely geometric.
In the strong magnetic field conduction of electrons restrict to the edges of the material.
Chern number is topological invariant.
Weyl – 2 fold degeneracy, chirality - +1, -1
Dirac – 4 fold degeneracy, chirality - 0

## Slide 30: Theory
Slide 20 – Topological Properties
Surface Spectral Function:
Calculated from the surface Green's function of the Wannier Hamiltonian. Represents the surface electronic density of states as a function of momentum and energy. Theoretical equivalent of an ARPES intensity map.
Bright regions correspond to electronic states with high spectral weight. Bulk states appear as projected bulk bands. Surface states appear as sharp features that are absent or weak in the bulk spectrum. In topological materials, topological surface states may bridge bulk band gaps.
Identifies surface-localized electronic states. Allows direct comparison with ARPES experiments. Reveals signatures of non-trivial band topology.
Fermi Arc Surface Map
Constant-energy surface spectral weight map, typically at or near the Fermi energy. Shows the momentum-space distribution of surface electronic states.
Ordinary metals: closed Fermi contours. Weyl semimetals: open surface states called Fermi arcs. Fermi arcs connect projections of Weyl nodes with opposite chirality.
One of the strongest signatures of Weyl semimetals. Provides evidence for topological surface states. Can be directly compared with ARPES Fermi-surface measurements.

## Slide 31: Theory
Slide 20 – Angle-Resolved Photoemission Spectroscopy (ARPES)
Photons eject electrons from a material surface via the photoelectric effect. The kinetic energy and emission angle of the electrons are measured. Electronic band structure E(k) is reconstructed from these measurements.
Measured Quantities
Binding Energy EB=hν−ϕ−Ekin ​
hν: photon energy ϕ: work function Ekin: measured kinetic energy
Crystal Momentum k∥ ​=ℏ2mEkin ​ ​
sinθθ: electron emission angle
ARPES Output
Band dispersion: E vs k
Fermi surface maps: intensity at EF ​Surface states and topological states
Fermi arcs in Weyl semimetals
ARPES?
Direct probe of electronic band structure.
Highly surface sensitive (top few atomic layers).Powerful tool for identifying topological surface states and Fermi arcs.