## Slide 1
Investigation of the role of Microstructural Refinement on Hydrogen Storage behavior of the β-Mg17Al12 Intermetallic
Sibriyana Antanessian
Co-authors:
Prof. Jacques Huot
Dr. Babak Omranpour Shahreza
University of Ottawa
22 June 2026

## Slide 2
Introduction – Sources of energy
Storage method | Hydrogen content (wt.%) | Volumetric density (g/L) | Volumetric energy density (MJ/L)
Compression |  |  | 
700 bars, RT, (inlc. Type IV tank) | 5.7 | 40.8 | 4.9
Liquid hydrogen |  |  | 
1 bar, − 253 ◦C (inlc. tank) | 14 | 51 | 6.12
Cryo-compression |  |  | 
350 bar, − 253 ◦C | 100 | 80 | 9.6
Metal hydrides |  |  | 
MgH2 | 7.6 | 110 | 13.2
FeTiH2 | 1.89 | 114 | 13.7
Complex hydrides |  |  | 
NaAlH4 | 7.5 | 80 | 9.6
Physical adsorbents |  |  | 
Activated carbon @77 K and 30–60 bar | 5 | 38.5 | 2.4
Liquid hydrogen organic carriers |  |  | 
Methylcyclohexane/ toluene | 6.2 | 47.3 | 5.68

## Slide 3
Introduction – Sources of energy
Advantages:
Good safety
Possibility of reversible hydrogen storage
Tunability by processing
Disadvantages:
Slow hydrogenation/dehydrogenation kinetics in many systems
Difficult activation
Industrial scale-up problem
Hydrogen Absorption is Exothermic
Hydrogen Desorption is Endothermic

## Slide 4
Introduction – Solid state hydrogen storage
Mg
A material for solid-state hydrogen storage
High capacity
Low density
Abundant and low cost
Challenge: pure Mg / MgH₂ still shows slow kinetics and high desorption temperature.
High theoretical H₂ capacity
Stores much more hydrogen than many conventional intermetallic hydrides.
Lightweight and abundant
Low density, high natural abundance, and relatively low cost
Why not pure Mg alone?
Its main limitations are slow sorption kinetics and the need for relatively high operating temperature. This is why alloying and processing become essential.
Reversible solid-state storage
Hydrogen can be repeatedly absorbed and released, enabling rechargeable storage behavior.
Safe and compact concept
Solid-state storage offers better volumetric packing and safer handling than compressed gas.
Material choice
Why Mg-based hydrides?

## Slide 5
Introduction – Solid state hydrogen storage
Modifies Mg hydrogenation
Al changes the reaction pathway of Mg without trapping hydrogen in its own stable hydride.
In general
Mg–Al alloys keep the advantages of Mg while providing a tunable intermetallic system for better kinetics, thermodynamics, and processing studies.
Can lower effective hydride stability
Compared with pure MgH₂, the alloy’s diffusion pathway can make hydrogen release easier under practical conditions
Material choice
Why Mg–Al alloys?
Mg base
Al modifier
+
intermetallic design
β-Mg₁₇Al₁₂
γ-Mg₂Al₃
Forms useful intermetallic
The Mg–Al system provides well-defined phases such as β-Mg₁₇Al₁₂ for structure–property studies.

## Slide 6
Introduction – Hydrogenation mechanism of Mg17Al12
β-Mg₁₇Al₁₂ hydrogenates through two reversible plateaus:
The first plateau forms MgH₂ + Al3Mg2 and the second plateau further converts the Al-rich intermediate to additional MgH₂ + Al.
Starting phase
Mg₁₇Al₁₂
Reaction equations
Mg₁₇Al₁₂ + 9 H₂ ⇌ 9 MgH₂ + 4 Al₃Mg₂
4 Al₃Mg₂ + 8 H₂ ⇌ 8 MgH₂ + 12 Al
Theoretical uptake
Step 1 = 2.40 wt.% H₂
Step 2 = 2.04 wt.% H₂
Total = 4.40 wt.% H₂
At 350 °C
Peq,1 ≈ 7.9 bar | Pₑq,2 ≈ 12.3 bar
1st plateau
9 MgH₂ + 4 Al₃Mg₂
+ 9 H₂
Step 1
2nd plateau
17 MgH₂ + 12 Al
+ 8 H₂
Step 2

## Slide 7
Materials and Methods
Mg ingot: commercial purity (99.98%)-Magnesium Electron
Al granuls: 99.90% - Alfa Aesar
(1)
Melting pure Mg into a graphite crucible inside a Norax Canada Induction Furnace under a protective CO2/SF6 atmosphere (0.553% SF6, balance CO2)
(2)
Adding Aluminum at 700 °C
Maintaining for 15 min at a similar temperature
(3)
Stirring and skimming the melt periodically
Casting into a steel permanent mold preheated to 400 °C
Casting of the samples was performed at McGill University by Mr. Orhan Selcuk Sari and Dr. Raul Arriaga Benitez under supervision of Professor Mehriban Pekguleryuz.

## Slide 8
Materials and Methods
Ball-milling
As-cast Mg17Al12
Mechanical Ball-milling for 15, 30, and 60 min
Argon-filled milling jar with ball-to-powder ratio: 10:1
Hydrogenation
Filed and ball-milled Mg17Al12
Vacuum: 30 min
Process Temperature: 350 °C
Hydrogen Pressure: at 50 bars H2
Home-made Sievert Apparatus

## Slide 9
Materials and Methods- Characterization
DSC
Activation energy (Kissinger plot)
Hydrogen desorption temperature
X-ray diffraction
Phase identification
Crystallite size Evaluation
Microstrain evaluation

## Slide 10
Results – Effect of filing and ball milling on the microstructure
Mg17Al12 | Crystallite Size [nm] | Microstrain [%e0] | Lattice Parameter a [Å] | Cell Volume [Å3]
Filed | 26.0(4) | 0. 00(2) | 10.5278(8) | 1166.8(3)
Ball-Milled (15 minutes) | 11.7 (3) | 0.221(8) | 10.530(3) | 1167.6(9)
Ball-Milled (30 minutes) | 8.6 (2) | 0.161(1) | 10.539(3) | 1170.4(9)
Ball-Milled (60 minutes) | 8.2 (2) | 0.16(2) | 10.528(4) | 1167(1)
26.0 (4)→ 11.7 (3) nm
Crystallite size
0.00 (2) → 0.221(8)
Microstrain
The hydrogenation experiments were carried out on the 15 min ball‑milled sample.
Lattice parameter / cell volume
≈ unchanged
Only β‑Mg₁₇Al₁₂ peaks
No significant Al, Mg, Fe, or oxide peaks detected.
As-cast Mg17Al12
Ball-milled for 30 minutes
Ball-milled for 60 minutes
Ball-milled for 15 minutes

## Slide 11
Preliminary results – Phase characterization of dihydride filed Mg17Al12
Filed Mg17Al12 (Mg-Al-1) | Crystallite Size [nm] | Microstrain [%e0] | Lattice Parameter a [Å] | Cell Volume [Å3]
Dehydride | >100 | 0. 0273(7) | 10.5224(2) | 1165.06(7)
XRD pattern of the filed Mg₁₇Al₁₂ sample after three complete
absorption/desorption cycles
No residual MgH₂ peaks are apparent
Notes: We further examined the dihydride filed samples by XRD to investigate the formed phases after hydrogen desorption.
XRD pattern on dihydride sample showed only Mg17Al12 peaks, and no trace of MgH2 or remained Al or Mg.
Which suggest that although hydrogen desorption was partial based on the Sievert measurements, the amount of other phases in the dihydride sample was marginal that the XRD could not detect them.

## Slide 12
4.21 wt%
BM · cycle 1
4.23 wt%
BM · cycle 2
First and second hydrogenation curves
BM · cycle 1
BM · cycle 2
Results and Discussion- Hydrogenation behavior at 50 Bars H2 and 350 ºC
15 min ball‑milled Mg17Al12
First and second hydrogenation curves
2.97 wt%
2.82 wt%
Filed Mg17Al12

## Slide 13
Preliminary results – Characterization of hydrogenation products
MgH₂ + γ‑Mg₂Al₃
Observed phase products after hydrogenation:
Filed-Hydrided
Ball-milled Hydrided
Filed Mg17Al12
Ball-milled Mg17Al12

## Slide 14
Results and Discussion- DSC results and activation energy
Ball‑milled Mg17Al12, at 2 bars Argon
Phase diagram of binary Mg-Al alloy
Peak 1 is associated with the decomposition of MgH2
Peak 2 is associated with the decomposition of Mg2Al3
Peak 3 is associated with the melting point of Mg17Al12
2
1
3

## Slide 15
Results and Discussion- Activation Energy
Sample | MgH2 decomposition | Mg2Al3 decomposition | Literature reported for MgH2
Activation Energy [kJ/ mol] | 162.2 ± 6.8 | 222.8 ± 36.1 | 260.4
Dehydrogenation Temperature [℃] | 398 | 412 | 414
MgH2
Mg2Al3

## Slide 16
Conclusions
01
Ball milling effectively refined the β-Mg₁₇Al₁₂ microstructure without introducing detectable impurity phases.
02
Hydrogenation of β-Mg₁₇Al₁₂ followed the expected Mg–Al reaction pathway, forming MgH₂ and γ-Mg₂Al₃.
03
At 350 °C and 50 bar H₂, ball milling strongly improved hydrogen uptake compared with the filed sample.
04
Ball-milling effectively reduced the activation energy of MgH2 dehydrogenation.

## Slide 17
Acknowledgment
Prof. Jacques Huot
Dr. Babak Omranpour Shahreza
Prof. Mehriban Pekguleryuz
Dr. Raphaël Gervais Lavoie
PhD. Orhan Selcuk Sari

## Slide 18
The adjective for metal is metallic, but not so for Iron, which is ironic.
Thank You!

## Slide 19
Sievert Apparatus
Gas reservoir: The first chamber where a known amount of hydrogen is stored before being released to the sample.
Sample reactor: The chamber where the solid material is placed. It is often surrounded by a furnace or cooling bath to control the hydrogenation temperature.
Isolation valve: The critical component that separates the two volumes. Opening this valve starts the expansion and subsequent hydrogenation.
Pressure transducer: Sensors that monitor the pressure drop as the material "soaks up" the hydrogen atoms into its crystal structure.
Vacuum and inlet lines:Used to purge the system and introduce fresh hydrogen or inert gases like Argon for volume calibration
Dosing
Known amount of H2 loaded to chamber at a specific pressure
Expansion
A valve opens, allowing gas to flow into the sample chamber
Equilibrium
The gas molecules physically or chemically bond with the material.
Calculation
The final pressure is measured. If the sample absorbed gas, will be lower than the theoretical expansion-only pressure.

## Slide 20
Sievert Apparatus
Goal: Δna= ninitial - nfinal
Step A: Initial State (Gas in Reference Cell only) Before opening the valve to the sample, you calculate the moles of gas in the reference volume
P1: Initial pressure in the reference cell.
Tref: Temperature of the reference cell.
R: Gas constant
Step B: Final State (Gas expanded into Sample Cell)
P1: Final equilibrium pressure.
Pvoid: The free space in the sample cell (Total cell volume minus the volume of the solid sample).
Step C: Solving for absorption
Combining these, the moles absorbed (Δna) are:
)
Step D: Converting to weight percentage
To make the data useful for material science, the moles of hydrogen are converted to a mass ratio:
MH2= Molar mass of hydrogen (~2.016 g/mol)
msample = Initial mass of the dry sample.

## Slide 21
P-C-T and Vantt Hoff
Usually, people measure equilibrium pressure at different temperatures using PCT curves.
If we plot versus :
ΔH=−(slope)×R
In easy way: It tells us how much hydrogen pressure is needed to keep the hydride stable at a given temperature, or at what pressure absorption and desorption are balanced.
So:
(Absorption)
(desorption)
(equilibrium)

## Slide 22
WDS/EPMA
EPMA = Electron Probe Microanalysis:
A very tiny electron beam is focused onto a small point on the sample.
When the electrons hit the sample, the atoms inside the material get excited and emit X-rays.
Those X-rays are special because each element gives its own characteristic X-ray energy.
So, by measuring the X-rays, the machine can tell which elements are there.
The key difference between WDS/EPMA and SEM/EDS is EPMA separates X-rays one wavelength at a time and then the detector measures that selected wavelength.

## Slide 23
Activation energy estimation and Kissinger plot
Differential Scanning Calorimetry (DSC) apparatus works by measuring the difference in the amount of heat required to increase the temperature of a sample compared to an inert reference material.
Core Components:
Sample and Reference Pans: A small amount of the test material (typically 1–15 mg) is placed in a metal pan (often aluminum), while the reference pan is usually left empty.
Furnace(s): Depending on the design, both pans are housed in either a single shared furnace or two independent furnaces.
Sensors (Thermocouples): High-precision sensors monitor the temperature and heat flow of both pans continuously.
Purge Gas System: An inert gas like nitrogen or helium flows through the chamber to prevent oxidation or other unwanted atmospheric reactions.

## Slide 24
Activation energy estimation and Kissinger plot
Activation Energy
is the minimum amount of energy required for a chemical reaction to occur, representing the potential energy barrier between reactants and products. It dictates the temperature dependence of a reaction rate.
The Kissinger method is based on the following linear relationship:
So, if we plot ( versus
Calculate Ea from the Slope:
Slope:
R = 8.314 J/mol.K

## Slide 25
High Entropy Alloys
HEAs are a novel class of materials composed of five or more principal elements, typically in equimolar or near-equimolar ratios each typically ~5 to 35 at.%.
A useful quantitative descriptor is the configurational entropy of mixing (ideal solution):
For Equiatomic
So:
= R. (Ln5) ≈ 1.61R
When increases, the stabilizing term becomes larger in magnitude.

## Slide 26
Laves Phase
Laves phases are intermetallic compounds that have a stoichiometry of AB2 and are formed when the atomic size ratio is between 1.05 and 1.67.
There are three classes of Laves phases, namely, cubic MgCu2 (C15), hexagonal MgZn2 (C14), and hexagonal MgNi2 (C36)
In these compounds, the A atoms take up ordered positions as in diamond, hexagonal diamond or related structure while the B atoms take up tetrahedral positions around A atoms.
C14 Laves phases matter because they are often hard, ordered intermetallics with distinct mechanical, magnetic, and hydrogen-storage behavior. In hydrogen-storage research, many alloys based on Ti-, Zr-, V-, Nb-, Fe-, Mn-, or Cr-containing systems can crystallize in a single C14 Laves phase.

## Slide 27
X-Ray Diffraction
Check out MyScopeTM, (available at https://myscope.training/XRD_Primary_optics).
Notes: The X-ray source sends X-rays to the sample. Inside the sample, atoms are arranged in parallel planes. The X-rays hit these planes and are reflected. At certain angles, the reflected X-rays become strong and reach the detector. The detector records a peak.

## Slide 28
X-Ray Diffraction
Braggs Law: To find peak position to the distance between planes in the crystal
nλ=2dsinθ
Scherrer equation: To estimate crystallite size
β = peak broadening or FWHM in radians
K = shape factor, often about 0.9
Lattice parameter relation for cubic crystals
a = lattice parameter
hkl = Miller indices of the plane
Williamson–Hall equation: To separate peak broadening due to small crystallite size from peak broadening due to strain
D = Crystallite size
ɛ = microstrain

## Slide 29
X-Ray Diffraction
Step Size
Parameter | What it does | If too low | If too high
Voltage (kV) | Controls X-ray energy (how hard electrons hit) | weak X-ray generation | more background, more tube stress
Current (mA) | Controls X-ray intensity (how many electrons hit) | weak peaks | overheating risk
Step size (°) | Controls angular resolution of scan points | long scan if too small | poor peak definition if too large

## Slide 30
X-Ray Diffraction
Phase | Crystal structure basis | Main expected peaks, 2θ (°) with Cu Kα | Notes
Mg | hcp α-Mg | 32.2, 34.4, 36.6, 47.8, 57.4, 63.1, 68.6, 70.0 | The strongest/common Mg reflections are usually around 32–37° and 47–57°. (MDPI)
MgH₂ | tetragonal β-MgH₂ | 27.6–28.0, 35.6–35.9, 39.5–40.0, 54.2–54.8, 57.9, 61.6 | A reported set of characteristic β-MgH₂ peaks is 27.63°, 35.62°, 39.48°, 54.21°. (PMC)
Mg₁₇Al₁₂ | cubic, I-43m | 16.8, 20.6, 23.9, 26.7, 29.3, 31.7, 34.0, 36.1, 38.2, 40.1, 42.0, 43.8 | In Mg alloys, one commonly noticed Mg₁₇Al₁₂ reflection is near 42.2°; the rest here are expected from the reported cubic cell. (SciOpen)
Mg₂Al₃/ Al₄₅Mg₂₈ / Al₃Mg₂ | cubic, Fd-3m | 10.4, 12.5, 13.7, 15.4, 16.3, 17.8, 18.6, 19.9, 20.6, 21.8, 22.5, 23.6, 25.2, 26.8, 28.2, 29.7, 31.0 | Because the unit cell is very large, many peaks appear at low angles and can be crowded. (LARO)
Al | fcc Al | 38.5, 44.8, 65.2, 78.3, 82.5, 99.2 | These are the classic Al peaks; 38.5° and 44.8° are usually the easiest to spot. (ResearchGate)
Al₃Y | cubic Pm-3m | 21.0, 29.8, 36.7, 42.7, 48.0, 52.9, 62.0, 66.2, 70.3, 74.3, 78.2 | These are expected positions from the reported cubic Al₃Y cell. (MDPI)