## Slide 1
HTS coated conductor coatings in haloscopes for dark matter search
V. Springel et al. 2005
Joffre Gutierrez Royo

## Slide 2
Guilherme Telles1, Teresa Puig1, Ahmed Irfan1, Neil Lamas1, Luca Benedetti1, Xavier Granados1, Rafael Garcia2, Julia Mundet2, Jessica Golm3, Walter Wuensch3, Sergio Calatroni3, Alejandro Benedicto Díaz Morcillo4, Jordi Miralda Escudé5, Babette Dobrich6, Igor Irastorza7
1- Institut de Ciència de Materials de Barcelona, ICMAB-CSIC, Bellaterra (Spain)
2- Institut de Física d'Altes Energies, IFAE, Bellaterra (Spain)
3- CERN - The European Organization for Nuclear Research, Geneva (Switzerland)
4- Information and Communications Technologies Dept., Technical University of Cartagena (Spain)
5- Institut de Ciencies del Cosmos, ICCUB, Universitat de Barcelona, Barcelona (Spain)
6- Max-Planck-Institut fur Physik, MPP, Garching (Germany)
7- Center for Astroparticles and High Energy Physics (CAPA), Universidad de Zaragoza (Spain)
Aknowledgements

## Slide 3
We are trying to detect the AXION, an excellent dark matter candidate
The axion is a hypothetical elementary particle that emerges very naturally when trying to solve the strong CP problem in QCD.
Very light (ma)
Extremely weakly interacting
Couples to photons (gag ) very feebly.
arXiv:2504.00079 [hep-ph]

## Slide 4
We are trying to detect the AXION, an excellent dark matter candidate
The axion is a hypothetical elementary particle that emerges very naturally when trying to solve the strong CP problem in QCD.
Very light (ma)
Extremely weakly interacting
Couples to photons (gag ) very feebly.
Why axions can be cold dark matter
Axions fit every criterion for cold dark matter:
✔ Produced cold: non-thermal, non-relativistic
✔ Extremely long-lived: > age of universe
✔ Weakly interacting: won’t scatter or dissipate energy
✔ Abundant: natural cosmological production gives the right density
✔ Predictive: oscillating fields, couplings to photons, etc.
In one stroke axions solves the CP problem and the dark matter mystery
arXiv:2504.00079 [hep-ph]

## Slide 5
Axions can be detected through the Primakoff effect
gag
Haloscope’s detection principle
B
P. Sikivie, Phys. Rev. Lett. 52, 695 (1984)
I. G. Irastorza & J. Redondo, Prog. Part. Nucl. Phys. 102,89 (2018)

## Slide 6
Axions can be detected through the Primakoff effect
gag
Cavity’s quality factor
Magnetic field
Cavity’s volume
Axion density
We want
High-Q (low-Rs) cavities under high-B fields
Haloscope’s detection principle
B
P. Sikivie, Phys. Rev. Lett. 52, 695 (1984)
High Temperature Superconductors (HTS) can be ideal materials
I. G. Irastorza & J. Redondo, Prog. Part. Nucl. Phys. 102,89 (2018)

## Slide 7
Superconductors are the materials with the lowest resistance

## Slide 8
Cavity coated with LTS pure Nb
Q0  1010
But Nb cavities’ Q-factor dramatically decreases in the presence of a few mT
High-purity LTS Nb coated cavities are used due to their very high-Q

## Slide 9
The mixed state in HTS allows
superconductivity to survive up to very high-magnetic fields

## Slide 10
The mixed state in HTS allows
superconductivity to survive up to very high-magnetic fields
Magnetic phase diagram of HTS
In the mixed state quantized magnetic field lines called vortices penetrate the material.
The trade off is the penetration of superconducting vortices which generate dissipation when move

## Slide 11
Pinning centers are introduced in the material
to stop (or reduce) the movement of vortices
Some material defects act as pinning centers for vortices
if pinning centers can keep Rs low
In RF applications (like haloscopes) the depinning frequency separates low from high dissipation regimes

## Slide 12
1 – REBCO HTS and its surface resistance
Outline
3 – REBCO coated haloscopes for cold DM detection
2 – How we coat surfaces with REBCO

## Slide 13
1 – REBCO HTS and its surface resistance
Outline
3 – REBCO coated haloscopes for cold DM detection
2 – How we coat surfaces with REBCO

## Slide 14
Coated Conductors solve the problem of needing a textured substrate
to obtain high-quality REBCO
Tc ≈ 91 K
Hc2 (4.2K) > 100 T
Why REBa2Cu3O7-x?
but REBCO needs epitaxy

## Slide 15
Cu ~ 20 mm
(electrical contact)
Ag ~ 2 mm (protection)
REBCO HTS ~ 1 – 3 mm
Buffers ~ 0.2 – 1 mm (provide texture)
Metallic Substrate ~ 30 – 100 mm
(provides flexibility)
Coated Conductors solve the problem of needing a textured substrate
to obtain high-quality REBCO
In collaboration with:
CCs are commercially available with different widths in Km length
Tc ≈ 91 K
Hc2 (4.2K) > 100 T
Why REBCO?
but REBCO needs epitaxy

## Slide 16
T = 50 K, n = 8 GHz
At intermediate and low temperatures, Rs of high-pinning REBCO shows a weak magnetic field dependence
REBCO CCs have lower Rs than Cu
ideal materials for low-Rs (high-Q cavities) at high magnetic fields
T = 10 K, n = 8 GHz
T. Puig et al, Supercond. Sci. Technol. 32 (2019)
A. Romanov, et al. Scientific reports 10 (2020)
Lower pinning
REBCO CC
Higher pinning
REBCO CC
The lower the operating temperature, the larger the benefit from using REBCO
Cu
Cu

## Slide 17
1 – REBCO HTS and its surface resistance
Outline
3 – REBCO coated haloscopes for cold DM detection
2 – How we coat surfaces with REBCO

## Slide 18
We have developed a scalable CC coating technique for large surfaces
Target
0
1
2
3
5
4
6
8
9
7
Design of a custom plastic adapter
Pressure measurements
Custom 3D-printed metallic adapter
Coated conductor preparation
Placement and protection
Homogenizers and adapter
Soldering
Soldered coating (excess tin)
Delaminated coating w/ protrusions
Coated component
Hexagonal cavity component
10
We have developed technology to automatize all the steps

## Slide 19
1 – REBCO HTS and its surface resistance
Outline
3 – REBCO coated haloscopes for cold DM detection
2 – How we coat surfaces with REBCO

## Slide 20
HTS coated haloscopes outperform state of the art Cu haloscopes
Progress on HTS Coatings of Cavities and Characterization
13
B-field
Q0
Copper: 40k
Analysed with https://www.arpe.upc.edu/
Original RADES Cavity
Very low amount of flux used
Factor 4 – 6 better than Cu
Not dettached!

## Slide 21
Progress on HTS Coatings of Cavities and Characterization
13
B-field
Q0
Q0
Copper: 40k
Copper: 80k
Analysed with https://www.arpe.upc.edu/
Hexagonal Cavity
First iteration
Dettachment in 2/6 pieces
High Q-factor preserved
Low field dependence (parallel)
Factor 5 – 8 better than Cu
660k Q if not dettached?
Original RADES Cavity
Very low amount of flux used
Factor 4 – 6 better than Cu
Not dettached!
HTS coated haloscopes outperform state of the art Cu haloscopes
Preliminary results!

## Slide 22
Progress on HTS Coatings of Cavities and Characterization
13
B-field
Q0
Q0
Copper: 40k
Copper: 80k
Analysed with https://www.arpe.upc.edu/
Hexagonal Cavity
First iteration
Dettachment in 2/6 pieces
High Q-factor preserved
Low field dependence (parallel)
Factor 5 – 8 better than Cu
660k Q if not dettached?
Original RADES Cavity
Very low amount of flux used
Factor 4 – 6 better than Cu
Not dettached!
Prediction if not dettached
HTS coated haloscopes outperform state of the art Cu haloscopes
Preliminary results!
The geometry of the haloscope has to be adapted to the HTS

## Slide 23
The search for Cold DM Axions is challenging but HTS coated haloscopes can help.
Conclusions

## Slide 24
The search for Cold DM Axions is challenging but HTS coated haloscopes can help.
HTS enhances the sensitivity (Q-factor) of resonant cavities and can operate under high magnetic fields.
Conclusions

## Slide 25
The search for Cold DM Axions is challenging but HTS coated haloscopes can help.
HTS enhances the sensitivity (Q-factor) of resonant cavities and can operate under high magnetic fields.
A robust coating technology adapted to complex surfaces is being developed and automatized.
Conclusions

## Slide 26
The search for Cold DM Axions is challenging but HTS coated haloscopes can help.
HTS enhances the sensitivity (Q-factor) of resonant cavities and can operate under high magnetic fields.
A robust coating technology adapted to complex surfaces is being developed and automatized.
Cooperation between HEP and HTS may lead to new leaps in technology.
Conclusions

## Slide 27
REBCO CCs’ Rs(H) shows a stronger dependence than Cu
for n << np and 2Bc1 < B << Bc2
In agreement with N. Belk et al. Phys. Rev. B 53 1996
Normal conductors:
Superconductors:
S. Calatroni and R. Vaglio, IEEE TAS 27, 2017
(B independent)
Experimentally REBCO:
Going to lower frequencies benefits a lot REBCO CC as compared to Cu
T = 50 K
N. Tagdulang, Ph.D. Thesis, UPC (2024)

## Slide 28
Million quality factor: depends on the frequency
Progress on HTS Coatings of Cavities and Characterization
14
Q0
Copper: 80k
Analysed with https://www.arpe.upc.edu/
As reported by Jessica Golm
Hexagonal Cavity
First iteration
Dettachment in 2/6 pieces
High Q-factor preserved
Low field dependence (parallel)
Factor 5 – 8 better than Cu
6.5e5 Q if not dettached?
Prediction if not dettached
CAPP’s 3rd Gen. Cavities
 | RADES | CAPP | 
T (K) | 5 | < 1 | 
f (GHz) | 9.2 | 2.3 | 5.4
Q | 6.5e5 | 3.5e6 | 1.3e7
What would our Q-factor be at 2.3 and 5.4 GHz?
From Dahno Ahn’s presentation at the 18th PATRAS Workshop
We are already matching CAPP’s 2.3 GHz cavity!
But how can we improve?
Higher REBCO ratio (12 mm tapes in 14 mm facets)
More well-aligned facets
Flux-free solder
Solder vs. Glue

## Slide 29
Initial study shows that CCs have a weak dependence with the RF power
P. Krkotic, et al. Supercond. Sci. Technol. 35 (2022)
T = 50 K, n = 8 GHz
Opens the possibility for high-power applications
Medicine: Compact linacs
High-energy physics: Muon collider

## Slide 30
TE111
B
B
B and E configurations
TE010

## Slide 31
Magnetic phase diagram of HTS
Vortex length scales:
Distance upon which magnetic field decays.
Distance upon which the order parameter decays.
Vortex in HTS carries a quantum of flux
Characterized by mixed state with
quantized magnetic field penetration
called vortices.
The mixed state in HTS allows
superconductivity to survive up to very high-magnetic fields
When vortices move (due to Lorentz like forces) generate dissipation

## Slide 32
Material defects: Strategy to pin vortices
Some material defects act as pinning centers for vortices
In DC pinning centres provide lossless operation until a certain critical current density
Immobilization of vortices is key for lossless operation

## Slide 33
The surface resistance of an HTS under B is dominated by vortices
Some material defects act as pinning centers for vortices
if pinning centers modulate dissipation
RF
A. Romanov, et al. Scientific reports 10 (2020)