## Slide 1
Slide 1/12
IMPLEMENTATION OF RESILIENCE PLANS AT THE NATIONAL ACCELERATOR CENTER
M. Rodríguez-Ramos, J. García-López, C. Torres-Muñoz, M.C. Jiménez-Ramos, J. Gómez Camacho, C. Guerrero and J.M. López Gutiérrez
Centro Nacional de Aceleradores. Universidad de Sevilla

## Slide 2
Slide 1/12
NATIONAL ACCELERATOR CENTER: FIRST ION ACCELERATOR FACILITY IN SPAIN
The National Accelerator Center (CNA) is a research center with particle accelerators oriented toward user service.
It is a mix center belonging to the University of Seville, the Regional Government of Andalusia, and the Spanish National Research Council (CSIC).
Located at Parque Científico y Tecnológico Cartuja C/ Thomas Alva Edison 7 (Seville, Spain).
AstroHEP

## Slide 3
Slide 1/12
NATIONAL ACCELERATOR CENTER: FIRST ION ACCELERATOR FACILITY IN SPAIN
The National Accelerator Center (CNA) is a research center with particle accelerators oriented toward user service.
It is a mix center belonging to the University of Seville, the Regional Government of Andalusia, and the Spanish National Research Council (CSIC).
Located at Parque Científico y Tecnológico Cartuja C/ Thomas Alva Edison 7 (Seville, Spain).
AstroHEP

## Slide 4
Slide 2/12
The CNA is part of a distributed Singular Scientific and Technical Infrastructure (ICTS): IABA together with CMAM (Autonomous University of Madrid).
Six main facilities:
3 MV tandem accelerator
18 MeV proton cyclotron
Tandetron AMS
Compact accelerator for radiocarbon
60Co irradiator
PET/CT scanner
Ion Beam Techniques (IBA)
Materials Modification
Low energy nuclear physics
Irradiation Damage
INFRASTRUCTURE FOR ACCELERATOR-BASED APPLICATIONS
AstroHEP

## Slide 5
1.1
1.2
1.3
1.4
Activity 1.1: Irradiation of detectors with accelerators.
Activity 1.3: Exploitations of European Infrastructures of Nuclear Physics.
Activity 1.2: Accelerator Mass Spectrometry.
Activity 1.4: Developments for ion beam therapy.
Complementary R&D&I Plan for Astrophysics and High-Energy Physics
Development of Advanced Scientific Instrumentation for National and International Infrastructures in Astrophysics and High-Energy Physics.
J. García López
J.M. López Gutiérrez
J. Gómez Camacho
C. Guerrero Sánchez
M.C. Jiménez Ramos
Slide 3/12
AstroHEP
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments

## Slide 6
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments
1.4: Developments for ion beam therapy
IP: M. Carmen Jiménez Ramos. Univ. de Sevilla.
Goal: Design and manufacture of a new beam pulsing system for the external line of the CNA cyclotron (for radiobiology studies in FLASH mode).
Irradiation of cell cultures in collaboration with research centers as IFIC, CABIMER & UV.
Operating voltage: from 1 kV to 26 kV
Pulse rise and fall times: < 900 ns
Repetition rate: from 1 Hz to 1 kHz
Pulse width: from 500 ns to DC
Robot for sample replacement
Mecanismos Técnicos y de Laboratorio SL
Collaboration with researchers from the AITANA group at IFIC.
Camera design to deflect the beam. Neptury company
AstroHEP
Slide 4/12

## Slide 7
Slide 5/12
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments
1.1: Irradiation of detectors with accelerators
IP: Javier García López. Univ. de Sevilla.
Goal: Improvement and upgrade of the 3 MV Tandem and cyclotron accelerators at the National Accelerator Center for radiation detector studies.
3 MV Tandem
AstroHEP

## Slide 8
Slide 5/12
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments
1.1: Irradiation of detectors with accelerators
IP: Javier García López. Univ. de Sevilla.
Goal: Improvement and upgrade of the 3 MV Tandem and cyclotron accelerators at the National Accelerator Center for radiation detector studies.
3 MV Tandem
Buncher for ns pulses
of H, D and He beams
Neutron spectroscopy
(See J. Bartolomé talk)
New infrastructures: Sinergy with CERN DRD3 & n-ToF collaborations
AstroHEP

## Slide 9
Slide 5/12
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments
1.1: Irradiation of detectors with accelerators
IP: Javier García López. Univ. de Sevilla.
Goal: Improvement and upgrade of the 3 MV Tandem and cyclotron accelerators at the National Accelerator Center for radiation detector studies.
New infrastructures: Sinergy with CERN DRD3 & n-ToF collaborations
3 MV Tandem
Buncher for ns pulses
of H, D and He beams
Neutron spectroscopy
(See J. Bartolomé talk)
X-ray detector
+ Preamps
Motorized
micrometric slits
Study of semiconductor detectors
(This talk)
AstroHEP

## Slide 10
Slide 6/12
AL 1.1: STUDY OF A NEW TYPE OF 4H-SIC SENSORS FOR NUCLEAR FUSION APPLICATIONS
https://static.wixstatic.com/media/8d3e15_a058e93808bc4c3f8cddbf092298a8aa~mv2.gif
AstroHEP
Ion diagnostics must be resilient enough to operate under the harsh radiation and high temperatures of a fusion reactor.

## Slide 11
Slide 6/12
AL 1.1: STUDY OF A NEW TYPE OF 4H-SIC SENSORS FOR NUCLEAR FUSION APPLICATIONS
  Provided by the IMB-CNM-CSIC group
n+ type 4H-SiC pn junction sensor manufactured at IMB-CNM.
Active area of 3x3 mm2 with ~50 mm active region.
Non-metalized surface, with only a guard ring structure.
Ion diagnostics must be resilient enough to operate under the harsh radiation and high temperatures of a fusion reactor.
AstroHEP

## Slide 12
Slide 6/12
AL 1.1: STUDY OF A NEW TYPE OF 4H-SIC SENSORS FOR NUCLEAR FUSION APPLICATIONS
  Provided by the IMB-CNM-CSIC group
AstroHEP
4H-SiC detectors operate up to 450 ℃ with excellent energy resolution (≲2%) (J. Radiat. Phys. Chem. 2024, 214, 111283).
Ion diagnostics must be resilient enough to operate under the harsh radiation and high temperatures of a fusion reactor.

## Slide 13
Slide 6/12
AL 1.1: STUDY OF A NEW TYPE OF 4H-SIC SENSORS FOR NUCLEAR FUSION APPLICATIONS
  Provided by the IMB-CNM-CSIC group
AstroHEP
Detector radiation hardness was studied at room temperature up to fluences of 5×10¹¹ ions/cm², showing a significant decrease in charge collection with increasing fluence (J. Radiat. Phys. Chem 2020, 177, 190100
Ion diagnostics must be resilient enough to operate under the harsh radiation and high temperatures of a fusion reactor.

## Slide 14
Slide 7/12
ACCELERATORS FOR STUDYING RADIATION INDUCED DEFECTS IN DETECTORS
Nuclear Microprobe line
Tandem room
Focusing the beam down to micrometer dimensions, which enables localized irradiation on small-scale devices.
Controlled beam rate using micrometric slits to avoid additional damage during characterization.
Tunable particle energy within the MeV range (3.5 MeV He++).
New ceramic heater installed, capable of heating samples up to 1200 °C.
The ion beam microprobe linked to a particle accelerator constitutes an powerful tool to characterize radiation detectors.
AstroHEP

## Slide 15
Slide 8/12
PIXE AS AN EFFECTIVE METHOD TO MEASURE ACCUMULATED ION DOSE
AstroHEP
The ceramic heater generates electronic noise, making direct measurement impossible.
An indirect system is used to determine the accumulated fluence during controlled high-temperature damage.

## Slide 16
Slide 8/12
PIXE AS AN EFFECTIVE METHOD TO MEASURE ACCUMULATED ION DOSE
AstroHEP
The ceramic heater generates electronic noise, making direct measurement impossible.
An indirect system is used to determine the accumulated fluence during controlled high-temperature damage.
X-ray detector installed at the ion beam microprobe.
PIXE detects X-rays generated in the SiC detector during alpha particle exposure.
X-ray yield is proportional to ion fluence.
Enables real-time monitoring of delivered fluence.

## Slide 17
Slide 9/12
The scanning system allows controlled damage using the focused ion beam.
Ten 100 × 100 µm² areas with different fluences, first at 400ºC and room temperature.
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP

## Slide 18
Slide 9/12
The scanning system allows controlled damage using the focused ion beam.
Ten 100 × 100 µm² areas with different fluences, first at 400ºC and room temperature.
Post-irradiation analysis via IBIC to assess charge collection efficiency.
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
RT
400
Fluence (ions/cm2) | Fluence (ions/cm2)
1x1011 | 3x1012
3x1011 | 5x1012
5x1011 | 8x1012
8x1011 | 1x1013
1x1012 | Pristine

## Slide 19
Slide 10/12
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
Vbias
Direction of electric field
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
IBIC technique is an analytical tool based on the creation of electrons/holes by ionizing radiation using single ions.
Ions lose their energy dE/dx.
Creation of charge pairs e/h.

## Slide 20
Slide 10/12
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
Vbias
Direction of electric field
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
IBIC technique is an analytical tool based on the creation of electrons/holes by ionizing radiation using single ions.
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
Signal

## Slide 21
Slide 10/12
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
100%
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
IBIC signal.
IBIC technique is an analytical tool based on the creation of electrons/holes by ionizing radiation using single ions.
Vbias
Vout
Direction of electric field
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Signal
N
100%

## Slide 22
Slide 10/12
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
IBIC signal.
100%
N
100%
<100%
Vbias
Vout
Direction of electric field
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Signal
Traps induced by radiation damage
Presence of defects, impurities or recombination centers affect the collection of carriers and hence the current.

## Slide 23
Slide 10/12
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
Presence of defects, impurities or recombination centers affect the collection of carriers and hence the current.
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
IBIC signal.
Traps induced by radiation damage
Synchronization of the scanning system with the DAQ enables the creation of 2D maps, allowing precise localization of the damaged areas.
100%
N
100%
<100%
Vbias
Vout
Direction of electric field
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Signal

## Slide 24
Slide 10/12
RADIATION HARDNESS: ION BEAM–INDUCED DEFECTS AT DIFFERENT TEMPERATURES
AstroHEP
Presence of defects, impurities or recombination centers affect the collection of carriers and hence the current.
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
IBIC signal.
Traps induced by radiation damage
Synchronization of the scanning system with the DAQ enables the creation of 2D maps, allowing precise localization of the damaged areas.
100%
N
100%
<100%
Vbias
Vout
Direction of electric field
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Signal

## Slide 25
Slide 11/12
DAMAGE AT HIGH TEMPERATURE ENHANCES THE RESPONSE OF THE DETECTOR
AstroHEP

## Slide 26
Slide 11/12
DAMAGE AT HIGH TEMPERATURE ENHANCES THE RESPONSE OF THE DETECTOR
AstroHEP
Room temperature

## Slide 27
Slide 11/12
DAMAGE AT HIGH TEMPERATURE ENHANCES THE RESPONSE OF THE DETECTOR
AstroHEP
T=400ºC
Room temperature

## Slide 28
Slide 11/12
DAMAGE AT HIGH TEMPERATURE ENHANCES THE RESPONSE OF THE DETECTOR
AstroHEP
The CCE decreases with fluence, making some damaged regions inaccessible.
The CCE is better preserved at high temperatures due to the dynamic annealing mechanism.
T=400ºC
Room temperature

## Slide 29
Slide 12/12
CONCLUSIONS
AstroHEP
The new infrastructures acquired through Action Plan 1.1 enhance CNA’s capabilities for radiation-detection studies.
A new thermal heater installed at the microprobe helps to investigate detector behavior at high temperatures.
The 4H-SiC CCE decreases with increasing fluence at all temperatures.
Operating the device at high temperatures reduces spectrometric degradation and extends its lifetime.

## Slide 30
ACKNOWLEDGEMENTS
AstroHEP
Activity 1.1: Irradiation of detectors with accelerators. (ASTRO21/1.1/1).
Actuación 1.2 Accelerator Mass Spectrometry. (ASTRO21/1.2/2).
Actuación 1.3 Exploitations of European Infrastructures of Nuclear Physics. (ASTRO21/1.3/3).
Actuación 1.4 Developments for ion beam therapy. (ASTRO21/1.4/4).
Actividades del CNA para los "upgrades" de alta luminosidad de CMS y DRDs del ECFA (PID2023-148418NB-C44).

## Slide 31
Thank you for your attention

## Slide 32
BACKUP
Slide 11/12
AstroHEP

## Slide 33
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments
1.2: Accelerator Mass Spectrometry
IP: José María López Gutiérrez. Univ. de Sevilla.
SARA: Spanish Accelerator for Radionuclide Analysis
Goal: Improvement of the 1 MV Accelerator Mass Spectrometry (AMS) system for astrophysics experiments.
Main action: Installation of a new 120º injector to enhance resolution and consequently reduce measurement background.
Studies to be applied to: Meteorite dating, cosmic rays, nucleosynthesis, isotopic anomalies…
AstroHEP

## Slide 34
Action Line 1: Development of state-of-the-art instrumentation for future Particle and Nuclear Physics experiments
1.3. Exploitations of European Infrastructures of Nuclear Physics
IPs: Carlos Guerrero, J. Gomez-Camacho. Univ. de Sevilla.
Goal: Improvement and upgrade of the 3 MV Tandem and cyclotron accelerators at the National Accelerator Center for radiation detector studies.
Instrumentation
Magnetron Sputtering chamber to produce targets to be used in radioactive beam experiments at CERN-ISOLDE and LNS-Catania
Moderators and shielding to improve the HISPANOS neutrón Beam Line , to complement the measurements done at CERN- nTOF.
AstroHEP

## Slide 35
KEY INFRASTRUCTURE ACQUIRED
The total investment in infrastructure at the CNA has been 1095049.40 €.
Buncher for pulsed
H, D and He beams: 94.000 €
Charge preamplifiers:
34.000 €
Injector for AMS:
430.000 €
magnetrón-sputtering chamber:
128.000 €
Switched HV power supply:
64.000 €
Motorized micrometric slits: 184.000 €
High-resolution X-ray detector: 24.000 €
AstroHEP

## Slide 36
CONCLUSIONS: OBJETIVES OF THE COMPLEMENTARY PLAN AT THE CNA
Add an image
Add an image
Add an image
Add an image
Improvement and upgrade of the 3 MV Tandem and cyclotron accelerators at the National Accelerator Center for radiation detector studies
Accelerator Mass Spectrometry
Exploitation of European infrastructures in nuclear physics
Developments for ion beam therapy
AstroHEP

## Slide 37
Slide 6/12
IMPROVING DETECTOR PERFORMANCE THROUGH DIFFERENT MECHANISMS
AstroHEP
Intrinsic or radiation-induced trapping centers (defects, impurities, …) in the lattice structure can capture free charge carriers, leading to signal degradation.
Lan Luo et al,. Phys. Status Solidi A,2025, 222: 2400840.
Dynamic annealing: defect recombination during irradiation at high temperature that mitigates damage accumulation.
Trap filling: Illumination fills active traps, reducing carrier trapping and improving charge collection.
Photo-detrapping: Illumination with a light source can release trapped carriers by exciting them with photons.