## Slide 1
Nuclear laser spectroscopy
of 229Thorium in CaF2 crystals
Thorsten SCHUMM
TU Wien, Atominstitut
PSAS2026 18.05.2026
Notes: 15 s  0:15

## Slide 2: OUTLINE
The „solid state approach“ to 229Th nuclear spectroscopy
Basic concept and implementation
Nuclear quadrupole structure
Nuclear – solid coupling
Separating nuclear properties and material parameters
JILA experiment
Absolute Mössbauer spectroscopy
Temperature depencence
Towards a solid-state nuclear clock
OKAYAMA experiment
Multiple defect centers
Site-dependent properties
Notes: 40 s  0:55

## Slide 3: …any questions?…any time!
or contact:
thorsten.schumm@tuwien.ac.at
Notes: 85 s  3:30

## Slide 4: Concept: Nuclear laser excitation
10-10 m
eV
0
1.0
discrete energy levels
ground state
excited states
Atomic quantum state manipulation
laser spectroscopy
atomic clocks, quantum sensing
quantum computation, communication
many-body physics (BEC…)
fundamental physics
Notes: 40 s  0:55

## Slide 5: Concept: Nuclear laser excitation
eV
0
1.0
discrete energy levels
ground state
excited states
Atomic quantum state manipulation
laser spectroscopy
atomic clocks, quantum sensing
quantum computation, communication
many-body physics (BEC…)
fundamental physics
MeV
0
1.0
ground state
excited states
10-15 m
Nuclear quantum state manipulation?
laser spectroscopy???
material science
fundamental physics
…
Notes: 40 s  0:55

## Slide 6: Concept: 229Th nuclear laser excitation
10-15 m
229Th isomer state
229Th ground state
M1 transition
E  8 eV (150 nm)   min. – h.
Notes: A valence Neutron!
Possible material for a nuclear clock
Enhanced robustness
40 s  0:55

## Slide 7: Concept: 229Th nuclear laser excitation
10-15 m
229Th isomer state
229Th ground state
M1 transition
E  8 eV (150 nm)   min. – h.
laser excitation???
Notes: 40 s  0:55

## Slide 8: Concept: 229Th nuclear laser excitation in CaF2
10-15 m
229Th isomer state
229Th ground state
M1 transition
E  8 eV (150 nm)   min. – h.
laser excitation???
The „solid state approach“:
Th nuclei inside VUV transparent material
large band (~10 eV) gap  fluoride crystals
doping, implantation, diffusion…
control of electronic environment: [Rn]
a solid-state optical nuclear clock?
Notes: 40 s  0:55

## Slide 9: Fabrication of Th:CaF2 in Vienna
> 10 years of painful method development…
dedicated lab for growth of radioactive dopants (only one in Europe)
miniaturized crystal growth to increase doping concentration
fluorine annealing to reduce defects
in-house cutting + polishing
characterization (optical, radiological)
1 crystal (attempt) takes 5 days
currently working on:
pulling single crystal fibers
growing bulk ThF4 crystals
Notes: 40 s  0:55

## Slide 10: Fabrication of Th:CaF2 in Vienna
X2: cm-3
19 May 2021
C13: cm-3
7 Dec 2020
C10: cm-3
23 Nov 2020
3 crystals from Vienna with different „history“ and concentration
…will be used in ALL experiments shown today
* apart from the UCLA experiment on slide 4
3 mm
1 mm
Notes: 40 s  0:55

## Slide 11: Simulation of Th:CaF2 in Vienna
CaF2 crystal structure
put 229Th here!
Th4+ replaces Ca2+
low doping limit >0.1% (no interactions between Th?)
Ionic crystal  2+ charge compensation ([Rn] config.)
  2 extra (interstitial) fluorines (several spatial arrangements)
  1 Ca vacancy (nearest neighbor)
  …?
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
Ca
Ca
Ca
Th
Th
F
F
e-
e-
Notes: 40 s  0:55

## Slide 12: Simulation of Th:CaF2 in Vienna
CaF2 crystal structure
put 229Th here!
Th4+ replaces Ca2+
low doping limit >0.1% (no interactions between Th?)
Ionic crystal  2+ charge compensation ([Rn] config.)
  2 extra (interstitial) fluorines (several spatial arrangements)
  1 Ca vacancy (nearest neighbor)
  …?
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
F
Ca
Ca
Ca
Th
Th
F
F
e-
e-
pristine CaF2
Ca vacancy
2F interstitials
2F interstitials
Vienna is the „Mekka“ of density functional theory…
Notes: 40 s  0:55

## Slide 13: First laser excitation of 229Th in 2024
PTB Experiment
Notes: 40 s  0:55

## Slide 14: First laser excitation of 229Th in 2024
PTB Experiment
Notes: 40 s  0:55

## Slide 15: First laser excitation of 229Th in 2024
PTB Experiment
scanning for almost a year…
Notes: 40 s  0:55

## Slide 16: First laser excitation of 229Th in 2024
PTB Experiment
= 2020.409(7) THz
670(102) s (in crystal)
laser linewidth limited
Notes: 40 s  0:55

## Slide 17: First laser excitation of 229Th in 2024
PTB Experiment
UCLA Experiment
Host: CaF2
Host: LiSrAlF6
Notes: 40 s  0:55

## Slide 18: First laser excitation of 229Th in 2024
PTB Experiment
UCLA Experiment
Host: CaF2
Host: LiSrAlF6
Isomer energy:
8.338(24) eV or 148.71(42) nm
Isomer lifetime:
670(102) s (in crystal)
Isomer energy:
148.38219(4)stat (20)sys nm
Isomer lifetime:
568(13)stat (20)sys s (in crystal)
April 2024
July 2024
Notes: 40 s  0:55

## Slide 19: …any questions?…any time!
or contact:
thorsten.schumm@tuwien.ac.at
Notes: 85 s  3:30

## Slide 20: OUTLINE
The „solid state approach“ to 229Th nuclear spectroscopy
Basic concept and implementation
Nuclear quadrupole structure
Nuclear – solid coupling
Separating nuclear properties and material parameters
JILA experiment
Absolute Mössbauer spectroscopy
Temperature depencence
Towards a solid-state nuclear clock
OKAYAMA experiment
Multiple defect centers
Site-dependent properties
Notes: 40 s  0:55

## Slide 21: Nuclear quadrupole structure in 229Th:CaF2
229Th isomer state
229Th ground state
M1 transition
E  8 eV   min. – h.
What about interactions between crystal and nuclear levels?
????
Notes: 40 s  0:55

## Slide 22: Nuclear quadrupole structure in 229Th:CaF2
Quadrupole structure determined by nuclear and material parameters
Q – (intrinsic) quadrupole moment
Vzz – electric field gradient (EFG)
– anisotropie parameter
„universal“
host-specific
Notes: 40 s  0:55

## Slide 23: Nuclear quadrupole structure in 229Th:CaF2
Quadrupole structure determined by nuclear and material parameters
Q – (intrinsic) quadrupole moment
Vzz – electric field gradient (EFG)
– anisotropie parameter
„universal“
host-specific
can we see these quadrupole levels…?
Notes: 40 s  0:55

## Slide 24: OUTLINE
The „solid state approach“ to a Th-229 nuclear clock
Basic concept and implementation
Nuclear quadrupole structure
Nuclear – solid coupling
Separating nuclear properties and material parameters
JILA experiment
Absolute Mössbauer spectroscopy
Temperature depencence
The EFG “mystery“
OKAYAMA experiment
Multiple defect centers
Site-dependent properties
Notes: 40 s  0:55

## Slide 25: VUV frequency comb precision spectroscopy
4 strong, 2 weak lines observed
absolute frequency determination with reference to Sr clock
JILA experiment
Notes: 40 s  0:55

## Slide 26: VUV frequency comb precision spectroscopy
JILA experiment vs. PTB/UCLA
PTB/TUW spectra
~ 7 GHz
JILA lines
covering 400 MHz
individual lines ~ 30 kHz
accuracy ~1 kHz
= 2 020 407 384 335(2) kHz
Notes: 40 s  0:55

## Slide 27: VUV frequency comb precision spectroscopy
JILA experiment vs. PTB/UCLA
PTB/TUW spectra
~ 7 GHz
JILA lines
covering 400 MHz
individual lines ~ 30 kHz
accuracy ~1 kHz
September 2024
same crystals X2 and C10 used at PTB and JILA
= 2 020 407 384 335(2) kHz
Notes: 40 s  0:55

## Slide 28: Nuclear quadrupole structure in 229Th:CaF2
4 strong + 1 additional line observed  asignement to nuclear quadrupole structure
absolute frequency determination
(let‘s not totally forget about the 2 weak lines)
JILA experiment
Notes: 40 s  0:55

## Slide 29: Nuclear quadrupole structure in 229Th:CaF2
4 strong + 1 additional line observed  asignement to nuclear quadrupole structure
absolute frequency determination
(let‘s not totally forget about the 2 weak lines)
JILA experiment
„traditional“ Mössbauer spectroscopy
Notes: 40 s  0:55

## Slide 30: Nuclear quadrupole structure in 229Th:CaF2
4 strong + 1 additional line observed  asignement to nuclear quadrupole structure
absolute frequency determination
(let‘s not totally forget about the 2 weak lines)
JILA experiment
„traditional“ Mössbauer spectroscopy
VUV laser
Notes: 40 s  0:55

## Slide 31: Nuclear quadrupole structure in 229Th:CaF2
Quadrupole structure determined by nuclear and material parameters
Q – (intrinsic) quadrupole moment
Vzz – electric field gradient (EFG)
– anisotropie parameter
change in quadrupole moment…
„universal“
host-specific
= 1.791(2)%
Notes: 40 s  0:55

## Slide 32: Nuclear quadrupole structure in 229Th:CaF2
Quadrupole structure determined by nuclear and material parameters
Q – (intrinsic) quadrupole moment
Vzz – electric field gradient (EFG)
– anisotropie parameter
change in quadrupole moment…
„universal“
host-specific
= 1.791(2)%
Notes: 40 s  0:55

## Slide 33: Nuclear quadrupole structure in 229Th:CaF2
Quadrupole structure determined by nuclear and material parameters
Q – (intrinsic) quadrupole moment
Vzz – electric field gradient (EFG)
– anisotropie parameter
change in quadrupole moment…
Extracted electrical field gradient (EFG)
„universal“
host-specific
= 1.791(2)%
= 109.1(7) V/
= 0.59163(5)
extremely well reproduced over 3 different crystals
Notes: 40 s  0:55

## Slide 34: Temperature dependence of spectroscopy lines
tracing 4 strongest lines over temperature
JILA experiment
EFG and eta parameter „well behaved“
compatible with thermal expansion
interesting cancellellation in (B) transition (clock?)
strong eta indicates breaking of lattice symmetry
transitions now clearly depend on
host material and temperature (CaF2, LiSaF6…)
Notes: 40 s  0:55

## Slide 35: Temperature dependence of spectroscopy lines
tracing 4 strongest lines over temperature
JILA experiment
EFG and eta parameter „well behaved“
compatible with thermal expansion
interesting cancellellation in (B) transition (clock?)
strong eta indicated breaking of lattice symmetry
transitions clearly depend on
host material and temperature
Notes: 40 s  0:55

## Slide 36: Towards a 229Th:CaF2 solid-state nuclear clock
JILA experiment
(B) transition
(C) transition
vanishing T dependence
line for thermometry
transition frequencies consistent within ~kHz over different crystals
linewidth 10-100 kHz, scaling with concentration („micro-strain“)
Continuous interrogation at fixed T (over 1 year) within 1 kHz
Notes: 40 s  0:55

## Slide 37: Towards a 229Th:CaF2 solid-state nuclear clock
JILA experiment
(B) transition
(C) transition
vanishing T dependence
line for thermometry
transition frequencies consistent within ~kHz over different crystals
linewidth 10-100 kHz, scaling with concentration („micro-strain“)
Continuous interrogation at fixed T (over 1 year) within 1 kHz
Notes: 40 s  0:55

## Slide 38: …any questions?…any time!
or contact:
thorsten.schumm@tuwien.ac.at
Notes: 85 s  3:30

## Slide 39: OUTLINE
The „solid state approach“ to a Th-229 nuclear clock
Basic concept and implementation
Nuclear quadrupole structure
Nuclear – solid coupling
Separating nuclear properties and material parameters
JILA experiment
Absolute Mössbauer spectroscopy
Temperature depencence
Towards a solid-state nuclear clock
OKAYAMA experiment
Multiple defect centers
Site-dependent properties
Notes: 40 s  0:55

## Slide 40: Multiple doping sites in a single crystal
Okayama experiment
4-wave mixing laser similar to PTB/UCLA
linewidth 30 MHz  resolve Q-structure
factor 50 higher excitation rate than JILA
detection system taken from SPring-8
3 crystals from Vienna (always the same)
Notes: 40 s  0:55

## Slide 41: Multiple doping sites in a single crystal
Okayama experiment
at least 4 different Th sites identified in all 3 crystals
one of them is „JILA site“ (site 2)
missing 6th line of „JILA site“ observed
Relative occurences of sites changes with concentration
?
?
Notes: 40 s  0:55

## Slide 42: Multiple doping sites in a single crystal
Okayama experiment
JILA site
0 EFG!
tentative assignement: single Th and 2Th cluster without local charge compensation
Notes: 40 s  0:55

## Slide 43: Multiple doping sites in a single crystal
Okayama experiment
JILA site
0 EFG!
>90%
Notes: 40 s  0:55

## Slide 44: Multiple doping sites in a single crystal
Okayama experiment
JILA site
0 EFG!
>90%
selective laser excitation of nuclei in specific sites in the crystal “…beyond Mössbauer“
Notes: 40 s  0:55

## Slide 45: Multiple doping sites in a single crystal
Okayama experiment
isomer lifetime DOES NOT seem to depend (much) on Th doping site
(all measurements at room temperature)
Notes: 40 s  0:55

## Slide 46: Multiple doping sites in a single crystal
Okayama experiment
isomer lifetime DOES NOT seem to depend (much) on Th doping site
(all measurements at room temperature)
isomer laser quenching DOES depend on Th doping site
(all measurements at room temperature)
405 nm CW 10 mW quenching laser
Notes: 40 s  0:55

## Slide 47: Multiple doping sites in a single crystal
Okayama experiment
isomer lifetime DOES NOT seem to depend (much) on Th doping site
(all measurements at room temperature)
isomer laser quenchin DOES depend on Th doping site
(all measurements at room temperature)
405 nm CW 10 mW quenching laser
arXiv:2509.00041v1
Notes: 40 s  0:55

## Slide 48: …any questions?…last Chance!
or contact:
thorsten.schumm@tuwien.ac.at
Notes: 85 s  3:30

## Slide 49: Credits (most probably incomplete, I apologize!)
JILA measurements
C. Zhang, T. Ooi, J. Doyle, J. Higgins, J. Ye JILA
K. Beeks, F. Schaden, A. Leitner, T. Sikorsky, G. Kazakov, T. S. TU Wien
PTB measurements
J. Tidau, J. Thielking, G. Zitzer K. Zhang, M. Okhapkin, E. Peik PTB Braunschweig
F. Schaden, K. Beeks, T. Pronebner, I. Morawetz, T. Sikorsky, T. S. TU Wien
ISOLDE-CERN measurements
S. Kraemer, J. Moens, S. Bara, P. Chhetri, A. Claessens, T. Cocolios, KU Leuven
S. Geldhof, L. Pareire, S. Sels, A. Vantomme, M. Verlinde, P.v. Duppen
M. Athanasakis-Kaklamanakis, K. Chrysalidis, R. Henke CERN
K. Beeks, N. Hosseini, T. S. TU Wien
SPring-8/Okayama measurements
T. Masuda, A. Yoshimi, A. Fujieda, H. Hara, T. Hiraki, H. Kaino, Y. Miyamoto, Okayama University
K. Okai, S. Okubo, N. Sasao, S. Uetake, M. Yoshimura, K. Yoshimura, K. Suzuki
H. Fujimoto, T. Watanabe AIST Tsukuba
H. Haba, A. Yamaguchi, T. Yokokita, K. Tamasaku RIKEN
Y Kasamatsu, Y. Yasuda, Y. Shigekawa Osaka University
S. Kitao, M. Seto Kyoto University
K. Konashi, M. Watanabe Institute f. Material res. Tohoku
S. Stellmer, K. Beeks, F. Schaden, T. Sikorsky, T. S. TU Wien
Notes: 40 s  0:55

## Slide 50: THE END
Notes: 40 s  0:55