## Slide 1: Characterization of WBS using TPA-TCT Methodology and Experimental Applications on SiC samples
Jordi Duarte Campderrós¹
Marcos Fernández García²
Raúl Montero Santos⁴
Cristian Quintana San Emeterio²
Diego Rosich Velarde²
Iván Vila Álvarez³
¹ IFCA (UC-CSIC), ² Universidad de Cantabria and CSIC (ES), ³ Instituto de Física de Cantabria (CSIC-UC), ⁴ UPV

## Slide 2: Outline
Introducing TPA-TCT
Basic and advanced studies
Beyond the technique
Examples on WBS (SiC)

## Slide 3: Two Photon Absorption (TPA)
Strategies to maximize TPA gen:

## Slide 4: Transient Current Technique (TCT)
Signal generation:
DUTs:
Electric field
Weighting field
3D (25x100 um)
Bias tee:
DUT
SCOPE
BIAS

## Slide 5: TPA-TCT setup for SiC at SGIker facility (UPV)

## Slide 6: TPA-TCT setup for SiC at SGIker facility (UPV)

## Slide 7: TPA-TCT basic studies
Zscan signals
charge
profiles

## Slide 8: TPA-TCT derived studies
Determinación de las transiciones
Determinación indirecta de la capacidad vs bias
Estudio del vaciado y volumen activo
Estimación del dopado efectivo

## Slide 9: But there are more...
S. Pape: Techniques for the Investigation of Segmented Sensors Using the TPA-TCT
C. Quintana: Radiation hardness and radiation-induced charge multiplication in neutron-irradiated SiC p-in-n diodes characterized by TPA-TCT
WPC
WPC
TOT
1/TOT
Electric field estimation:
More complex structures:
Hexagonal 3D pixel
SiC LGAD
Clara Lasaosa PhD Thesis

## Slide 10: Beyond TPA-TCT
3PA excitation and more...
"Hibrid" experiments
Similar profiles
Less SPA
Better "practical"
resolution
Slope = 3 -> 3PA

## Slide 11: SiC samples – Fresh vs Irradiated detectors
Sample 1MW2 - non-irradiated​
Sample F2W1 – 1015 neq/cm2
Irradiated samples show a decrease in the maximum and integrated amount of collected charge
There is no saturation effect in the irradiated samples, they recover more signal as bias voltage is increased
Important leakage current increase, not only after irradiation but during operation in both!

## Slide 12: SiC samples – Forward bias and multiplication
WFs
Charge
Comparison Irradiated vs Fresh samples
Reference
Reverse
Forward
Multiplication

## Slide 13: Conclusions
Positive points​
High experimental versatility​
Large variety of achievable studies​
High-resolution 3D sampling with strong spatial selectivity​
Non-destructive access to the device bulk​ ​
Negative points​
Optical aberrations at high numerical apertures​
Strong sensitivity to the optical pulse structure​
Sensitivity to beam clipping

## Slide 14: ¡Gracias por vuestra atención!