## Slide 1: Ultra-pure electroforming at Boulby deep underground laboratory
K. Johnson, P. Knights, K. Nikolopoulos, G. Rogers, P. Scovell,
E. Shoemark-Banks, D. Spathara, P. Walters
IOP Joint APP and HEPP Conference – Edinburgh
09/04/2026

## Slide 2
Direct dark matter detection landscape

## Slide 3
Direct dark matter detection landscape
Increase exposure
Lower backgrounds

## Slide 4: Setup
Copper as a detector material
Copper is an attractive detector material for rare event searches
  No long-lived radio-isotopes – longest 67Cu: t1/2 = 62 h
  Commercially available at high-purity
  Good mechanical and electrical properties
  Favorable electrochemical properties – more on this later!
CUORE collaboration
https://cuoreexperiment.org
NEWS-G collaboration
https://www.snolab.ca/experiment/news-g/

## Slide 5: Setup
Copper background
Copper can still represent an important background
Commercial copper contaminated - 238U and 232Th decay chains:
  Natural ore contamination
  Implanted during manufacture and handling
  Cosmogenic activation - 63Cu(n,⍺)60Co t1/2 = 5.27 yr
Simulated backgrounds for NEWS-G’s current detector
238U decay chain

## Slide 6: Setup
Electrodeposition
Deposit ions onto a cathode by applying a voltage
Governed by oxidation and reduction reactions
Deposited mass proportional to current
Molar mass
Current
No. e-
Faraday constant
Ion

## Slide 7
Species plating tendency governed by reduction potentials
Careful control of applied potential difference allows preferential plating of copper over contaminants
Used in industry to produce copper with excellent purity
Copper electrodeposition
I

## Slide 8
Ultra-pure copper electrodeposition
How this differs from industry – prioritise purity
Cu feedstock preparation
Procedure principally developed by PNNL for Majorana Demonstrator
Additive free electrolyte
Prioritise purity over speed -> careful voltage selection
Cleanroom environment
Stringent radiopure material and reagent selection
Purity monitoring
Comprehensive cleaning procedures
Plating underground -> reduce cosmogenic activation
NIMA 579 (2007) 486-489
RCTR 277 (2008) 103-110

## Slide 9
Results – ICPMS
Sample of copper | 232Th [uBq/kg] | 238U [uBq/kg]
Commercial C10100 | 8.7 ± 1.6 | 27.9 ± 1.9
NEWS-G plated copper NIMA 988 (2021) 164844 | <0.24 | <0.11
Majorana demonstrator electroformed NIMA 828 (2016) 22-36 | <0.119 | <0.099
Orders of magnitude improvement over commercial copper
Purity results often limited by available assay techniques -> can only set limits

## Slide 10
How this is/can be used for experiments
Electroplating
Electroforming
Cu plated onto existing structure or components
Acts as an ultra-pure shield
Reduce radon emanation
Cu plated onto a mould (called mandrel)
Remove the mandrel leaving a pure copper structure
Construct large structures
NEWS-G electroplated Cu
NIMA 988 (2021) 164844
Majorana Demonstrator
Electroformed Cu
OSTI (2012) 1039850

## Slide 11: Setup
Electroforming facility at Boulby
1.1km underground at the UK’s deep underground laboratory Boulby
Dedicated ISO-6 cleanroom within the larger Boulby cleanroom
XIA UltraLow-1800 + ICP-MS on site at Boulby
Boulby underground lab
https://www.boulby.stfc.ac.uk/Pages/home.aspx
Front. Phys. 2023 11:1310146
JINST 2025 20 P06010
See posters by B. Green and K. Johnson
And talks by A. Hamer and P. Scovell

## Slide 12
Recirculating filters
Steel cylindrical mandrel
5.5N Cu feedstock
Cu bus bar
Inlets
CuSO4 electrolyte
Electroforming bath at Boulby
Ti anodes
Small setup used to plate smaller components
Larger setup’s first goal to electroform a 30 cm spherical proportional counter: DarkSPHERE-30
Electroforming facility at Boulby
Near-future plans

## Slide 13: Setup
Copper plated onto stainless steel cylinder
Peeled copper off mandrel -> ICPMS and XIA results pending analysis
Can use flattened copper from cylindrical mandrel as tray for XIA
Current status

## Slide 14
Phys. Rev. D 108, 112006
O(
)
Physics Potential
Fully electroformed spherical proportional counters will have world leading sensitivity to low-mass dark matter
DarkSPHERE-30 to begin construction
Alloys being explored to improve the properties of electroformed copper – PureAlloys project
  NIMA 1082 (2026) 170970
  Communications Physics (2025) 8 464
L. Milligan’s and P. Walters’ talks

## Slide 15
Summary
Copper electroforming for radio-pure detectors
Orders of magnitude improvement in radiopurity over commercial Cu
Electroforming facility constructed at Boulby
First copper produced
Work ongoing to electroform a ⌀30 cm SPC
Many experiments exploring the use of electroformed and plated Cu