## Slide 1: Nottingham – Glasgow Optical Work on Alumina Coatings
15th January 2026
Scott Fitzgerald
On behalf of the Glasgow coatings group

## Slide 2: Introduction – Why is alumina interesting?
To improve the sensitivity of gravitational wave detectors, future test-mass coatings require reduced thermal noise.
Mirror coatings have alternating layers of materials with low and high refractive indices.
Silica (SiO2) is often used as a low-index layer but is unsuitable for use in cryogenic detectors because of a mechanical loss peak at 20K.
Al2O3 is interesting for cryogenic detectors to replace SiO2 as a low-index partner material for coating stacks.
1
Previously investigated by R. Robie, M. Abernathy, S. Penn, D. Crooks et al, I. Pinto, J. Franc et al, M. Molina-Ruiz and others.

## Slide 3: Optical investigations of Al2O3
Photothermal common-path interferometry (PCI) used to measure absorption.
Works by measuring the effect of a thermal lens generated by a pump beam on a crossing probe beam.
More absorption = stronger thermal lens, so more measured effect.
Effect of heat-treatment on absorption of Al2O3 deposited by Reactive Low Voltage Ion Plating measured at 1064nm and 1550nm.
Heat treatment is usually used to improve optical absorption and reduce the loss of coating materials.
2

## Slide 4
Al2O3 absorption measurements
1064 nm measurements: as deposited mean absorption of ~5ppm, drops to ~0.2ppm after 500°C HT.
1550 nm measurements: as deposited mean absorption of ~4.2ppm, drops to ~1.7ppm after 550°C HT.
ppm = parts per million 1ppm = 0.0001%
Al2O3 A2 slice ADP Absorption Measurement - 1064nm
Al2O3 A2 slice 500°C Absorption Measurement - 1064nm
Measurements by S. Fitzgerald and G. McGhee
3

## Slide 5
κ is a measure of thickness-independent absorption.
Order of magnitude variation between IBS and RLVIP Al2O3.
Order of magnitude variation between 1064 nm and 1550 nm.
RLVIP Al2O3 has comparable κ to aLIGO coatings at 1064 nm.
4

## Slide 6: Summary
RLVIP Al2O3 coating investigated at 1064nm and 1550nm.
Heat treated to 400°C, 500°C, 550°C, 600°C and 800°C.
Sub-0.2 ppm absorption minimum for 1064nm at 500°C (500nm coating) for RLVIP deposition.
Order of magnitude improvement in absorption vs IBS Al2O3.
Ongoing Work
Investigating heat treatment time vs absorption.
Modelling for possible stack designs.
5

## Slide 7: Thank you! Any questions?
s.fitzgerald@research.gla.ac.uk