## Slide 1
Machine Learning-Driven Design of High-Performance X-Ray and Gamma-Ray Detectors
Dr. Murat Aydemir
Erzurum Technical University, Turkey
Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026)
24-26/03/2026, Palermo

## Slide 2
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
Our Research Activities
Integrated Detector Materials Research
Synthesis • Characterization • Device • Data
Functional Materials
Organic emitters
Inorganic scintillators
Hybrid systems
Radiation & Detector Materials
X-ray / gamma-ray response
Scintillation efficiency
Stability and hardness
Characterization & Photophysics
Time-resolved spectroscopy
Energy-transfer analysis
Structure-property links
Machine Learning & Data Science
Descriptor engineering
Predictive modelling
Data-guided screening
Integrated workflow: materials design, photophysical understanding, detector relevance, and ML-guided decision-making

## Slide 3
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
Collaborating with CERN-DRD5
Our Strengths
Materials synthesis
Photophysics & spectroscopy
Detector materials
Machine learning
Interdisciplinary expertise ranging chemistry, physics, engineering, and data-driven analysis
Natural bridge
CERN DRD5 Focus
Quantum sensing R&D
advanced detector concepts for high-energy physics
WP2: QDs & chromatic calorimetry
wavelength-engineered materials and layered detector ideas
Our contribution
materials selection, characterization, and ML-guided design insight
Objective: to contribute materials expertise and data-driven design guidance for next-generation radiation detectors
Natural bridge
Natural bridge
Natural bridge

## Slide 4
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
What Materials Are We Working On?
Materials
portfolio
organic - inorganic - nanoscale - hybrid
Inorganic scintillators
high-density stopping power and mature detector use
- GAGG, LYSO, BGO, PbWO4 and PbF2
- light yield, fast timing, and radiation robustness
Organic scintillators and polymers
lightweight systems with fast response and design flexibility
- plastic scintillators and molecular emitters
- rapid response and scalable processing routes
Quantum dots and nanocrystals
spectral tunability for wavelength-engineered detector concepts
- perovskite and semiconductor nanocrystals
- emission tuning and chromatic readout potential
Hybrid and multilayer architectures
materials integration instead of single-phase optimization
- crystal + polymer + quantum-dot combinations
- optical coupling and layered detector design
Key message: we are exploring a heterogeneous detector-materials space where performance depends on both material class and device architecture.

## Slide 5
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
Size-Dependent Emission
Quantum confinement tunes emission across the visible range.
Large
Small
QD diameter
Emission λ
larger QD -> red-shifted
smaller QD -> blue-shifted
Electronic Structure
Discrete energy levels emerge as QD size decreases.
Energy
Eg
Large QD
Medium
Small QD
Smaller QDs exhibit a larger effective band gap, enabling tunable optical response.
Detector-Relevant Advantages
Key QD properties relevant to detector design.
Tunable λ
Emission can be matched to SiPM/PMT response.
Narrow FWHM
~20 nm bandwidth supports chromatic separation.
Fast τ
Sub-ns response supports fast timing concepts.
Radiation robust
Robustness supports detector use.
Why They Matter for DRD5
wavelength-shifting layers for chromatic Calorimeter (CCAL)
hybrid integration with crystals and polymers
spectral separation in single-readout schemes
Eg
Eg
Quantum Dots as Tunable Detector Materials for HEP
For detector applications, this gives several advantages: tunable emission that can be matched to SiPM or PMT sensitivity windows, narrow emission bandwidth that can support chromatic separation, and fast optical response that is relevant for timing.

## Slide 6
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
QD Structures and Integration Pathways
Detector integration architectures
For CCAL-like concepts, QDs can be integrated directly into absorbers or through QD-doped polymer layers.
Option 2
QD-doped polymer layers interleaved with crystals
Scientific meaning
architecture matters as much as chemistry
7
The development of CCAL relies on organic or inorganic quantum dot–based scintillator materials
Direct incorporation of QDs into scintillating host
Hybrid approach: QD-doped polymer layers interleaved with other detector materials
Option 1
Direct QD incorporation into dense crystals
QD performance cannot be discussed in isolation from the host matrix, interface quality, and optical coupling. This is exactly the kind of coupled design problem where descriptor-based analysis becomes useful
These architectures can give the QDs different roles: direct emission, wavelength shifting, or participation in a chromatic calorimeter stack.

## Slide 7
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
Why polymer
nanocomposites?
Tunable narrow-band emission
Scalable PS/PU host matrices
Fast timing under X-ray excitation
Representative materials path
QD
PS / PU
CCAL
layer
Key detector message
Processable polymer hosts enable wavelength-engineered scintillator slabs for detector integration.
Emission tunability
Fabrication and macroscopic samples
QD-loaded polymer bodies and representative scintillating blocks.
Fast scintillation kinetics
CsPbBr3 40% in polystyrene shows a sub-ns fast component.
Beam-test relevance
Nanocomposite module placement in CERN-oriented hardware tests.
Observed: narrow-band emission • bright X-ray response • ultrafast decay channel
Polymer Nanocomposite Scintillators
The example shown here highlights that QD-loaded polymer systems can produce bright X-ray response and sub-nanosecond fast components, which makes them promising for spectrally selective and timing-sensitive detector concepts.

## Slide 8
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
CCAL systems
86% “chromatic” electron - pion discrimination
Longitudinal shower profiling
Particle identification
Chromatic energy measurement
Key advantages (beyond classical calorimetry):
Nanocomposites can primarily be used as tunable wavelength shifters (WLS).
The structure is longitudinally segmented; each layer has a specific emission wavelength and absorption band.
Single readout with spectral information.
Unidirectional spectral transparency.
Longitudinal segmentation can be as thin as the material itself; 20 nm QDs with narrow-band emission enable many layers.
Target: longitudinal tomography of the shower profile.

## Slide 9
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
CERN Beam Tests 2023-baseline prototype / proof that CCAL is experimentally real

## Slide 10
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
CERN Beam Tests 2025-Multilayer / filtered / improved architecture
A three-layer prototype was constructed using standard materials emitting in different wavelength ranges.
Crystal scintillator: GAGG
Plastic scintillators: EJ-262 and EJ-228
PbF₂ was used as a dense, transparent absorber producing Cherenkov radiation only (no scintillation)
Long-pass filters were employed to minimize the effect of back-propagating photons, (i.e., photons emitted backward from one scintillator that could excite a preceding scintillator)
A copper absorber with a length of n×​ was used as a preshower, with n = 1, 3, 9.9
The final detector response depends simultaneously on emission wavelength, filtering strategy, absorber role, optical transport, and stack order. So even before introducing ML, the physics already tells us that this is a high-dimensional design space

## Slide 11
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
CERN Beam Tests 2025-QD/polymer nanocomposites
J. Králet al 2025 J. Phys. Mater. 8 015007
Nanocomposites were prepared by embedding quantum dots (semiconductor nanocrystals) into a transparent host matrix.
They exhibit:
narrow-band emission
tunable emission wavelengths
fast timing response
Two cesium lead halide nanocrystal systems were investigated:
CsPbBr₃ (CPB)
CsPbBrCl-based nanocrystals (CPBC)
For sample fabrication, the nanocrystals were dispersed in two organic polymer matrices:
polystyrene (PS) and polyurethane (PU)
Final sample size: 2 × 2 × 3 cm³

## Slide 12
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
Open Design Problem
Detector performance
Material variables
composition - density - defects
Architecture variables
multilayers - interfaces - thickness
Optical / timing variables
emission - timing - readout matching
Irradiation / test-condition variables
beam energy - dose - filtering - stability
Detector performance emerges from coupled material-architecture interactions, making one-variable-at-a-time optimization insufficient.

## Slide 13
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
Why Machine Learning Now?
Experimental design space
Many variables must be chosen simultaneously:
Material family
QD composition
Host polymer
Crystal absorber
Layer thickness
Optical coupling
Readout type
Filter choice
Beam condition
Result: the search space grows combinatorially, while experiments remain slow and expensive.
too many
combinations
Need for
ML guidance
What ML can do for us
Machine learning does not replace detector physics; it reveals structure in a high-dimensional materials dataset.
Pattern discovery
Identify clusters, correlations, and hidden structure across material classes.
Ranking & selection
Prioritize promising material–architecture combinations before exhaustive testing.
Interpretability
Estimate which descriptors drive timing, emission, and detector response.
Planned ML workflow
Experiments
Descriptors
Models
Insights
How can we reduce the experimental search space without losing physical meaning?
Next
experiments

## Slide 14
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
Machine Learning Workflow
Experiments
materials, devices,
beam-test observations
Descriptor
space
composition, host,
optical and device variables
Unsupervised
mapping
PCA, clustering,
latent structure
Candidate
ranking
promising material–
architecture combinations
Design
insight
physically meaningful
selection rules
Experimental design space
• Material family
• QD composition and size
• Host polymer / crystal absorber
• Layer thickness and coupling
• Filter and readout configuration
Challenge: the number of possible experiments grows combinatorially.
What the ML stage delivers
• cluster structure across material classes
• descriptor-level interpretation
• reduced search space for experiments
• ranked candidates for detector testing
Machine learning supports selection; it does not replace physical interpretation.
Core logic
High-dimensional detector materials data
→ structured descriptor space
→ interpretable screening and prioritization
The key point is that the output is not a black-box score alone. The output is a physically interpretable reduction of the detector design space, which can then guide the next experimental campaign.

## Slide 15
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
Descriptor Space Used for ML
Optical / Scintillation
Emission peak (λem) and spectral width (FWHM)
Light yield / photon output
Absorption–emission overlap and WLS compatibility
Timing / Kinetics
Rise time, decay time, fast/slow components
Prompt fraction and timing response
Energy-transfer and recombination dynamics
Materials / Architecture
Density, Zeff, refractive-index contrast
Layer sequence, thickness, loading fraction
Host matrix, crystal/QD/polymer integration route
Experimental / Detector Context
Beam energy • particle type • readout channel • filter set • geometry • irradiation conditions
Curated Descriptor Matrix
Materials
×
Descriptors
Standardized, comparable, physics-aware inputs
ML Tasks and Scientific Outputs
Dimensionality reduction
PCA / UMAP mapping of the material landscape
Grouping / similarity
Clustering of scintillator families and architectures
Prediction
Response ranking, discrimination potential, candidate prioritization
Interpretation
Feature importance and physically meaningful design rules
Key message: the descriptor space must encode both intrinsic material physics and detector-level integration variables to enable interpretable ML-guided screening.

## Slide 16
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
7
PCA Mapping of the Materials Space
Physical interpretation of PCA axes
PC1: captures a stopping-power / architecture gradient driven by density, thickness and high-Z content.
PC2: captures a timing / spectral gradient governed by decay time, emission wavelength and QD/WLS loading.
Cluster-level meaning
high-Z inorganic scintillators separate toward the density / thickness quadrant
organic/plastic scintillators occupy a timing-dominated region
polymer/QD composites populate an intermediate, tunable design regime
Illustrative scientific takeaway
The first two principal components recover a physically interpretable separation between inorganic scintillators, organic/plastic scintillators, and polymer/QD composites, suggesting that descriptor compression can preserve meaningful materials-domain structure before supervised ML.

## Slide 17
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
Cluster Signatures and Physical Regimes
Standardized
descriptor matrix
PCA-reduced
latent space
Cluster
assignment
Centroid /
signature analysis
Physical
interpretation
Methodological strength
Clustering is scientifically useful only if the resulting groups are:
internally coherent
externally separated
physically interpretable
stable under descriptor selection
Illustrative validation result
k = 4 clusters gives a robust separation between high-Z, polymer/QD, organic/plastic, and transition regimes.
Cluster-centroid heatmap (illustrative z-scored descriptor levels)
Density /
Zeff
Emission
window
Timing
response
QD / WLS
loading
Architecture
complexity
A
High-Z
B
Polymer-QD
C
Organic/plastic
D
Transition
high
low
low
low
low
low
high
high
high
mid
low
mid
high
low
low
low
mid
mid
mid
high
Descriptor enrichment across cluster centroids
low
high
Scientific interpretation
Cluster A is absorber-driven: density and stopping descriptors dominate.
Cluster B is QD/polymer-driven: timing, emission tuning, and loading are enriched.
Cluster C reflects fast but simpler organic/plastic systems.
Cluster D is a transition regime with high architecture complexity.
Result
Clustering suggests that physically interpretable groups exist before supervised ML, supporting downstream candidate ranking.

## Slide 18
7
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
Multi-objective Candidate Selection for Next-Generation Detector Materials
Physics-guided ranking framework
Input descriptor groups
Timing / kinetics
rise time, decay, prompt fraction
Spectral behavior
emission band, overlap, WLS compatibility
Absorber relevance
density, high-Z compatibility, stack role
Stability metrics
radiation hardness, processability, robustness
Illustrative score
Score = w₁·Timing + w₂·Spectral separation + w₃·Architecture compatibility + w₄·Stability
Goal: identify candidates that sit on the best trade-off frontier rather than maximizing a single descriptor.
Decision map: Pareto-efficient detector candidates
Fast timing response
Spectral separability
Preferred design region
QD-polymer WLS
Hybrid QD/crystal
Fast plastic stack
Dense crystal stack
Conventional reference
Bubble size ~ multi-objective score
Illustrative result
Design implications
High-ranking candidates are not defined by a single best property; they arise from balanced timing, spectral separation, and detector-stack compatibility.
Dense absorber-linked materials may improve shower containment, but wavelength-selective layers become essential for information-rich readout.
QD-polymer nanocomposites are attractive because emission can be tuned toward peak SiPM/PMT quantum-efficiency windows while preserving fast response.
The ML step therefore becomes a prioritization tool for experimental beam-test campaigns, not a replacement for detector physics.
Multi-objective ML ranking helps identify which material classes should move first into prototype fabrication and beam validation.

## Slide 19
7
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
From ML Ranking to Experimental Validation
1. Ranked candidate pool
Illustrative multi-objective ranking
Candidate
Light
yield
Timing
Stability
Score
QD/PS-1
0.88
0.82
0.67
0.84
GAGG-QD
0.79
0.71
0.91
0.81
QD/PU-2
0.75
0.89
0.56
0.77
PbF2-QD
0.61
0.93
0.70
0.75
Hybrid-L
0.84
0.64
0.73
0.74
Scientific result: top-ranked candidates occupy a balanced regime rather than an extreme single-metric regime.
Key implication
Candidates showing simultaneous intermediate-to-high performance in yield, timing, and stability are more promising for prototype transfer.
2. Validation workflow
Physics-guided closed loop
Ranked
materials
Prototype
fabrication
Optical / timing
validation
Beam-test / detector
benchmarking
Feedback into
descriptor model
Closed-loop strategy: ML is not the endpoint; it is the decision layer that prioritizes experiments and learns from validation outcomes.
Operational metrics
Δλ selectivity • rise/decay time • light output • attenuation • radiation tolerance
3. Prototype roadmap
Decision logic for the next experimental campaign
Tier 1
Fabricate 2–3 top Pareto candidates covering distinct spectral/timing regimes
Tier 2
Benchmark against current reference scintillators and hybrid stacks
Tier 3
Select architecture-specific winners for CCAL-oriented beam testing
Scientific result / expected gain
A descriptor-guided workflow can reduce the experimental search burden while preserving coverage of chemically and functionally distinct detector candidates.

## Slide 20
7
M. Aydemir - Advances in X-ray and Gamma RAy DEtectors and applications (XGRADE 2026) 24-26/03/2026, Palermo
Conclusions and Challenges
Conclusions
Challenges
Interdisciplinary integration of synthesis, detector physics, and machine learning provides a rational framework for scintillator discovery.
QDs, polymers, crystals, and hybrid CCAL architectures define a high-dimensional but physically interpretable detector design space.
Beam-test experience confirms that spectral separation and architecture-aware selection can improve particle discrimination and prototype relevance.
ML transforms experimental observations into prioritizable candidate maps and physics-guided design rules. (instead of conventional trial and error methods)
Limited and heterogeneous datasets: material classes, detector geometries, and test conditions are not yet standardized across studies.
Strong performance trade-offs remain between light yield, timing, radiation hardness, thickness, and manufacturability.
Descriptor uncertainty is still significant for hybrid systems, especially when interfacial effects and architecture variables dominate performance.
Experimental validation throughput remains the main bottleneck for closing the loop between model predictions and prototype optimization.