## Slide 1: 4H-SiC LGADs: fabrication-stability optimization using TCAD simulations
Tobiáš Vasiljev

## Slide 2: Low-Gain Avalanche Diode (LGAD)
~ PiN diode + internal charge multiplication
already in use on Silicon in the LHC
+ Superior timing resolution, SNR, low energy detection
- Performance degradation with radiation damage, needs cooling
Applications in HEP, Medical devices, Space
Notes: klasická PN diode s širokou bulk vrstvou pro generování eh párů -> špatné časové rozlišení
LGAD: multiplikativní vrstva -> koncentrace E pole do špičky -> vysoký koeficient nárazové ionizace -> užší bulk, lepší časové rozlišení

## Slide 3: Why wide-bandgap (SiC)
Higher electric field before breakdown (10x),
faster charge collection (2x), higher thermal conductivity (3x),
very low intrinsic carrier concentration (~0), high radiation hardness,
temperature stability
Difficult fabrication without defects, difficult simulation in TCAD
Notes: vysoká radiační odolnost
nízká intrinzická koncentrace nosičů náboje -> nízký unikající proud, fungování při pokojových teplotách
vyšší driftová rychlost nosičů -> rychlá odezva, vysokofrekvenční aplikace
Hojně využíváno ve výkonové elektronice, v autoprůmyslu
Náročný na výrobu (bez defektů)
Obtížné numerické simulace, nepřesné parametry

## Slide 4: Simulation Model – fabrication process simulation
Monte Carlo model was determined to be the most accurate,
especially in lower concentrations
1x50 µm 2D cutout
vortex count ~ 9000
electrical simulation time ~ 1-6 hours
SIMS measurements of doping
inaccurate in low concentrations
Doping structure was simulated
with Monte Carlo simulations
and from analytic tables
(Synopsys Sentaurus TCAD)
Arbitrary units used (a.u.)

## Slide 5: Simulation Model – particle strike
Arbitrary units used (a.u.)
Minimum ionizing particle flown through the whole length
~55 e-h pairs/µm
(Both operating at 300 V reverse bias,
same geometry)

## Slide 6: Model Calibration With Matching CV Curves
using nominal values from production results
in an inaccurate simulation model
“large” discrepancy in Nitrogen dose (5%)
Arbitrary units used (a.u.)
!
epitaxy layer length
Nitrogen gain layer dose
resulting matched structure
bulk concentration

## Slide 7: Sensitivity to Nitrogen Dose (Gain layer size/shape)
TCAD Avalanche multiplication models may not be accurate

## Slide 8: Sensitivity to Angle of Ion Implantation
matched model shows a secondary “parasitic” junction
Arbitrary units used (a.u.)

## Slide 9: Channelling mitigation
varying low concentration values
due to channelling at 0 deg implant
Ion implantation angle
set to 5 deg
Arbitrary units used (a.u.)

## Slide 10: Segmentation strategies

## Slide 11: Larger 2D simulations - segmentation
24 simulations per design – point charge generation
vortex count ~ 120 000
simulation time ~ 15 – 60 hours (for 1 point generation)
Electric Field
Doping Concentration

## Slide 12
Generated charge is pulled through a low field region, doesn’t get multiplied
potential lines

## Slide 14: Zero gain region between pixels/strips
TPA-TCT measurements

## Slide 15: Trench isolation

## Slide 16: Trench isolation – no zero-gain region
Electric field gets concentrated
around the trench, affecting the
detector performance
perfectly shaped potential lines

## Slide 17: Summary
We established a 4H-SiC LGAD simulation model and used it to improve the reproducibility our first-generations prototypes
We extended the simulation model to study different segmentation strategies
Future work:
Further optimize the doping structure for maximum reproducibility and lifespan
Simulate more segmentation strategies, compare with measurements
Investigate the zero-gain region further

## Slide 19: IV characteristics