## Slide 1
.
G. Laštovička-Medin,a G. Kramberger,b , I. Mandić, b H. Ji,c M. Liu,c Z. Li,c J. Lu,c Z.Li,d and M. Rebarze
aFaculty of Natural Sciences and Mathematics, University of Montenegro, Dzordza Vashingtona bb,, 81000, Podgorica, Montenegro,
bJozef Stefan Institute, Jamova cesta 39, 10 000 Ljubljana, Slovenia
cInstitute of Microelectronics of the Chinese Academy of Sciences ,3 Beitucheng West Road, Chaoyang District, Beijing, China
dThe School of Integrated Circuits, Ludong University, Yantai 264025, China
eELI Beamlines Facility, The Extreme Light Infrastructure ERIC, Za Radnicí 835, 25241 Dolní Břežany, Czech Republic
CERN-DRD3 WP2 project:
Novel silicon 3D-trench pixel detectors based on 8-inch CMOS process (IME)
Self-quenching of 3D trench detectors: Geometry driven gain & fast timing
PSD14, 31 August - 3 September, 2026, Queen Mary University of London, UK

## Slide 2: Outline
Gain in silicon and motivation
Overview of 3D IME-CAS devices produced in 8 INCH CMOS compatible technology
Two Photon Absorption - Transient Current Technique studies
Improvements of the design – future work
Measurements of impact ionization in silicon using Straw (cylindrical) 3D IME-CAS
Future work & Conclusions

## Slide 3: Motivation: radiation hard, fast device with the intrinsic gain

## Slide 4: Motivation: radiation hard device with gain

## Slide 5
IME-CAS devices overview
Columns as narrow as 0.5 µm with aspect ratios of close to 100:1.
The devices as thin as 30 µm
Pixel detectors with cell sizes down to 15x15 µm2.
Unlike in LGADs the gain is achieved simply by geometry and is much less affected by precise doping levels of columns.
As the gain is achieved by geometry and doesn’t critically depend on doping levels they are much more radiation hard than LGAD detectors.

## Slide 6
Non- HEP structures – array if tiny columns (straws
HEP structure – pixel detector
Different IME-CAS structures
Same as gaseous detector tube

## Slide 7: 3D STRAW TUBES Impact ionization studies
From Neff=1e12-1e14 cm-3
no gain up to some 30-40 V and then rapid increase
At the z=15 mm one can calculate analytically the gain – so fitting and extraction of impact ionization is straightforward
Gain
E [V/mm]
a=0.5 mm and b=10 mm
Vbias [V]
Ideal structures to study impact ionization – especially after irradiation – as the field can be solved analytically
Experimentally this is very complicated, but we managed to do it.
Therefore, we will be able to study impact ionization at severe fluences.

## Slide 8
Characterization technique: Two Photon Absorption - TCT
Generation of free carriers by light and observing their drift – Transient Current Technique – has been a workhorse in many semiconductor detectors (lots of advantages):
➢ Two photon absorption is a step forward as it allows a very localized deposition in a voxel (~ 1-2 mm x 10 mm) . The key is to have very fast ~100 fs laser pulse focused to 1 mm with high enough energy
➢ 3D detectors are actually one of the best (if not the best) case studies for these techinque
➢ Large Laser facilities (such as ELI beams in Prague) allow even more photon absorption 3PA (longer wavelengths and more power) reaching very small voxel sizes

## Slide 9
TCT set at at ELI
The sample is electrically connected by wire
bonds: the junction electrode is connected to high voltage (HV) via the Bias T circuit (Particulars BT-01), while the trench electrodes are grounded. The transient (RF) signals, decoupled from the HV by the Bias-T, are amplified by a wideband amplifier (Particulars AM-02 A, 3GHz, 53dB) and digitized by a 2.5GHz, 20 GS/s oscilloscope.

## Slide 10
Investigated Devices
1
2

## Slide 11: 3D trench with square shape
Column readout
Trench electrode (V bias)
1

## Slide 12
FWHM of the profile is close to the nominal thickness which is 30 um.
We checked profiles in a few different points with very similar results.
Z- Scan

## Slide 13
Waveforms at two biases:
20 V and 60 V
Another indicator of charge multiplication is the extended duration of the induced signals which results from the drift of the secondary holes to the ohmic contacts after the primary electrons undergo multiplication. Obviously enlarged amplitude can be seen.

## Slide 14
Charge collection and gain confirmation
After the initial depletion
phase the device becomes fully depleted at around 25V, where the collected charge reaches a plateau.
Steep increase of the collected charge that coincides with the rise in the leakage current clearly shows the avalanche breakdown

## Slide 15
Gain Depth Dependence
At 60 V and at the depth of 25 µm
the gain is around G=Q(V)/Q(Vfd)∼7.5
Tip of n+ electrode
Illustration of focal point at the tip positon and TPA ellipsoidal voxel
“cigar”
leaving
active area
TPA “cigar” leaving active area.

## Slide 16: Why don’t we see early breakdown?
Tentative explanation:
For vey narrow column the gain in a small volume creates enough charge even for mip to screen the field – self quenching
➢ For conventional 3D this is not the case – 10 µm column is too large
➢ Along the electrode the difference is very small – small density no large screening
Smaller density, smaller screening
Higher density, higher screening

## Slide 17
Gain self-quenching demonstrated
Gain suprression is observed
Screening observed- gain depends on carrier density
The small column diameter – gain stabilizer

## Slide 18
Slew Rate Depth profiling
  Signal becomes slower and arrives later with increasing depth.
Position (x,y) where z-scan was performed.
Large slew rate difference across the sensor results in hit position dependent jitter for MIPS:
  ➢ Timing distributions will be skewed – different to LGADs
When the “cigar” enters substrate the carriers need to diffuse to the active zone – longer signals

## Slide 19
Already shown in previous slide but here magnified ( selected time window reagion ).

## Slide 20: Rise Time & Time of Arrival Depth Profiling
Position (x,y) where z-scan was performed and the RT and ToA are extracted (from corresponding waveforms)
ToA and RT is increasing with increasing depth;
gain increases but also screening effect (slower movement of clouds of holes).
When the “cigar” enters substrate the carriers need to diffuse to the active zone – longer signals

## Slide 21
2 μm
17 μm
33 μm
Charge [a.u.]
35 um
35 um
Charge vs. X
Charge vs. Y

## Slide 22
2 μm
17 μm
33 μm
RT [ns]
Lateral variation of Rise Time (RT):
In X direction

## Slide 23
ToA
Lateral variation of ToA:
In X direction
2 μm
17 μm
33 μm

## Slide 24: Rise Time spread
2 μm
17 μm
33 μm
RT [ns]
RT [ns]
RT [ns]
35 um
Depth: 2 µm
Depth: 18 µm
Depth: 17 µm
TPA vortex covers different el field regions

## Slide 25: ToA spread
2 μm
17 μm
33 μm
ToA [ns]
Distribution of ToA at different depths is much more homogenous than rise time. However shifts towards bigger values with depth is clear. Also RMS increases vs depth from 59.3 ps close to top surface to 83.9 ps close to the bottom.
35 um
35 um
RMS:59.3 ns
RMS:83.9 ns
RMS:77.2ns
Simulated ToA spread of 80 ps at 62 V is in excellent agreement with TPA-TCT measurements (77.2 ps). (S9mulation performed by G. Kramberger (TREDI2026)

## Slide 26: 2D Gain Map
Pulse energy: 15 pJ
Depth: 17 um

## Slide 27: Irradiated 3D Trench device
5x1015 neq/cm2

## Slide 28
Gain after irradiation and other control plots plots
at +200C (RT)
We see changes in performance:
➢ no plateau at full depletion but continuous increase of charge (trapping – geometry related);
➢ onset of gain at about the same voltage;
➢ slightly less gain and larger depth dependence;
+200C
-200C
Before irradiation
After irradiation
(trapping – geometry related

## Slide 29
RMS, MAD (ToA)
at RT (red)
-250C (blue)
ToA [ns]
2D image of ToA
at RT (left)
at -250C (right)
ToA after irradiation

## Slide 30
2D image of Rise Time
RMS, MAD (Rise Time)
at RT (red)
-250C (blue)
RT after irradiation
RT [ns]
at Room Temp
-250C

## Slide 31
ToA, RT at low and room temperature
Significant reduction at low temperature

## Slide 32
ToA, RT at low and room temperature

## Slide 33
2 μm
17 μm
33 μm
ToA [ns]
35 um
35 um
RMS:37.8ns
RMS:47.5 ns
RMS:22.7 ns
ToA vs. depth before and after irradiation
Depth: 2 µm
Depth: 17 µm
Depth: 35 µm
RMS: 59.3 ps
RMS:77.2 ps
RMS:83.9 ps
Before
irradiation
Quite significant improvement
(not yet fully understood) in ToA
(CFD@0.5 from ~80 ps to 50 ps:
➢ trapping reduces longer tails
➢ larger space charge leads to
gradients in field – faster
collection
After irradiation

## Slide 34: Straw Tube IME-CAS Detectors

## Slide 35: 2D of Charge, Rise time and ToA distribution before and after irradiation

## Slide 36: RMS of RT and ToA before and after irradiation

## Slide 37
Other control plots

## Slide 38: Impact Ionization Study
In the first approximation field can be calculated analytically and also the gain:
➢ up to 1016 cm-2 the changes to Neffcan be ignored
➢ short distances render trapping of the drifting charge negligible
➢ TPA allow injection away from the tip where analytical calculation is more reliable
➢ TPA allows also studies of charge screening effects
Extending the studies to very high fluences – above 1017 cm-2 will reveal the answer if silicon gain devices can be operated - this is the key question for Silicon in FCC-hh. Without gain we know silicon will fail.
  ➢ a clear underestimation of the charge by the literature models
  ➢ no impact of radiation up to 5e15 cm-2
  ➢ extraction of parameters depends critically on “wire dimensions” (column width + doping layer) - we are now expanding the studies to more columns widths for more reliable extraction.

## Slide 39
Optimization of geometry to achieve better timing performance is underway
Trench-column 2E/nE devices Timing resolution of 20 ps Improvement of simulation tools
Optimization parameters:
PP – pixel pitch
PW – pixel width
ED – electrode distance PT - Thickness
REF: M. Puklavec, Small cell 3D detectors with intrinsic gain, TREDI2026; https://indico.cern.ch/event/1586892/contributions/6846212
IDEAL 4D Tracking Device

## Slide 40: Conclusion
Silicon/Semiconductor gain devices are in the focus of R&D activities. LGADs still dominate – to be used for the first time in ATLAS/CMS, but others, SiEM and 3D detectors are also gaining momentum.
➢ Very small pitch and thickness 3D devices were produced with controllable gain (35x35x30 µm3 cells) owing to 8” CMOS and DRIE processing at IME.
➢ Gains of up to around 10 were measured with devices fully functional at moderate voltages 62 V with only up to 20-30% gain variation across the cell was observed. Being thin these devices would have much better noise performance than standard 3D sensors.
➢ Devices were not optimized for timing and their timing performance is not excellent:
➢ Weighting field (distortion) contribution dominates the timing resolution
➢ rise time variation across the cell can lead to jitter variations - mapping for ToA and dV/dt of the device shows this
Extremely small single cell cylindrical devices are ideal for impact ionization measurements at extreme fluences.
2 more runs with timing optimized devices will following until the end of 2027
devices optimized for timing applications will be included
➢ impact ionization measurements over the large fluence range
Future PLAN:

## Slide 41: Thank you for your attention!
Funding:
Research was partially funded through the project “TAIDA: Technological Advancement and Innovation for Detectors at Accelerators”, Contract No. 0402- 082/23-1740/5 (funding agency: Ministry of Education, Science and Innovation in Montenegro).
For device fabrication, the authors acknowledge fundings from National Natural Science Foundation of China under Grant 12375188 and in part by the National Key Research and Development Program of China under Grant 2023YFF0719600.
This project has received funding also from the European Union’s Horizon Europe Research and Innovation programme under Grant Agreement No 101057511 (EURO-LABS).

## Slide 42
2 μm
17 μm
33 μm
RT [ns]
35 um
35 um
RMS:36ns
RMS:52.6ns
RMS:48.3ns
RT vs depth after irradiation