## Slide 1
Systematic Study of Proton- and Neutron-Induced Radiation Damage in 4H-SiC PN Diodes
Sebastian Onder, Peter Fischer, Stefan Gundacker, Matthias Knopf, Daniel Radmanovac, Simon Waid, and Thomas Bergauer
PSD14
04.09.2026

## Slide 2
4H-SiC for Radiation Detection
High Energy Physics
No cooling, SiC LGADs
Proton/Ion therapy
Beam monitoring, dosimetry
Attractive for power electronics & automotive industry ⇒ Increased availability and lower costs
Wide bandgap (Si: 1.12eV, 4H-SiC: 3.26eV)
  low leakage current & thermal noise at room temperature and after irradiation ⇒ no cooling
  insensitive to visible light, thermal robustness (up to 300°C)
Low doped & high quality material <100µm thick (Si: ~300µm) + higher εi ⇒ less signal yield
Symbolic image. Taken from: https://www.nature.com/articles/d41586-021-00408-1
Munoz et. al., „Characterization of 4H-SiC p-n Junction Detectors for Alpha Particle Detection in Plasma Diagnostics“, Talk at 3rd DRD3 Week, 2025
Upcoming: Fusion Diagnostics

## Slide 3
I-V
C-V
Radiation damage in 4H-SiC is dominated by deep level traps (Z1/2, EH4/5, EH6/7):
  Negligible increase in leakage current
  Voltage-independent, flatlining capacitance
  Loss of rectification
TCAD radiation damage model:
  Preliminary Vienna model for neutron irradiation yields qualitative results
  Based on small fluence range and single devices per fluence
  ⇒ larger study with more fluences and more samples
Radiation Damage in 4H-SiC
Common defect energy levels in 4H-SiC
P. Gaggl, et. al. (2024). TCAD modeling of radiation-induced defects in 4H-SiC diodes. NIM A, 170015. https://doi.org/10.1016/j.nima.2024.170015

## Slide 4
181 total PN diodes included in study:
  2 epitaxial thicknesses: 50µm and 100µm
  3 device areas: 3x3mm², 1x2mm², 1x1mm²
  Average doping of 3-5e14cm-3 (depending on epi thickness) ⇒ 100um only partially depleted
4-6 diodes per particle, epi thickness and fluence
24 GeV protons (CERN IRRAD): 8 fluences, 5e12 - 5e15 p/cm²
Neutrons (JSI): 11 fluences, 1e13 - 1e18 neq,Si/cm²
Characterization techniques:
  I-V and C-V
  UV-laser-based CCE measurements
Irradiation Campaign
50um/ 100um
~350um
3mm
1mm
2mm
3-5e14/cm-3
1e18/cm-3

## Slide 5
Bias-independent capacitance after 3e13 p/cm² resp. 5e13 neq,Si/cm²
CV Characteristics
I-V/C-V probe station
Chuck (HV)
Probe needles (GND)
f=100kHz, VAC=250mV
forward
reverse

## Slide 6
Capacitance vs. Fluence
Removal of active donors
Epitaxial layer compensated and becomes semi-insulating
Substrate compensated
Geometric capacitances of epi thickness
Geometric capacitances of epi + substrate
unirrad
50um/ 100um
~350um

## Slide 7
Up to 1e13/cm²:
  Characteristic turn-on voltage of ~2.7V
  Ideality factor jumps from ~1.2 to ~2 (see backup)
Up to ~5e14/cm²:
  Forward current reduction
  Turn-on voltage gradually shifted to higher voltage (on-resistance increase due to compensation)
From ~5e14/cm²:
  Forward current becomes similar to reverse current
  Total loss of rectification
Forward IV Characteristics
Loss of rectification

## Slide 8
<1e14/cm²: transient-dominated, likely slow detrapping (τ ~ 40s)
1e14/cm² to 5e16/cm²: current grows with V, but decreases with fluence → field-driven generation/emmission and compensation compete
From 2e17/cm²: generation-dominated, increase to nA currents
Reverse IV Characteristics
behaviour is analogous in 100µm (see back up)

## Slide 9
Leakage stays below 10pA/mm², followed by sharp increase >2e17neq,Si/cm² to nA/mm²
Not compatible with established damage model in Si (ΔI = αΦV)
Reverse IV vs. Fluence
transient- dominated
Field-driven emmission/generation vs. compensation (mechanism to be investigated)
generation- dominated
Protons exhibit less current

## Slide 10
CCE determined relative to unirradiated device @1kV
Lower CCE in 100um samples → likely an artifact of partial depletion
Slightly stronger decline of CCE from 24GeV protons (other way around in Si)
CCE vs. Fluence
CSA
CCE measurement principle using a UV laser and charge sensitive amplifier (CSA)
UV laser 375nm (237µm absorption length)
Cividec Cx-l

## Slide 11
4H-SiC falls below 50% by approx. one order of magnitude earlier than Si
⇒ In terms of charge collection, 4H-SiC PN diodes are not radiation harder than Si
CCE: 4H-SiC vs. Si
50%

## Slide 12
Large irradiation study on 4H-SiC PN-diodes: 181 diodes, 24 GeV protons & reactor neutrons, 2 epi thicknesses, fluences over >4 orders of magnitude
CV / doping: donor removal up to ~1e13; device then becomes semi-insulating (geometric capacitance)
Forward IV: turn-on shifts to higher voltage ⇒ progressive loss of rectification
Reverse IV: leakage stays remarkably low (<10 pA/mm²) up to 2e17; not described by the Si damage model (ΔI = αΦV)
CCE: drops below 50% roughly one order of magnitude earlier than Si ⇒ In terms of charge collection, 4H-SiC PN diodes are not radiation harder than silicon
  Bad news for HEP applications: MIP detection becomes very challenging ⇒ SiC LGADs
  Ion therapy and fusion: higher energy deposition of particles compensates for lower CCE i.e. low leakage and thermal robustness still offer significant advantages
Outlook: dataset feeds refinement of the Vienna TCAD damage model; hardness-factor / NIEL analysis follows (e.g. protons degrade CCE slightly faster); temperature dependent studies in the next step
Summary

## Slide 13
Thank you!
This work was supported by the Austrian research promotion agency FFG, project number 883652.
Production and development of the 4H-SiC samples was supported by the Spanish State Research Agency (AEI) and the European Regional Development Fund (ERDF), ref. RTC-2017-6369-3.
The production of the planar 6''-SiC samples has been supported in part by the RD50 collaboration (RD50-SiC-LGAD common project)
This project has received funding from the European Union’s Horizon Europe Research and Innovation programme under Grant Agreement No 101057511 (EURO-LABS)."
Special thanks to colleagues from CTU and FZU Prague for organizing the irradiation at CERN IRRAD and letting us participate with the devices irradiated as part of this study.

## Slide 14
Back Up

## Slide 15
181 total diodes included in study
  PN diodes
  3 areas: 3x3mm², 1x2mm², 1x1mm²
Irradiated using
  24 GeV protons (CERN IRRAD)
  Neutrons (JSI)
Devices Under Test
Fluence (p/cm² resp. neq,Si/cm²) | 5e12 | 1e13 | 3e13 | 5e13 | 7e13 | 1e14 | 5e14 | 1e15 | 5e15 | 1e16 | 5e16 | 2e17 | 5e17 | 1e18
24GeV Protons 50µm | 5 | 5 | 5 | - | 5 | 5 | 5 | 5 | 5 | - | - | - | - | -
24GeV Protons 100µm | 5 | 5 | 5 | - | 5 | 5 | 5 | 5 | 5 | - | - | - | - | -
Neutrons 50µm | 5 | 4 | - | 5 | - | 4 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5
Neutrons 100µm | 6 | 4 | - | 6 | - | 4 | 6 | 4 | 6 | 4 | 6 | 5 | 5 | 5

## Slide 16
CV curves flatten out after 3e13p/cm² resp. 5e13neq,Si/cm² ⇒ Decrease of effective doping concentration only visible up to 1e13/cm²
Donor Removal
 | g (cm-1) | Avg. Neff,0 (1014cm-3)
Protons 50µm | 13.4 ± 0.7 | 2.91 ± 0.15
Protons 100µm | 11.9 ± 1.9 | 5.00 ± 0.05
Neutrons 50µm | 13.6 ± 0.9 | 3.53 ± 0.11
Neutrons 100µm | 14.1 ± 0.7 | 3.78 ± 0.05

## Slide 17
Ideality factor jumps from ~1.1-1.2 to ~2 within one fluence step
Forward IV - Ideality Factor
Ideality factor n | Pristine | 5E12 (p/cm² resp. neq,Si/cm²) | 1E13 (p/cm² resp. neq,Si/cm²)
Proton 50 µm | 1.19 ± 0.06 | 2.00 ± 0.03 | 2.10 ± 0.04
Proton 100 µm | 1.17 ± 0.01 | 1.93 ± 0.01 | 2.01 ± 0.04
Neutron 50 µm | 1.11 ± 0.11 | – | 2.01 ± 0.01
Neutron 100 µm | 1.13 ± 0.17 | – | 1.99 ± 0.04

## Slide 18
As the turn-on voltage grows beyond 1e13/cm² the on-resistance explodes
⇒ diodes become increasingly semi-insulating
On-Resistance vs. Fluence

## Slide 19
375nm laser (absorption length of ~237µm)
Charge information via Cividec Cx-L charge sensitive amplifier
CCE determined relative to unirradiated device
CCE vs. Fluence
CSA
CCE measurement principle using a UV laser and charge sensitive amplifier (CSA)
UV laser

## Slide 20
CCE at a Glance

## Slide 21
Reverse IV at a Glance

## Slide 22
Irradiation can change atomic composition of 4H-SiC
Neutrons:
  Main process: neutron capture
  Mainly turns Si and C into other Si and C isotopes
24GeV protons:
  Creates a large array of spallation products, see https://doi.org/10.1134/S1063782607030190
  Creates a concentration of ~1e13 to ~1e16/cm³ of stable isotopes across the probed dose range (1e13 to 1e16 p/cm²)
  Among the stable isotopes are e.g. N, Al, O, Na
  Radiation damage from protons potentially more complex than from neutrons
Damage by 24GeV Protons

## Slide 23
Radiation damage model (preliminary) via radiation induced traps for simulation in TCAD
Material and defect parameters deviate across literature:
  Initial guesses from literature
  Optimized by fitting simulation results to measurement
Qualitative agreement
I-V
C-V
(most significant trap levels)
Radiation Damage Model
Sebastian Onder Vienna Conference on Instrumentation 2025
P. Gaggl, et. al. (2024). TCAD modeling of radiation-induced defects in 4H-SiC diodes. NIM A, 170015. https://doi.org/10.1016/j.nima.2024.170015
J. Burin, et.al. (2024). TCAD Simulations of Radiation Damage in 4H-SiC. Austrochip 2024. https://doi.org/10.1109/Austrochip62761.2024.10716221.

## Slide 24
Collaboration Partner: ion beam radiotherapy center MedAustron
Low leakage currents, after irradiation and at room-temperature ⇒ DC readout
Insensitive to visible light, better tissue equivalence
Beam monitoring for clinical therapy beams (p+ and 12C)
Microdosimetry: single particle dose deposition on length scale of cells (<10µm) ⇒ thin sensors
Medical Applications: Beam Monitor & Dosimetry
UHDR beam monitor prototype (planar SiC sensor)
New SiC-based beam monitor for a wide dynamic beam intensity range and FLASH-like beams in the future
Soon: SiC Microdosimeter
(50µm x 50µm pitch, 10µm epi)

## Slide 25
Lower CCE in 100um samples → likely an artifact of partial depletion
Slightly stronger decline of CCE from 24GeV protons (other way around in Si)
CCE vs. Fluence