## Slide 1
daniele.alfiero@cern.ch
28.05.2026
Radiation Effects in Silicon Photonics Micro-Ring Modulators and Waveguides for High-Energy Physics
Daniele Alfiero
Seminar
University of Birmingham

## Slide 2
Outline
Introduction
  Silicon Photonics for high-speed links in particle detectors
  Ring modulators and waveguides
Irradiation campaigns
  X-ray test on ring modulators:
    Electro-optic frequency response
    Localized thermal annealing
  Neutron and X-ray tests on waveguides:
    Radiation-induced attenuation (RIA)
  Heavy ion test on waveguides:
    Optical single-event transients (OSETs)
    TCAD simulations
Conclusions and future work

## Slide 3
3
Introduction
Silicon Photonics for High-Energy Physics

## Slide 4
Introduction – Silicon Photonics for High-Energy Physics
Silicon Photonics
High-speed data transmission
Low mass
Low power consumption
Radiation hardness
CMOS compatible process flow
Particle sensor
PD
>> 100 m Single-mode fibers
Front-End
Back-End
PIC
Si-PIC
4x25 Gbps
5 Gbps
PIC: Photonic Integrated Circuit
PD: Photodiode
Biereigel

## Slide 5
Input light
Multiplexer
λ1
λ2
λ3
λ4
Introduction – Overview of a SiPh-based transceiver
Demultiplexer
Si-PIC
Rx
Rx
Rx
Rx
Commercial
off-the-shelf
components,
FPGAs, etc.
Mirco-Ring Modulators (RM)
Waveguides
two of the main photonic components exposed to radiation !
fiber array unit
unmodulated light
FAU
modulated light

## Slide 6
Introduction – Light coupling and waveguides
Vertical coupler
Angle of incidence
~ 10° off-vertical
Optical fiber
Edge coupler
Optical fiber
 | Edge | Vertical
Insertion Loss | ✓ | ✖
Bandwidth | ✓ | ✖
Packaging Complexity | O | ✓
Wafer Level Probing | O | ✓
Si waveguide
SiO2 substrate
Waveguides cross-section
(a)
(b)
(c)
|E| [a.u.]
strip
rib
(deep etch)
rib
(shallow etch)
Si
SiO2
380 nm
220 nm

## Slide 7
Optical power
Wavelength
Si
5 μm
Introduction – Ring Modulators
Input light
Output light
Working principle:
  Light coupled into the silicon micro-ring
  Destructive interference  resonance
Free Spectral Range
(FSR)
SiO2
Top view
: effective refractive index
: round trip length

## Slide 8
Introduction – Ring Modulators
ΔV
OMA: Optical Modulation Amplitude
ME: Modulation Efficiency
Popt
time
How do we modulate it?
  Modulation of the resonance peak through the applied voltage
    Injection/depletion of carriers  variation of the effective refractive index
Optical power
Wavelength
V
V0
V1
P1
P0
OMA
ME
Phase shifter cross-section
X
X
Modulation
Efficiency

## Slide 9
Introduction – Tungsten micro-heaters
µ-heater
Si waveguide
300 K
400 K
  Tungsten µ-heater to shift the resonance wavelength
  Localized heating
  Thermo-optic coefficient of silicon stronger than electrical modulation but slower
  Thermal shift coefficient of 70 pm/°C for O-band (1310 nm) and 80 pm/°C for C-band (1550 nm) ring modulators, significantly larger than the modulation efficiency (35 pm/V)
  µ-heaters can be used for localized thermal annealing
µ-heater’s electrical power and temperature
SiO2

## Slide 10
10
Ring Modulators
X-ray irradiation tests

## Slide 11
X-ray testing of Ring Modulators – Motivation
Static Test
  Characterization of ring modulators and photodiodes under ionizing radiation
  Online acquisition of electrical (I-V) and optical (spectra) device parameters
  Investigation of temperature effects and thermal annealing post-irradiation
Dynamic Test
  Measurement of electro-optic (EO) frequency response of ring modulators under ionizing radiation
  Analysis across different temperatures and in the 10 MHz - 25 GHz frequency range
  Investigation of thermal annealing during and after irradiation
Optical fiber
array
PIC
Temperature
sensor
5 mm
5 mm
Total ionizing dose (TID) reached:
Irradiation time:
Dose rate:

## Slide 12
Static X-ray test – Results
V0
V1
ME
  Reduction in ME strongly dependent on temperature
  RMs at intermediate temperature range [50°C - 150°C] degrades faster than RM at room temperature
  One hour annealing at 270°C effectively restores ME to pre-irrad values
  Pinch-off of the p-slab caused by positive charge accumulation
  Increase in the breakdown voltage confirms the pinch-off mechanism
pre-irrad
irrad
post-irrad

## Slide 13
Dynamic X-ray test – EO frequency response (S21)
  EO frequency response (S21) measured online using a VNA (Vector Network Analyzer) and a high-speed photodiode
  TID damage is frequency dependent and saturates around 2 MGy for room temperature device
  RM at 170°C thanks to the µ-heater continuously anneal TID damage

## Slide 14
Dynamic X-ray test – S21 at single frequency
  S21 measurements are consistent with ME results from the static X-ray test:
    Faster degradation observed in the intermediate temperature range compared to room temperature device
    After irradiation, tried shorter annealing than in previous test: 10 minutes at 230°C sufficient to recover the EO frequency response
pre-irrad
irrad
post-irrad
pre-irrad
irrad
post-irrad

## Slide 15
Dynamic X-ray test – RMo2: annealing during irradiation
  After reaching the TID target of 10 MGy, a thermal annealing step was performed only for RMo2 while keeping irradiating
  RMo2 (only) kept at 230°C for approximately 30 minutes, while measurement loop was continuing for other devices
  After the annealing step, the temperature was lowered back to 73°C
pre-irrad
irrad
post-irrad
pre-irrad
irrad
post-irrad

## Slide 16
Dynamic X-ray test – RMo2: annealing during irradiation
  TID damage resumes following almost the same degradation trend as observed at the beginning of the irradiation
  After localized thermal annealing, radiation damage does not accumulate with previous one

## Slide 17
Dynamic X-ray test – Eye diagrams
  Eye diagrams at 25 Gbps were acquired from the irradiated sample and compared with those from non-irradiated devices
  No evidence of degradation after thermal annealing
  Eye diagram parameters do not show differences compared to non-irradiated ring modulators

## Slide 18
18
Waveguides
Irradiation campaigns and TCAD simulations

## Slide 19
Neutron test – Setup
  Evaluation of radiation-induced attenuation (RIA) in SiPh waveguides
  Measurements of different waveguide types in the two optical bands (O-band at 1310 nm and C-band at 1550 nm)
Neutron fluence reached:
Peak beam neutron energy:
Irradiation time:
optical switch
optical spectrum
analyzer
bunker
walls
single mode
optical fibres
polarization controller
P
I
C
1-2
P
I
C
3
superluminescent diode
O- & C-band
neutron beam

## Slide 20
Neutron test – Optical transmission spectra measurements
slope = RIA
  Linear fit for the calculation of the RIA (‘cut-back’ method)
  The variation of the slope gives the RIA
  The variation of the y-intercept gives the variation in the grating coupler response (if any)
optical spectrum analyzer
l

## Slide 21
Neutron test – RIA in waveguides
(a)
(b)
(c)
|E| [a.u.]
WG
SKT
FC
  Waveguides in O-band show a higher RIA than their counterpart in the C-band
  Attention must be taken when designing a PIC

## Slide 22
Neutron test – Explaining the results
  Defected-induced energy states reduce the optical absorption length
  Displacement damage (DD)
Creation of multiple defect species
Generation of trap states
Indirectly ionizing radiation
+
+
+
+
-
-
-
-
C. Scharf, F. Feindt, and R. Klanner, “Influence of radiation damage on the absorption of near-infrared light in silicon,” Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment, vol. 968, p. 163955, 2020. [Online]. Available:
https://www.sciencedirect.com/science/article/pii/S0168900220304277
  Both studies show a larger increase in the absorption coefficient at 1310 nm compared to 1550 nm
E. Fretwurst, R. Klanner, J. Schwandt, and A. Vauth, “Study of the v20 state in neutron-irradiated silicon using photon-absorption measurements,” Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment, vol. 1053, p. 168353, 2023. [Online]. Available:
https://www.sciencedirect.com/science/article/pii/S0168900223003431
1310 nm
1550 nm

## Slide 23
X-ray test – RIA in waveguides
  Same setup as for the neutron test
  X-ray test to decouple the RIA from non-ionizing and ionizing radiation
  RIA saturates, confirming our previous measurements and some results found in literature
Si
SiO2
+
+
+
+
+
+
+
+
+
+
+
  Hypothesis: the accumulation of positive charges in the SiO2 and at the Si/SiO2 interface pushes free carriers in the waveguide (slightly p-doped) toward the center, increasing their overlap with the optical mode and enhancing absorption due to free-carrier absorption
Many thanks to Carlos Solans Sanchez and the ATLAS Tracking Detectors (EP-ATL-TRK) group for providing access to their X-ray facility, and to Kourosh Sarbandi for assistance with the dosimetry!

## Slide 24
Heavy ion test – Setup
  Evaluation of optical single-event transients (OSETs) in SiPh waveguides
  First heavy-ion test for OSETs (no tests for OSETs have been reported in the literature)
Max. LET available from the ion cocktail:
Ion flux:
Angles of incidence:
PIC
waveguide
7.5 mm
24-ch
fiber-array
unit
DFB
LASER
1310 nm
polarization controller
LASER
controller
reference
receiver
oscilloscope
This activity has received funding from the European Union's 2020 research and innovation programme under grant agreement No 101008126, corresponding to the RADNEXT project.

## Slide 25
Heavy ion test – What is an OSET?
Ion strike
Si
SiO2
Si
SiO2
OSET: single-event transient in the optical domain

## Slide 26
Si
Light propagation in the waveguide
Ion strike
Output power
Time
OSET
2
3
4
1
1
2
3
4
Initial carrier generation from ion strike [100 ps to 1 ns]
Peak of carrier generation and optical attenuation
Recombination mechanisms [tens of ns]
Complete recovery from the transient event [after 100 ns]
(unit interval for a bit at 25 Gbps is 40 ps)
Heavy ion test – What is an OSET?

## Slide 27
Heavy ion test – Measurements
  For perpendicular strike, OSETs were observed only for the heaviest ion (124Xe35+, LET of 61.3 MeV·cm2/mg)
  The ratio was approximately of 1 hits/min, with maximum amplitude of transient of 1.5 %
  Maximum transient amplitude of 4 % with highest LET and angle of incidence of 75°
  Two-peaks distribution of the transient amplitude because of the L-shaped waveguide

## Slide 28
Heavy ion test – TCAD simulations
  Sentaurus TCAD is a powerful tool to combine:
    Electrical simulations  carrier generation, diffusion and recombination from the heavy ion strike (variation in the complex refractive index due to the different number of carriers)
    Electromagnetic simulations  finite-difference time-domain (FDTD) solver to compute the electromagnetic field propagation
sprocess
snmesh
sdevice
Creation of the 3D strip waveguide structure
Generation of the mesh
Transient simulation of the heavy ion strike event
emw
FDTD simulations for different time steps

## Slide 29
Heavy ion test – TCAD simulations
  Starting from the LET of 61.3 MeV·cm2/mg we can set a defined number of electron-hole pairs generated per volume within the TCAD simulation (details of the calculations in the backup)
  Amplitude of the transient matches well the measurements
  Good match also for the left-hand side of the transient (initial charge generation)
  The transient amplitude shows a good matching also when the angle of incidence is changed
  Overestimation of the recombination time constant (for now used the pre-defined TCAD values, trying with different recombination parameters)

## Slide 30
Heavy ion test – Surface recombination
  By reducing the surface recombination velocity from the default value, we match not only the amplitude of the OSET but also the typical recovery time

## Slide 31
Conclusions…
Dynamic X-ray irradiation test on SiPh ring modulators have demonstrated the susceptibility of the electro-optic frequency response to TID damage (pinch-off mechanism of the silicon slab).
Localized thermal annealing using the built-in micro-heaters restores completely the performance. No sign of degradation in the eye diagrams after thermal annealing.
Neutron and X-ray irradiation tests on SiPh waveguides highlighted evidence of radiation-induced attenuation that must considered for future PIC designs.
Heavy ion testing demonstrated non-significant influence of OSETs in the SiPh waveguides transmission. Transient amplitude with LET up to 61.3 MeV·cm2/mg and angle of incidence of 75° remained below 4 %.
TCAD simulations of OSETs events show a good agreement with the measured transient, both in amplitude and recombination time.
…and future work
Write the thesis 🫠

## Slide 32
Thank you for your attention!
daniele.alfiero@cern.ch

## Slide 33
Backup

## Slide 34
Optical datalinks in High-Energy Physics
Optical data link are vital parts of modern High Energy Physics (HEP) experiments
  CERN experiments exploit tens of thousands of custom optical datalinks
All these links utilize conventional discrete components
  Directly modulated lasers and normal-incidence p-i-n photodiodes
  Mature technologies and thoroughly studied characteristics under irradiation
We are reaching the limits what can be done with conventional links: few × 1015 n/cm2
The placement already restricted by radiation levels during the experiment lifetime
The final runs of High-Luminosity LHC and future accelerators
require even higher levels of radiation tolerance
Integrated particle fluence in 1 MeV neutron equivalent per cm2, for the CMS Phase-2 tracker.
[The Phase-2 Upgrade of the CMS Tracker]
Interaction point
One quarter cross section of CMS experiment
\\\\
\
no-go zone

## Slide 35
Introduction – Ring Modulators
Optical data out
Input LASER
Δλ(V)
p
n

## Slide 36
*https://doi.org/10.1017/CBO9781316084168.006
Si waveguide
Grating coupler
Angle of incidence
off-vertical
Optical fiber
Buried Oxide (BOX)
Introduction – Optical coupling
light
spacer
GC periodic cross-section

## Slide 37
Single Mode
Optical fibers
Optical switch
DAQ
(electrical switch)
Heater
Power Supply
Electrical cables
C-band
Tunable LASER
Optical Power Meter
|
|
C-band
O-band
|
μheaters
DUTs
|
Bias and Idle Sourcemeters
X-ray
machine
System
PIC
Peltier cell
Polarization controller
O-band
Tunable LASER
Optical Power Meter
Polarization controller
Static
X-ray Test
Setup

## Slide 38
Static X-ray Test – Setup
VNA
X-ray machine
Optical
switch
Power supplies
Sourcemeters
O-band laser
+
Optical power meter
Polarization controller

## Slide 39
Static X-ray Test – IVs pre-irrad

## Slide 40
Single Mode
Optical fibres
Optical switch
Heater
Power Supply
Electrical cables
|
O-band
μheaters
DUTs
DC Sourcemeter
O-band
Tunable LASER
Optical Power Meter
Polarization controller
|
|
VNA
(Vector Network Analyzer)
Out «B»
Photodetector
RF switch
Bias
tee
Out «A»
Port 1
Port 2
SystemPIC
X-ray
machine
Dynamic
X-ray Test
Setup

## Slide 41
Dynamic X-ray Test – Setup
X-ray machine
Optical switch
Power supply
Sourcemeters
O-band laser
+
Optical power meter
Polarization controllers
DAQ
C-band laser
+
Optical power meter

## Slide 42
Dynamic X-ray test – RM efficiency
RM efficiency, defined as:
of the irradiated sample did not change after exposure to 12.3 MGy, following the annealing procedure
V0
V1
Input
Laser
X
OMA

## Slide 43
Optical Spectrum Analyser
SLED C-band
SLED O-band
Polarization Controllers
DFB LASER
Sourcemeters
DAQ
TEC
Sheet resistance
Waveguides
Beam distance: 4.5 cm for sheet resistance - 6.05 cm for cSKT, cWG, oSKT, oWG – 6.65 cm for cFC, oFC, Nonlinearity
Optical switch +
optical powermeters +
optical attenuator
Neutron test – Setup

## Slide 44
Neutron test – Explaining the results

## Slide 45
If we plot the increase in linear loss together with the RIA coefficient for the oWG waveguides, the discrepancy between the two measurements becomes evident.
The RIA coefficient, calculated from the increase in linear loss for the 10.4 mm sample, shows a much smaller increase with neutron fluence compared to the other waveguides. This is likely due to a photobleaching effect that induces partial annealing in the waveguide when high optical power is injected. This observation should be emphasized in a potential publication, as it is both important for understanding the behaviour of the device. However, at the same time, this is promising for our application, since it indicates that the calculated RIA coefficient is likely an overestimation.
N.B. For a mistake in the acquisition loop, I forgot to set the attenuation to 25dB in the idle time, that’s why we have this annealing effect. The power into the waveguide during the test was (calculated from ). Even if this was a mistake, it actually gives us an extra data point which is really useful.
Neutron test – oWG annealing

## Slide 46
X-ray test – GC variation

## Slide 47
Heavy ion test – Setup

## Slide 48
Heavy ion test – TCAD simulation
TCAD mesh

## Slide 49
Heavy ion test – TCAD simulation

## Slide 50
Heavy ion test – TCAD simulation
For a defined value of we can find the corresponding :
Selected for all simulations

## Slide 51
Heavy ion test – TCAD simulations

## Slide 52
Heavy ion test – Recombination mechanisms