## Slide 1
Thin Film SRF Cavity Developments at STFC Daresbury Laboratory
Daniel Seal
On behalf of the TF-SRF team

## Slide 2
Bulk Niobium: The Benchmark
Image © STFC John Dawson
  Q0 = how efficiently a cavity stores energy
  Eacc = average E-field seen by the beam
  The material of choice for ~ 60 years
  Highest Tc, Bc1, Bsh of any element
  Excellent SRF performance with very low RF losses
  Complex and costly fabrication and surface processing
  Approaching fundamental limits
    Q0 = 1010 – 1011 at 2 K
    Eacc < 50 MV/m
P. Kneisel et al., Nuclear Instruments and Methods in Physics Research A 774 (2015) 133–150

## Slide 3
Future Directions: From Bulk Niobium to Thin Films
Image courtesy: C. Antoine
Protection, low secondary emission yield
High Tc SC
S-I-S multilayers
Structure, high thermal conductivity (Copper ?)
External layer, optimized for thermal transfer
High purity Niobium Optimized only for thermal conduction
Native oxide
Unstable upon annealing
RF side
Helium side
Today
Future
Niobium or…?
Native oxide
Not optimized for thermal transfer
C. Antoine, IPAC 2023
RF losses always happen in surface

## Slide 4
Why Thin Films?
Image © STFC John Dawson
Courtesy of C. Antoine (CEA)
Q0
Eacc
Nb : Limits @ 2 K, 1.3 GHz :
Accelerating gradient, Eacc ~ 55 MV/m (± 5 MV/m)
(Geometry : B/Eacc ~ 4.2 mT/(MV/m))
Surface resistance, Rs = RBCS + Rrés.
High field dissipations
Quench
P = const, ↑
Investment +
Power consumption
Q0 ↑ Costs ↓
Investment
Eacc ↑ Costs ↓
Aimed performance
Present state

## Slide 5
Superconductors Being Considered
Material | Tc (K) | Bsh (mT)@ 0 K
Pb | 7.1 | 100
Nb | 9.2 | 219
NbTiN | 17.3 | 439
V3Si | 17.0 | 490
Nb3Sn | 18.3 | 425
NbN | 17.3 | 214
Nb3Al | 18.5-19.1 | 
MgB2 | 39.0 | 170
High Bsh  High Eacc  fewer cavities
High Tc  High Q0  less cooling
Why thin film on copper?
Cheaper than Nb
Higher thermal conductivity
Easily machinable
Courtesy of C. Antoine (CEA)
↓ Infrastructure cost
↓ Cryogenic cost
Best alternative: Nb3Sn/Nb from Sn vapour diffusion – Q0 ~ 1010, Eacc ~ 20 MV/m at 4.2 K

## Slide 6
Why Nb3Sn?
Image © STFC John Dawson
Moving from 2 K to 4.5 K reduces cryogenic power by factor 3!
S. Posen, Supercond. Sci. Technol. 30 (2017) 033004
2 K (Bulk Nb)
4.5 K (Thin Film)
Infrastructure
Operation
Estimated cryogenic costs of ESS (M€):
40
25
4
11
C. Antoine, IPAC 2023

## Slide 7
Thin Film SRF Development

## Slide 8
How a Thin Film SRF Cavity is Developed
Cavity Forming
Surface Polishing
SC property evaluation
RF test
SC Film Coating &
Surface Analysis
Post Treatments
Courtesy of C. Pira (INFN)
Most developments so far have been on planar samples

## Slide 9
R&D on Planar Samples
Rapid, low-cost deposition and testing in custom-built facilities
Simple and consistent substrate preparation
Systematic optimisation of deposition parameters
Easy superconducting measurements & surface analysis
Reduce risk of failure for full cavity coatings

## Slide 10
High Throughput Cryogenic Sample Testing
DC
Used for initial thin film optimisation
What is its Tc?
What is its behaviour under ‘cavity-like’ parallel DC magnetic fields?
Four-point probe
Magnetic Tc
Magnetic field penetration
RF
A ‘good’ DC sample might be ‘bad’ for RF
Crucial measurements of TF RF performance
What is its Rs?
Multiple sample tests per week
7.8 GHz Choke Cavity
Courtesy of L. Smith (STFC), D. Turner (LU)

## Slide 11
Optimising Thin Film Deposition Parameters
RF surface resistance improves at lower power applied to the target cathode
Nb3Sn/Cu
Deposition temperature is a critical parameter for Nb/Cu performance – optimal ~ 530 °C
Nb/Cu

## Slide 12
From Samples to Cavities

## Slide 13
6 GHz Split Cavity Development
How does a cavity behave on a curved surface
Can be deposited in a closed or open geometry
Visual inspections & some surface analysis
Can be utilised for higher Tc materials
Courtesy of N. Leicester, D. Turner (LU)

## Slide 14
Development of a 1.3 GHz Split Cavity
RF design based on single-cell 1.3 GHz TESLA cavity split longitudinally
Cavity manufactured at STFC RAL Space
Aluminium and copper versions manufactured
Designed for testing in LHe-free cryostat
Courtesy of M. Dissanayake Mudiyanselage (LU)
Courtesy of L. Bushnell, M. Beardsley (STFC)

## Slide 15
1.3 GHz Cavity Depositions

## Slide 16
First Nb3Sn-Coated 1.3 GHz Cavity
No cylindrical Nb3Sn target exists
A trial facility developed using 2 x planar Nb3Sn magnetrons
Heating up to 650 °C
First run using deposition parameters established on planar samples
Planar magnetron
Cavity supported by heating stage, in the central chamber.
Successful trial run of first Nb3Sn/Nb 1.3 GHz Cavity
Nb
Nb3Sn
Courtesy of C. Benjamin, R. Valizadeh, J. Conlon (STFC)

## Slide 17
A New Dedicated Cavity Deposition Facility
Cu mock cavity segments
Nb Cylindrical Magnetron
The new facility is currently being developed in ISO 6 cleanroom.
A dedicated facility for single and two-cell 1.3 GHz cavities with fully integrated heating stage.
Initial tests with Nb cylindrical target and mock Cu cavities
Courtesy of C. Benjamin, R. Valizadeh, J. Conlon (STFC)

## Slide 18
1.3 GHz Cavity Testing

## Slide 19
SRF Testing Facilities
CI RF Bunker
SuRF Lab
Low power testing with cryocoolers
High power testing with LHe – including cleanroom & HPR infrastructure

## Slide 20
A High-Throughput Cryogenic RF Test Facility
Mounted 1.3 GHz cavity & heat link
Heat shield & MLI
OVC
Magnetic shields
LLRF System
Conduction cooling with 2.7 W/4.2 K cryocooler

## Slide 21
Facility Commissioning
Successful preliminary tests of a bulk Nb 1.3 GHz cavity
  Base pressure ~ 10-7 mbar
  Base temperature ~ 3.2 K
  Cooldown time ~ 14 hours
Successful preliminary tests of a bulk Nb 1.3 GHz cavity:
  Q0(T)
  Q0(Eacc)
  f(T)
   Rs(T)
Cryocooler based facility ~ 1-2 Cavities/Week

## Slide 22
High Power Cavity Testing
LHe-free facility ~ 2 tests/year
  Only good cavities will be tested after pre-screening in cryocooler based facility
Full Q0 vs Eacc test with LHe
Testing with existing STFC/DL LHe infrastructure mainly used for ESS & PIP-II cavity tests
Upgrades now allow for:
  A single RF system for 650 and 700 MHz, and 1.3 GHz
  P ≤ 200 W, T = 2 & 4.2 K
  Capability for 9-cell tests
Commissioning ongoing:
  Initial cryogenic tests successful
  Plans for first bulk Nb cavity (treated at CEA) RF test in July

## Slide 23
Outlook

## Slide 24
Thin Film SRF Capability at STFC Daresbury Laboratory
Materials characterisation
Planar RF testing
1.3 GHz cavity deposition
6 GHz cavity development
Planar sample deposition
Conduction-cooled RF testing
High-power RF testing
Future accelerator applications
Ultimate Goal:
1.3 GHz Nb3Sn/Cu coated cavities
Entire workflow now established in-house
Ready for an intensive programme of cavity optimisation and qualification
Last 12 years
Now

## Slide 25
International Collaborations
ARIES
(2017-2021) WP15
Small samples, effect of substrate on superconducting thin film quality
IFAST
(2021-2025) WP9
1st Nb3Sn coated Nb cavity
iSAS
(2024-2028) WP3
Nb3Sn coated Cu cavities
QPR tests
R&D on Nb3Sn thin films deposited with PVD and ALD
Functional layers
Magnetic field trapping
Mechanical properties and tunability
EPITA
(2026-2030) WP4
Nb3Sn coated Cu cavities
Horizontal RF test
Conduction cooling
TRL-3
TRL-4
TRL-5
TRL-6
Notes: All WPs and tasks within were led by my colleagues

## Slide 26
Conclusions
  Thin film SRF research at STFC Daresbury Laboratory (ASTeC + CI) has progressed from planar sample studies to cavity development.
  Dedicated infrastructure established for both thin film cavity deposition and cryogenic RF testing of 1.3 and 6 GHz cavities.
  New capabilities enable a coordinated a fully in-house workflow from thin film deposition to RF performance evaluation.
  STFC Daresbury Laboratory is now well positioned for an intensive programme of thin film SRF cavity R&D to develop the next generation of accelerator technology.
  Collaborations with international partners is the key to success

## Slide 27
Acknowledgements
STFC-ASTeC: O. B. Malyshev, R. Valizadeh, L. Smith, J. Conlon, C. Benjamin, S. Pattalwar, A. Blackett-May, A. Vick, A. Wheelhouse, S. Wilde, A. Palmer, A. Wootten, P. McGuinness, K. Sian, T. Sian, O. Poynton, J. Rigby, A. Ashraf, I. Skachko, Z. Bilques, P. Smith, A. Baig
STFC-TD: M. Pendleton, D. Mason, G. Miller, S. Bibby-Trevor, R. McAllister, B. Fell, M. Kane, D. Skae, C. Hill
STFC-RAL Space: M. Beardsley, L. Bushnell
STFC-ISIS: G. Stenning
Lancaster University/CI: G. Burt, N. Leicester, H. Marks, A. Mogheyseh, M. Dissanayake Mudiyanselage, D. Turner
Liverpool University/CI: J. Bradley, S. Simon
EPITA WP4 and iSAS WP3 collaborators (> 15 international organisations, > 50 people)