## Slide 1: ALICE ITS3 MOSAIX sensor measurements and developments for ePIC SVT
Gregor Eberwein (MIT) on behalf of ALICE
CPAD Seattle, 22 Oct. 2026
The work of the MIT HI group and MIT PixElφ Lab was supported by US DOE-NP and by the SVT-EIC project

## Slide 2: ALICE – A Large Ion Collider Experiment
Study of strongly interacting matter at extreme densities (QGP) in heavy-ion collisions at the LHC (CERN)
Low momentum (≲ 1 GeV/c) particle reconstruction
  New inner tracker for Run 4 (2030)

## Slide 3: ALICE Inner Tracking System 3 (ITS3)
Improved low pT physics performance – low material budget, air cooling, small inner radius
→ bent, wafer-scale monolithic active pixel sensors (MAPS) – in total just 6 sensors for entire inner barrel
L0
L1
L2
Beampipe
r=24 mm
ITS2 half-barrel – currently installed
ITS3 half-barrel – engineering model
266 mm
r=19 mm

## Slide 4: ePIC – electron-Proton and Ion Collider
Study of strongly interacting matter in electron-ion collisions at the future Electron-Ion Collider (EIC) at BNL
Low mass detectors with high spatial resolution tracking essential (e.g. scattered e- measurements)
  Tracker installation in 2032

## Slide 5: ePIC Silicon Vertex Tracker (SVT)
2x L0
2x L1
4x L2
Inner barrel - based on
bent, wafer-scale MAPS
84 cm
Outer tracker - based on large-area MAPS of same type
Total ~8.5 m2 of silicon
266 mm

## Slide 6: MOSAIX
300 mm (12 in)
ER2 run: 65nm, stitched, wafer-scale, CMOS, MAPS

## Slide 7: MOSAIX
SEGMENT (SEG)
266 mm
19 mm
babyMOSAIX
ER2 run: 65nm, stitched, wafer-scale, CMOS, MAPS
300 mm (12 in)

## Slide 8: MOSAIX
L0
L1
L2
Beampipe
266 mm
300 mm (12 in)

## Slide 9: MOSAIX
L0
L1
L2
Beampipe
266 mm
300 mm (12 in)

## Slide 10: MOSAIX
L0
L1
L2
Beampipe
266 mm
300 mm (12 in)

## Slide 11: MOSAIX
L0
L1
L2
Beampipe
266 mm
flexible when thinned to <50 µm !
300 mm (12 in)

## Slide 12: MOSAIX design
1x
1x
12x
3 functional blocks:
  1x Left-Endcap (LEC)
  12x Repeated Sensor Unit (RSU)
  1x Right-Endcap (REC)
…
…
…
…
266 mm
SEGMENT (SEG)
144x

## Slide 13: MOSAIX design
12x
12 independent tiles per RSU
Each tile is switched (service node)
Overall: 12 RSUs x 12 tiles = 144 tiles
144 x 160 Mb/s transmission
144 biasing/periphery blocks
288 local power domains
444 × 156 pixels/tile 20.8 x 22.8 µm2 pixels
~ 10 Mpx/SEGMENT
Service Node
Biasing/periphery blocks for each tile
Clk & ctrl

## Slide 14: MOSAIX design
12x
Biasing/periphery blocks for each tile
160 Mb/s data link
per tile
Service Node
Clk & ctrl
12 independent tiles per RSU
Each tile is switched (service node)
Overall: 12 RSUs x 12 tiles = 144 tiles
144 x 160 Mb/s transmission
144 biasing/periphery blocks
288 local power domains
444 × 156 pixels/tile 20.8 x 22.8 µm2 pixels
~ 10 Mpx/SEGMENT

## Slide 15: MOSAIX design
12x
Biasing/periphery blocks for each tile
Power
I/O
8 x 10 Gb/s transmitter with lpGBT logic encoded
4 x global power domains +TX domain
Analog monitoring ADC
2 slow control endpoints
CLK, SYNC, RST
12 independent tiles per RSU
Each tile is switched (service node)
Overall: 12 RSUs x 12 tiles = 144 tiles
144 x 160 Mb/s transmission
144 biasing/periphery blocks
288 local power domains
Power
160 Mb/s data link
per tile
Service Node
Clk & ctrl
444 × 156 pixels/tile 20.8 x 22.8 µm2 pixels
~ 10 Mpx/SEGMENT

## Slide 16: MOSAIX design
12x
Biasing/periphery blocks for each tile
Power
I/O
12 independent tiles per RSU
Each tile is switched (service node)
Overall: 12 RSUs x 12 tiles = 144 tiles
144 x 160 Mb/s transmission
144 biasing/periphery blocks
288 local power domains
Power
160 Mb/s data link
per tile
Service Node
Clk & ctrl
Note: powering from LEC only feasible when limiting the number of enabled tiles
8 x 10 Gb/s transmitter with lpGBT logic encoded
4 x global power domains +TX domain
Analog monitoring ADC
2 slow control endpoints
CLK, SYNC, RST
444 × 156 pixels/tile 20.8 x 22.8 µm2 pixels
~ 10 Mpx/SEGMENT

## Slide 17: MOSAIX wafer probing
12x
On-wafer testing of full MOSAIX production (2 x 25 wafers): max. coverage on functionality, including high-speed tests
Note: Test beam measurements and irradiation campaigns performed on carrier PCB’s, not covered here

## Slide 18: MOSAIX wafer probing – thinned layers
Developed procedure to test 50 µm thinned layers of any size
  Custom handling tool to pick-up and transfer thinned layers
  Custom mylar cover sheet allows to uniformly suck silicon layers flat onto the chuck
Thinned L2 layer
Handling tool
wafer chuck

## Slide 19: MOSAIX wafer probing – high-speed
12x
FPGA
High-speed FPC
Power
Wafer
Probecard
Commercial FPGA (Arria10 + Enclustra baseboard) – uniform test infrastructure across carrier PCB’s/test beams/detector models
Custom high-speed FPC (flexible printed circuit) –simulations and material choice, in-house production

## Slide 20: MOSAIX wafer probing – high-speed
12x
Probecard
Bottom view – needles exposed
Needles
Vertical probe needles, embedded in MLO (multilayer organic material)
  High-speed vertical probecard co-developed with industry partner – low inductance, and impedance matching for stable 10.24 Gbps transmission
Large advancement over standard cantilever probecards (also produced, baseline, no high-speed tests possible)
Probecard
Wafer
Probecard
Wafer
10.24 Gbps
vertical
cantilever
10.24 Gbps

## Slide 21: High-speed capability
12x
Probecard
FPC
Wafer
Breakout
FPGA
FPC
Breakout
FPGA
SEGMENT
Carrier PCB
Wire bonds
5.12 Gbps
PRBS
10.24 Gbps
PRBS
Wafer probing at 10.24 Gbps achieved!
(BER@FPGA <1e-12,
see later)

## Slide 22: Testing sequence
Primary sequence
GSVDD
PSUB

## Slide 23: Testing sequence
1 wafer, 5 SEG
Primary sequence
GSVDD
PSUB
Checking Service registers and Service Nodes

## Slide 24: Testing sequence
1 wafer, 5 SEG
Primary sequence
GSVDD
GAVDD
GDVDD
PSUB
Global power up
Core and service registers

## Slide 25: Testing sequence
1 wafer, 5 SEG
Primary sequence
Tile sequence
GSVDD
GAVDD
GDVDD
PSUB
1-by-1 tile testing: power, registers, data, DACs, pixels

## Slide 26: Testing sequence
Primary sequence
Tile sequence
GSVDD
GAVDD
GDVDD
PSUB
1-by-1 tile testing: power, registers, data, DACs, pixels
1 wafer, 5 SEG
Tile data transmission with other active tiles – Bit Error Count
NO PIXEL ACTIVITY
READOUT
Weakness solved: unshielded in-metal stack area found and closed (next run)
1 wafer, 5 SEG

## Slide 27: Testing sequence
1 wafer, 5 SEG
Primary sequence
Tile sequence
GSVDD
GAVDD
GDVDD
PSUB
1-by-1 tile testing: power, registers, data, DACs, pixels
Defect pixels – one RSU

## Slide 28: Testing sequence
1 wafer, 5 SEG
Primary sequence
Tile sequence
GSVDD
GAVDD
GDVDD
PSUB
1-by-1 tile testing: power, registers, data, DACs, pixels
Threshold scan – one tile

## Slide 29: Testing sequence
1 wafer, 5 SEG
Primary sequence
Tile sequence
High-speed sequence
GSVDD
GAVDD
GDVDD
TXVDD
PSUB
High-speed serializer and full data path

## Slide 30: Testing sequence
1 wafer, 5 SEG
Primary sequence
Tile sequence
High-speed sequence
GSVDD
GAVDD
GDVDD
TXVDD
PSUB
High-speed serializer and full data path
300s
1 SEGMENT
High-speed channel Bit Error Rate (BER) PseudoRandomBinarySequence (PRBS)
300s
Channel 0
Channel 1
Channel 2
Channel 3
Channel 4
Channel 5
Channel 6
Channel 7

## Slide 31: Testing sequence
Primary sequence
Tile sequence
High-speed sequence
GSVDD
GAVDD
GDVDD
TXVDD
PSUB
MOSAIX chip is (nearly) fully functional – crosstalk on tile links addressed in next submission (ER3)

## Slide 32: Layer yield – maximum layer size
from 40 wafers

## Slide 33: Layer yield – maximum layer size
Effort on yield improvement in collaboration with the foundry ongoing
At >98% tile yield, we can build:
2x ITS3 or
1x SVT half barrel
from 40 wafers

## Slide 34: Wafer probing extensions and SVT QC
SVT foresees a production of:
  75 ER3 wafers (inner barrel)
  330 LAS wafers (outer barrel)
  LAS: Large Area Sensor – MOSAIX derived, with same pad structure
SEGMENT
Probecard
LAS
75x
330x

## Slide 35: Wafer probing extensions and SVT QC
SVT foresees a production of:
  75 ER3 wafers (inner barrel)
  330 LAS wafers (outer barrel)
  LAS: Large Area Sensor – MOSAIX derived, with same pad structure
Large volume requires fast QC procedures - paralellization required:
SEGMENT
Probecard
LAS
Probecard
LEC
Probecard
75x
330x

## Slide 36: Wafer probing extensions and SVT QC
SVT foresees a production of:
  75 ER3 wafers (inner barrel)
  330 LAS wafers (outer barrel)
  LAS: Large Area Sensor – MOSAIX derived, with same pad structure
Large volume requires fast QC procedures - paralellization required:
  LEC + REC probecards -> allows full powering of all tiles in parallel
SEGMENT
Probecard
LAS
Probecard
Probecard
LEC
REC
Probecard
Probecard
75x
330x

## Slide 37: Wafer probing extensions and SVT QC
SEGMENT
Probecard
LAS
SVT foresees a production of:
  75 ER3 wafers (inner barrel)
  330 LAS wafers (outer barrel)
  LAS: Large Area Sensor – MOSAIX derived, with same pad structure
Large volume requires fast QC procedures - paralellization required:
  LEC + REC probecards -> allows full powering of all tiles in parallel
  Multiple dies in parallel
Probecard
Probecard
LEC
REC
LAS
SEGMENT
Probecard
Probecard
Probecard
Probecard
Probecard
Probecard
75x
330x

## Slide 38: Wafer probing extensions and SVT QC
Vertical probecard for LEC (current)
Additional REC probecard (to be produced)
-> Full chip powering (all tiles in parallel)
LEC
REC

## Slide 39: Wafer probing extensions and SVT QC
SEGMENT
Probecard
1x
Parallelization of sensor testing:
Up to 3 SEG in parallel (depending on arrangement)

## Slide 40: Wafer probing extensions and SVT QC
Probecard
2x
Probecard
Parallelization of sensor testing:
Up to 3 SEG in parallel (depending on arrangement)

## Slide 41: Wafer probing extensions and SVT QC
Probecard
3x
Probecard
Probecard
Parallelization of sensor testing:
Up to 3 SEG in parallel (depending on arrangement)
Adaptable to LAS
Estimated reduction of total QC testing time for one site from ~560 to ~110 calendar days!

## Slide 42: Summary
MOSAIX chip (nearly) fully functional
  On track for ER3 submission by end of year
  Transmission weakness found and fix implemented
  Manufacturing yield improvement ongoing
Testing infrastructure for highly complex chip in full operation
Wafer probing at 10.24 Gbps achieved
  Essential to fully exercise all chip blocks on-wafer
  Custom high-speed chain wafer-to-FPGA developed
High-volume SVT production QC readiness
  Dual-sided powering and multi-probecard system

## Slide 43: BACKUP

## Slide 44: Mechanics integration

## Slide 45: Block digaram detailed

## Slide 46: Analog pixel frontend

## Slide 47: MAPS pixel cross section

## Slide 48: Testbeam - detection efficiency / fhr

## Slide 49: Yield – thinned layers example
Thinned layers tile yield
1x L0: 99%
1x L1: 99%
2x L2: 73% / 63%

## Slide 50: SVT

## Slide 51
LEC
12x RSU
REC
12 tiles,12 pixel variants
Each tile is switched
Overall: 12*12 = 144 tiles
144 * 160 Mb/s transmission
144 biasing/periphery blocks
288 local power domains
One tile ~ one pixel sensor
1x Segment
8x 10 Gb/s transmitter
lpGBT logic/encoded
5x global power domains
Analog monitoring/testout
Slow control/clk/sync/rst
Service nodes
5x global power domains
Tile
Mosaix anatomy
Notes: 48 service nodes, 24 low swing buffers, 444x156 ~70k pixels per tile, 20.8 x 22.8 um
On SRV nodes:
A slow control endpoint accessible through the SRV interface • Controls the SBB tile configuration – Data buffers, driver strengths, etc • Controls the analog monitoring – Supply voltages – Bias currents – Bias voltages • Controls the tile power switches • Controls the tile reset • All services nodes must be configured before global supplies are switched on!
Power pads takes up most of real-estate – E-links (all differential CLPS): • Clock - input • Reset - input • Sync - input • 2x slow control – SRV and CORE input/output – Data (all differential): • 8x high-speed channels (4 top, 4 bottom) – 2x analog monitoring • No connection to FPC – 2x testout • No connection to FPC

## Slide 52: Wafer prober upgrade
New platen, allowing for two probecards at once:
Cantilever for REC powering (to be produced)
Vertical for LEC (as is)
Requires new microscope travel range
Installation complete, incl. dark box (sources, laser)
Taken into operation again