## Slide 1: Solvent coating of wavelength shifting materials for next-generation photodetector systems
Rado Razakamiandra
October 21st, 2026
CPAD 2026 at Seattle

## Slide 2: Workflow
WLS powder
Solvent
substrate
Spectroscopy
Spraying using an airbrush
Before/after cycle
Solvent: solution to dissolve the wavelength-shifting powder
Substrate: the material on which the WLS is to be deposited
Spectroscopy:
  Measurement of the WLS-shifted and transmitted light.
  Measurement of light attenuation to check coating uniformity.
Coating thickness measurement
Transmittance measurement at VUV range

## Slide 3: Motivation of solvent coating
Noble liquid detectors (dark matter, neutrino experiments, nuclear and particle physics):
  Detecting scintillation light (128 nm for LAr) requires wavelength shifting to the wavelength range the PMTs or SiPMs can detect.
Investigation of solvent coating of p-terphenyl (pTP) onto an acrylic substrate:
  Low cost
  Can accelerate coating a large-area photodetector once automated.
Advantages of using an acrylic:
  Low weight
  More radiopure than a typical glass substrate.
PMMA
DELTA PhotoCollector (F. Cavanna, W. Shi’s talk)

## Slide 4: Selection of materials
Need: material transparent to the emission spectrum of pTP
UV-transparent acrylic cutoff: ~260 nm
Acetone, Toluene, and THF can all dissolve pTP
Cutoff of acetone: ~330 nm  not selected
Toluene is used for consistency across samples.
pTP absorption (blue) and emission (red) spectra
Transmittance of the acrylics
Transmittance of the solvents

## Slide 5: Attenuation length of the 320 nm and 350 nm light in the UV-transparent acrylic
Method:
  Perform a Beer-Lambert fit on the transmittance of the UV-transparent acrylics with different thicknesses
  Where is the source, is the attenuation coefficient, and the thickness.
Measurement using a UV-vis spectrophotometer:
  Stacks of multiple acrylic sheets were made to achieve the desired thickness (no bulk acrylic available).
  We accounted for losses due to Fresnel reflections at the air/acrylic and acrylic/air interfaces.
Attenuation lengths :

## Slide 6: Setup of the spectroscopy
UV source
Spectrometer
Acrylic sample
Fiber optics
UV LED
Spectrometer
air
UV LED:
  285 nm for the pTP emission measurement.
  340 nm for the uniformity scan of the samples
Spectrometer: OceanOptics USB2000+ with a wavelength range of 200 nm to 1000 nm

## Slide 7: pTP deposited samples and uniformity
pTP samples were prepared by hand spraying
  No 285 nm light gets through
  Reemission at ~320 – 450 nm
  Spike at 470 nm: noise
A 340 nm wavelength was used to scan the sample’s uniformity before and after the cryogenic cycle
  Mean transmission unchanged
  Spread increased slightly; no visible detachment
Before cryogenic cycle
After cryogenic cycle
Integral of the spectra normalized by the source.
Number of spectra
Transmission of the pTP-deposited sample. Source wavelength: 285 nm

## Slide 8: Thickness and roughness of the pTP layer
substrate’s surface
Variation of the pTP deposited layer
The measurement was done with white-light interferometry
Profile lines on the surface of the pTP-deposited layer and the acrylic substrate.
Example of sample’s thickness and roughness:
  pTP layer thickness
  Surface roughness of

## Slide 9: Setup of wavelength shifting efficiency measurement
Instituto de Física Corpuscular (IFIC), CSIC and Universitat de València, Valencia, Spain
Measurement done at IFIC
The deuterium lamp is used for this measurement
Monochromator: scans the wavelength
Atmosphere of the sample and PMT: argon gas

## Slide 10: Wavelength shifting efficiency measurement at IFIC
Areal density:
   per-sample relative uncertainty of
Transmittance (T): corrected by the PMT’s quantum efficiency
  at 130 nm for
  : UV photons emitted (all directions) per incident VUV photon
  K: collection factor, fraction of the emitted UV photons that reach the photocathode
    K rises with density
  MC of the IFIC setup: over the model parameter range (preliminary MC)

## Slide 11: Solvent coating automation using a repurposed 3D printer
Goal: improve sample reproducibility by limiting the sprayer's degrees of freedom.
Sprayer: airbrush
  Switch: operated by a servo motor
Sprayer’s motion: controlled by the printer board.
Sample size: tunable, up to , limited by the printer size
Operational; uniformity and efficiency characterization in progress.
Scaling up: using larger printer (up to and an industrial sprayer gun.
Hand-sprayed
3d printer sprayed

## Slide 12: Summary and Future works
Solvent coating technique developed from TRL1 to TRL4 over 2 years with local small funds support
Spray deposition on acrylic: a PhotoCollector option for DELTA (F. Cavanna), alongside industrial PVD (M. Vicenzi)
pTP spray-coated on 3 mm UVT acrylic; no detachment after one cycle
IFIC, 130 nm: Transmittance rises from 150 µg/cm² to 1100 µg/cm²
≈ 65–100% with the MC collection factor (preliminary)
Characterization of the automated sprayer:
  Measuring the pTP layer’s uniformity and deposition efficiency
Diffuse reflectance and transmittance at 350 nm vs density:
  film scattering; fixes K in the MC
Integrating-sphere quantum yield of spray-deposited films (with BNL)
Building a 15 × 15 cm² prototype: coated plate + WLS-doped plate + SiPMs
A technical paper is in preparation, coming out soon.

## Slide 13: Backup

## Slide 14
Backup: ε_WLS with the MC collection factor (preliminary)
K from pTP-SD-sim (F. Cavanna): MC of the IFIC setup
  gap 7 mm, MgF₂ window, Ø 23 mm photocathode, measured beam profile
  continuous pTP film; re-emitted light scattered in the film
  scattering parameters bracketed a priori, not fitted
ε_WLS = T / K: band over the bracket; points for two example parameter sets
  Flat within errors
Lower bound 2T (K ≤ 50%) is 2.5–5× below