## Slide 1: TCAD simulation I E. Giulio Villani
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 2
Overview
Introduction, needs for TCAD simulations
Transport regimes and related equations
Discretization techniques: meshing
Discretization of semiconductor equations: Scharfetter-Gummel technique
Examples
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 3
Introduction
TCAD (Technology Computer Aided Design) divides into three groups:
  Process simulation, i.e. simulation of fabrication process steps (oxidation, implantation, diffusion…)
  Device simulation, i.e. simulation of the thermal/electrical/optical behavior of electronic devices,(IV,CV, frequency response…)
  Device modeling, i.e. creating compact behavioral models for devices for circuit simulation (SPICE, Cadence…)
Epitax growth
N++ implant
P++ implant
SiO2 etch
1
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 4
Introduction
  Reasons why TCAD simulations are needed:
    Market demands cycle of design to production of 18 months or less. Typically 2-3 months required for wafer tape out implies short time for development
    Reduce cost to run experiments on new devices and circuits
Shrinking product life cycles in semiconductor industry over time
2
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 5
Introduction
  Main components of semiconductor device simulation include description of electronic structure, driving forces and transport phenomena
  The two kernels of semiconductor transport equations and fields that drive charge flow are coupled to each other and needs solving self-consistently
Electronic structure/lattice dynamics
Transport equations
Electromagnetic Fields
Device simulation
3
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 6
Transport regimes
L: device length
le-e: electron-electron scattering length le-ph: electron-phonon scattering length : electron wavelength
Usually only the quasi-static electric fields from the solution of Poisson’s equation are necessary for EM solutions
Transport regime in semiconductors depends on length scale
Modern Silicon technology already requires tools to describe transport in quantum regime [D. K. Ferry and S. M. Goodnick, Transport in Nanostructures, 1997]
4
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 7
Transport regimes
Charge carrier dynamics in Si detectors usually does not require QM
Semiclassical laws of motions apply
Drift-diffusion equations are valid, provided the electron gas is in thermal equilibrium with lattice temperature (Tn = TL)
(Segre’, Nuclei and Particles, Vol. II)
5
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 8
Drift diffusion model
The semiconductor equations derived from 1st moment of BTE are referred to as Drift Diffusion model
The model consists of Poisson's equation, continuity and current density equations for electrons and holes
They express charge and momentum conservation
Their self-consistent solutions are obtained via discretization, using finite element methods (FEM)
6
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 9
Discretization and meshing
The device simulations process consists of two steps:
1: The test volume is obtained through grid generation (‘mesh generation’ )
2: Solve the discretized differential equations using Finite-Boxes method (box integration method) . This method integrates PDEs over the test volume.
7
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 10
The meshing used in most finite elements methods (FEM) relies on Delaunay triangulations:
the interior of the circumsphere of each element contains no mesh vertices.
The Delaunay triangulation of a discrete point set P in general corresponds to the dual graph of the Voronoi diagram for P
the set of all locations x closest to Pi than to any other point of the grid
The Delaunay triangulation with all the circumcircles and their centres
Discretization and meshing
Connecting the centres of the circumcircles produces the Voronoi diagram (in red).
8
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 11
Voronoi boxes do not overlap (each circumcircle does not include a point of another triangle). Each can be uniquely assigned to its corresponding grid points.
Voronoi boxes do overlap (each circumcircle does include a point of another triangle). Each cannot be uniquely assigned to its corresponding grid points. Wrong volumes calculated
Correct Delaunay triangulation guarantees element-volume conservation, important in many problems (diffusion, charge generation, et cetera)
Delaunay triangulation maximizes the minimum angle.
Discretization and meshing
9
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 12
Discretization of equations imposes some constraints on spatial and temporal mesh size
Mesh size should be smaller than Debye length (i.e. the characteristic length for screening of field by charges) where charge variations in space have to be resolved
Discretization and meshing
10
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 13
Also temporal ‘mesh’ size should be smaller than the dielectric relaxation time tdr (i.e. time it takes to charge fluctuations to decay under the field they produce)
Time interval bigger than tdr might give unrealistic transient results (‘oscillations’ in estimated transient currents)
: :
Discretization and meshing
11
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 14
Box integration method
Discretization of Poisson’s and continuity equations is done via Box Integration method
The LHS of equations is transformed via Gauss’ theorem and integrated over a Voronoi box Ωk of point Pk
12
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 15
Example of Poisson’s discretization
Assume that the electric potential is linearly varying over each elementary domain
,
,
Box integration method
13
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 16
Components of D vector along sides Li,j,k
Flux of D vector associated to node k:
Discretization of RHS is obtained by multiplying the node value of charge by the area of the portion of the Voronoi box
+ ]
Box integration method
14
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 17
Summing over all points Pk of Voronoi boxes
Same approach to discretize continuity equations for electrons and holes
Box integration method
15
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 18
Scharfetter-Gummel discretization
In case of no strong generation-recombination current density varies little within each domain
Still this implies an exponential dependence of electron / hole density with position along grid’s edge
Using previous discretization method would require very dense mesh: Scharfetter-Gummel technique includes such dependence, requiring less grid points [D. L. Scharfetter and H. K. Gummel, “Large-signal analysis of a silicon read diode oscillator,” IEEE Trans. Electron Devices, vol. ED-16, pp. 64–77, Jan. 1969].
from
16
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 19
Assume u varies linearly along the edge and current density ≃ constant over the domain
Define reduced current and assume and average diffusion along the edge
Obtain first order equation in n along the edge
Scharfetter-Gummel discretization
17
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 20
Integrate from node i to node j, i.e. for lk=[0, Lk]
Obtain expression relating potential and carriers concentration
Scharfetter-Gummel discretization
18
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 21
Obtain the flux of current density relative to node k
Scharfetter –Gummel discretization requires less fine mesh as the exponential dependence of carriers concentration is included in the discretization scheme
It also depends on boundary values, i.e. 2D and 3D cases can be reduced to local 1D cases
Scharfetter-Gummel discretization
19
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 22
Examples from Synopsys TCAD (more on this from N. Owen lectures)
Beside electrical simulations, simulation of processes of device fabrication is possible
Most of the typical fabrication process steps can be simulated
Simulated process steps for LGAD fabrication
p++
P-epi
Nwell-GR
Nwell
Simulation examples
20
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 23
Simulation examples
High energy implants of ions can be simulated, either analytically or via MC
Creation of defects following implantation can be simulated
SIMS and Pearson IV distribution – 31P
SIMS, Pearson IV distribution and MC run – 11B
21
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 24
Simulation examples
At least with As, MC (SRIM) and SPROCESS predictions on doping seem to agree within ≈ 20%
Note: SRIM assumes amorphous Si, <100> used for SPROCESS, but 1D
SRIM (Stopping and Range of Ions in Matter, http://www.srim.org/)
22
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 25
Electrical simulation of a CMOS sensors (OVERMOS)
A TCAD model of fabrication process of OVERMOS has been developed to investigate and predict the performances of the sensor
Simulation examples
Photograph of OVERMOS test structure and simulated cell
Photograph of OVERMOS cell and .gds layout
40um
40um
23
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 26
Simulation examples
Internal field configuration vs. bias and temperature
DC and AC characteristics can be obtained from the simulated model
3D simulated cell
Xsection showing potential and depletion Vbias = 10 V
GND
Vbias
SiPoly to simulate non reflective BC
Surface plot of x-field and depletion Vbias = 10 V
T = 300 K
24
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 27
Charge collection is simulated using laser light injection and compared with test results
Laser beam is 5 x 5 um2 around 4.5 ns pulse width, 1064 nm wavelength,
These values are introduced in the simulator
Test setup for charge collection measurement
Simulation examples
Charge is injected via laser at three different locations on cell. Results are mirrored to obtain a map of collected charge vs. position
25
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 28
Effects of SiO2 reflection and attenuation of IR light can be implemented
Quantum yield of optical generation, polarization, tilting, pulse width et cetera can all be included in the simulation
TCAD simulations of non-irradiated OVERMOS reproduce experimental results, both in DC and in CC, with maximum discrepancy of the order of 20%
Simulation examples
Transient of charge collection measurement and simulation
26
Instrumentation Training Lectures, Oxford 30/05/2023

## Slide 29
Introduction to simulation
Needs and transport regimes
Meshing and discretization. Intro to DD model discretization. SG method
Some examples of TCAD simulations: process and electrical device simulations, charge collection
27
    Thank you
    giulio.villani@stfc.ac.uk
TCAD and simulation I
Instrumentation Training Lectures, Oxford 30/05/2023