## Slide 1: HEP InP Update June 22, 2026

## Slide 2: Undoped Structure
Anode
Cathode
L = 5mm
350µm
InP
x
y

## Slide 3: Importing Optical Generation Profile into SDE
;;; 4. Load optical generation profile
;; -- Get the node number of the opticalprofile tool for this experiment --
(define ref_node "@node|opticalprofile@")
;; -- Construct path to the scaled optical generation file --
(define OptFile (string-append "scaled_Gopt_node" ref_node ".plx"))
;; -- Define the 1D external profile --
(sdedr:define-1d-external-profile "1d_opt_def" OptFile
"Scale" 1.0 "Range" 0 T)
(sdedr:define-refeval-window "globalopt_window" "Line"
(position 0 0 0)
(position L 0 0))
;; "Positive" = profile runs from Y=0 upward (cathode to anode)
(sdedr:define-analytical-profile-placement "1d_opt_place"
"1d_opt_def" "globalopt_window"
"Positive" "NoReplace" "Eval")
T = Thickness (350µm)
L = Lateral length of the device (5mm)

## Slide 4: Importing Optical Generation into SDevice
#if "@light@" == "on"
Optics( OpticalGeneration( ReadFromFile() ) ) #endif
File {
Grid = "@tdr@"
Parameters = "@parameter@"
Plot = "@tdrdat@"
Current = "@plot@"
Output = "@log@"
OpticalGenerationInput= "@tdr@"
}

## Slide 6
Anode is located at y=0
Cathode is located at y=350

## Slide 7
Temp = -15°C
Linear

## Slide 8
Temp = -15°C
Log

## Slide 9
Temp = 15°C
Linear

## Slide 10
Temp = 15°C
Log

## Slide 11
Temp = 30°C
Linear

## Slide 12
Temp = 30°C
Log

## Slide 15: Still waiting for trap on simulation results

## Slide 16: Basic Schematic
Gold (100nm)
Chromium (10nm)
InP:Fe (350µm)
Chromium (10nm)
Gold (100nm)
5mm
5mm
2mm
2mm
Incident Beam

## Slide 17: 2D TCAD Simulation
Anode
Cathode
L = 5mm
350µm
InP
x
y
Chromium
Gold
10nm (0.01µm)
100nm (0.1µm)
Chromium
Gold

## Slide 19
Temp = -15°C
Linear

## Slide 20
Temp = -15°C
Log

## Slide 21
Temp = 15°C
Linear

## Slide 22
Temp = 15°C
Log

## Slide 23
Log

## Slide 24: Still waiting for trap on simulation results

## Slide 25: Backup Slides

## Slide 26: Contact Check
2mm
5mm

## Slide 27
Anode is located at y=0
Cathode is located at y=350