## Slide 1
E. G. Villani
TCAD simulation of
CMOS LGAD
E.G.Villani, Oxford, Sep. 2021

## Slide 2
Overview
Introduction: UFSD based on LGAD for HGTD
Initial investigation on Thin LGAD: TCAD process and simulation
Summary and Conclusions
1
E.G.Villani, Oxford, Sep. 2021

## Slide 3
ATLAS HGTD aimed at suppressing pile up effects in ITK
Individual sensor size of HGTD 1.3 x1.3 mm2, for a total area 6.4 m2 and 3.6 Mchannels
Timing measurement at track level, rather than at individual hit
‘Real’ 4D tracking would require higher spatial resolution, increasing power requirement and RO complexity
Ultimately a monolithic approach, combining sensors and RO on the same substrate, might offer the solution
E.G.Villani, Oxford, Sep. 2021
1
  LGAD for HGTD

## Slide 4
LGAD project (Oxford, RAL, Birmingham, OU) with foundry Te2v focused on HGTD specs (ATLAS – CMS?): currently testing the fabricated devices
A number of different commercial foundries propose SiPM for imaging, TOF
4 mm
1 mm
2 mm
2x2-1 mm
E.G.Villani, Oxford, Sep. 2021
WF2 diced
2
  LGAD for HGTD

## Slide 5
TJ SiPM made of SPADs arrays with pull-up resistor. Fully depleted SPAD using HR epi material in 180 nm CMOS process. Epitaxial thickness of 5.5 – 9 um
Investigation using TCAD of possible performances of similar solution
E.G.Villani, Oxford, Sep. 2021
3

## Slide 6
Time resolution in time-tagging detector consists of several terms
  minimized by high SR (slew rate) // CFD
  minimized high RO TI SNR // high SNR of sensor
  Landau fluctuations to be evaluated in each specific scenario (MIP, light…)
  minimized by uniform fields , e.g. thickness << pitch
  conversion time (might be an issue later on)
Also from Ramo’s:
Decrease thickness d increases SR: 10 um (our current Te2v devices have 50 um epi)
At the same time decrease C to avoid noise increase: 50 um cell (current Te2v devices 1 x 1 mm2)
E.G.Villani, Oxford, Sep. 2021
4
  ‘Thin’ LGAD

## Slide 7
E.G.Villani, Oxford, Sep. 2021
5
Started from real Te2v process information
Modified some steps (i.e. avoid excessive substrate diffusion, reduce GL/JTE doping)
This process should be available by most CMOS foundries
LGAD only
JTE P31 IMPLANT (7,27)
EPITAX growth
10 um
SUBS
DRIVE IN [GL implant]
Oxidation
Resist depo
JTE etch
Strip resist
JTE drive in
Resist depo
Pstop implant
Strip resist
Resist depo
ACTIVE etch
Strip resist
Oxidation
Resist depo
B11 GL implant
Strip resist
Resist depo
SHN implant (A&JTE)
Strip resist
LTO deposit
ACTIVATION
LTO DENSIFICATION
Resist depo
CONTACTS ETCHING
Strip resist
METAL DEPOSITION
Electrodes with Al WF
in SDEVICE
REMESHING FOR DEVICE
SIMULATION
IV plots
Charge collection
SDEVICE
SPROCESS
  TCAD Simulation

## Slide 8
E.G.Villani, Oxford, Sep. 2021
6
  TCAD Simulation
TCAD simulations compare well with Te2v process
Thermal oxide growth, MC B implantation, Analytical P/As implantation have been SIMS compared

## Slide 9
  Thin epitaxial LGAD
Vbias 40 V
50 um cell, with 10 um HR epitaxial thickness
Diffusion from substrate into the epitaxial affects its overall doping :change the drive in to reduce it
Effective epi thickness < 10 um, with depletion at relatively low voltage
JTE still needed to increase the BV
For array one might reduce p-stop width to achieve total depletion, but need to investigate X-talk
LGAD
PIN
50 um
Cathode
P-stop
JTE
GL
Substrate
Epi
PIN
LGAD 1.35e13 200
Epi
E.G.Villani, Oxford, Sep. 2021
7
10 um
P++
P++

## Slide 10
Around 5 um of epi are fully depleted  30 V
to maximise speed of response the velocity of carriers should be saturated (F >= 1e4 V/cm)
JTE effective but can be optimized
  Thin epitaxial LGAD simulation
LGAD
1
2
LGAD
PIN
GL @ different Vbias
LGAD
PIN
Vbias 40 V
Vbias 40 V
E.G.Villani, Oxford, Sep. 2021
8
GL
Vbias

## Slide 11
IV plots show BV around 50 V for LGAD 1.35 200 and around 90 V for PIN
CV @ depletion around 50 fF
  Thin epitaxial LGAD simulation DC and CV
T = 300 K
F = 1e4 Hz
E.G.Villani, Oxford, Sep. 2021
9

## Slide 12
  Thin epitaxial LGAD simulation Slew rate
Vbias [V] | Ipk [uA]PIN | SR max [nA/ps] | Ipk [uA] LGAD | SR max [nA/ps]
20 | 1.21 | 118 | .25 | 28
40 | 1.28 | 127 | 1.86 | 105
60 | 1.33 | 130 | 6.9 | 138
Initial transient of 100 ns to bias the device
Central  MIP hit @ 100 ns ( constant 80 e/um)
Peak current Ipk for PIN  1.3 uA
Peak current Ipk for LGAD increases with Vbias
SR = dI/dt : SR(I)MAX up to 138 nA/ps
T = 300 K
E.G.Villani, Oxford, Sep. 2021
10

## Slide 13
  Thin epitaxial LGAD simulation
  Slew rate
1mm LGAD
Te2v 1mm LGAD
Te2v 1mm PIN
Te2v 1mm LGAD
Thin 5 um LGAD (TCAD)
T = 300 K
E.G.Villani, Oxford, Sep. 2021
SR comparison with Te2v devices
Predicted increased SR  x 5
11

## Slide 14
  Thin epitaxial LGAD simulation collected charge
Vbias [V] | Qcoll PIN [e]@ 5ns | Qcoll LGAD [e] @5ns
20 | 830 | 640
40 | 857 | 2542
60 | 905 | 9680
Collected charge from integration of device current
Around 10 gain charge max w.r.t. PIN
T = 300 K
E.G.Villani, Oxford, Sep. 2021
12

## Slide 15
Vbias [V] | Vpk [mV]PIN | SR max [V/ps] PIN | Vpk [mV] LGAD | SR max [mV/ps] LGAD
20 | -11 | -0.23 | -2.2 | -0.03
40 | -11 | -0.24 | -16.8 | -0.19
60 | -12 | -0.25 | -61.2 | -0.88
The RO (integrated or not) is AC coupled from the UFD
Cin  CUFD (also area limitations)
Rin : S/N  10 for Ipkmin
transient voltage across Rin
(SRLGAD / SRPIN )MAX  3.5
(SRLGAD )MAX  0.9 mV/ps
  Thin epitaxial LGAD simulation RO requirements
T = 300 K
E.G.Villani, Oxford, Sep. 2021
13

## Slide 16
  Thin epitaxial LGAD simulation DC and CV
‘Ultimate’ time resolution dictated by the jitter of the sensor
overestimated jitter (F: excess noise factor)
E.G.Villani, Oxford, Sep. 2021
14

## Slide 17
Some initial studies on high granularity and very thin CMOS LGAD with a view to investigate 4D tracking
Cell investigated is 50 um size for 10 um epitaxial thickness
TCAD simulations built on ‘real’ process, used for current LGAD devices (Te2v)
Two different GL profiles investigated, minimum BV  62 V for LGAD and  90 V for PIN
Preliminary simulations show around 138 nA/ps SR (i.e.  x5 than our current LGAD) and gain .w.r.t. PIN in charge collected around 10
Sensor’s jitter < 1 ps achievable
Additional studies on array of cells / 3D cells are planned THANK YOU
  Summary and Conclusions
E.G.Villani, Oxford, Sep. 2021
15