Review: "Characterization of Indium Phosphide Detectors
with Red Laser TCT and Minimum-Ionizing Charged Particles"

Internal review document

Colour coding: Must fix (error or missing content required for a complete paper); Suggestion (would strengthen the paper); Note (housekeeping / open to-do items).

# Abstract

- [Must fix] Fluence inconsistency: The abstract states "up to 10^15 n_eq/cm^2" but only 10^13 and 10^14 samples are characterized; 10^16 sensors show immediate breakdown. Revise to clarify that irradiation was performed to 10^16, but results are reported for the characterizable range of 10^13-10^14 n_eq/cm^2.

- [Must fix] Quantify "modest" radiation damage: State a representative CCE value at 10^14 n_eq/cm^2 relative to unirradiated at a given bias voltage to substantiate the qualitative claim.

- [Suggestion] Add model outputs: The model also extracts electron mobility, trapping time, and trapping length — arguably the most physically interesting outputs — which should appear in the abstract.

- [Suggestion] Temperature dependence: Improved signal recovery at -20°C is a key practical result absent from the abstract.

- [Suggestion] Timing resolution number: The ~25-30 ps timing resolution appears only in the conclusions. State it (with conditions) in the abstract.

# Introduction

- [Must fix] Fluence inconsistency: Introduction says "up to 10^14 n_eq/cm^2", abstract says "10^15", Methods lists four fluences including 10^16. Bring all three into agreement.

- [Suggestion] Strengthen physics motivation: Add one sentence explicitly connecting the high electron mobility to the expected timing performance before the section roadmap.

- [Note] Section title cross-reference: Introduction refers to "Section X" as "Signal Modeling"; actual title is "Signal Modeling in InP" — check all cross-references.

# Methods

- [Suggestion] Nuclear isomer / activation: move to Results: The gamma spectroscopy observation of 114m-In (49.5-day half-life, 190 keV transition, decay to 114-Cd/114-Sn) is an experimental result and belongs in Results, where it also directly grounds the activation caveat in the conclusions. The practical reason for the long cool-down period can remain in Methods.

- [Suggestion] Fluence scaling caveat: The Si-based scaling convention is noted as possibly not applying to InP, but the issue is not revisited quantitatively in the damage parameter discussion. Either quantify the uncertainty here or cross-reference the results section.

- [Note] Open to-do: fluence numbers: Confirm n_eq/cm^2 estimates from Gregor (Ljubljana) — flagged in TODO.md.

- [Note] Open to-do: author list: Add Ljubljana co-authors; confirm ANL and UIC affiliations (TODO.md).

- [Note] Open to-do: seed grant number: Acknowledgments placeholder "no. xxx" must be filled before submission.

# Signal Modeling

- [Suggestion] Justify hole neglect quantitatively: State an order-of-magnitude estimate of the hole contribution to the pulse integral from the mobility ratio, rather than just asserting it is negligible.

- [Suggestion] CCE formula limiting cases: Confirm in the text that the CCE formula gives 1 at τ→∞ and 0 at τ→0, to help readers follow the derivation.

- [Suggestion] Restore waveform analysis sketch: The commented-out schematic figure illustrating the drift triangle, bandwidth, echo train, and ring would substantially help readers follow the three-stage instrumental model.

- [Note] Stopping power file: Confirm that stopping_power_modeling_earl.tex is deliberately excluded from the current build.

# Results and Discussion

## Laser TCT

- [Must fix] No numerical results stated: The laser TCT subsection has almost no numerical prose. State representative values for pulse height, signal length, rise time at two or more bias voltages from Fig. 3.

- [Must fix] Polarity asymmetry unexplained: The polarity asymmetry is shown but not explained or quantified. State the physical reason (electron vs hole drift, mobility asymmetry) and give a representative amplitude ratio between the two polarities.

- [Suggestion] Reconcile figure captions: Fig. 2 caption says "displaying negative bias voltages" but Fig. 3 shows both polarities. Unify the caption language and clarify which figure shows what.

## Betascope, unirradiated (Sr-90)

- [Must fix] Quantitative results missing: Rise times (~200 ps) and timing resolutions (~30 ps) are stated in a single sentence without conditions (bias, temperature, polarity) and without reference to specific figure panels. Add conditions and figure references.

- [Must fix] Physically imprecise phrasing: "Inverse relationship between pulse height and temperature" is ambiguous — if pulse height increases as temperature decreases, say that directly.

- [Suggestion] Quantify temperature effect: State the magnitude of the improvement from +20 to -20°C in pulse height and collected charge for the unirradiated device.

- [Suggestion] Broaden comparison to silicon: The comparison to silicon currently cites only silicon LGADs (with gain). Add a comparison to standard silicon pin diodes, which is more relevant for a material without charge multiplication.

## Signal model fits, unirradiated

- [Suggestion] Quantify Q0 agreement: State the typical fitted Q0 value and its uncertainty; "good agreement with 8 fC" is qualitative.

- [Suggestion] State extracted mobility: The fitted electron mobility from Fig. 8c should be stated and compared to the literature value of 4600 cm^2/(V·s) to validate the model.

- [Suggestion] Discuss trapping time: The trapping time τ from unirradiated fits (Fig. 8d) is presented but not discussed. Is it consistent with known Fe trap properties in InP:Fe?

## Irradiation: I-V and C-V

- [Suggestion] Nuance the α comparison to silicon: The comparison (α_InP ≈ 3× α_Si) and the conclusion "less radiation hard" is misleading without noting that the Si value is defined under full depletion while InP α is strongly bias-dependent. Acknowledge this explicitly.

- [Suggestion] Quantify volume uncertainty: The effective volume is an upper bound (E-field simulation shows a larger true volume), but the magnitude of the resulting uncertainty in α is not stated. Add an estimate.

- [Suggestion] Expand C-V discussion: One sentence for four figures is insufficient. Add a brief physical interpretation of why capacitance is insensitive to irradiation in a bulk quasi-resistive material with no depletion region.

## Irradiation: betascope signal

- [Must fix] State numerical irradiation results: Timing resolution and collected charge for irradiated samples at representative conditions (400 V, +20°C and -20°C, both fluences) are never stated numerically. Add these.

- [Must fix] Quantify temperature recovery: The temperature recovery effect is stated qualitatively. State the fractional improvement in collected charge from +20 to -20°C at each fluence and a representative bias.

- [Suggestion] Connect rise time trend to physics: Mention in this subsection that the shorter rise times at higher fluence reflect trapping-limited collection (not just quote the trend), bridging to the conclusions.

## Irradiation: signal model fits

- [Must fix] State CCE numbers: CCE vs voltage (Fig. 10) and CCE vs fluence (Fig. 11a) are the central quantitative results. State the CCE at 10^14 n_eq/cm^2 at 300 V and its ratio to the unirradiated value.

- [Must fix] Discuss trapping distance trend: The trapping distance vs fluence (Fig. 11b) is presented without prose. State the trend and its physical meaning.

- [Suggestion] Validate fixed-transit-time assumption: Briefly note what would change if the transit time and amplitude were not fixed to unirradiated values in the irradiated fits, or confirm the assumption is validated by comparison.

# Conclusions

- [Must fix] Complete placeholder sentences: "We observe that leakage currents in diodes before the onset of breakdown…", "It was found that…", and "This observation…" are incomplete and must be finished before circulation.

- [Must fix] Convert bullet list to prose: The bullet list at the end of the conclusions signals an unfinished manuscript and must be absorbed into prose.

- [Must fix] State timing resolution in results: The "below 25 ps" number appears only in conclusions. State it first in the results section.

- [Must fix] Activation: cite the observation: The activation caveat references an observation that is currently in Methods. Move the observation to Results (as discussed under Methods above) and cite it here.

- [Suggestion] Complete polarity asymmetry sentence: The sentence about hole drift (trailing ellipsis) needs to be completed with a quantitative comparison.

- [Suggestion] Add comparison to other semiconductors: A brief comparison of α for InP against SiC, GaAs, and CdTe (flagged in the bullet list) belongs in the irradiation results discussion with a summary mention here.

- [Suggestion] Sharpen thin-film outlook: Specify which properties (carrier lifetime, trap density, mobility) are most important to compare between crystalline and amorphous InP, to make the forward-looking statement concrete.

# Cross-cutting and General

- [Must fix] Add performance comparison table: No table compares InP metrics (CCE, timing resolution, rise time, damage parameter α) to silicon. This is standard in characterization papers and will be expected by referees.

- [Must fix] Macro usage: Macros for 113-In, 114-In, 114m-In, 114-Cd, and 114-Sn are defined but usage should be verified; remove any that are unused before submission.

- [Suggestion] Numerical results for all key figures: Each key figure needs at least one sentence in the text quoting a representative number, not just a trend description. Figures most in need: Figs. 3 (laser TCT characterization), 6 (betascope unirradiated), and Figs. 10-11 (irradiation model results).

- [Suggestion] Remove draft artefacts from appendix: The blue editorial note ("Jenni: added blank page here…") must be removed. Add a reference from the main text directing readers to the appendix.

- [Suggestion] Reconsider "MIPs" in title: "Minimum-Ionizing Charged Particles" in the title is slightly imprecise since 90-Sr betas are used. Consider "...with Red Laser Transient Current Technique and Sr-90 Beta Particles" for accuracy.

- [Note] Caption grammar: "for a InP 1-ch device" should be "for an InP 1-ch device" in Fig. 6 caption and appendix Fig. A2 caption.

- [Note] Fig. 2 vs Fig. 3 captions: Reconcile the inconsistency in which polarity/polarities are shown between the two laser TCT figures.

- [Note] Taylor figure: Verify that the zoomed-in E-field figure from Taylor (flagged as done in TODO.md) is the correct version in the current build.