## Slide 1: How the discovery of Cold Noise delayed the production of ATLAS ITk strip tracker modules by a year AKA FUN WITH LASERS Andy Blue

## Slide 2
Short-strip module
Hybrids
ITk Strip Barrel Modules
Short-strip module
Strip
Long-strip module
Strip
Powerboard

## Slide 3
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Cold Noise Observations
Short-strip module
Strip Row 1
Strip direction
Strip Row 4

## Slide 4
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Cold Noise Observations
Short-strip module

## Slide 5
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Worsens with load on DC-DC converter.
  Can increase load by shunting current on ABCs.
-50C, shunts on
-50C, shunts off
-35C, shunts off
Cold Noise Observations

## Slide 6
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Worsens with load on DC-DC converter.
  Can increase load by shunting current on ABCs.
Noise “freezes-in” during 1st thermal cycle.
  Persists while warming.
  Occasionally have residual “cold” noise at room temp!
+20C
+20C
-10C
-10C
-50C
1st thermal cycle
Cold Noise Observations

## Slide 7
+20C
+20C
+20C
Bake-out
+20C
+20C
+40C
Cold Noise Observations
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Worsens with load on DC-DC converter.
  Can increase load by shunting current on ABCs.
Noise “freezes-in” during 1st thermal cycle.
  Persists while warming.
  Occasionally have residual “cold” noise at room temp!
    But can “bake-out” by going warmer.

## Slide 8
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Worsens with load on DC-DC converter.
  Can increase load by shunting current on ABCs.
Noise “freezes-in” during 1st thermal cycle.
  Persists while warming.
  Occasionally have residual “cold” noise at room temp!
    But can “bake-out” by going warmer.
Glue dependence:
Severity varies greatly among “nearly identical” epoxies.
  Unable to correlate with any info in data sheets…
Cold Noise Observations
-50C
AA-Bond F112 Eccobond F112 Polaris

## Slide 9
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Worsens with load on DC-DC converter.
  Can increase load by shunting current on ABCs.
Noise “freezes-in” during 1st thermal cycle.
  Persists while warming.
  Occasionally have residual “cold” noise at room temp!
    But can “bake-out” by going warmer.
Glue dependence:
Severity varies greatly among “nearly identical” epoxies.
  Unable to correlate with any info in data sheets…
Thicker glue layers under PB and hybrid(s) can reduce CN.
Cold Noise Observations
-50C
AA-BOND F112
Nominal glue thickness
Double glue thickness

## Slide 10
Early Observations:
Only appears on the strip rows under the hybrids & PB.
Tends to appear in certain regions.
  Correlated with glue under hybrids.
Worsens with load on DC-DC converter.
  Can increase load by shunting current on ABCs.
Noise “freezes-in” during 1st thermal cycle.
  Persists while warming.
  Occasionally have residual “cold” noise at room temp!
    But can “bake-out” by going warmer.
Glue dependence:
Severity varies greatly among “nearly identical” epoxies.
  Unable to correlate with any info in data sheets…
Thicker glue layers under PB and hybrid(s) can reduce CN.
Softer “glues” (Sylgard encapsulant, SE-4445 gel) remove CN.
  Only diagnostic, not suitable for detector.
Cold Noise Observations

## Slide 11
Finding the source of vibrations

## Slide 12
Powerboard is instigator of Cold Noise
  Powerboard electrically bypassed - CN is removed
“Singing” capacitors known phenomenon when dielectric used in capacitor has piezoelectric effect
  Occurs with a oscillating voltage on capacitors
  Buck converter a potential candidate for singing capacitors
Cold Noise Instigator
HV switch
Buck converter
Powerboard
AMAC
Autonomous Monitor and Control (AMAC)

## Slide 13
Propagating wave - Vibromoeter
Cant remove the source of vibration
Need to understand how vibration is propagating
Use a Vibrometer
  Non-contact measurement
  No mass loading
  Laser spot 40 µm
  Sensitive to MHz range
Upgraded Vibrometer with 2D scanning
  Single point measurements across module
  Stitched together measurements in phase
    Magnetic trigger on buck converter as reference
Capacitor amplitude approx. 1 nm
  Amplitude is dependent on power draw of powerboard
Vibrations propagate across Silicon at same wavelength as calculated ~1.3 mm
The wavelength on the PCB is ~400 µm
CN connected to wavelength in Silicon so interested in scan of back side of module
2D scanning vibrometer
Module

## Slide 14
Propagating Wave in Silicon Sensor
Propagation across the silicon sensor
Window cut in pcb readout board for module to scan the pack of the sensor
Module powered in climate chamber at -60C
Vibrometer scan through 9 pane window
Si Strip Sensor
Al backside
2D Scanning vibrometer
10cm
Climate Chamber
Strip Sensor

## Slide 15
Power Board
1cm
Hybrid
Glue
Pattern
(approx.)
Glue
Pattern
(approx.)
Hybrid
Propagating Wave in Silicon Sensor
Height
Vibrometer scan of Silicon sensor from the back of module while in climate chamber at -60C
Strip Sensor
Si Strip Sensor

## Slide 16
Hybrid
Glue
Pattern
(approx.)
Glue
Pattern
(approx.)
Hybrid
Propagating Wave in Silicon Sensor
CN strips
The glue gaps allow the waves to pass through
The glue under the hybrids dampens the vibrations
There is an interference pattern between the caps
The C2 cap has strong oscillations when at full power
The location of CN readout is not clearly correlated to the wave pattern
Height
Power Board
1cm

## Slide 17
CERN’s bPOL (on ITk strip module) and FEAST DCDC power converters used in multiple experiments
0.5 nm vibrations seen on both versions
FEAST has been running in CMS operationally for over a year
These capacitor vibrations are the same as our module
Source and scale of vibrations not unique to ATLAS ITk strip
FEAST module is currently in CMS
We Are Not Alone
Capacitor vibration