## Slide 1: XPS measurements of sodium in Bridgman-grown CuInSe2+x
by
Sunyoung Park, C. H. Champness and I. Shih
Electrical and Computer Eng., Dept.
McGill University
Sunyoung Park
Ph.D. student

## Slide 2
Glass substrate
Earlier cell
Mo
p CuInSe2
n CdS
ZnO i
ZnO cond
Metal grid evap.
hν
J-V characteristics under simulated AM 1.5
conditions of a Cu(In,Ga)Se and a CuInSe2 cell.
The cells are AR-coated.
Cell temperature is 25 °C
(Hedstrom and Ohlsen, 1993)
Glass substrate
Later cell
Mo
p Cu(In,Ga)Se2
n CdS
ZnO i
ZnO cond
hν
Sputtered
Solution grown
(50 nm)
2 µm
Sputtered

## Slide 3: Solar cell efficiency with added Na2Se (Nakada and Ohbo, 1997)

## Slide 4: A quartz ampoule with Cu, In, Se, and Na
Se
In
Cu
Na

## Slide 5: Bridgman Growth Apparatus

## Slide 6: Bridgman-grown ingot

## Slide 7: Bridgman-grown ingot
CuInSe2+x
n-type
If
[Na]>[Na]crit =2x+δ

## Slide 8: Before abrasion
Chart: Ar etching (s)
| 0 | 1 | 2 | 7 | 12 | 42 | 72 | 132
Se3d | 16.33 | 24.44 | 28.39 | 32.06 | 34.27 | 34.8 | 34.94 | 35.7
In3d | 56.81 | 51.12 | 45.21 | 37.26 | 33.26 | 27.26 | 26.25 | 26.25
Cu2p3 | 26.85 | 24.44 | 26.41 | 30.68 | 32.48 | 37.94 | 38.81 | 38.81

## Slide 9: After abrasion
Chart: Ar etching (s)
| 0 | 1 | 11 | 41 | 71
Se3d | 39.29 | 40.47 | 39.84 | 39.44 | 39.5
In3d | 29.91 | 28.95 | 29.86 | 28.76 | 28.99
Cu2p3 | 30.8 | 30.58 | 30.3 | 31.8 | 31.52

## Slide 10: XPS survey scans for different locations of an ingot
Chart: Binding Energy (eV)

## Slide 11: Na1s scan
Chart: Binding Energy (eV)

## Slide 12: Na1s scan
Chart: HMB56 (3 at. % Na) curved
| 0 | 1 | 6 | 16 | 46 | 106 | 116 | 126 | 136 | 146 | 156
Se3d | 40.59 | 44.08 | 47.1 | 46.49 | 45.21 | 43.11 | 43.79 | 43.5 | 42.98 | 43.14 | 43.58
In3d | 25.27 | 27.72 | 30.49 | 35.12 | 42.06 | 48.14 | 48.24 | 49.03 | 49.87 | 50.12 | 49.33
Cu2p | 2.08 | 3.44 | 4.1 | 4.99 | 6.78 | 7 | 6.12 | 6.36 | 6.05 | 6.18 | 6.09
Na1s | 32.06 | 24.76 | 18.31 | 13.4 | 5.94 | 1.75 | 1.84 | 1.11 | 1.1 | 0.56 | 1

## Slide 13: [Cu]surf vs. [Na]surf
Chart: Na at. % (of 4 elements) at surface
| 48 | 0 | 3 | 58 | 9 | 26 | 40
Bulk n-type | 8 | 24 | 11 | 11 | 14 | 7 | 8
Bulk p-type | 28 | 11 | 24 | 28 | 10 | 4 | 11

## Slide 14: [Cu]surf vs. [Na]melt
Chart: Na at. % (of CuInSe2) in melt
| 3 | 0.5 | 1 | 2 | 0.3 | 6 | 5
Bulk n-type | 8 | 24 | 11 | 11 | 14 | 7 | 8
Bulk p-type | 28 | 11 | 24 | 28 | 10 | 17 | 11

## Slide 15: [Se]surf vs. [Na]sulf
Chart: Na at. % (of 4 elements) at surface
| 48 | 0 | 3 | 58 | 9 | 26 | 40
Bulk n-type | 25 | 15 | 58 | 0 | 14 | 35 | 25
Bulk p-type | 39 | 17 | 34 | 30 | 48 | 70 | 43

## Slide 16: Conclusions
The present results in Bridgman-grown CuInSe2+x demonstrate that:
(1) The main variations in ternary composition occur in the first 100 nm from the ingot surface, even without Na addition.
(2) With increase of up to about 1 at. % of added elemental Na to the melt, the relative surface concentration of Cu is decreased and that of Se, in p-type (bulk) material, is increased.
(3) The Na is mostly present in a 0.2 micron surface layer and none is detected by XPS in the bulk.
(4) The reduction of Cu proportion at the surface occurs with and without added Na but is accentuated with up to 1 at. % of added Na in the melt.
(5) Some of the XPS results may have been affected by the abundant carbon present.
(6) For samples exposed to air, the addition of Na gives rise to the extra compounds CuSe2, Na2SeO4, and Na2SeO3, at least at the surface.

## Slide 17: Speculation
CuInSe2
or
Cu(InGa)Se2
p
Low Cu
Ternary
n
CdS
hν
CdS
interface
Lower recombination
interface
Low Cu ternary/CuInSe2
n/p interface
The End

## Slide 18
The End