## Slide 1: Mechanical photons at McGill
Current goals
Partial levitation and ultrahigh Q MEMS
Wavelength-scale optical cavities
Photonic crystal reflectors
MEMS materials research

## Slide 2: Mechanical systems = force sensors
cantilever
deflection measurement
sample exerts forces
on cantilever
Electronic forces (Grütter Lab, McGill)
Nuclear forces (Rugar Lab, IBM)
Typical force measurement:
See also
gravity wave detectors
accelerometers in phones & cars
electronic filters (also in phones)

## Slide 3: Optomechanics, and you
New functionality through radiation forces, e.g.:
Laser cooling & observation of quantum motion
Detecting the “hiss” from incident photons
Mechanically squeezing light
Wavelength conversion & qubit transduction
Our focus
Laser-enhanced micromechanical sensors (MEMS)
New geometries and new types of coupling
Example system (ours, coincidentally)
mirror
mirror
100-nm-thick “trampoline”
laser input

## Slide 4
Quantum sensing and information transfer
photon
“superposition”
information transfer
optical fiber
information transfer
“superposition”
CHINGGGGGGGGGG!
(entangled)

## Slide 5: Optomechanics, and you
New functionality through radiation forces, e.g.:
Laser cooling & observation of quantum motion
Detecting the “hiss” from incident photons
Mechanically squeezing light
Wavelength conversion & qubit transduction
Our focus
Laser-enhanced micromechanical sensors (MEMS)
New geometries and new types of coupling
Example system (ours, coincidentally)
mirror
mirror
100-nm-thick “trampoline”
laser input

## Slide 6: Example: “quadratic” optical spring
mirror
mirror
membrane
laser input
Empty Cavity Resonances
λ/2
λ/2
stable spring
Resonant input light
Enhanced radiation forces in cavity
Dielectrics drawn to antinodes
Resonant frequency coupled to position
Same per-watt efficiency as dipole trap
Optical levitation? (“trapping”)
cavity photons
curvature
energy
Notes: U(x) = \frac{1}{2} {\color{Red} n_\gamma} \hbar \left(\color{Magenta}\frac{\partial\omega_\gamma}{\partial x^2} \color{black}\right ) {\color{Blue} x^2 }

## Slide 7: Reduced damping & noise via levitation
Optical levitation
laser-tuned mechanical frequency
laser-tuned mechanical damping
predicted to ring for weeks
(lasers have very low noise)
VERY sensitive! (in theory)
Flexible materials
fixed frequency
fixed damping / force noise
rings for 10’s - 100’s of seconds
!!!
damping
force noise

## Slide 8: A “practical” goal: mostly levitated systems
weak mechanical spring from materials
strong optical spring from cavity light
enhanced mechanical properties
could approach levitated limits
easier to integrate with other systems
Fabrication at McGill
100-nm-thick nitride on silicon
1 μm
200 μm
nitride

## Slide 9: Partial levitation improves performance
material parameters
laser
Oscillator Position
Time
Trapped MEMS
faster response
less dissipation
# oscillations before energy is gone
Modified High-Quality MEMS:
Notes: \color{blue}m\color{black}} \ddot{x} + \color{blue}\gamma_m\color{black} \dot{x} + (\color{blue}k_m\color{black} + \color{red} k_L \color{black}) x = 0
\color{blue}m\color{black} \ddot{x} + (\color{blue}k_m + i \gamma_m \color{black} + \color{red} k_L \color{black}) x = 0

## Slide 10: Encouraging results (Caltech, 2012)
low bare Q
tether modes
pop-up
(no cavity)
Free-space standing wave trap ~ 10W
50x increase in mechanical Q!
K. K. Ni et. al. PRL 108, 214302 (2012)

## Slide 11: Increasing the per-photon trap strength
Center of mass and torsional trapping
Tilt (aboot the z-axis) tunes scattering rate between transverse modes
Tunable quadratic coupling for both center-of-mass and torsional motion
~10 MHz trap = no problem
Optical perturbation theory
T. Müller, C. Reinhardt, J. C. Sankey, PRA (2015)
Limitations on partial levitation
High laser power & melting
Low untrapped Q
Hybridization with untrapped modes

## Slide 12: Nanofabrication at McGill
Photolithography and reactive ion etch
KOH or TMAH wet etch
SiN
Si
SiN
SiN
SiN
Si
SiN
Si
SiN
Process flow
Start with nitride on silicon
Photolithography to define structures
Reactive ion etch to remove SiN
KOH dip to etch silicon wafer
SiN on Si
SiN on Si
released
nitride
photoresist on SiN

## Slide 13: Fabrication attempts & initial success
Low-stress nitride test
Price = $0
Floppy
Optically lossy (boo!)
High-stress nitride
Low optical loss
Potato-chipping (boo!)
Stiffer (boo?)
Latest iteration
High yield
No potatoes
High starting Q
(not actually glowing)
custom chip carrier (important)
curling
Christoph Reinhardt

## Slide 14: Mechanical characterization in UHV
cleaved optical fiber
sample
interference
Performance
Typical frequency ~ 50 kHz
“Typical” Q ~ 10-35 million
Initial Goal
Trap to Q ~ 200 million?
Limitations on trapping
High laser power & melting
We have a stupid high untrapped Q
Will these work in our cavities?
Hybridization with untrapped modes

## Slide 15: Homemade trampolines in a cavity
Tina Müller
Christoph Reinhardt
Mirror
Mirror
UHV chamber
Cavity hold time ~ “Finesse”
Membrane Position (Piezo Volts)
Cavity Length (Piezo Volts)
Finesse
λ/2
Processed membrane: ~ zero absorption
λ/2
Small trampoline we don’t care about: diffraction losses (expected)
Membrane / trampoline goes here
Limitations on trapping
High laser power & melting
Low untrapped Q
Will these work in our cavities?
Hybridization with untrapped modes

## Slide 16: Torsional mode = no tether mixing
Torsional mode (TM) levitation
No hybridization with low-frequency modes (by symmetry)
First hybridization with “flappy” disc mode
1500 x Q enhancement possible (Q ~ billion??)
Q-Enhancement
Trap Strength (MHz)
Trap Strength (kHz)
Q-Enhancement Frequency (kHz)
T. Müller, C. Reinhardt, J. C. Sankey, PRA (2015)
increased laser spot size
previously inaccessible
Tina Müller
COMSOL simulations of optically trapped mechanical modes
Limitations on trapping
High laser power & melting
Low untrapped Q
Will these work in our cavities
Hybridization with untrapped modes
No potato chips allowed

## Slide 17: Single-crystal silicon fab
Tina Müller
Simon Bernard
Next step: delicate mechanical (and photonic) structures!

## Slide 18: New material: single-crystal diamond
Single-crystal diamond (DOI)
Higher unstressed Q than Si (new)
High power handling
Contains embedded quantum systems (NV, SiV centers)
Initial ArCl etch of e6 diamond
Alumina hard mask
Optical grade diamond
Collaboration with Ye Tao & Christian Degen @ ETH

## Slide 19: Related goals II: really short cavities
“Compound input mirror”
Membrane as “movable Bragg layer”
Input transmission coupled to membrane motion
Alex Kato
Kyle Johnson
Vincent Dumont

## Slide 20: Stronger coupling to smaller devices
high-reflectivity mirror coating
laser ablation, glass melts, reflow
freshly-cleaved fiber
Ablated fibers courtesy of Jakob Reichel Group
Fiber-based microcavities
Shorter cavity = more bounces per second = stronger coupling
Confined optical mode = naturally addresses smaller, lighter MEMS
Compact, fiber-coupled package
Fiber Mirror Fabrication with 40W CO2 laser

## Slide 21
new dot

## Slide 22: Really short full cavities
Laser-ablated, coated fiber mirrors
Goal: cavity length ~ wavelength
Stronger per-photon force (shorter round-trip time)
Suited for smaller MEMS
Fiber-coupled input and output
Max
Ruf
Erika
Janitz
Alex
Bourassa
Interferometer Image
ablation dip
< 0.2 nm roughness!
Mirrors
cavity lengths
~ 10’s of μm
Mirror Fabrication
~25,000

## Slide 23: Related goals I: Wifflebranes®
simulated input pulse
resonances in photonic crystal
increased reflectivity by removing material
(Solgaard group, Stanford)
Collaboration with Yves-Alain Peter (Polytechnique)
Simon Bernard
Predictions (MEEP)
Resonant reflection of one wavelength
Subsequent HF (acid) dips thin membrane, widen holes
  Controlled tuning of resonance
Resonance tuning with HF

## Slide 24: Preliminary results
Fabrication in silicon nitride
Electron beam instead of photolith
No surprise: new surprises
Resonance tuned with HF
Next step: measure actual reflectivity with a cavity.
Simon Bernard
Why? Why?!
Tuning the resonance post fabrication

## Slide 25: Less force noise & higher Q’s: cryostat
At Low Temperature
Reduced force noise, higher bare Q
Quantum experiments more accessible
Fiber input, same hardware
Vary temperature & trap to study dissipation
Incoming upgrade: 10 mK (!)
3K - 300K
(hang from springs)

## Slide 26: Unrelated advertisement: spin transfer
N-V magnetometry of magnetic nanocircuits
All-electrical FMR on protected magnetic nanocircuit
Imaging of dynamics with N-V defects in diamond
Nanoscale magnetic elements, sub-wavelength techniques
Coherent coupling between N-V spins and magnons?
Zackary Flansberry
Simulated Dynamics
Fabricated
Contacts
collaboration with Wife (McGill) & Michel Pioro-Ladrière (Sherbrooke)

## Slide 27: Summary Flip the slide, Sankey.
Current & future goals
Partial levitation and ultrahigh Q MEMS
Wavelength-scale optical cavities
Photonic crystal reflectors
MEMS materials research
Nanoscale magnetic circuits

## Slide 28
Chandra Curry
Christoph Reinhardt
Max Ruf
Andre Diamant- Boustead
Abeer Barasheed
Chris McNally
Tina Müller
Simon Bernard
Me
Laurent René de Cotret
Alexandre Bourassa
Echo
André Provost
Bogdan Piciu
McGill Optomechanics Lab